## Slide 1
PHOTOCATHODE STUDIES
Electron Energy Analyzer
NEA Cathodes (GaAs)
Multi-alkali Cathodes

## Slide 2: 2D ENERGY ANALYZER FOR ELECTRON BEAMS
Purpose - Measuring the transverse and longitudinal energy distribution of electrons
e
e
e
e
e
e
e
e
e
e
e

## Slide 3: Principle of operation
First Marking Electrode
Varying Magnetic Field
Second Marking Electrode
Beam Current Detector
Longitudinal Energy
Transverse
Energy

## Slide 4: Electron Energy Analyzer
RFA
(2nd marking electrode)
Magnet Coils
Gun
( 1st marking electrode)
Electron source
(Thermionic gun with energy shaping assembly)

## Slide 5: Features
Improved version of the Energy analyzer originally developed at Max Planck Institute by Orlov
Use of double lock-in technique and better electrode design.
Can be used at 1nA/mm2 and hence with lower intensity tunable wavelength light sources.
Can obtain better energy resolution (<10meV).

## Slide 6: NEA Semiconductor Cathodes
Focused on GaAs
Study of surface roughness on emittance
Surface preparation/activation techniques

## Slide 7: Surface roughness of GaAs
Surfaces were imaged to a resolution of less than 1 nm using Atomic Force Microscopy
Found more than 10 times rise in rms roughness after activation and use in gun.
Major cause thought to be repetitive heat cleaning for prolonged periods.
Roughness not detectable under optical microscope and wafer doesn’t loose mirror like look

## Slide 8: Surface Roughness of GaAs
Atomically polished surface
Roughness = 0.5nm(rms)
Activated surface removed from gun
Roughness = 6nm(rms)

## Slide 9: Effect on transverse energy

## Slide 10: Effect on transverse energy

## Slide 11: Effect on transverse energy

## Slide 12: Future Work
Look at energy distributions/emittance from flat and rough surface
Look into effect of low temperature
Techniques for activation that maintain the surface quality – Cleaving in vacuum, MBE
Energy distributions of multi-alkali cathodes