## Slide 1: Measuring the growth of alkali antimonides using in-situ X-ray Diffraction and X-ray Reflectivity
Miguel Ruiz-Osés
Postdoc Stony Brook University
Contact: mruizoses@gmail.com
2nd Photocathode Physics for Photoinjectors workshop, Cornell 10/07/2012

## Slide 2
RHIC: Relativistic Heavy Ion Collider
R&D Collider Department
NSLS: National Synchrotron Light Source
Brookhaven National Laboratory

## Slide 3
Introduction:
Alkali antimonide cathodes are critical both for high-average current photoinjectors and for high quantum efficiency photodetectors.
Problems-Challenges:
Extreme vacuum sensitivity, non-reproducibility and poor lifetime.
Photoinjectors performance:
  QE of 2-6% at 532 nm and >10% at 355 nm
  QE unchanged at cryogenic temperature
  > 50 mA from 7 mm radius spot
  High Uniformity
  Emittance

## Slide 4
Study of the growth parameters, including both transparent and metallic substrates, sputtered and evaporated films, variation of growth time and temperatures and post-growth annealing processes. RECIPE
By means of these Techniques…
X-Ray Diffraction in-situ growth
XPS: Chemistry of growth (Susanne’s Talk)
Techniques:
Effort to improve the performance of alkali antimonides ( K2CsSb) based on characterization of cathode formation during growth.
Approach:
Correlation Between Material Properties and Performance
Goal:

## Slide 5
XRD: Atomic arrangement of materials.
Monochromatic X-Ray
Coherent X-Ray scattering = f( e- distribution in sample)
“The intensity and spatial distributions of the scattered X-rays form a specific
diffraction pattern which is the “fingerprint” of the sample.
monocrystaline
polycristaline
2D area detector
XRD Crystalline structure during growth

## Slide 6
Horizontal evaporation of three sources:
140
25
T(C)
t
Sb
K
Cs
Recipe:
100
Experimental set up: K2CsSb cathodes growth
Sb
K
Cs
FTM
P=1x10-10 mbar
QE(%)
t
K
Cs
QE during growth (532 nm laser)
X-rays
Detector

## Slide 7
in-situ X-ray diff during deposition.
UHV system (2x10-10 Torr base pressure)
Residual Gas Analyzer (RGA)
Heating/cooling substrate/cathode
Load lock (fast exchange of substrates)
Horizontal deposition of Sb, K and Cs.
4 axis diffractometer UHV chamber
Beam Energy = 10 keV, λ = 1.2398 Å
Mono Resolution (ΔE/E) = ~ 2x10-4
Flux = ~ 2x1012 ph/sec @ 300 mA
Spot Size = ~ 1 x 0.5 mm2
nu - 2θ
(table)
Evaporators
zeta - θ
(sample)
X-rays
X21/NSLS Beamline
Portable chamber!
Camera 1
Camera 2
Two 2D detectors (Pilatus 100K):

## Slide 8
α: Swing angle
D: Distance sample-detector
XL, YL, ZL: Lab coordinates
XL
YL
1
2
D
α
X-rays
Diffractometer plane
  XRR movie while evaporation
Camera 1: Scan in diff plane
Detector 1
ZL
  Ɵ-2Ɵ WAXS
  (after evaporation)

## Slide 9
ZL
XL
YL
1
α’
D’
X-rays
  XRD movie while evaporation
α’= 25˚
Diffractometer plane
Camera 2: Scan out of diff plane
Detector 2
Detector 1
ZL

## Slide 10
X-Ray reflectivity (XRR)
Wide Angle X Ray Scattering (WAXS)
  thickness of thin film layers
  density and composition of thin film layers
  roughness of films and interfaces
Camera 1
Camera 2
  phase composition (what phases are present)
  quantitative phase analysis- (how much of each phase is present)
  unit cell lattice parameters
  crystal structure
  average crystallite size of nanocrystalline samples
  crystallite microstrain
  texture
  residual stress (really residual strain)
FIXED ANGLE α
SCAN IN ANGLE
FIXED ANGLE α’
Wide Angle X Ray Scattering (WAXS)
Set of data
QE(%)
t
K
Cs
QE measurement during growth

## Slide 11: 165Å Sb at RT on Si(100)
0Å
165Å
time
14.9˚
39.3˚
Influence of the Sb structure on the growth of the cathode:
Correlation between structure of Sb and the final structure of the cathode?
Is the substrate having an influence in the Sb growth?
Is there a correlation between reactivity, QE and roughness?
Camera 1: XRR
Camera 2: WAXS
Sb peaks
(012)
(104)
(110)
(003)

## Slide 12: K at 140C
Camera 1
Camera 2
time
~10Å
~290Å
~495Å
~500Å
K3Sb peaks (K diffusion into Sb)
Sb peaks
(012)
(104)
(110)
(220)
(111)
(420)
2000 s
3800 s
4645 s
4697 s
QE(%)=0.1%

## Slide 13: Cs at 130C
0Å
25Å
763Å
0Å
901Å
Camera 1
Camera 2
time
QE(%)=1.4%
700s
1220s
4400s
5000s
700 s
1220 s
4400 s
5000 s
K2CsSb peaks
28˚
23.8˚
(111)
(220)
(420)
(200)
(220)
(222)
(400)
(331)
(420)
K3Sb peaks

## Slide 14: Cathodes comparison
Cathode2
QE(%)=0.4%
QE(%)=3.7%
100C
Cathode 1
Sb
K3Sb
K2CsSb
(012)
(104)
(110)
(003)
(111)
(220)
(420)
QE(%)=1.4%
QE(%)=0.1%
RT
RT vs 100C Sb evaporation: Starting configuration of Sb different in both cases.
Succesfull experiments measuring QE+XRD while growing cathodes!

## Slide 15
Differences between RT and 100C evaporation of Sb
RT evaporation smaller grains
100C deposition bigger grains

## Slide 16: K3Sb formation:
Cathode 1
(012)
Cathode2
QE(%)=0.4%
QE(%)=0.1%
Camera 1
Camera 2
137Å
205Å
312Å
0s
1180s
1840s
2820s
K3Sb peaks
Sb peaks
Camera 1
Camera 2
time
~10Å
~290Å
~495Å
~500Å
2000 s
3800 s
4645 s
4697 s
1. Start K reaction
1
2
2. K is not initially sticking
3
3. Low intensity fringes and larger background= rougher surface enhanced reaction rate
RT
100 C

## Slide 17
Cathode 1
K2CsSb
Cathode2
QE(%)=3.7%
QE(%)=1.4%
249Å Cs
756Å Cs
Comparison of Crystal structure and Final QE: K2CsSb
WAXS camera 1 after evaporation…

## Slide 18
Identifying phases….
Comparison of Crystal structure and Final QE: K2CsSb cathodes
K2CsSb

## Slide 19
Evolution of Crystal structure during K2CsSb growth
15 nm Sb 100C
70 nm K
50 nm K
150 nm Cs

## Slide 20
Sb evaporated at 100C
Clear [003] texture
Add Potassium at 135C
Textured final film
But not K3Sb
Add Cesium at 135C
Textured final film
Both [220] & [222]
K2CsSb Cathode texture
Final QE 6.3% @ 532nm
Sb
K
Cs

## Slide 21
Diffusion length of K
15 nm Sb + 90 nm K
100 nm Sb + 310 nm K + 200 nm K

## Slide 22
Coating of cathodes for experimental transfer
No Carbon
Carbon

## Slide 23
Successful In-situ XRD experiment to visualize crystalline growth correlated with QE measurement.(20 cathodes in total)
Evidence of Sb effect on final QE performance.
Evidence of texturing in final “good”cathodes
Diffusion length studies of K into Sb
Capping cathodes attempt
Conclusions XRD:

## Slide 24: Thanks to:
X. Liang, E. Muller, M. Gaowei, I. Ben-Zvi, Stony Brook University
J. Smedley, K. Attenkofer, T. Rao, Brookhaven National Lab
T. Vecchione , H. Padmore, Lawrence Berkeley Lab
S. Schubert, Helmhotlz Zentrum Berlin, Germany
DOE Office of Science, Basic Energy Sciences

## Slide 26
QE(%) 062012 532 nm = 1.2
QE(%) 062112 532 nm = 1.8
Spectral response

## Slide 27: Deposition system at Collider-Accelerator Department (CAD)
Main chamber
Potassium cell
Cessium cell
Antimony cell
How do we transport the cathode from the deposition chamber to the gun-injector?

## Slide 28
Transport cart
Controllers rack
Deposition chamber
Transport cart attached to depo-chamber for cathode growing and transport to gun.

## Slide 29
Transport cart
SRF Gun
Attachment of transport cart into the gun for cathode installation.
Tests with the gun….

## Slide 31
Powder Diffraction Files

## Slide 32
Calibration of two cameras

## Slide 36
EDX : final Sb thickness: (36 nm cath 1, 40 nm cath 2).
In line with expected totals based on FTM values.
SEM and EDX after brief exposure to air
Segregation of K and uniform coverage of Cs and Sb:
(K forms islands during deposition or that air exposure preferentially removes K).
Sb and Cs were found in the correct stoichiometric ratio (~1:1), however a dearth of K was observed.
Microscopy:
UHV-AFM
QE(%)=1.1%
K2CsSb
SEM
EDX:Energy Dispersive X-rays

## Slide 37
First Cathode
Full Cathode
QE(%)=1.4%
No cathode

## Slide 38
S116
S123
S143
S154
First Cath
Second Cath
First layer
First layer
Second layer
Second layer
QE~1.4%
QE~2.7%
QE~3.7%
QE~2.9%
K2CsSb cathodes comparison_P1