## Slide 1: Reduction of emittance from metals to less than thermal
Jun Feng
Lawrence Berkeley National Laboratory
Acknowledgements
Mike Greaves, W. Wan, D. Dowell, H. A. Padmore

## Slide 2
Outline
Free electron metals and surface states
Experimental setup to measure QE and momentum
QE measurements on Ag(111)
Implication for other design of low emittance materials

## Slide 3: Background: emittance of a free electron metal including kT
Wan, Dowell, Jun, Vecchione, Padmore
manuscript in preparation
Application of the 3 step model including kT
  Main Consequence: Minimum emittance with a free electron metal is 0.23 microns
  One way to decrease emittance is to limit angular emission use bandstructure
0.5 eV excess energy
Linear dependence
+ small kT tail
More detail about the theory in Weishi’s talk tomorrow

## Slide 4: One bandstructure example: photoemitted electrons from surface states
Ag (111)
very narrow energy width (9 meV)
very close to the Fermi level (65 meV)
Small transverse momentum cutoff
Can be seen in narrow angular cone width
Result is much lower emittance than normal free electron metals
Fermi
level
eq: Ag(111) emittance ~0.078micron

## Slide 5: Photoemitted electrons from surface states
We know the dispersion of surface states from previous work
  we know the emittance will be << than a free electron metal
What we don’t know is the photocurrent in the surface state channel
  Is it greater or less than would be predicted by the 3 step model?
    it would be useless to have reduced emittance if the QE is smaller than normal FE metals
Most important measurement is the spectral dependence of QE for p and s polarized light
  surface state cannot be excited in s-polarization (ie. E vector parallel to surface)

## Slide 6: Setup
Verdi
700-1000 nm psec Laser Oscillator (MIRA, 76 MHz)
Pulse Picker
UHV
Chamber
1.2 W mode locked
37 mW
T0 diode
M1
M1’
2nd harmonic LBO
M3
M2
Fiber to spectrometer
7.5mW
375 µW, 5-6 eV,3.8 MHz
h=20%
4th harmonic BBO
h= 5%
Monochromator
M4
Laser Plasma Source
4-9 MHz
40µW, 250nm
ARPES
QE(E) measurement
Techniques:
Ultra-low energy Angle Resolved Photoelectron Spectroscopy (ARPES)
Angle Resolved Electron Yield (AREY)
Low Energy Electron Diffraction (LEED)
Energy dependent yield
Full measurement of momentum distribution and yield as function of:
  Polarization, Photon energy.
  Photon incidence angle
  Surface preparation
Notes: Change Slide to “Sources” and include Plasma Source.
1.2 W @ 856 nm, 76Mhz;
250mW 2nd Harmonic
200µW Fourth Harmonic
Pulse Picked: 30mW picked,

## Slide 7: System for ARPES and yield measurements
4th harmonic system + time of flight analyzer
2nd harmonic system
Laser plasma + mono

## Slide 8: Preparation of atomically perfect single crystal surfaces
Step 1
Ion Bombard
1 kV Ar+ Ion
10 Å Removed
Step 2
Anneal
Ramp high temp
Dwell 10 minutes
Cool RT
Step 3
LEED
Verify Surface Order
ln(current/T2)
Work function is checked by Fowler technique

## Slide 9: ARPES by TOF method
x,y
Δt
Electrons
Light
Sample
Measure position and time of flight of the electron in parallel plate geometry using Time of Flight (TOF).
resolution: 4.8meV
(x,y,t) for each event
Time Resolution: 165ps
Spatial Resolution: 128µm
Maximum Count Rate: 1.5M cps

## Slide 10: Angular distribution confirms surface state: eg. Cu(111)
I(kx,ky), E = Efermi
Emission is not isotropic as for a free electron metal
Emission localized in energy and momentum
Maximum transverse momentum limited
I(E, ky), kx = 0
E [eV]

## Slide 11
Wavelength dependent QE measurement for Ag(111)
Normal incidence
70 degree incidence
S polarized
  Fowler like behavior to ~ 250 nm (5 eV)
P polarized
  Large QE enhancement, particularly close to threshold
    Non-Fowler like behavior close to threshold
Fowler-like
Non-Fowler-like
Jun, Mike, Wan, Dowell, Padmore
manuscript in preparation

## Slide 12
Clean surface
Sputtered surface
Angle dependent QE measurement at 266 nm for Ag(111)
Photon energy 4.67 eV compared to 4.45 eV work function: 0.22 eV excess energy
QE at 70 degrees incidence ~ 100 x QE at normal incidence!
Sputtering ( ~ 10 Angstroms) mostly eliminates the enhancement
Enhancement attributed to high density of surface states 0.065 eV from the Fermi Level
More detail about the theory in Weishi’s talk tomorrow

## Slide 13
  Mo(110) higher density of surface states?
  layered compounds more than 1 contributing surface
  bulk crystals direct gap semiconductors
  exotic systems states localized at the Fermi level
Are there any better systems?

## Slide 14
Topological insulator Bi2Se3
bottom of
conduction band
(doped)
surface states
Dirac point
- note small
width in k
YuQi Xia:Princeton thesis, 2010
doping tuned Dirac point energy
Doping brings Dirac point to Fermi level
Dotted line shows Ag(111) width at Ef

## Slide 15
Conclusions
Surface states give the following advantages over normal metals
  Large reduction in transverse momentum
  Large increase in yield
Vacuum requirements compatible with VHF and DC photoguns
  Ag(111) relatively unreactive: surface state behavior constant at 4e-10 Torr for many days
May be much better systems
  Mo(110) higher density of surface states?
  layered compounds more than 1 contributing surface
  bulk crystals direct gap semiconductors
  exotic systems states localized at the Fermi level