## Slide 1: CEBAF Upgrade cavity
G. Ciovati for the JLab SRF Group
TTC Topical Meeting on CW SRF
Cornell Univ., June 12th-14th, 2013

## Slide 2: CEBAF’s Evolution to 12 GeV
CHL-2
Upgrade magnets and power supplies
42 1st -generation SRF cryomodules ‘91-’93 -- ≥ 25 MV
10 reprocessed ’06-’09 -- 50 MV
4 2nd-generation cryomodules – ’11-’12
6 2nd-generation cryomodules – ’13
  ≥ 108 MV avg.
300 W @ 2.07K
2nd generation cavity: 0.7 m, “Low loss” cell shape, 1.497 GHz, 8 cavities/cryomodule
Pair of 0.5 m cavities:, “Original” cell shape 1.497 GHz, 8 cavities/cryomodule
All cavities made from “RRR-grade”
sheet metal niobium

## Slide 3: Cavity Designs
HG shape was optimized to lower Ep/Eacc, reducing the risk of FE
LL shape was optimized to lower the wall loss [(R/Q)G]
Four 7-cell Nb cavities of each shape were built, tested and installed in a prototype cryomodule (Renascence)
Both types of cavities performed well w.r.t.:
  Susceptibility to FE and MP
  Adequacy of HOM damping
  Stability of field flatness
The LL-shape was chosen because of ~20% lower Pwall than HG-shape
J. Sekutowicz et al., PAC’03, p. 1395.

## Slide 4: Prototype cavities – VT results
Cavities treated by BCP
C. Reece et al., PAC’05, TPPT081.

## Slide 5: Upgrade cavity – Initial Configuration
Warm ceramic RF window
Cu-plated waveguide between RT and 2 K
l/4 waveguide RF input coupler
Piezo element (2)
Stepper motor tuner drive
Titanium helium vessel
RF reference probe
HOM coupler (4)
Thermal problem area
1 m
Fundamental Power Coupler (FPC)

## Slide 6: Issues and Solutions
C. Reece et al., SRF’07, p. 540.

## Slide 7: Updated cavity treatment: “light” EP+120C bake
30 mm EP: increase gradient
HPR
120C bake: increase Q0
Adopted as final surface treatment of Upgrade cavities
C. Reece et al., PAC’09, p. 2126.

## Slide 8: Cavity treatments – Production process
  160 µm BCP and pre-tuned by vendor
  Receipt inspection – mechanical and rf
  US >> Bake: 600 C, 10 hrs
  US >> EP: 30 µm, @20C regulated by external water spray
  US >> Tune
  Helium vessel welding
  Flange lapping
  HPR
  Partial assembly
  HPR >> dry in Class 10 cleanroom
  Final assembly, leak check
  Bake: 120 C, 24 hrs
  Vertical test @ 2.07 K
  HPR >> dry in Class 10
  String assembly
A. Reilly et al., SRF’11, TUPO061.

## Slide 9: Cavities Vertical Test results
96% of the cavities were qualified (61% with a single RF test)
A. Burrill et al., IPAC’12, p. 2423.

## Slide 10: Upgrade cavity – Optimized Configuration
l/4 waveguide RF input coupler
Fundamental Power Coupler (FPC)
Cu-plated waveguide between RT and 2 K
Warm ceramic RF window
SST helium vessel
HOM coupler (2)
RF reference probe
Warm tuner actuator not shown

## Slide 11: Integrated Cavity - Features (1)
No stiffening rings, to increase tunability
New helium vessel design, to replace titanium with stainless steel for cost and joint reliability
New tuner interface, mounts to stainless steel helium vessel endplates and allows use of proven scissor-jack tuner
C. Reece et al., SRF’07, p. 536.

## Slide 12: Integrated Cavity - Features (2)
Optimized waveguide input coupler geometry for Qext = 3.2×107
Nb HOM coupler probes confidently cooled
Optimized position and orientation of HOM couplers (now only on “field probe” side) for HOM damping

## Slide 13: C100 Cryomodules
Each cavity is powered individually to determine its maximum gradient while measuring the corresponding heat load
All the other operational systems such as tuners, HOM couplers, valves and instrumentation are qualified.
Pressure sensitivity: ~220 Hz/Torr
Lorentz force detuning: ~ -1.6 Hz/(MV/m)2
J. Hogan et al., IPAC’12, p. 2429.

## Slide 14: 2 K Dynamic Heat Load vs. Cavity Gradients in CEBAF
Chart: 
Qo = 4.3e9
Qo = 4.3e9
Qo = 6.5e9
Best for 12 GeV CMs LL
C50 | 18.9825 | 18.4555 | 16.4086 | 13.8993 | 21.4264 | 20.8707 | 18.9825 | 18.239 | 8.0056 | 18.6103 | 22.5982 | 20.4679 | 19.5948 | 9.1772 | 22.0726 | 17.5238 | 27.9154 | 24.0731 | 10.6819 | 25.1463 | 18.597 | 16.6065 | 19.7734 | 20.6331 | 10.8418 | 23.187 | 22.0726 | 19.843 | 16.8871 | 12.2501 | 13.4986 | 8.1122 | 24.3365 | 18.9825 | 11.4572 | 13.9577 | 10.908 | 27.9154 | 17.031 | 23.1494
C100 in Testlab HTB
C100-1, 2, 4, 5 | 21.1699 | 22.7761 | 35.796 | 20.8025 | 23.544 | 27.5217 | 25.4237 | 21.7886 | 30.2415 | 31.3266 | 31.5946 | 22.9664 | 21.1288 | 23.0067 | 11.5524 | 21.1504 | 12.6251 | 27.6133 | 28.6324 | 27.0481 | 27.7776 | 29.4983 | 28.0279 | 28.1419 | 28.9686 | 28.5031 | 29.3426 | 27.8165 | 29.3677 | 28.8121 | 29.1406 | 30.2514
0.7 m cavities
0.5 m cavities

## Slide 15: Bang for the Cryo Buck
Chart: 2 K Heat Load vs. Cavity Gradients in CEBAF
C100 in Testlab HTB
Qo = 5e9
Qo = 3e9
Qo = 0.8e9
C100-1, 2, 4, 5 | 0.59518 | 0.55321 | 0.37155 | 0.57205 | 0.5649 | 0.50869 | 0.52313 | 0.61041 | 0.48146 | 0.51394 | 0.46084 | 0.64007 | 0.64273 | 0.6146 | 0.7756 | 0.61228 | 0.66534 | 0.53742 | 0.44984 | 0.52277 | 0.46872 | 0.49833 | 0.4995 | 0.4925 | 0.49778 | 0.45188 | 0.46758 | 0.45297 | 0.51008 | 0.5102 | 0.53328 | 0.3656
Golden Opportunities | 0.92169 | 2.3042 | 1.8958 | 1.6118
2.07 K

## Slide 16: Conclusions
JLab has successfully developed a multi-cell SRF cavity for the 12 GeV Upgrade of CEBAF
The cavities meet the project specification of Eacc=19.2 MV/m with Q0 ≥ 8×109 at 2.07 K in CW operation
During the prototyping phase, improvements of cavity surface treatment methods lead to a change in the processing procedures initially envisioned.
Changes to multiples components of the “integrated” cavity assembly resulted from testing of prototypes in a cryomodule
JLab has accrued a broad experience on the design of cavities and components for CW applications
There is room for improvement, particularly on lowering the cryogenic losses.

## Slide 17: Acknwoledgments
C. E. Reece for providing some of the slides for this presentation