## Slide 1: CW SRF Photoinjector Experience at HZB
Andrew Burrill for the HZB Team

## Slide 2: Motivation
HZB is building a 50 MeV, 100 mA c.w. ERL that will utilize a SRF photoinjector with a CsK2Sb photocathode.
How do we try to ensure success?
A multi-stage SRF photoinjector development program.
  4 x 1.3 GHz SRF photoinjectors will be tested
  Gun 0.1 and Gun 0.2 are 1.5 cell 1.3 GHz guns utilizing a Pb photocathode
    Gun 0.1 – back wall Pb coated
    Gun 0.2 – removable Nb plug Pb coated
    Collaboration with DESY, JLab, BNL, NCBJ
  Gun 1 (1.4 cell 1.3 GHz – CsK2Sb photocathode) –in fabrication
  Gun 2 (1.X cell 1.3 GHz – CsK2Sb photocathode) –in design
    Addition of 115 kW input couplers

## Slide 3: First step: SC RF Gun0
EM design: Highest fields at cathode region
SC lead cathode on half- cell backwall: QEPb~10.QENb
Study beam dynamics at short pulses, ERL parameter range
Input coupler
Pick-up probe
Lead cathode,
Tc= 7.2 K
Excited p-TM010 mode
Original design by
Jacek Sekutowicz
Frequency p-mode | 1300 MHz
Epeak/Eacc | 1.86
Hpeak/Eacc | 4.4 mT/(MV/m)
Geometry factor | 212.2 W
R/Q (linac, b=1) | 190 W
Sekutowicz et al., Proc. PAC 2009
TTF-III FPC: QL= 1.109-6.106
including 3-stub tuner

## Slide 4: Gun 0 - Test Plan
Install the photoinjector in HoBiCaT
  study RF properties, Q vs. E, LLRF, microphonics, operation with TTF-III coupler, SC solenoid, steering magnet
Connect a diagnostic beamline
  Stripline BPM, 2 Faraday Cups, viewscreens and THZ diagnostics
Study the cathode
  measure QE, QE map, emission surface, thermal emittance and dark current before and after laser cleaning
Learn how all the systems work
Determine what needs improvement for Gun 1 & 2
Repeat

## Slide 5: Extension of the HoBiCaT Cavity Test Facility
Laser
hut
Laser beamline
HoBiCaT cryostat
Diagnostic
e- beamline
C
o
n
t
r
o
l
ro
o
m

## Slide 6: Cathode deposition at NCBJ (formerly IPJ Andre Soltan Swierk)
Plasma arc
depositon setup
in 30° configuration
Cavity with helium vessel
Mask to protect cavity
Final diameter
by BCP + special
mask: 5 mm
16 x 5min depositions result
in a few hundred nm thick
Pb cathode film
Pb cathode film
R. Nietubyc
P. Strzyzewski et al.,
Phys. Scr. T123 (2006)
Cavity without helium vessel

## Slide 7: Gun 0.1 RF measurements: Vertical and Horizontal tests (JLab and HZB)
Vertical test after fabrication, treatment and mounting Q0>1.1010
for Epeak<35 MV/m
After lead deposition Q drops significantly and field emission (FE)
onset lowered
Cavity was then vented, assembled
with TTF-III coupler and sent to HZB
Installation in HoBiCaT further Q degradation, FE onset 12 MV/m
After additional cooldown cycle
even worse, cavity collects residual
gases?
Excimer Laser cleaning of lead cathode increased onset of FE to 15 MV/m
Note: Horizontal RF tests at bc~3-4, error bar!
w/o cathode
+ cathode
horizontal
A. Neumann et al., SRF 2011

## Slide 8: Improvement of QE after laser cleaning and RF processing.
after
4th round
pre
cleaning
after
1st round
R. Barday et al., Proc. of PSTP 2011
KrF excimer laser at 248 nm with 0.045 mJ/mm2 to 0.23 mJ/mm2. Each round consisted of 300.000 shots in 10 min.
Found that laser cleaning improves QE, lowers workfunction and moves dark current onset to higher gradients
Laser cleaning required to control state of the cathode surface, as contaminants increase work function and lower QE
10-5

## Slide 9: Results from emittance measurements
Measured emittance scaling with laser spot size by solenoid scan technique.
Emittance contributions from space charge, aberrations, & astigmatism.
Setup model to estimate effect of irregular surface: local QE variation and presence of droplets and protrusions.
Protrusions cause longitudinal field enhancement and transverse defocusing field.
Findings: Emittance is dominated by beam expansion due to transverse field of these protrusions.
Emission spot imaged with solenoid on first view screen
J. Völker, Master thesis, HU Berlin, 2012

## Slide 10: Superconducting Solenoid Experience
Conduction Cooled by 1.8K
Fixed position (no mover for Gun0.1)
Lessons learnt from Gun0.1
  Cooling issues: solenoid got warm for current I > 5 A, OK for operation between 2…3 A – due to incoming leads in vacuum with poor heat intercept.
  Field shape: rather short effective length (low L/R)  spherical aberrations.
  Alignment issues: Solenoid movers required for beam based alignment

## Slide 11: Gun0.2: Upgrades and modifications
Modifications cavity 0.1  0.2
Introduce Stiff back plate (30 mm thick) with opening for Nb cathode plug.
LHe vessel demountable.
Saclay-style tuner push/pull rear wall.
JLab
NCBJ
back wall
plug
Upgrade beamline:
Installed solenoid mover allowing beam based alignment.
Replaced uncoated Ce:YAG screens with ITO coated Ce:YAG to avoid charging up phenomena.
Included slit mask in first cross for phase space measurements.
Put in segmented Faraday cup in dispersive arm to improve energy resolution.
Sol mover
A. Frahm

## Slide 12: Gun0.2 RF and beam measurement results
Removable cathode plug helps decoupling cavity treatment (HPR, BCP) and cathode preparation.
RF processing increased achievable peak field from 20 to 28 MV/m, limited by field emission and quench.
Qo performance decrease at HoBiCaT due to lack of magnetic shielding and cold leak.
A. Burrill, et al., Proc. of IPAC 2013, WEPWO002
Measured emittance with solenoid scan and slit mask, phase space with slit mask.
Emittance of 0.2 three times lower than 0.1, improved cathode surface with less protrusions. Shorter arc and slit aperture avoid formation and reach of micro-droplets
M. Schmeißer, et al., Proc. of IPAC 2013, MOPFI002

## Slide 13: Gun0.2 Tuner and microphonics
By adding a Saclay style tuner to Gun0.2 we were better able to lock the laser to the LLRF and cavity.
Tuner range was found to be linear
Transfer functions measured at various power levels, cavity appears very stable.
Chart: Gun 0.2 Tuner Range

## Slide 14: Operating Experience Summary
Several successful and insightful runs have been carried out with the Pb/Nb gun
Cavity RF performance suffers compared to VTA
  Magnetic shielding
  Cold leak
  Contamination
Beamline diagnostics worked very well
Solenoid mover helps with beam based alignment
  Care needs to be taken in solenoid design and heat intercepts
  Steering magnet also critical to getting beam out of gun
Pb cathode demonstrated and results closely match those from the cathode test system
  Laser cleaning works as expected, QE slightly lower than the bench measurements
  Cathode surface critical to emittance and dark current minimization
  Cathode plug greatly improves cleaning and sputtering processes.
Cavity tuner works well, LLRF control of cavity functioned as expected.
By addressing these items this Gun could be used as a long term electron source for a low average current application

## Slide 15: Acknowledgments
Thanks to our collaborators
Thanks to A. Neumann and T. Kamps for their slides
Thank you.
The End!

## Slide 16: Extra Slides

## Slide 17: Gun 0.1 Dark current studies
First laser cleaning treatment of cathode
increased onset level of field emission!
Dark current focussed by SC solenoid before laser cleaning
14.6 MV/m
15.0 MV/m
15.6 MV/m
15.9 MV/m
16.4 MV/m
Fowler-Nordheim fit of dark current/field emission shows reduction of field enhancement factor bNF.
Effectively emitting tip area, Ae, increases