## Slide 1: High Q R&D at Fermilab
Anna Grassellino
TTC Topical Meeting on CW SCRF
Cornell University, June 13th 2013

## Slide 2
Outline
What is typical Q and, in particular, residual and BCS resistance for standard treatments, as a function of field? (study performed at 1.3 GHz)
New processing techniques for Q maximization (studies performed at 1.3 GHz)
Transferring high Q recipes to 650 MHz cavities for PX

## Slide 3
What is Q and Rs(B) for standard treatments?

## Slide 4
Field Dependence of Surface Resistance for typical treatments
Q = G/Rs, where Rs = RBCS(T) + Rs
Crucial question – how does medium field Q-slope emerge from its components RBCS (B) and Rs (B)?
Answering allows:
  Obtain Rs(B,T) predictions for any standard treatment (EP, BCP, mild bake, anneal…) to design accelerators -> missing input for optimization
  Baseline for comparison with new, innovative treatments
  Fundamental understanding of “Q-slopes”

## Slide 5
Approach
Obtain as many Q(B,T) measurements as practical at ALL fields (not only at a single low field as is customary)
At each fixed field fit corresponding Q(T) to extract Rres
  Also gives Rbcs(T) = Rs(T)-Rres
Bath temperature
A. Romanenko and A.Grassellino
http://arxiv.org/abs/1304.4516

## Slide 6
Results (1.3 GHz)
Medium field Q slope is a combination of both R0(B) and RBCS(B)
RBCS decreases but becomes strongly field dependent after 120C
Medium field Q slope is NOT due to thermal feedback
Stronger R0(B) for BCP vs EP
A. Romanenko and A.Grassellino
http://arxiv.org/abs/1304.4516

## Slide 7
New surface processing techniques
for Q maximization

## Slide 8
A.Grassellino et al, http://arxiv.org/abs/1305.2182
Annealing with caps+ no chemistry produces extra-low residual resistance
Systematically low R0
Extra cost savings from skipping the post furnace chemical processing
See also G. Ciovati, Phys. Rev. ST Accel. Beams 13, 022002 (2010)
1.3 GHz, 2K

## Slide 9
Long annealing produces extra-low R0(B)

## Slide 10
Heat treatments in nitrogen produce unprecedented values of RBCS(B)
A.Grassellino et al,
http://arxiv.org/abs/1306.0288
1.3 GHz, 2K

## Slide 11
Heat treatments in nitrogen produce unprecedented values of BCS
1.3 GHz, 2K
1.3 GHz, 2K
1.3 GHz, 2K
Q curves as a function of material removal via EP post-nitrogen treatment:

## Slide 12
Is doping with interstitial impurities a long sought solution to the medium field Q-slope?

## Slide 13
Doping with interstitial impurities: a solution for MFQS?
The cavity baked with argon
Cavity baked at 800C for an hour in UHV, followed by an hour at 800C in partial pressure ~2x10-2 T of Argon  Q ~1x107
Then ~ 7 micron removal via EP  again anti-Qslope!
Interesting note: anti-Q-slope result recently reported by Jlab also has argon injection at high T in the preparation steps
Interstial impurities doping may be the common root of the anti-slope results
A.Grassellino et al,
http://arxiv.org/abs/1306.0288
1.3 GHz, 2K

## Slide 14
Applying the high Q recipes
to 650 MHz cavities for PX (first results)

## Slide 15
Applying the findings to 650 MHz PX cavities
Very low residual resistance (~2 nΩ) even with just baseline EP or BCP (indication of frequency dependence of residual resistance?)
Cavities have not been high temperature baked yet
HF rinse successful in raising Q! ~ 40%
Slope due to both residual and BCS
Will try annealing with caps and nitrogen/argon treatments next

## Slide 16
Conclusions
Different recipes found for Q maximization for different applications
  For applications requiring extra high Q, no operating T constraints (ie cavity QED): anneal followed by no chemistry, long anneals
  For large CW machines, where operating T range is constrained to above 1.8K: two new surface treatments have been found which:
    Reverse medium field Q-slope!
    Up to 150% gain in Q in the T range of interest for CW accelerators
Recipes are extremely simple, can be replicated at any lab with access to a standard hydrogen degassing furnace
FNAL will try soon interstitial doping on 3.9 GHz cavity: potential for even larger gains!
An improvement in BCS has the advantage to be “robust” and fully maintained in cryomodule

## Slide 17
The work presented comes from a team effort:
A.Grassellino, A.Romanenko, O.Melnychuk, A.Crawford, A.Rowe, M.Wong, D.Sergatskov, T.Khabiboulline, A. Sukhanov, Y.Trenikhina, F.Barkov, D.Bice, B.Stone, C.Baker, Y. Pischalnikov, C. Ginsburg, V.Yakovlev, R.D.Kephart

## Slide 18
 | N total | Mean | sigma | Minimum | Median | Maximum
Not tumbled | 11 | 2.6 | 0.50796 | 1.43 | 2.73 | 3.14
Tumbled | 11 | 2.69273 | 0.71337 | 1.53 | 2.51 | 4.24
 | N total | Mean | sigma | Minimum | Median | Maximum
Not tumbled | 10 | 1.777 | 0.39556 | 1.16 | 1.95 | 2.17
Tumbled | 11 | 1.89182 | 0.52759 | 0.99 | 1.98 | 2.87

## Slide 19
Heating is negligible, Rbcs increase with field is a genuine effect
Thermal feedback does not explain the medium field Q slope
From combined T-map/RF measurements

## Slide 20
After 800C 10 min with N plus 5 micron EP
(perfectly smooth, nothing noticeable)
After 800C 10 min with N plus 5 micron EP
plus 15 micron BCP, signs of preferential etching

## Slide 21: Nitrided surfaces: laser microscopy – post chemistry (10 minutes nitridization plus 10 microns BCP)
10x
20x
50x
100x