## Slide 1: High Q R&D at Cornell
Fumio Furuta
Cornell University
TTC topical-meeting on CW SRF 2013
Ithaca, NY, 13June2013

## Slide 2
What are the best surface treatment?

## Slide 3: Required cavity specs
Chart: Eacc [MV/m]
| 16.2
Cornell ERL, 1.3GHz, 1.8K | 20000000000
KEK ERL, 1.3GHz, 2K | 10000000000
XFEL, 1.3GHz, 2K | 10000000000
ILC BL, 1.3GHz, 2K | 8000000000 | 10000000000
ILC ACD, 1.3GHz, 2K | 8000000000 | 10000000000
Jlab Upgrade, 1.5GHz, 2.07K | 8000000000
Cornell ERL
KEK ERL
Jlab upgrade
XFEL
ILC, BCD& ACD

## Slide 4: Surface treatments
Material | Bulk removal | Degassing | Light removal | 120C Bake | Additional
Fine grain Large grain | BCP EP CBP Mirror finish CBP | 600C 650C 750C 800C >800C | BCP EP | 24hrs 48hrs | HF rinse
ILC, KEK-ERL
XFEL
Jlab upgrade
Cornell ERL
Many R&Ds on parameter optimization are done and on going.
-How much removal?
-How long bake?

## Slide 5: Degassing in TM-furnace
Design
Max Temp. 1450C
Vac. 1.0e-8 Torr
T-M Vacuum furnace at Newman lab.

## Slide 6: TM-Furnace qualification

## Slide 7: Series test of IS-5
Chart: Eacc [MV/m]
| 44.730000000000011 | 44.3 | 43.58 | 42.99 | 42.24 | 41.94 | 41.01 | 39.910000000000004 | 39.11 | 37.950000000000003 | 37.1 | 36.230000000000011 | 35.1 | 34 | 33.07 | 32.090000000000003 | 31.04 | 30.06 | 29.130000000000031 | 28.110000000000031 | 27.12 | 26.06 | 25.09 | 24.03 | 23.05 | 22.09 | 20.939999999999987 | 20.04 | 19.059999999999999 | 18.2 | 17.12 | 16.079999999999988 | 14.98 | 14.01 | 13.02 | 11.89 | 11.1 | 10.02 | 9.0500000000000007 | 8.15 | 7.09 | 6.09 | 5.04 | 3.9899999999999998 | 3.11
Best at KEK, EP'ed | 10800000000 | 10900000000 | 11100000000 | 11400000000 | 11500000000 | 11700000000 | 12100000000 | 12300000000 | 12600000000 | 13100000000 | 13400000000 | 13700000000 | 14300000000 | 14600000000 | 15000000000 | 15300000000 | 15500000000 | 15800000000 | 16000000000 | 16200000000 | 16500000000 | 16800000000 | 17000000000 | 17300000000 | 17500000000 | 17900000000 | 18300000000 | 18500000000 | 19000000000 | 19300000000 | 19700000000 | 20000000000 | 21100000000 | 21600000000 | 22200000000 | 22400000000 | 22500000000 | 22900000000 | 23400000000 | 23500000000 | 23900000000 | 23800000000 | 23800000000 | 24300000000 | 24100000000
mirror finish+BCP(10um) | 362675248.9814 | 393361205.301 | 418248025.5249 | 438551194.7454 | 439935643.9549 | 431863739.4087 | 386966526.7536 | 365458990.4109 | 321436853.6653 | 273718423.0553 | 249825778.2075 | 212998727.2377 | 186330043.1644 | 158778722.189 | 145805910.9863 | 134847117.1137
+850C*48h bake | 23025647979.6127 | 12266641918.6727 | 9790534085.7609 | 7043867437.4395 | 5500141936.9819 | 8696742801.4129 | 16563673468.9333 | 19847754426.8609 | 23632646264.56 | 24492054885.7377 | 23835159814.9839 | 25380938419.8611 | 23091009224.72 | 23995552911.5243 | 20353384862.0895 | 4688177181.4579 | 3748035288.7501 | 3224533528.642 | 2745771861.2369 | 2298588737.8205 | 2013337970.4993 | 1799832622.3583 | 1522258710.1077 | 1319371899.2063 | 20924866569.918 | 21612529409.6365
+BCP(10um) | 20955494067.0417 | 20618369509.7341 | 21388955785.5158 | 21757538662.8522 | 20715359110.2734 | 23914129394.6143 | 21890232797.1602 | 19638184490.076 | 19853775135.1621 | 21394537377.7241 | 20090872680.5045 | 19963020608.3844 | 20632510258.9684 | 20192295229.7033 | 20275122752.2113 | 19155400853.9009 | 19064212817.7869 | 17236936717.0697 | 16124379393.0557 | 17176239025.2626 | 16837170812.5767 | 15551699229.4434 | 14780835015.6271 | 11636608217.8565 | 11692187903.5009 | 9708860636.0503 | 8397970012.5251 | 6951483475.6435 | 5796250097.982 | 4775435234.6419 | 4920570953.7281 | 3999789224.4784 | 3510260171.728 | 3034402469.2837 | 2603921481.4475 | 2337919461.2382 | 2161223008.7265
+120C bake | 25140000000 | 27837000000 | 28623000000 | 29728000000 | 28545000000 | 29274000000 | 28574000000 | 29338000000 | 26919000000 | 24202000000 | 25070000000 | 24042000000 | 24247000000 | 22768000000 | 21397000000 | 22836000000 | 20508000000 | 20640000000 | 21683000000 | 21651000000 | 21659000000 | 20382000000 | 20209000000 | 18208000000 | 16275000000 | 16626000000 | 14823000000 | 12400000000 | 10861000000 | 10049000000 | 7613500000 | 5896200000 | 5201400000 | 4126400000 | 3176600000 | 2383600000 | 2374300000 | 2865900000
+ HF rinse | 18461000000 | 22107000000 | 22385000000 | 24390000000 | 23474000000 | 23267000000 | 24295000000 | 25785000000 | 26181000000 | 24623000000 | 22728000000 | 21356000000 | 20529000000 | 19981000000 | 18854000000 | 19480000000 | 18655000000 | 17600000000 | 17309000000 | 9830100000 | 16066000000 | 14604000000 | 13464000000 | 11241000000 | 9781700000 | 8465000000 | 6989900000 | 6079400000 | 5316300000 | 4486500000 | 3865900000
2K meas.
IS-5 series test
Limited by Q-slope, no detectable radiation

## Slide 8: T-map for single/multi-cell
8
17 [sensors/board] *38 [boards/cell]
= 646 [sensors /cell]
11 [sensors/board]x 24 [boards/cell]
= 264 [sensors/cell]
x 7 [cell/cavity]
=1,848 [sensors

## Slide 9: Multi-cell T-map
before
after
@20MV/m

## Slide 10: Coupon study
Process coupon (φ11mm) with VEP.

## Slide 11: Coupon image
11mA/cm2
15mA/cm2
28mA/cm2
37mA/cm2
equator
iris
Surface roughness analysis is on going.

## Slide 12: What are the best surface treatment?
Chart: Eacc [MV/m]
| 16.2
Cornell ERL, 1.3GHz, 1.8K | 20000000000
KEK ERL, 1.3GHz, 2K | 10000000000
XFEL, 1.3GHz, 2K | 10000000000
ILC BL, 1.3GHz, 2K | 8000000000 | 10000000000
ILC ACD, 1.3GHz, 2K | 8000000000 | 10000000000
Jlab Upgrade, 1.5GHz, 2.07K | 8000000000
High Qo
High gradient
BCP
Alternative shape,
(LL, RE, LSF)
Large grain?
120C bake
TESLA shape
12
EP
HF rinse?

## Slide 13: Summary
Systematic high Qo study on surface treatments are on going at Cornell SRF group, such as parameter optimization of BCP, VEP, CBP and furnace bake with T-map or Coupon analysis.
High Qo specs of Cornell ERL cavity has been demonstrated with simple recipe. Next step is demonstration of high yield with this simple recipe.