## Slide 1: Optimization of Vortex Pinning by Nanoparticles Using Large-Scale Simulations of Time-Dependent Ginzburg-Landau Equations
Virtual International Workshop on Nb3Sn SRF
Science, Technology, and Applications (Nb3SnSRF’20)
10 November 2020
Alexei Koshelev1, Roland Willa1,2, Ivan Sadovskyy1,3,
Andreas Glatz1,4
1 Materials science division, Argonne National Laboratory, USA
2 Karlsruhe Inst. of technology, Germany
3 Station Q, Microsoft, Santa Barbara, USA
4 Department of Physics, Northern Illinois Univ., USA
Phys. Rev. B 93, 060508(R) (2016)
Phys. Rev. B, 98, 054517 (2018)
Sup. Sci. Techn., 31, 014001(2018)

## Slide 2: Strong Pinning by inclusions in REBCO films
Best practical way to enhance critical currents
Platform for 2G HTS cables
Isolated particles (BZO, BHO, BSO, …)
MacManus-Driscoll et al., APL 2004
Song et al., APL 2006
Gutiérrez et al., Nat. Mat. 2007, APL 2007,
Obradors et al., SuST 2008
Kim et al., APL 2007
Yamasaki et al., SuST 2008
Polat et al., PR B 2011
Miura et al., PR B 2011, SUST 2013, NPG Asia Mat. 2017
REBCO=REBa2Cu3O7+d
RE = Y, Dy, Er …
BZO=BaZrO3, BHO=BaHfO3
Nanorods; Nanorods + Particles
Kang et al., Science 2006
Varanasi et al., SuST 2007, JAP 2007, APL 2008
Maiorov et al., Nat. Mat. 2009
Selvamanickam et al., APL 2015
Notes: 1. The best superconductor for power application at liquid nitrogen at present is YBCO
2. Significant progress has been achieved in enhancing its critical current
3. The best practical way to enhance pinning is to introduce nanoscale inclusions: platform for 2G HTS cables

## Slide 3: Exploration of pinning using time-dependent Ginzburg-landau model
GOAL: Quantify pinning by large-size defects
OUTLINE:
TDGL model
Single inclusion
          Single vortex: anisotropy and size dependence of pin-breaking force
          Vortex lattice: Transitions between different occupation states
Finite inclusion density
          Critical current vs Magnetic field
          Pinning regimes
Optimal particle density and diameter for fixed magnetic field

## Slide 4: Time-dependent Ginzburg-Landau (TDGL) model
Total current:
xx,y=1, xz=1/g
Infinite-l approximation (high magnetic fields), A=x(0,Bz,-By)
e(r) ⟶ pinning potential
z(r,t ) = Langevin noise
Length | Magn. Field | Current density
xab(T) | Hc2(T) | J0
Units:
Dynamics of superconducting order parameter y(r,t)
Jdp ≈ 0.385 J0
For e(r)=1:
Static model:
Valid near Tc
Can be derived microscopically (Gor’kov 1959)
Dynamics almost never realistic
Not crucial for pinning problems (quasistatic)
GPU code details: Sadovskyy et al., Journ. Comp. Phys. 294, 639 (2015)
Notes: TDGL= Very efficient way to optimize pinning
Dynamics of the order parameter. Not realistic – not very crucial for pinning
Infinite-lambda approximation - large fields

## Slide 5: Individual pinning site
Parameters:
Pinning energy Up
Pin-breaking force fp
fL
fp
Small defects, a<x: fp= Up /x
Large defects , a>x:
Vortex line energy scale
a

## Slide 6: Individual pinning site
Parameters:
Pinning energy Up
Pin-breaking force fp
fL
fp
Small defects, a<x: fp= Up /x
Large defects , a>x:
Naively fp = Up /a
not correct
Vortex line energy scale
a

## Slide 7: Depinning from large particle
a=16 x, Lz=50 x, g=1
Pin breaking force
J
B
Notes: Depinning from large-size defect is instability event mostly determined by properties of vortex line

## Slide 8: Single inclusion interacting with vortex lattice
Setup:
Nv = 36 vortex lines
single inclusion with diameter a
anisotropy g = 5
Lz=50-100x, Lx=(3/4)1/2Ly=6a0
Protocol:
Prepare pinned state
Increase current j
Monitor electric field E(t)
and lattice displacement x(t)
Extract fp from critical current jc
fp=Nv LzF0 jc/c
Willa et al.,Phys. Rev. B, 98, 054517 (2018)

## Slide 9: Single Defect: Depinning Process
1-0-1 scenario
1-1 scenario
Depinning process is strongly affected
by next approaching vortex
Enhanced by large anisotropy, g = 5

## Slide 10: Single large Defect: Depinning Process
1-1 scenario
1-2-1 scenario

## Slide 11: Pin-Beaking Force vs magnetic field
First-order transition in the ground state

## Slide 12: Different defect sizes

## Slide 13: Finite defect density
Field dependences of the critical current and pinning regimes
System size: 100x100x50 x3
[256x256x128 mesh points]
g = 5
jc
105 steps/current
106 steps/current
Sup. Sci. Techn., 31, 014001(2018)

## Slide 14: Field Dependence of critical current
Several regimes:
Power law at low fields with a smaller power than expected from strong pinning theory, amax~0.3
Rapid drop followed by peak/plateau
Typical fields are not sensitive to density
16
8
4
2
1
0.5
0.25
1.8
4.8
large inclusions: a = 4x

## Slide 15: Pin occupation
B=0.03Hc2
B=0.2Hc2
unoccupied
single-occupied
double-occupied

## Slide 16: large inclusions: Field Dependence of critical current
  May pin multiple vortices at the same time
  The double-occupancy is accompanied by a peak in the critical current
16
8
4
2
1
0.5
0.25
1.8
4.8

## Slide 17: Optimal particle Size and density at fixed magnetic field
System size: 100x100x50 x3
[256x256x128 mesh points]
Simulation time=105 per current
Occupied volume fraction f  npVp
Overlap: f  f - f2/2
diameter a and density np
Phys. Rev. B 93, 060508(R) (2016)

## Slide 18: Evolution of critical current with increasing density
IVs for different numbers of particles (occupied volume fractions)
Mechanisms of maximum:
Reducing cross section for current flow
Vortex hoping between particles
Maximum shifts to higher density
for higher field

## Slide 19: Optimal parameters
Critical current vs particle density
for different particle sizes
Global maximum for B=0.05Hc2: a ≈ 4.2x, volume fraction ≈ 0.19

## Slide 20: Compare optimal configurations
For B = 0.1Hc2
Parallel walls Jc= 0.4Jdp
Hexagonal lattice columns || H, Jc = 0.32Jdp
Random columns || H, Jc = 0.091Jdp
Random spheres, Jc of 0.061Jdp
J,H || walls
Limitations
H || columns, single field
none
H || columns
Kimmel et al., Phys. Rev. E 96, 013318 (2017)
Sadovskyy et al., PNAS 116 (21) 10291 (2019)
Optimal pinning depends on application
Notes: walls: b=2, l=9; hex columns d=3
Random columns; a=3, f=0.2

## Slide 21: Summary
Single inclusion:
  Pin-breaking force depends on magnetic field
  Change to pin occupation states ⟶ Dips in the pin-breaking force
Finite density:
  Pinning regimes ⟷ average occupation numbers of inclusions
  Peak effects at small densities
Optimal size and density depend on B
Pinning by spherical inclusions