## Slide 1: Nb3Sn growth by sequential sputtering: film morphology and its RF properties
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu
Md Nizam Sayeed, Hani E. Elsayed-Ali (Old Dominion University)
Uttar Pudasaini, Charles E. Reece (Jefferson Lab)
Grigory V. Eremeev (Fermilab)

## Slide 2: Outline
Research motivation
Research approach
Characterization results
Summary
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 3
Research motivation
Why Nb3Sn and why magnetron sputtering?
Phase | Tc (K) | Hsh (mT)
Nb | 9.25 | 200
Nb3Sn | 18.3 | 400
Nb cavities are approaching the intrinsic material limit.
Higher Tc and Hsh of Nb3Sn promise potential cavity operation at higher temperatures and higher Eacc.
Disadvantage- brittle structure and lower thermal conductivity.
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 4
Research motivation
Limitation of vapor diffused film:
Patchy regions with low Sn composition
Stoichiometry control
Advantages of magnetron sputtering:
Stoichiometry of Nb and Sn can be controlled.
Relatively less annealing temperature is required- possible to use in copper cavities.
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu
[1] U. Pudasaini, contribution at The 8th Thin films and new ideas for SRF Workshop, 2018.
[2] Becker, Chaoyue, et al. Applied Physics Letters 106.8 (2015): 082602.
Why Nb3Sn and why magnetron sputtering?
Thin patchy region with lower Sn concentration
Figure: SEM image of vapor diffused Nb3Sn film [1].
Figure: Sn concentration gradient on vapor diffused Nb3Sn film [2].

## Slide 5: Research goals
Growth technique of Nb3Sn by magnetron sputtering.
Measurement of RF superconducting properties of the fabricated films.
Design of a magnetron sputtering system of single-cell cavity coating.
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 6: Nb3Sn by multilayer sequential sputtering
Multilple layers of Nb and Sn sputter sequentially.
Deposition rate: 1 Å/s.
Sputtering pressure: 3 mTorr 20 SCCM.
Substrate rotation: 30 rpm.
Multilayers annealed: 850- 1200 °C, 1- 12 h.
Ar gas
Substrate
Nb target
Ar+
DC
Vacuum pump
Sn target
RF
Figure: Schematic diagram of the sequential sputter deposition.
Sn film
Nb film
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 7: Nb3Sn by multilayer sequential sputtering
Parameters to optimize
  Effect of annealing temperature and time,
  Effect of thickness,
  Effect of substrate temperature,
  Effect of annealing ramp rate.
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 8: Effect of annealing temperature
1 µm thick multilayer of Nb (20 nm thick) and Sn (10 nm thick) deposited.
Annealed temperature: 850, 950, 1000, 1100, and 1200 °C for 3 h.
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 9: Structural properties
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu
Figure: X-ray diffraction pattern of as-deposited and annealed films.
As-deposited film
Annealed film at 950 °C

## Slide 10: Effect of annealing temperature
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu
As-deposited
Annealed- 850 °C 3 h
Annealed- 1000 °C 3 h
Annealed- 1100 °C 3 h
Annealed- 1200 °C 3 h
Annealed- 950 °C 3 h

## Slide 11: Effect of annealing temperature
As-deposited
Annealed- 850 °C 3 h
Annealed- 1000 °C 3 h
Annealed- 1100 °C 3 h
Annealed- 1200 °C 3 h
Annealed- 950 °C 3 h
Sn ~ 23.2 %
Sn ~ 21.6 %
Sn ~ 21.6 %
Sn ~ 0.8 %
Sn ~ 6.1 %
Sn ~ 19.6 %
Tc 17.61 K
Tc 17.63 K
Tc 17.66 K
Tc 17.53 K
Tc 7.9 K
M.N. Sayeed et al. https://doi.org/10.1016/j.jallcom.2019.06.017
Figure: Resistivity vs temperature.
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 12: Effect of thickness
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu
Nb:Sn 20 nm:10 nm
Nb:Sn 30 nm:10 nm
Nb:Sn 10 nm:10 nm
Nb:Sn 40 nm:10 nm
Nb:Sn 20 nm:10 nm
Nb:Sn 50 nm:25 nm
Nb:Sn 10 nm:5 nm
Nb:Sn 200 nm:100 nm
As-deposited Sn ~ 43.6 %
As-deposited Sn ~ 20.3 %
As-deposited Sn ~ 16 %
As-deposited Sn ~ 28.4 %
Annealed Sn ~ 23.8 %
Tc 17.93 K
Annealed Sn ~ 23 %
Tc 17.84 K
Annealed Sn ~ 21.4 %
Tc 17.56 K
Annealed Sn ~ 20.2 %
Tc 17.54 K
As-deposited Sn ~ 29.5 %
As-deposited Sn ~ 27.2 %
As-deposited Sn ~ 20 %
As-deposited Sn ~ 28.9 %
Annealed Sn ~ 23.1 %
Tc 17.82 K
Annealed Sn ~ 21.7 %
Tc 17.83 K
Annealed Sn ~ 22.4 %
Tc 17.83 K
Annealed Sn ~ 21.4 %
Tc 17.84 K

## Slide 13: Effect of Nb buffer layer thickness
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu
No buffer layer
20 nm buffer layer
100 nm buffer layer
Sn ~22 %
Sn ~22 %
Sn ~23 %
Tc 17.82 K
Tc 17.81 K
Tc 17.75 K
Figure: SEM images of the annealed films with different buffer layer thicknesses.
M.N. Sayeed et al. https://doi.org/10.18429/JACoW-SRF2019-TUP079

## Slide 14: Origin of voids- TEM analysis
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 15: Origin of voids- TEM analysis
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 16: Effect of substrate temperature
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu
1 µm
Room temperature
250 °C

## Slide 17
RF surface resistant measurement
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu
Residual resistance: 3.87 ± 0.28 mΩ
Gap: 2.519 ± 0.963 meV
Critical temperature: 17.2 K

## Slide 18: Summary- Sequential sputtering
Superconducting Nb3Sn with a Tc up to 17.93 K have been achieved.
Film morphology modified with niobium buffer layer and increased substrate temperature.
Significant Sn evaporation above 950 °C.
Sn evaporation was not affected much by varied thickness.
Layer thickness should be thin to avoid delamination.
Problem to solve- voids on the surface, Sn composition control.
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 19: Acknowledgement
This material is based upon work supported by the U.S. Department of Energy, Office of Science, Office of Nuclear Physics.
Drs. Michael Kelley, Anne-Marie Valente-Feliciano, Gianluigi Ciovati, Pashupati Dhakal, Jae-Yel Lee.
Jefferson Lab technical staffs- Peter Owen, Pete Kushnick, Joshua Spradlin.
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu

## Slide 20
THANK YOU!
Frank Batten College of
Engineering & Technology
Old Dominion University: www.eng.odu.edu