## Slide 1: Surface Resistance, Frequency Dependence, and Field Limitation in Nb3Sn Cavities
Ryan Porter
Cornell University
Supported by:
U.S. DOE award DE-SC0008431: 1.3 GHz coatings + tests
NSF Award 1734189: 2.6 GHz + 3.9 GHz coatings + tests
Center for Bright Beams , NSF Award PHY-1549132: material studies
This works make use of Cornell Center for Materials Research, NSF MRSEC program (DMR-1719875)

## Slide 2: Current performance
Data taken at 4.2 K using 1.3 GHz ILC single-cells
How does performance vary with frequency?
What limits quality factors?
Q = 2·1010
What limits maximum gradients?
Eacc max ~ 17 MV/m

## Slide 3
High Frequency Cavities

## Slide 4: High Frequency Nb3Sn
All 4.2 K

## Slide 5: Cryo-Efficiency
1.3 GHz Nb at 2K
2.6 GHz Nb3Sn at 4.2K
1.3 GHz Nb3Sn at 4.2K

## Slide 6: Quench Field Frequency Dependence
The 2.6 GHz Nb3Sn cavities’ quench field is consistent with 1.3_GHz Nb3Sn cavities.
Results show quench defect does not depend on frequency!
-> Limits possible defects that cause quench
2.6 GHz
3.9 GHz (preliminary)
Quench Mechanism Frequency Independent

## Slide 7
Surface Resistance

## Slide 8: Increasing Efficiency
0 nΩ
16 nΩ
Trapped magnetic flux
“Double Gap”
BCS Resistance
Ambient fields
Thermal gradients
Surface resistance at 4.2 K and 10 MV/m
Thermal gradients
Notes: This is what I have figured out over the last 3 years

## Slide 9: Thermal currents
Nb
Nb3Sn
HOT
COLD
S – Seebeck coefficient
Generated B field
Induced thermocurrent
Cooling in a large thermal gradient will generate a large amount of trapped flux!
Slide from Daniel Hall
‘Solved’ (for Nb3Sn on Nb) by slow-cooling cavity

## Slide 10: Increasing Efficiency
0 nΩ
16 nΩ
Trapped magnetic flux
“Double Gap”
BCS Resistance
Ambient fields
Thermal gradients
Surface resistance at 4.2 K and 10 MV/m
Thermal gradients
Good magnetic shielding can eliminate
Notes: This is what I have figured out over the last 3 years

## Slide 11: “Double Gap”
RBCS for 2 Gaps (3 MV/m)
R0 ~ 5.5 nΩ (from trapped magnetic flux)
Temperature dependent resistance shows two slope behavior

## Slide 12: Tin Depleted Regions
Good Fit
Bad Fit
Data from: A. Godeke, Supercond. Sci. Tech, 2006
Model 1: Sn depleted regions (fit p, R0, vary at. % Sn)
R = (1-p)·RBCS(25%* Sn) + p·RBCS2( x-% Sn) + R0
p = percent of surface 2nd material
2.6 GHz
p ~ 1·10-5
(Possible) Conclusion: Presence of low Sn-content Nb3Sn
Is this related to quench?
S. Ginnett, “Two-Gap Superconductivity in Nb3Sn SRF Cavities,” Cornell CLASSE REU Report, Aug. 2020, https://cornell.app.box.com/s/uyq28qj9q7vuxu1mn6appcuoiv9m4hek

## Slide 13: Normal Layers
Nb
3 µm Nb3Sn
~5 nm Oxide
Model 2: Proximity coupled normal layer:
Oxide layer on surface
  Normal conducting?
Thin layer of Sn?
Normal layer “proximity coupled” to superconductor
  Normal layer gains superconductivity
  Depresses superconductivity nearby
Using model by Gurevich and Kubo
  Solves Usadel Equations

## Slide 14: Normal Layers
Model 2: Proximity coupled normal layer:
Can fit data nicely for some parameter sets
Need more experimental data to narrow down correct model
Conclusion: Other models could explain ‘double gaps’
S. Ginnett, “Two-Gap Superconductivity in Nb3Sn SRF Cavities,” Cornell CLASSE REU Report, Aug. 2020, https://cornell.app.box.com/s/uyq28qj9q7vuxu1mn6appcuoiv9m4hek

## Slide 15: Removing Second Gap
Good news:
Removing ‘second gap’ will reduce resistance
May be over-estimating BCS-resistance of good Nb3Sn
  By how much?
  Needs more modeling/work
S. Ginnett, “Two-Gap Superconductivity in Nb3Sn SRF Cavities,” Cornell CLASSE REU Report, Aug. 2020, https://cornell.app.box.com/s/uyq28qj9q7vuxu1mn6appcuoiv9m4hek
Potential improvement
4.2 K
2.6 GHz

## Slide 16: Increasing Efficiency
0 nΩ
16 nΩ
Trapped magnetic flux
“Double Gap”
BCS Resistance
Surface resistance at 4.2 K and 10 MV/m
Q = 2·1010
4·1010
Could remove?
Notes: This is what I have figured out over the last 3 years

## Slide 17
Quench Field Limitations

## Slide 18: Limitations in quench field
Fermilab’s best cavity
Nb3Sn cavities consistently quench at fields between 14_and 18_MV/m in CW operation
The superheating field suggests we can achieve fields up to 96 MV/m!
14 MV/m
18 MV/m
Conclusion: Small Range of Quench Fields

## Slide 19: What is limiting the quench field?

## Slide 20: Quench Field Impact of Sn Depletion
Could Sn depleted regions (directly) cause quench?
  Quench field change with temperature too small

## Slide 21
Quench 4.2 K vs 2 K
  Quench fields within ~1% (~3.4% error bar)
No temperature dependence of quench field!
  Limits possible quench mechanisms
Quench Field Temperature Dependence
Q vs E to Quench at 4.2 K and 1.7 K
and 2.6 GHz
Conclusion: 1. Quench Mechanism Temperature Independent
2. Sn-depleted regions are not (directly) responsible for quench
Notes: Rules out Sn depleted as quench on second slide. Show my plot.

## Slide 22
Thermometry

## Slide 23: T-Map experiment
T-Map sensor
Niobium surface
Thermal paste
Pogo stick
Connector leads
Use temperature map to look for quench mechanism/site:
T-Map board

## Slide 24: Localised quench
Nb3Sn cavities are limited by a quench at a localized spot
What could be at fault?
Conclusion: Quench is localized

## Slide 25: What is happening at the surface?
Cut out this region and examined with microscopy
Nothing obvious except Nb grain boundary cliff
  Rough Surface
Nb3Sn surface
Nb substrate grain boundary?
Quench Site

## Slide 26: Quench Videos
~1 Minute
Exposure Picture
Old Systems
Old New System
50 kHz
Video

## Slide 27: Cavity Quench
Preliminary. Only finished commissioning. Have seen interesting dynamics.
Have seen temperature jumps.

## Slide 28: Near quench behavior
Measure temperature of sensor near the quench point as field is increased
Sudden jumps in temperature
Temperature
Max Field
Time

## Slide 29: Near quench behaviour
Previous conclusion: The sudden nature of these jumps and hysteresis suggests flux entry
Conclusion: Vortex entry a candidate for quench

## Slide 30: Grain boundary flux penetration
Increasing current across boundary
Power dissipated
Ahmad Sheikhzada and Alex Gurevich
Physical Review B 95, 214507 (2017)
arXiv:1702.02843
Notes: Grain acts as Josephson Junction. Flux expands across whole boundary. Blocks Current.

## Slide 31: Surface Roughness
Nb3Sn we create is rougher than EP Nb
  ~1 µm peak to peak
This causes large enhancement of the surface magnetic field

## Slide 32: Grain Boundary Flux Penetration (BYU)
Center for Bright Beams (CBB): A. R. Pack, M. Transtrum (BYU): MOP017
Poor grain boundary geometry -> lower flux entry field
Geometry effect: T, f independent*
Ginzburg-Landau Simulation of Vortex Nucleation In Grain Boundaries
*in cavity operating range (f << 1/Tvortex nucleation, T << Tc)
Hsh Reduction from Surface Defect

## Slide 33: Grain Boundary Pinning (BYU)
A. R. Pack, M. Transtrum (BYU):
Conclusion: Grain boundary geometry/roughness lowers quench field
See M. Transtrum’s Tuesday talk “Time-Dependent Ginzburg Landau simulations to guide Nb3Sn SRF cavity development”

## Slide 34
Thermal Modeling
20 K
2.015 K
2 K Helium
3 µm Nb3Sn +
3 mm Nb +
3 µm Nb3Sn
T

## Slide 35: Thermal Modeling
Wrote multilayer thermal equilibrium solver
  Based on Cornell HEAT code
  Temperature dependent conductivities, resistances, etc.
Modeling temperature jump (equilibrium)
Model: smallest jump: ~750 µW
Temperature on Outside of Cavity vs r
Problem:
~40 µW (in 1 µm radius area) causes thermal runaway in pure Nb3Sn
Observed Temperature Rise*
*Assuming Kapitza resistance is the same as Nb, 0.35 sensor efficiency.

## Slide 36
A small region of normal conducting will not cause thermal runaway
Beyond a critical size it will cause thermal runaway
Thermal Runaway in Single Material

## Slide 37
If a defect is generating heat, there will be a critical heat load before quench
Beyond heat load, quench occurs
Q < Qcrit
Q > Qcrit
Qcrit ~ 40 µW in Nb3Sn
Thermal Runaway in Single Material

## Slide 38: Thermal Runaway in Single Material
1D model: infinite volume of material. Spherically symmetric defect (radius r0) in the middle. Integrate heat over a sphere radius r.
k is more of the form below and involves elliptical integrals. Computation is then numerical.
For Nb3Sn critical size (T(r0) = Tc_effective) is ~1 µm, and for Nb is about ~100 µm
Niobium can support a much larger normal conducting region than Nb3Sn

## Slide 39: Thermal Runaway in Bilayer material
Since the critical size in Nb3Sn is smaller than Nb, Nb3Sn could enter local runaway, until it is in good enough contact with the Nb
  Contact with Nb thermally stabilizes the region
Rough guess, 3 µm radius as stable gets ~1 mW heating
  Roughly observed heating in experiment from 1 jump*
kNb3Sn < kNb
kNb3Sn
kNb

## Slide 40: Can Normal Regions Form in the Model?
See stable normal conducting regions in model
Size determined by film thickness + thermal parameters

## Slide 41: Revisiting Temperature Jumps
Alt. interpretation: Jumps caused by normal islands forming. Quantized nature is because size/heating is characteristic of film.

## Slide 42: Experimental Data Summary for Quench Mechanism
Narrow range of quench fields
Quench localized
Quench site warms just before quench + quantized
  Vortex entry?
  Thermal effect/’local quench’?
High surface roughness -> Can decrease quench field
No temperature dependence
No frequency dependence
Likely have Sn depleted regions

## Slide 43: Conclusions
Nb3Sn performs well at 2.6 GHz
  Same cryo-efficiency and Eacc while more compact
Quality factors limited by ‘double gap’
  Possibly caused by Sn-depleted regions
  Could potentially
What is main quench limitation?
  Vortex entry at grain boundary -> reduce roughness
  Sn depleted regions -> improve stoichiometry
  Local quench -> reduce film thickness
    Can be triggered by other mechanisms

## Slide 44: Acknowledgements
The Cornell Nb3Sn program is supported by:
U.S. DOE award DE-SC0008431: 1.3 GHz Nb3Sn tests and Nb3Sn R&D
NSF Award 1734189: 2.6 GHz and 3.9 GHz tests and R&D
Center for Bright Beam (NSF Award 1549132): Materials studies
This works make use of Cornell Center for Materials Research, NSF MRSEC program (DMR-1719875)
Prof. Matthias Liepe
Prof. Tomas Arias
Prof. David A. Muller
Prof. James P. Sethna
Prof. Mark Transtrum
Dr. Danilo Liarte
Dr. Zeming Sun
Dr. Daniel Hall
Paul Cueva
Nathan Sitaraman
James Maniscalco
Nilanjan Banerjee
Alden Pack
James Sears
Greg Kulina
John Kaufman
Holly Conklin
Terri Gruber
Paul Bishop
Sam Ginnett
with special thanks to