## Slide 1: Growth Studies and Optimization of Nb3Sn Coatings
Ryan Porter
Cornell University
Supported by:
U.S. DOE award DE-SC0008431: Coating Furnace Development + Cavity Coating
Center for Bright Beams , NSF Award PHY-1549132: material studies
This works make use of Cornell Center for Materials Research, NSF MRSEC program (DMR-1719875)

## Slide 2: Nb3Sn Coatings
2 μm
Nb3Sn forms a polycrystalline layer on the surface of the niobium
1 μm
≈3 μm
RF Surface
1 μm
Nb
Nb3Sn
Before Coating
After Coating

## Slide 3: Sn-Depleted Nb3Sn
Tc vs. Tin Content
A. Godeke, Supercond. Sci. Tech, 2006
Nb3Sn Phase Diagram
16 – 25% Sn
Nb3Sn
Sn-depleted Nb3Sn has poor superconducting properties
25% Sn
22% Sn
19% Sn
Nb
Sn
Nb3Sn Structure

## Slide 4: Sn Depleted Surface and Grains
Sn depleted regions on surface or in layer
Nb3Sn EDS Cross-section
Depleted Region
Sn Depleted Grain on Surface
Annealed too long
2 µm of Nb3Sn

## Slide 5: Thin Regions
Nb substrate
Nb3Sn
400 nm
Not thick enough
to fully shield RF
No Thin Regions
Has Thin Regions
D. L. Hall et. al. “First Results From New Single-cell Nb3Sn Cavities Coated at Cornll University,” in proc. of IPAC17, Copenhagen, Denmark, 2017
Q vs E at 4.2 K of Nb3Sn Cavities

## Slide 6: Resolving thin film regions
Red: too thin Blue: sufficiently thick
Not pre-anodised
Pre-anodised substrate
Growing the substrate oxide prior to coating suppresses the formation of thin film regions

## Slide 7: Surface Roughness and Quench Fields
Surface Roughness:
Rough surface → increased magnetic field on some surfaces
  Quench field decreased by 1/3 (?)
Poor grain boundary geometry can decrease magnetic flux entry barrier
  A. R. Pack, M. Transtrum (BYU): SRF’19 conference (Dresden): MOP017
Enhancement Factor (Hrough/Hsmooth)

## Slide 8: Questions To Answer
Why do Sn depleted regions form?
Why do thin regions form? Why does anodization prevent it?
Why is the Nb3Sn surface rough? Can we fix it?

## Slide 9: The Nb3Sn Vapor Diffusion Process
UHV Furnace
Coating chamber
S. Posen and M. Liepe, Phys. Rev. ST Accel. Beams 15, 112001 (2014).
Tin source
Secondary heater
Primary heater
Cavity
Nucleation agent (SnCl2 )
“Wuppertal” configuration, i.e., with secondary heater for the tin source
Optimized nucleation and temperature profile

## Slide 10: Layer Growth Studies
Time
Temperature
500 C
1100 C
1350 C
Nucleation
Coating
Anneal
Want to understand how surface grows
Stop growth at different steps and examine surface
Notes: Why does this work? Well, let’s take a stop-motion capture of the growth of the layer, as we move from the nucleation stage, in which the layer is seeded with tin, and the coating stage, in which the layer grows.

## Slide 11: Stop-motion sequence
Time
Temperature
START
Pre-anodised
Not pre-anodised
2 µm
70 nm oxide
5 nm oxide
1 µm
1 µm
Notes: Oxide is about 70 nm thick, naturally is 5 nm

## Slide 12: Stop-motion sequence
Pre-anodised substrate
Not pre-anodised
2 µm
Time
Temperature
500°C
1 µm
1 µm

## Slide 13: Stop-motion sequence
Not pre-anodised
Time
Temperature
500°C
200 nm
50
%
0
Niobium + Sn rich ‘blob’ (NbSn2 + Sn liquid?) + Nb3Sn
1 µm

## Slide 14: Stop-motion sequence
Pre-anodised substrate
Time
Temperature
500°C
200 nm
50
%
0
Niobium + Sn rich ‘blob’ (NbSn2 + Sn liquid?) + Nb3Sn blobs + oxide layer + Nb3Sn forming under the oxide
1 µm

## Slide 15: Stop-motion sequence
Pre-anodised substrate
Not pre-anodised
2 µm
Time
Temperature
500°C
1 µm
1 µm

## Slide 16: Stop-motion sequence
Pre-anodised substrate
Not pre-anodised
2 µm
Time
Temperature
800°C
1 µm
1 µm

## Slide 17: Stop-motion sequence
200nm
Not pre-anodised
50
%
0
Time
Temperature
800°C
Niobium + Thin Nb3Sn Layer + amorphous Nb3Sn + Nb6Sn5
1 µm

## Slide 18: Stop-motion sequence
Time
Temperature
800°C
Niobium + Thin Nb3Sn Layer + amorphous Nb3Sn + Nb6Sn5
Pre-anodised substrate
50
%
0
100 nm
1 µm

## Slide 19: Initial Growth: Lessons
non-preanodized
preanodized
nucleation
800° C
50
%
0
200nm
Sn
Non-anodized:
Nb + Sn diffusion
N. Sitaraman, T. Arias
D. Muller, P. Cueva
Simulation of Diffusion and Growth
TEM/EDX of Nb3Sn Throughout Growth
Initial growth:
Thin Nb3Sn forms very early
Nb3Sn
Nb
Nb
Sn
Sn
Anodized:
Oxide acts as barrier
Creates more Sn nucleation sites
NbOx
Nb
Nb
Sn
Nb3Sn
Nb3Sn

## Slide 20: Stop-motion sequence
Pre-anodised substrate
Not pre-anodised
2 µm
Time
Temperature
800°C
1 µm
1 µm

## Slide 21: Stop-motion sequence
Pre-anodised substrate
Not pre-anodised
2 µm
Time
Temperature
875°C
1 µm
1 µm

## Slide 22: Stop-motion sequence
Not pre-anodised
1 µm
200nm
50
%
0
Time
Temperature
875°C
Sn-Rich regions phase-transition to Nb3Sn and break into crystals

## Slide 23: Stop-motion sequence
Pre-anodised substrate
200nm
50
%
0
Time
Temperature
875°C
1 µm
Sn-Rich regions phase-transition to Nb3Sn and break into crystals

## Slide 24: Stop-motion sequence
Pre-anodised substrate
Not pre-anodised
2 µm
Time
Temperature
875°C
1 µm
1 µm

## Slide 25: Stop-motion sequence
Pre-anodised substrate
Not pre-anodised
2 µm
Time
Temperature
950°C
2 µm
2 µm

## Slide 26: Stop-motion sequence
Pre-anodised substrate
Not pre-anodised
2 µm
Time
Temperature
1120°C
2 µm
2 µm

## Slide 27: Theory Insights
[0.1 ns runtime]
Key Takeaways:
Sn diffusion through Nb3Sn Crystal slow
  Fast through grain boundaries
Energetically favorable to grow Sn-depleted Nb3Sn if out of Sn
Theoretically Calculated Phase Diagram
N. S. Sitaraman et. al., “Ab Initio Study of Antisite Defects in Nb3Sn: Phase Diagram and Impact on Superconductivity,” https://arxiv.org/abs/1912.07576
Sn
Nb3Sn
Nb
Nb
Sn
Nathan Sitaraman
Notes: We need to be able to alter the prevalence of all these features to see how they affect the quench field. We’re using sample studies, as well as simulation codes, to understand how the layer growth works, and how we can modify the coating recipe to change RF performance – show movie before this

## Slide 28: Nb3Sn growth mechanism
Slow
Fast
Early growth:
Sn + Nb diffuses through Nb3Sn
Later growth:
Tin moves down through grain boundaries
Sn
Nb3Sn
Nb
Sn
Nb3Sn
Nb
Sn
Nb3Sn
Sn
Sn
Nb
Nb

## Slide 29: Why do thin regions form?
‘Poor’ nucleation creates some large single grain Nb3Sn
Slow Sn diffusion slows growth
Nb3Sn
Nb
Diffusion Limited Growth
1 µm
1 µm
2 µm

## Slide 30: Why do Sn Depleted Regions Form?
Nb3Sn EDS Cross-section
Depleted Region
time (Hours)
Excess surface tin (arb. units)
time (Hours)
Excess surface tin (arb. units)
More Nucleation Agent
No available Sn
Available Sn!
Sn depleted region formed by running out of Sn
Can fix by adding more Sn at key time
Don’t anneal for too long
Nb3+Sn1-
Nb3Sn
Grain Boundaries
Nb3+Sn1-
Nb
Nb3Sn
Available Tin During Coating

## Slide 31: Why is Nb3Sn Rough?
Nb3Sn roughness comes from growth
  Bad Sn nucleation -> rough surface
  Good Sn nucleation -> smooth surface
2 μm
200 nm
200 nm
200 nm
500 C
800 C
875 C
2 µm
2 µm
2 µm
Nb3Sn Growth:
50
%
0

## Slide 32: Questions Answered
Why do Sn depleted regions form?
  Running out of Sn
  Kinetic process
Why do thin regions form?
  Nb3Sn forms early without an oxide barrier
  Sparse nucleation sites
  Anodization improves both
Why is the Nb3Sn surface rough? Can we fix it?
  Poor nucleation likely causes some roughness

## Slide 33: Conclusions
Insights:
Nb3Sn forms early in the process
Oxide layer acts as a barrier, delaying growth and creating more nucleation sites
Thin regions and rough surface come from ‘poor’ nucleation
Sn diffusion through crystal slow, through grain boundary fast
Proposed optimizations:
Better nucleation to reduce roughness
More SnCl2 to prevent Sn-depleted pockets

## Slide 34: Acknowledgements
The Cornell Nb3Sn program is supported by:
U.S. DOE award DE-SC0008431: Coating furnace development + cavity coatings/tests
Center for Bright Beam (NSF Award 1549132)
This works make use of Cornell Center for Materials Research, NSF MRSEC program (DMR-1719875)
Prof. Matthias Liepe
Prof. Tomas Arias
Prof. David A. Muller
Dr. Daniel Hall
Paul Cueva
Nathan Sitaraman
Michelle Kelley
James Sears
Greg Kulina
John Kaufman
Holly Conklin
Terri Gruber
Paul Bishop Katherine (Jixun) Ding
with special thanks to