## Slide 1: Investigation of Nb3Sn Thin Films using Magnetic Field Penetration Measurements
PhD Graduate Student
International workshop on SRF Science, Technology and Applications (Nb3SnSRF20), Cornell, Nov. 10, 2020.
This work is supported by NSF Grants PHY-1734075 and PHY-1416051, and DOE Awards DE-SC0010081 and DE-SC0019399

## Slide 2: MOTIVATION
Bulk Nb
Insulating layers
Superconducting layers
Typical Nb cavity
Single Cell SRF Cavity
Multilayer Structure
Bulk Nb
Layered
Nb3Sn is the most promising material for superconducting layers

## Slide 3
Design, build and calibrate a simple, efficient and accurate technique to measure onset magnetic field penetration directly through bulk, thin film and multilayer superconducting samples.
OBJECTIVE
Superconducting Magnet
Sample
Hall probe
Basic experimental setup

## Slide 4
Adapted from C. Z. Antoine et al 2019 Supercond. Sci. Technol. 32 085005
The field lines in the Meissner state and in the mixed state

## Slide 5
DESIGN AND FABRICATION

## Slide 6: DETAILED EXPERIMENTAL SETUP
External (top) and internal (bottom) view of nonmagnetic container which supports the sample, solenoid magnet, and Hall probe symmetrically
To maintain fixed distance (0.5 mm) between the sample and the magnet
To keep sample intact during the experiment
To push the magnet down
To pass the high current
To measure onset penetration of the magnet field
To generate magnetic field parallel to the sample

## Slide 7
HALL PROBE CONFIGURATION
0.00 mm
4.00 mm
10.00 mm

## Slide 8
Field from the magnet on the sample
In the Meissner state the sample acts as a magnetic mirror.
Vertical component of the magnetic field cancels out.
The field felt by the sample is equal to twice the radial component of the magnetic field.
Since the radial magnetic field is parallel only to one side of the sample, this field configuration closely resembles the SRF cavities.
Field lines from the right half of solenoid magnet placed above the superconducting sample
( From Poisson Simulations)
Variation of the radial magnetic field along the sample radius at 100 A
(From Poisson Simulations)

## Slide 9: SUPERCONDUCTING SOLENOID MAGNET
NbTi Superconducting solenoid magnet before (top) and after (bottom) applying an epoxy
Magnet winding setup

## Slide 10
CALIBRATION

## Slide 11
STEP 1: With No Sample at 4.35 K

## Slide 12
Separation between magnet and the sensor, d (mm) | Magnetic Field for 100 A (mT) |  | Percentage Difference
 | Simulation | Experimental | 
1.368 | 517 | 445 | 13.90%
1.815 | 445 | 445 | 0%
STEP 1: With No Sample
1.815-1.368= 0.447 mm difference
Correction factor
Finding the correction factor to match experimental field with the simulation

## Slide 13
551 mT at 100 A
STEP 2: With Sample
Poisson Simulation for
d= 1.018 +0.447= 1.465 mm
Correction factor
Simulation of surface field by adding correction factor
Maximum Surface Field = 5.51 mT/A

## Slide 14
29.9 A
At 4.35 K
At 1.97 K
 | First Critical Field of Nb (mT) | 
 | At 4.35 K | At 1.97 K
From Reference [9] | 135.60 | 166.12
Experimental | 134.44 | 164.75
STEP 2: With Sample- Nb foil (88.9 μm thick)
)

## Slide 15
Hall Probe response against 99.99% pure Pb, Ta, Nb samples (50 mm in diameter and 0.1 mm in thickness) while powering up the magnet with gradually increasing current
The calibration curve of the experimental setup
[7], [8], [9]
STEP 3: Using Bulk Superconductors (100.0 μm thick)

## Slide 16: THICKNESS EFFECT ON FIELD PENETRATION
A Nb foil (From Advent Research Materials Ltd ) was used.
Thickness was reduced by BCP starting from 125 μm.

## Slide 17: HYSTERISTIC BEHAVIOUR
At 4.35 K
At 1.97 K

## Slide 18: THIN FILM MEASUREMENTS

## Slide 19: MEASUREMENTS OF THIN FILM SUPERCONDUCTORS
Nb thin film with thickness 1.8 µm deposited on sapphire plate using Electron Cyclotron Resonance (ECR)
(From Anne- Marie Valente Feliciano, Jlab)
Nb3Sn thin film with thickness 1.5 µm deposited on sapphire plate using Magneton Sputtering
(From Nizam Sayeed, Jlab)
At 4.35 K
At 1.97 K
Nb
Nb3Sn

## Slide 20
CONCLUSION AND FUTURE WORK
The new experimental technique for magnetic field penetration measurements of superconducting samples was designed, built and calibrated successfully at Jefferson Lab. This technique is appropriate for bulk samples as well as thin films.
Future work mainly focus on thin film and multilayer measurements
We are more than happy to get samples from others for our measurements
  Samples should be 50 mm in diameter
isene001@odu.edu

## Slide 21: REFERENCES
[1] H. Padamsee, “RF superconductivity: Science, Technology and Applications”, Wiley-VCH, Weinheim, 2009, pp. 72-83.
[2] A. Gurevich, “Enhancement of rf breakdown field of superconductors by multilayer coating”, Appl. Phys. Lett. 88, 012511, 2006
[3] A. Gurevich, “Theory of RF superconductivity for resonant cavities”, Supercond. Sci. Technol. 30, 2017.
[4] C. Z. Antoine et al 2019 Supercond. Sci. Technol. 32 085005
[5] N. Katyan, C. Z. Antoine, “Characterization of thin films using local magnetometer”, presented at SRF 2015, Whistler, BC, Canada, paper TUPB058.
[6] O. B. Malyshev, L. Gurran, S. Pattalwar, N. Pattalwar, K. D. Dumbell, R. Valizadeh, A. Gurevich, “A facility for magnetic field penetration measurements on multilayer S-I-S structures ”, presented at SRF 2015,Whistler, BC, Canada, paper TUPB059.
[7] G. Chanin, J. P. Torre, “Critical Field Curve of Superconducting Lead”, Phys. Rev. B, Vol. 5, No. 11, 1972.
[8] C. H. Hinrichs, C. A. Swenson, “Superconducting critical field of tantalum as a function of temperature and pressure”, Phy. Rev. Vol. 123, No. 4, 1961.
[9] T. Junginger, S. H. Abidi, R. D. Maffett, T. Buck, M. H. Dehn, S. Gheidi, R. Kiefl, P. Kolb, D. Storey, E. Thoeng, W. Wasserman, R. E. Laxdal, “Field of first magnetic flux entry and pinning strength of superconductors for rf application measured with muon spin rotation”, Phy. Rev. Accel. Beam 21, 032002, 2018.
[10] I. H. Senevirathne, J. R. Delayen, G. Ciovati “Measurement Of The Magnetic Field Penetration Into Superconducting Thin Films”, presented at SRF 2019, Dresden, Germany, paper THP050

## Slide 22
Thank You !
Acknowledgement
Advisor : Jean Delayen
Alexander Gurevich
Gianluigi Ciovati
Anne-Marie Valente-Feliciano
Nizam Sayeed
Jlab SRF staff and the machine shop staff