## Slide 1: Persistence of the Nb(100) Surface Oxide Reconstruction at Elevated Temperatures
Caleb J. Thompson, Ali A. McMillan, Jacob D. Graham, Sarah A. Willson, Rachael G. Farber, and S. J. Sibener
Advisor: Steven Sibener
University of Chicago
Department of Chemistry
Nb3Sn SRF 2020

## Slide 2: Helium Atom Scattering Will Characterize Surface Oxide Behavior on Nb
HAS’s unique capability to analyze a high temperature regime of surface structures will provide novel insight into O and Sn behavior during Nb3Sn film growth on oxidized Nb.
High T/ Sn deposition
Tin
Center Niobium (BCC)
Corner Niobium (BCC)
Oxygen
well-known (3x1)-O Nb(100)
unknown O and Sn behavior

## Slide 3: What Are the Scientific Questions We Want to Answer?
What surface structure and chemical composition for the Nb(100) face interacts with deposited Sn?
How does the surface evolve structurally at elevated temperatures?
Does oxygen dissolve into the Nb bulk in the range of Sn deposition and Nb3Sn film growth?

## Slide 4: Variations in Surface Oxide Significantly Impact Nb3Sn Film Growth
Typical Nb3Sn film growth procedure
Understanding the oxide surface that interacts with Sn is critical to understanding Nb3Sn film growth.
R. D. Porter, T. Arias, P. Cueva, D. L. Hall, M. Liepe, J. T. Maniscalco, D. A. Mueller, N. Sitaraman. LINAC’18, Beijing, China, 462-465 (2018)
Oxide
Sn
Thick Nb3Sn
Thin Nb3Sn
500
700
900
1100
1300
1500
1700
(K)
1293 K
SnCl2  Sn + Cl2
 Nb3Sn forms

## Slide 5: Film Growth Occurs in High Temperature Regime of Niobium Oxide Surface Structure
Nb2O5
NbO2
NbO
Nb
NbO
?
1st order
Ea = 134 ± 16 kJ/mol
A = 8.0 107.0 ± 0.4 s-1
1st order
Ea = 180 ± 18 kJ/mol
A = 5.4 1010.0 ± 0.5 s-1
1st order
Ea = 174 ± 6 kJ/mol
A = 8.9 1010.0 ± 0.3 s-1
For Ts > 598 K
For Ts > ?
Ts = ?
Ts = ?
Kinetic Data: B. King, H. Patel, D. Gulino, B. Tatarchuk. Thin Solid Films. 192, 351-369 (1990).
Many studies confirm O dissolution of Nb2O5 above 598 K in UHV on (100), (110), (111), and polycrystalline Nb surfaces.

## Slide 6: Structure of the Surface at Elevated Temperatures Has Never Been Observed
Nb
NbO
?
For Ts > ?
Ts = ?
Ts = ?
Surface structure during these anneals has never been observed.
Auger Electron Spectroscopy Data
Data taken at room temperature!
H. H. Farrell, H. S. Isaacs, M. Strongin. Surf. Sci. 38, 31-52 (1973).
Thermal history (K)
0
800
1300
1800
2300

## Slide 7: NbO Surface Has Been Well Characterized at Low Temperatures
B. An, M. Xu, S. Fukuyama, and K. Yokogawa. Phys. Rev. B. 73, 205401 (2006).
R. D. Veit, N. A. Kautz, R. G. Farber, S. J. Sibener. Surf. Sci. 688, 63-68 (2019).
STM image of Nb(100) (3x1)-O
NbO superlattice structure on (100) is the (3x1)-O which has only been characterized at RT only.
Vbias = -0.5 V, I = -19 pA, TSTM = 300 K
Nb(100) (3x1)-O
Center Niobium (BCC)
Corner Niobium (BCC)
Oxygen
Surgers, C., Schock, M. & Lohneysen, H. v. Surf. Sci. 471, 209–218 (2001).
NbO on…
(100) has long-range order
(110) is quasi periodic
(111) has no long-range order

## Slide 8: Helium Atom Scattering (HAS) Is Uniquely Suited to Study Surface Structure and Dynamics
Strictly surface sensitive
Non-destructive
De Broglie wavelength well matched to atomic scale features
Well matched to single-phonon energies
Single translational degree of freedom for collisions
Scattering helium
Electron cloud
Surface lattice/phonons

## Slide 9: Helium Atom Scattering Instrument
He beam energy: 10 – 100 meV
Sample temperature: 300 – 2000 K
Incident and final angles are varied independently
  Incident angle: 20° – 40°
He
Helium Beam Source
Nozzle
Skimmer
Chopper Wheel
Rotatable
Detector Arm
Nb Sample
Bell Jar
LEED
Auger

## Slide 10: Oxygen Superlattice Diffraction Peaks Are Visible with HAS at 1130 K
A (3x1) superlattice diffraction peak appears in the direction
Each diffraction scan was taken 2-3 times (consecutively) to ensure there was no hysteresis.
LEED
Nb(100) (3x1)-O
(01)
The (3x1)-O superlattice appears to be stable up to at least TS = 1130 K.

## Slide 11: Intense Specular Peak in Other Azimuthal Alignment Allows Addition Intensity and Line Shape Analysis
Specular intensity is much higher when aligned along axis and appears to corroborate surface stability up to 1210 K.
LEED
Nb(100) (3x1)-O
Rotated azimuthal angle so He beam is aligned along the axis
Specular intensities are ~30x greater than in direction
(11)

## Slide 12: Debye-Waller Analysis Shows Similar Values Along Both Crystal Axes
Debye-Waller Analysis for |  | 
(K-1) | 0.0023 ± 0.0005 | 0.0020 ± 0.0004
 | 6.32 | 6.32
(Å-1) | 12.68 | 12.67
(meV), assumed | 7 | 7
(Å2 K-1) | (1.4 ± 0.3) x 10-5 | (1.2 ± 0.3) x 10-5
 | 0.0023 ± 0.0005 | 0.0020 ± 0.0004
 | 6.32 | 6.32
 | 12.68 | 12.67
 | 7 | 7
 | (1.4 ± 0.3) x 10-5 | (1.2 ± 0.3) x 10-5
[1] W. Weingarten. Phys. Rev. ST Accel. Beams. 14, 101002 (2011).
Note: calculated Debye temperature for NbO is 472 K [1]
Excellent fit of Debye-Waller analysis shows that thermal decay of specular is only due to increase in thermal vibrations and not structural changes.

## Slide 13: Specular Peak Lineshape Analysis Leads to Average Surface Domain Size
Average surface domain size is Å.
Specular peak in direction is
intense and narrow, so we can calculate the average surface domain size:
= peak broadening from average domain size
= experimental peak FWHM =
= instrument function =
Average surface domain size
Å

## Slide 14: Lineshape Analysis Confirms (3x1)-O Ladder Structure Stability to at Least 1130 K
Lineshape analysis verifies stable surface coherence length indicating both structure and order are stable up to at least 1130 K.
A change in the FWHM of the specular peak’s elastic portion in direction would indicate changes in surface order
Nearly constant peak widths point to surface stability through 1210 K

## Slide 15: AES Peak Analysis Reveals Constant Near Surface Oxygen Content Up to 1150 K
Relative peak intensities of O/Nb AES peaks do not significantly change, showing that surface structure, order, and composition persist up to 1130 K

## Slide 16: Conclusion
(3x1)-O Nb(100) reconstruction is stable and ordered up to 1150 K.
Nb SRF surface’s interaction with Sn is mediated by an oxide layer.
  Sn adsorption
  Sn diffusion
  Nb3Sn film growth
Understanding this oxide layer will provide a critical foundation for understanding Nb SRF cavities’ interaction with Sn and Nb3Sn growth.

## Slide 17: Future Work
Elucidate bonding at surface through surface phonons to understand surface’s initial reaction with deposited Sn.
Investigate mobility of extra O and Sn on surface to understand the role of excess oxygen on Nb3Sn film growth.
Creation
Annihilation
Bonding model
Characterize diffusion
Reveals
Diffusion constant
Diffusion mechanism
Diffusion activation energy
Anisotropy

## Slide 18: Acknowledgments
Prof. Steven Sibener
Prof. Tomas Arias
Dr. Jacob Graham
Alison McMillan
Michelle Kelley
CBB
Sibener Group