## Slide 1: Thin-film CVD Nb3Sn Coating Process Development for Copper SRF Cavities
Shawn McNeal Victor Arrieta Mohamed Cheikh
ULTRAMET
Pacoima, California
ultramet.com 818-899-0236
Nb3SnSRF’20
Virtual International Workshop on Nb3Sn SRF Science, Technology, and Applications
Online 10–13 November 2020
Hosted by the National Science Foundation Center for Bright Beams and Cornell University

## Slide 2
Company Overview
Ultramet SRF-related R&D Project Path for DOE-SBIR
  Thick-film CVD Niobium on Copper Cavity Optimization
  Copper Cavity Optimization
Current Project Status, Results and Path Forward
  Phase I: CVD Process Development for Nb3Sn
  Phase II: Precursor Development
  Thin-film Nb3Sn on copper ILC cavities
Conclusions and Path Forward
Acknowledgments
2
Agenda

## Slide 3
3
Company Overview
Privately owned company founded in 1970
– 75% Manufacturing (aerospace/medical)
– 25% R&D
Development and manufacture of advanced high temperature materials, primarily by chemical vapor deposition (CVD) technologies
Quality Management System based on ISO 9001-2015
TaC 3987
HfC 3947
C 3827
ZrC 3540
NbC 3500
W 3410
HfN 3305
HfB2 3250
Re 3180
TiC 3140
TaN 3100
TaB2 3093
ZrB2 3038
Ta 3014
BN 3000
ZrN 2980
TiN 2930
NbB2 2900
HfO2 2897
TiB2 2871
VC 2810
SiC 2797
WC 2777
ZrO2 2715
W2B 2671
Mo 2610
Nb 2468
Ir 2443
B4C 2350
NbN 2327
VN 2320
Hf 2227
B 2027
Rh 1966
Si3N4 1900
V 1890
Ta2O5 1872
Zr 1852
TiO2 1840
Pt 1772
SiO2 1723
Ti 1660
Fe 1535
Ni 1455
Si 1410
Cu 1083
Melting Points of Some Materials Deposited by Ultramet, °C
Isothermal heating and uniform temperature control
Metal
Chlorinator
Substrate
Induction coil
Rotating holder
To vacuum pump
Metal
Chlorinator
Substrate
Induction coil
Furnace
Rotating holder
To vacuum pump
Cold Wall Process
Hot Wall Process
Selective heating and preferential deposition

## Slide 4
CVD
CVI
UVCVD
Melt infiltrated CMCs
Ultramet Technologies
4

## Slide 5
5
SRF-SBIR R&D Project Path
Support
  HEP & NP DOE offices
  SRF Group at Cornell
  Jefferson Lab (JLab)
  Niowave
Ultramet SRF R&D Project Path (2005 to Present)
CVD fabrication of seamless bulk niobium cavity
High-RRR CVD niobium process evaluation and development
Thick-film CVD niobium-on-copper process development
CVD Nb3Sn process development
Thin-film CVD Nb3Sn-on-copper via pre-alloyed precursors
    UCLA
    Oak Ridge National Laboratory
    Florida State University (FSU) - MagLab
    Bailey Tool & Manufacturing

## Slide 6
6
SRF-SBIR R&D Project Path
2005 SBIR DOE Phase I
“Cost-Effective, High-Performance, High Purity Niobium Superconducting Radio Frequency Cavities”
Project Objectives
Establish benchmarks and feasibility of CVD-based SRF cavity fabrication
Evaluate CVD process purity (coupon level)
Demonstrate freestanding cavity fabrication capabilities
Atomic force spectroscopy: as-deposited CVD niobium ID surface roughness (312 nm) after mandrel removal (courtesy JLab)
UCLA: SQUID/Tc results
CVD niobium cavity
(of arbitrary design)

## Slide 7
7
2009 SBIR DOE Phase I with ORNL
“Cost-Effective, High-Performance, High Purity Niobium for Superconducting Radio Frequency Cavities”
Precursor | RRRa
Precursor A: Niowave RRR > 200 niobium scrap | 238
Precursor B: commercial niobium chip-scrap | Moderate
CVD coating 1 ¦ precursor A | 282
CVD coating 2 ¦ precursor A | 233
CVD coating 3 ¦ precursor B | 226
CVD coating 4 ¦ precursor B | 213
Solid molybdenum rod substrate used for all specimens. All niobium provided by Niowave was reported to be RRR>200.
a No heat treatment before RRR readings.
RRR Results for Ultramet CVD Niobium (ORNL)
SRF-SBIR R&D Project Path

## Slide 8
SRF-SBIR R&D Project Path
2012 SBIR DOE Phase I with Cornell’s SRF Group:
“Advanced Manufacturing and Testing of Seamless High Purity CVD Niobium Superconducting Radio Frequency Cavities”
RF test results: 3-GHz SRF niobium cavity
At 4.2 K, the CVD cavity reached an intrinsic quality factor of 7.4 × 107.
At 1.5 K the maximum field was limited by quench of the cavity at ~1.3 MV/m.
Intrinsic quality factor was limited by the residual surface resistance of ~570 nΩ.
Primary cause: surface defects caused by machining during mandrel removal.
8

## Slide 9
9
SRF-SBIR R&D Project Path
2016 SBIR DOE Phase I with Cornell’s SRF Group:
“Low Temperature CVD Process Development for Forming Niobium Layers on Copper”
2017 SBIR DOE Phase II with Cornell’s SRF Group:
“Fabrication and Testing of Thick Film CVD Niobium-lined Copper SRF Cavities for High Gradient Applications”
The most recent RF testing by Cornell of an Ultramet CVD niobium-lined seamless copper SRF ILC cavity demonstrated a quench field of ~ 5.5 MV/m and Q0 of ~2 × 109 at 2 K.

## Slide 10
10
Copper Cavity Optimization
Solution: mechanical grind followed by centrifugal barrel polish operation
Weld bead profile issues: random ID weld bead profile features

## Slide 11
11
Copper Cavity Optimization
Solution: seamless OFHC copper cavities developed by Bailey Tool with double weld scheme to strengthen flange-tube attachment
Double weld scheme
Seamless cavity equator ID surface profile
Single-weld scheme: mechanical stresses during centrifugal barrel polish led to failed flange welds.
Weld bead profile issues: random ID weld bead profile features

## Slide 12
12
2017 SBIR DOE Phase I with Cornell’s SRF Group “CVD Process Development of Thin Film Triniobium-Tin for SRF Applications”
2018 SBIR DOE Phase II with Cornell’s SRF Group and FSU - MagLab
“CVD Process Development of Thin Film Triniobium-Tin on Copper SRF Cavities”
Bailey Tool seamless cavities
Niowave welded cavities
Current Project

## Slide 13
13
CVD Nb3Sn Process Development
Phase I: 0.75″ diameter copper disk
ACI Alloys — arc-melted CVD precursors
Precursor development initiated
Phase I: RF test specimen: 5″ diameter Nb3Sn-coated copper disk
Measured 4.2 K average surface resistance of CVD Nb3Sn plates PN-10 and PN-11 vs. peak surface magnetic field on plate

## Slide 14
14
Nb3Sn Precursor Development
Phase I development involved ACI material with varied tin content.
Initial Phase II work continued with ACI Nb-Sn.
  Contaminant constituents found (copper, carbon, etc.)
  Insufficient homogeneity of precursor materials
FSU fabrication process for Nb-Sn compounds
  Process A: improved homogeneity, reduced contamination
  Process B: increased material yield
Precursor Supplier | Fabrication process | Precursor | Results
ACI | Arc melt | Nb:Sn-ACI | Contaminated coatings, ceased use
FSU | A | A-Nb:Sn-1 | Demonstration on coupons and ILC cavities
FSU | A | A-Nb:Sn-2 | Ultramet CVD process development
FSU | B | B-Nb-Sn-2 | Now In-process at FSU
16.5-µm thick tin at 24%; Nb3Sn coating applied to niobium coupon using FSU precursor A
SUMMARY

## Slide 15
Magnetization vs. temperature of different batches of FSU Nb-Sn precursor samples. Sharp transition is indicative of homogeneity of sample tested, and distribution in Tc between batches is within 0.5 K. [Data and description courtesy of FSU]
FSU Nb3Sn Precursor Development
Homogeneity of bulk material is important for achieving reliable CVD coating composition.
15
Results courtesy FSU

## Slide 16
16
First Ultramet CVD Nb3Sn coating on bare copper ILC cavity
Ultramet CVD Nb3Sn on bare Niowave welded copper cavity (SN43-45) using FSU A-Nb:Sn-1 precursor
Nb3Sn on Copper Cavity

## Slide 17
1
2
4
5
3
Site 1
Site 3
Site 5
Site 2
Site 4
17
Nb3Sn on Copper Cavity
First Ultramet CVD Nb3Sn coating on bare copper ILC cavity
SEM results mapping thickness of Ultramet CVD Nb3Sn coating on bare Niowave welded copper cavity (SN43-45) using precursor FSU A-Nb:Sn-1

## Slide 18
Nb3Sn on Copper Cavity
First Ultramet CVD Nb3Sn coating on bare copper ILC cavity
Site 1
Site 3
Site 5
Site 2
Site 4
1
5
4
3
2
18
EDS results showing Sn content of Ultramet CVD Nb3Sn coating on bare Niowave welded copper cavity (SN43-45) using precursor FSU A-Nb:Sn-1

## Slide 19
Hardness Vickers, 50-g load, 15-sec dwell time
EDS map indicates that there is no copper contamination (within EDS resolution limit).
Interface hardness indent does not show debonding at copper–Nb-Sn interface.
Process leads to good bonding.
Nb3Sn
(Sn: 21 atm%)
Copper
FSU Analysis of Ultramet Nb3Sn on Copper Sample
19
Results courtesy FSU

## Slide 20
20
Nb3Sn on Niobium-lined Copper Cavity
Second Ultramet CVD Nb3Sn coating on copper ILC cavity with CVD niobium interlayer
Ultramet CVD Nb3Sn on CVD niobium-lined Niowave welded copper cavity (SN19-20) using FSU A-Nb:Sn-1 precursor

## Slide 21
Site 1
Site 3
Site 5
Site 2
Site 4
1
2
3
4
5
21
Second Ultramet CVD Nb3Sn coating on copper ILC cavity with CVD niobium interlayer
Nb3Sn on Niobium-lined Copper Cavity
SEM results mapping thickness of Ultramet CVD Nb3Sn coating on CVD niobium-lined Niowave welded copper cavity (SN19-20) using precursor FSU A-Nb:Sn-1

## Slide 22
22
Second Ultramet CVD Nb3Sn coating on copper ILC cavity with CVD niobium interlayer
Site 1
Site 3
Site 5
Site 2
Site 4
1
5
4
3
2
Nb3Sn on Copper Cavity
EDS results showing tin content of Ultramet CVD Nb3Sn coating on niobium-lined Niowave copper cavity (SN19-20) using precursor FSU A-Nb:Sn-1

## Slide 23
23
Conclusions and Path Forward
Current effort
Identified and produced precursor materials for CVD of Nb3Sn in the A15 phase with a tin content at/near 24%
Continued precursor, CVD, and copper cavity fabrication optimization efforts
Vapor deposited well-adhered Nb3Sn coatings on OFHC copper, niobium, and molybdenum coupon substrates
Demonstrated ability to form uniform CVD Nb3Sn coatings with tin content of >20% on ID surface of OFHC copper cavities of full-scale single-cell ILC design with and without niobium interface coatings
Ongoing and future efforts
  Optimization of CVD reactor and process to reliably achieve uniform Nb3Sn coatings with the ideal 24% tin content
CVD Nb3Sn coat OFHC copper cavities suitable for RF testing at cryogenic temperatures by Cornell’s SRF Group

## Slide 24
24
Acknowledgments
DOE TPOC
Dr. Ken Marken
Florida State University - MagLab
Dr. Peter Lee
Dr. Shreyas Balachandran
Dr. David Larbalestier
Niowave
Dr. Terry Grimm
Mr. John Diemer
Bailey Tool & Manufacturing
Mr. John Buttles
Cornell & SRF Group
Dr. Matthias Liepe
Dr. Lou Hand
Mr. Charles McNeal
JLab
Dr. Charlie Reece
Dr. Larry Phillips
ACI Alloys, Inc.
Mr. Larry Albert
Oak Ridge
Dr. David Christen

## Slide 25
Mohamed Cheikh
mohamed.cheikh@ultramet.com
Questions?
Victor M. Arrieta
victor.arrieta@ultramet.com
ULTRAMET
ultramet.com
818-899-0236
12173 Montague St. | Pacoima CA 91331
Shawn R. McNeal
shawn.mcneal@ultramet.com
25