## Slide 1
Ab Initio Calculations on Point Defect Thermodynamics in Nb3Sn
Nathan Sitaraman, Michelle Kelley, André Fonseca, Zhaslan Baraissov, Ryan Porter, Zeming Sun, David Muller, Matthias Liepe, and Tomás Arias
NSF award PHY-1549132, the Center for Bright Beams
Nb3SnSRF’20
Center for Bright Beams

## Slide 2
Background: The Importance of Point Defects
What is a “point defect”?
Nb3SnSRF’20

## Slide 3
Background: The Importance of Point Defects
What is a “point defect”? -Antisite defects
Nb3SnSRF’20

## Slide 4
Background: The Importance of Point Defects
What is a “point defect”? -Antisite defects -Interstitials (O, H)
Nb3SnSRF’20

## Slide 5
Background: The Importance of Point Defects
What is a “point defect”? -Antisite defects -Interstitials (O, H)
Why study point defects?
Nb3SnSRF’20

## Slide 6
Background: The Importance of Point Defects
What is a “point defect”? -Antisite defects -Interstitials (O, H)
Why study point defects?
Understanding larger defects begins with understanding point defects
Nb3SnSRF’20

## Slide 7
Point defects during cavity cooldown
Nb3SnSRF’20

## Slide 8
Point defects during cavity cooldown
The coating process is long, but this talk is short.
Nb3SnSRF’20

## Slide 9
Point defects during cavity cooldown
The coating process is long, but this talk is short.
Let’s focus only on the cooldown step
Nb3SnSRF’20

## Slide 10
Antisite defects
Nb3SnSRF’20

## Slide 11
Antisite defects
Experimental studies have shown that grain boundaries contain excess tin immediately after coating stage
Nb3SnSRF’20
Jaeyel Lee et. al., Grain-boundary structure and segregation in Nb3Sn coatings on Nb for high-performance superconducting radiofrequency cavity applications, Acta Materialia 188,155 (2020)
Notes: Atom probe tomography, TEM

## Slide 12
Antisite defects
Experimental studies have shown that grain boundaries contain excess tin immediately after coating stage
After a long anneal step (3 hours), grain boundaries contain excess niobium
Nb3SnSRF’20
Jaeyel Lee et. al., Grain-boundary structure and segregation in Nb3Sn coatings on Nb for high-performance superconducting radiofrequency cavity applications, Acta Materialia 188,155 (2020)

## Slide 13
Antisite defects
Experimental studies have shown that grain boundaries contain excess tin immediately after coating stage
After a long anneal step (3 hours), grain boundaries contain excess niobium
In both cases, antisite defects infiltrate material around the boundary core.
Nb3SnSRF’20
Jaeyel Lee et. al., Grain-boundary structure and segregation in Nb3Sn coatings on Nb for high-performance superconducting radiofrequency cavity applications, Acta Materialia 188,155 (2020)

## Slide 14
Antisite defects
Experimental studies have shown that grain boundaries contain excess tin immediately after coating stage
After a long anneal step (3 hours), grain boundaries contain excess niobium
In both cases, antisite defects infiltrate material around the boundary core.
Both cases likely harm cavity performance (see following talk!)
Nb3SnSRF’20
Jaeyel Lee et. al., Grain-boundary structure and segregation in Nb3Sn coatings on Nb for high-performance superconducting radiofrequency cavity applications, Acta Materialia 188,155 (2020)
Notes: Both processes thermodynamically favorable, kinetics determine final GB composition

## Slide 15
Antisite defects
Eliminating tin antisite defects
Sn
Nb
Nb3SnSRF’20

## Slide 16
Antisite defects
Eliminating tin antisite defects
Niobium
Nb3SnSRF’20

## Slide 17
Antisite defects
Eliminating tin antisite defects
Niobium
Nb3SnSRF’20
Notes: At some time during the annealing step this happens, which is when this grain boundary effectively begins its annealing process

## Slide 18
Antisite defects
Eliminating tin antisite defects
Niobium
Niobium vacancy: 2.1 eV
Nb3SnSRF’20

## Slide 19
Antisite defects
Eliminating tin antisite defects
Niobium
Niobium vacancy: 2.1 eV
Nb3SnSRF’20

## Slide 20
Antisite defects
Eliminating tin antisite defects
Niobium
Niobium vacancy: 2.1 eV
Nb3SnSRF’20

## Slide 21
Antisite defects
Eliminating tin antisite defects
Niobium
Niobium vacancy: 2.1 eV
Nb3SnSRF’20

## Slide 22
Antisite defects
Eliminating tin antisite defects
Niobium
Niobium vacancy: 2.1 eV
Nb3SnSRF’20

## Slide 23
Antisite defects
Eliminating tin antisite defects
Niobium
Niobium vacancy: 2.1 eV
Nb3SnSRF’20

## Slide 24
Antisite defects
Eliminating tin antisite defects
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 1.2 eV
Nb3SnSRF’20

## Slide 25
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 1.2 eV
Nb3SnSRF’20

## Slide 26
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
Niobium
Nb3SnSRF’20

## Slide 27
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
Niobium
Niobium vacancy: 2.1 eV
Nb3SnSRF’20

## Slide 28
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
Niobium
Niobium vacancy: 2.1 eV
Nb3SnSRF’20

## Slide 29
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 2.3 eV
Nb3SnSRF’20

## Slide 30
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 2.3 eV
Nb3SnSRF’20

## Slide 31
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
  Total activation energy: 4.4 eV
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 2.3 eV
Nb3SnSRF’20

## Slide 32
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
  Total activation energy: 4.4 eV
  (tin on Nb site eliminated with same activation energy as before)
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 2.3 eV
Nb3SnSRF’20

## Slide 33
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
  Total activation energy: 4.4 eV
  (tin on Nb site eliminated with same activation energy as before)
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 2.3 eV
Nb3SnSRF’20

## Slide 34
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
  Total activation energy: 4.4 eV
  (tin on Nb site eliminated with same activation energy as before)
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 2.3 eV
Nb3SnSRF’20
Notes: Mention 2 hours on the same order of magnitude as the anneal step

## Slide 35
Antisite defects
Eliminating tin antisite defects
  Total activation energy: 3.3 eV
Creating niobium antisite defects
  Total activation energy: 4.4 eV
  (tin on Nb site eliminated with same activation energy as before)
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Want to ensure tin antisite defects are eliminated without allowing niobium antisite defect formation. How?
Niobium
Niobium vacancy: 2.1 eV
Hopping energy: 2.3 eV
Nb3SnSRF’20

## Slide 36
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Variations in effective annealing time
Nb3Sn
Nb3Sn
Nb3Sn
Antisite defects
T=0
Nb3SnSRF’20
Notes: Mention various sources of heterogeneity

## Slide 37
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Variations in effective annealing time
Nb3Sn
Nb3Sn
Nb3Sn
Antisite defects
T=15
Nb3SnSRF’20

## Slide 38
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Variations in effective annealing time
Nb3Sn
Nb3Sn
Nb3Sn
Antisite defects
T=30
Nb3SnSRF’20

## Slide 39
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Variations in effective annealing time
Nb3Sn
Nb3Sn
Nb3Sn
Antisite defects
T=45
Nb3SnSRF’20

## Slide 40
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Variations in effective annealing time
Nb3Sn
Nb3Sn
Nb3Sn
Antisite defects
T=60
Nb3SnSRF’20

## Slide 41
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Variations in effective annealing time
  Timing differences become less important at lower T
Nb3Sn
Nb3Sn
Nb3Sn
Antisite defects
T=60
Nb3SnSRF’20

## Slide 42
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Variations in effective annealing time
  Timing differences become less important at lower T
At 1300K (~1030C)
  1/(1 THz * e-ꞵ*3.3eV) = 6 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 30 hours
Nb3Sn
Nb3Sn
Nb3Sn
Antisite defects
T=60
Nb3SnSRF’20

## Slide 43
At 1400K (~1130C)
  1/(1 THz * e-ꞵ*3.3eV) = 0.8 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 2 hours
Variations in effective annealing time
  Timing differences become less important at lower T
At 1300K (~1030C)
  1/(1 THz * e-ꞵ*3.3eV) = 6 seconds
  1/(1 THz * e-ꞵ*4.4eV) = 30 hours
Longer anneal at cooler temperature may be better, especially in multi-cell coatings where inhomogeneities are most likely
Nb3Sn
Nb3Sn
Nb3Sn
Antisite defects
T=60
Nb3SnSRF’20

## Slide 44
Oxygen
Nb3SnSRF’20

## Slide 45
Oxygen
Oxide surface thought to play a key role in Nb cavity physics
Nb3SnSRF’20

## Slide 46
Oxygen
Oxide surface thought to play a key role in Nb cavity physics
Recent experiments begin to characterize Nb3Sn oxide surface
Nb3SnSRF’20
Niobium oxide
Nb3Sn crystal
Image by Zhaslan Baraissov
Notes: TEM

## Slide 47
Oxygen
Oxide surface thought to play a key role in Nb cavity physics
Recent experiments begin to characterize Nb3Sn oxide surface
How does this oxide form, and how does it compare to the Nb native oxide?
Nb3SnSRF’20
Niobium oxide
Nb3Sn crystal
Image by Zhaslan Baraissov

## Slide 48
Oxygen
For cavity grade Nb, the following is true under typical conditions:
  FO_int < FO_oxide< FO_gas
Nb NbOx O2
F
Nb3SnSRF’20

## Slide 49
Oxygen
For cavity grade Nb, the following is true under typical conditions:
  FO_int < FO_oxide< FO_gas
  Oxides form for kinetic reasons: at low T, O can’t diffuse fast enough to reach low-F interstitial sites deep in bulk
Nb NbOx O2
F
Nb3SnSRF’20

## Slide 50
Oxygen
For cavity grade Nb, the following is true under typical conditions:
  FO_int < FO_oxide< FO_gas
  Oxides form for kinetic reasons: at low T, O can’t diffuse fast enough to reach low-F interstitial sites deep in bulk
  Oxide formation rate complicated, but O diffusion rate simple: J = -D*⛛n
Nb NbOx O2
F
Nb3SnSRF’20

## Slide 51
Oxygen
For cavity grade Nb, the following is true under typical conditions:
  FO_int < FO_oxide< FO_gas
  Oxides form for kinetic reasons: at low T, O can’t diffuse fast enough to reach low-F interstitial sites deep in bulk
  Oxide formation rate complicated, but O diffusion rate simple: J = -D*⛛n
Nb NbOx O2
F
Hopping barrier
Nb3SnSRF’20

## Slide 52
Oxygen
For cavity grade Nb, the following is true under typical conditions:
  FO_int < FO_oxide< FO_gas
  Oxides form for kinetic reasons: at low T, O can’t diffuse fast enough to reach low-F interstitial sites deep in bulk
  Oxide formation rate complicated, but O diffusion rate simple: J = -D*⛛n
Nb NbOx O2
F
Hopping barrier
n
nmax
Nb3SnSRF’20

## Slide 53
Oxygen
For cavity grade Nb, the following is true under typical conditions:
  FO_int < FO_oxide< FO_gas
  Oxides form for kinetic reasons: at low T, O can’t diffuse fast enough to reach low-F interstitial sites deep in bulk
  Oxide formation rate complicated, but O diffusion rate simple: J = -D*⛛n
Nb NbOx O2
F
Hopping barrier
n
nmax
⛛n ∝ nmax
Nb3SnSRF’20
Notes: Concentration drops from limit nmax to deep bulk value over some distance

## Slide 54
Oxygen
For cavity grade Nb, the following is true under typical conditions:
  FO_int < FO_oxide< FO_gas
  Oxides form for kinetic reasons: at low T, O can’t diffuse fast enough to reach low-F interstitial sites deep in bulk
  Oxide formation rate complicated, but O diffusion rate simple: J = -D*⛛n
Nb NbOx O2
F
Hopping barrier
n
nmax
⛛n ∝ nmax ∝ eꞵ(E_ox - E_int)
Nb3SnSRF’20
Notes: NOT exponential

## Slide 55
Oxygen
For cavity grade Nb, the following is true under typical conditions:
  FO_int < FO_oxide< FO_gas
  Oxides form for kinetic reasons: at low T, O can’t diffuse fast enough to reach low-F interstitial sites deep in bulk
  Oxide formation rate complicated, but O diffusion rate simple: J = -D*⛛n
Nb NbOx O2
F
Hopping barrier
n
nmax
⛛n ∝ nmax ∝ eꞵ(E_ox - E_int)
Interstitial energy
Nb3SnSRF’20

## Slide 56
Oxygen
For cavity grade Nb, the following is true under typical conditions:
How do things change in an Nb3Sn cavity?
Nb NbOx O2
F
Nb3SnSRF’20

## Slide 57
Oxygen
For cavity grade Nb, the following is true under typical conditions:
How do things change in an Nb3Sn cavity?
Nb NbOx O2
F
?
Nb3Sn NbOx O2
F
Nb3SnSRF’20

## Slide 58
Oxygen
For cavity grade Nb, the following is true under typical conditions:
How do things change in an Nb3Sn cavity?
Nb NbOx O2
F
?
Nb3Sn NbOx O2
F
 | Barrier | E_ox-E_int | nmax (1000K)
Nb | 1.18 eV | -0.37 eV | 2.0 at. %
Nb3Sn | ? | ? | ?
Nb3SnSRF’20

## Slide 59
Oxygen
For cavity grade Nb, the following is true under typical conditions:
How do things change in an Nb3Sn cavity?
        Nb3Sn hopping barrier very similar to Nb
Nb NbOx O2
F
?
Nb3Sn NbOx O2
F
Nb Barrier
Nb3SnSRF’20
 | Barrier | E_ox-E_int | nmax (1000K)
Nb | 1.18 eV | -0.37 eV | 2.0 at. %
Nb3Sn | 1.22 eV | ? | ?
Nearest-neighbor
Next-nearest- neighbor

## Slide 60
Oxygen
For cavity grade Nb, the following is true under typical conditions:
How do things change in an Nb3Sn cavity?
        Nb3Sn hopping barrier very similar to Nb
        Nb3Sn interstitial energy much higher than Nb
Nb NbOx O2
F
?
Nb3Sn NbOx O2
F
Nb Barrier
Nb3SnSRF’20
Nearest-neighbor
Next-nearest- neighbor
 | Barrier | E_ox-E_int | nmax (1000K)
Nb | 1.18 eV | -0.37 eV | 2.0 at. %
Nb3Sn | 1.22 eV | -1.46 eV | ?

## Slide 61
Oxygen
For cavity grade Nb, the following is true under typical conditions:
How do things change in an Nb3Sn cavity?
        Nb3Sn hopping barrier very similar to Nb
        Nb3Sn interstitial energy much higher than Nb
        ⛛n, nmax much smaller in Nb3Sn
Nb NbOx O2
F
?
Nb3Sn NbOx O2
F
Nb Barrier
Nb3SnSRF’20
Nearest-neighbor
Next-nearest- neighbor
 | Barrier | E_ox-E_int | nmax (1000K)
Nb | 1.18 eV | -0.37 eV | 2.0 at. %
Nb3Sn | 1.22 eV | -1.46 eV | 10-5 at. %

## Slide 62
Oxygen
For cavity grade Nb, the following is true under typical conditions:
How do things change in an Nb3Sn cavity?
        Nb3Sn hopping barrier very similar to Nb
        Nb3Sn interstitial energy much higher than Nb
        ⛛n, nmax much smaller in Nb3Sn
Nb NbOx O2
F
?
Nb3Sn NbOx O2
F
Nb Barrier
Nb3SnSRF’20
Nearest-neighbor
Next-nearest- neighbor
 | Barrier | E_ox-E_int | nmax (1000K)
Nb | 1.18 eV | -0.37 eV | 2.0 at. %
Nb3Sn | 1.22 eV | -1.46 eV | 10-5 at. %
Native oxide may form at higher T, lower partial pressure than is typical for Nb

## Slide 63
Hydrogen
Nb3SnSRF’20

## Slide 64
Hydrogen
In niobium cavities, hydrogen is known for forming hydride precipitates at cryogenic temperatures (~100K).
[citations]
Nb3SnSRF’20
F. Barkov, A. Romanenko, Y. Trenikhina, and A. Grassellino, Precipitation of hydrides in high purity
niobium after different treatments, J. Appl. Phys. 114, 164904, 2013

## Slide 65
Hydrogen
In niobium cavities, hydrogen is known for forming hydride precipitates at cryogenic temperatures (~100K).
Previous studies have shown that hydrogen can affect the superconductivity of Nb3Sn wires
Nb3SnSRF’20
M. Takayasu et. al., Multifilamentary Nb3Sn wires reacted in hydrogen gas, proc. ICMC, Vol. 48, 2002
F. Barkov, A. Romanenko, Y. Trenikhina, and A. Grassellino, Precipitation of hydrides in high purity
niobium after different treatments, J. Appl. Phys. 114, 164904, 2013

## Slide 66
Hydrogen
In niobium cavities, hydrogen is known for forming hydride precipitates at cryogenic temperatures (~100K).
Previous studies have shown that hydrogen can affect the superconductivity of Nb3Sn wires
What role might hydrogen play in Nb3Sn cavities?
Nb3SnSRF’20
M. Takayasu et. al., Multifilamentary Nb3Sn wires reacted in hydrogen gas, proc. ICMC, Vol. 48, 2002
F. Barkov, A. Romanenko, Y. Trenikhina, and A. Grassellino, Precipitation of hydrides in high purity
niobium after different treatments, J. Appl. Phys. 114, 164904, 2013

## Slide 67
Hydrogen
Comparing Cu-Nb3Sn, Nb-Nb3Sn systems
Copper matrix
Nb3Sn Filaments
Nb3SnSRF’20

## Slide 68
Hydrogen
Comparing Cu-Nb3Sn, Nb-Nb3Sn systems
Hydrogen prefers Nb3Sn over Cu, explaining why Nb3Sn wires may be affected by hydrogen
Nb3Sn
Cu
Copper matrix
Nb3Sn Filaments
ECu- ENb3Sn | 0.76 eV
E
Nb3SnSRF’20

## Slide 69
Nb3Sn
Hydrogen
Comparing Cu-Nb3Sn, Nb-Nb3Sn systems
Hydrogen prefers Nb3Sn over Cu, explaining why Nb3Sn wires may be affected by hydrogen
However, hydrogen prefers Nb Over Nb3Sn, suggesting that cavity Nb3Sn should contain very little hydrogen
Nb
ECu- ENb3Sn | 0.76 eV
ENb- ENb3Sn | -0.08 eV
Copper matrix
Nb3Sn Filaments
E
Nb3SnSRF’20

## Slide 70
Nb3Sn
Hydrogen
Comparing Cu-Nb3Sn, Nb-Nb3Sn systems
Hydrogen prefers Nb3Sn over Cu, explaining why Nb3Sn wires may be affected by hydrogen
However, hydrogen prefers Nb Over Nb3Sn, suggesting that cavity Nb3Sn should contain very little hydrogen
For 1 at. % H in Nb, expect ~1 ppm H in Nb3Sn at 100K
Nb
Copper matrix
Nb3Sn Filaments
ECu- ENb3Sn | 0.76 eV
ENb- ENb3Sn | -0.08 eV
E
Nb3SnSRF’20

## Slide 71
Nb3Sn
Hydrogen
Comparing Cu-Nb3Sn, Nb-Nb3Sn systems
Hydrogen prefers Nb3Sn over Cu, explaining why Nb3Sn wires may be affected by hydrogen
However, hydrogen prefers Nb Over Nb3Sn, suggesting that cavity Nb3Sn should contain very little hydrogen
For 1 at. % H in Nb, expect ~1 ppm H in Nb3Sn at 100K
Unlikely to form hydride precipitates at Nb3Sn surface
Nb
Copper matrix
Nb3Sn Filaments
ECu- ENb3Sn | 0.76 eV
ENb- ENb3Sn | -0.08 eV
E
Nb3SnSRF’20
Notes: Emphasize copper for wire

## Slide 72
Conclusions
Nb3SnSRF’20
Notes: (and this is my final slide)

## Slide 73
Conclusions
Many unexplored degrees of freedom during cooldown process. Could further improve GB composition and control oxide formation.
Nb3SnSRF’20

## Slide 74
Conclusions
Many unexplored degrees of freedom during cooldown process. Could further improve GB composition and control oxide formation.
Sn antisite defect elimination, Nb antisite defect formation happen on different characteristic timescales
Nb3SnSRF’20

## Slide 75
Conclusions
Many unexplored degrees of freedom during cooldown process. Could further improve GB composition and control oxide formation.
Sn antisite defect elimination, Nb antisite defect formation happen on different characteristic timescales
  Can anneal at lower temperature to improve GB stoichiometry
Nb3SnSRF’20

## Slide 76
Conclusions
Many unexplored degrees of freedom during cooldown process. Could further improve GB composition and control oxide formation.
Sn antisite defect elimination, Nb antisite defect formation happen on different characteristic timescales
  Can anneal at lower temperature to improve GB stoichiometry
Oxygen diffusion through Nb3Sn should be very slow
Nb3SnSRF’20

## Slide 77
Conclusions
Many unexplored degrees of freedom during cooldown process. Could further improve GB composition and control oxide formation.
Sn antisite defect elimination, Nb antisite defect formation happen on different characteristic timescales
  Can anneal at lower temperature to improve GB stoichiometry
Oxygen diffusion through Nb3Sn should be very slow
  Surface oxide properties could be sensitive to cooldown rate, O2 partial pressure
Nb3SnSRF’20

## Slide 78
Conclusions
Many unexplored degrees of freedom during cooldown process. Could further improve GB composition and control oxide formation.
Sn antisite defect elimination, Nb antisite defect formation happen on different characteristic timescales
  Can anneal at lower temperature to improve GB stoichiometry
Oxygen diffusion through Nb3Sn should be very slow
  Surface oxide properties could be sensitive to cooldown rate, O2 partial pressure
Hydrogen nearly insoluble in Nb3Sn at cryogenic temperatures
Nb3SnSRF’20

## Slide 79
Conclusions
Many unexplored degrees of freedom during cooldown process. Could further improve GB composition and control oxide formation.
Sn antisite defect elimination, Nb antisite defect formation happen on different characteristic timescales
  Can anneal at lower temperature to improve GB stoichiometry
Oxygen diffusion through Nb3Sn should be very slow
  Surface oxide properties could be sensitive to cooldown rate, O2 partial pressure
Hydrogen nearly insoluble in Nb3Sn at cryogenic temperatures
  Less potential for surface hydride formation compared to Nb surface
Nb3SnSRF’20