## Slide 1: Investigation of Local Nonlinear Microwave Response of Nb3Sn in the Superconducting State
Bakhrom Oripov, Chung-Yang Wang and Steven Anlage
This work is funded by US Department of Energy
grant # DE-SC0017931 and QMC
10 November, 2020

## Slide 2
Nonlinear microwave microscopy of superconductors
Prior results on Nb bulk and thin film samples
Preliminary results on Nb3Sn/Nb coating
4. What is the origin of this data?
Where do we plan to go with this?
Presentation Outline

## Slide 3
Superconducting Radio Frequency Cavity
https://www.lhc-closer.es
Grassalino, SRF2019
2017
Notes: SRF Cavity
Continuous acceleration
Figure Merit, very good progress and room for improvement.

## Slide 4
Surface Defects:
Surface Roughness
Pits
Welds
Grain Boundaries
Nb Oxides
Hydrogen Poisoning
Magnetic Impurities
Trapped Flux
Nb
Nb on Copper
Cu
~1µm
Nb
Nb3Sn
~1µm
Nb3Sn
Nb
I
S
S
I
Engineered SIS structures
Gurevich, Appl. Phys. Lett. 88 012511, 2006
Current SRF Research Frontiers
Investigate these materials / issues with a microscope that induces nonlinear microwave response

## Slide 5
Probe
Sample
X scanner
Y scanner
Cold Plate
Z scanner
Cold Finger
Cryostat with
Temperature Control
Hrf
Jsurf
Brf
sample
Spectrum
Analyzer
f, Pf
2f, P2f
3f, P3f
MW
Source
f, Pi
Brf > 600 mT
Resolution < 100 nm
Cold Base
Near-Field Brf Microscope
Notes: Introduce setup
Why Harmonic response

## Slide 6
Advantages of this technique
  Local:
  By measuring Nonlinear response we have high SNR: Superconductor is the main source of Nonlinearity
BRF
rf currents
inhomogeneities
sample
Cavity
BRF
B=0
  SRF-like:
Brf m0Hc2,
Microwave,
Cryogenic
R=x,y
Magnetic
Write Head
Sample
Sample
R=x,y
z
Silver (3D) surface corresponds to
  The probe is somewhat “aggressive”
  Local RF critical field
  RF vortex semi-loop generation
  Traditional Rs measurements

## Slide 7
Prior results on Nb bulk and thin film samples
B. Oripov et al. Phys. Rev. Appl., vol. 11, no. 6, p. 64030, Jun. 2019.

## Slide 8
Third Harmonic Response (nV)
Hp1
Hp2
Hp3
+100 Offset
Hp0
T=9 K
T=8.5 K
Hp1
Hp2
Hp3
Hp0
f=4.38 GHz and Probe background nonlinearity subtracted
250
200
150
50
100
150
50
50
0
Input RF Field Amplitude (a.u.)
50
100
T=5.5K
T=6K
T=6.5K
T=7K
Hc1 ?
Bulk Nb Data: Periodicity in Harmonic Response
250
Third Harmonic Response (nV)
Input RF Field Amplitude (a.u.)
Grows with
decreasing
temperature
Notes: Very difficult to see anything at first
Line Cut1: Measurable V3 above an onset field, and periodic dips Hp 1 2 and 3
Different T, same but at lover H
Please look at low T, H features

## Slide 9
Nb on Copper Data
Low
field
Periodic
Periodic
Low
field
Notes: Hv is different
T dep is different

## Slide 10
Nb on Sapphire (JLab)
Nb on Cu (CERN)
TF-JLAB-ECR-Nb-aAl_2O_3-35_3
Nb on Cu
(ASTeC UK)
6.4 K
4.8 K
OLEG 24_02_16v1
Nb on Cu
(ASTeC UK)
OLEG 23_02_16v1
7.2 K
7.5 K
4 K
7 K
Low
field
Low
field
Periodic
Periodic
Similar results seen on other Nb Film samples

## Slide 11
Bulk Nb from Bieler/MSU
Bulk and Film samples can show either periodic or non-periodic
harmonic response depending on location
3.5 K
Low
field
Periodic
Bulk Nb from Ciovati/JLab
4 K
Similar results seen on other Bulk Nb samples

## Slide 12
J. Halbritter, ” On the Oxidation and on the Superconductivity of Niobium,” J. Appl. Phys. A 43, 1 (1987).
J. McDonald and John R. Clem, ” Microwave response and surface impedance of weak links,” Phys. Rev. B 56, 14723 (1997).
L. M. Xie, J. Wosik, and J. C. Wolfe, ” Nonlinear microwave absorption in weak-link Josephson junctions,” Phys. Rev. B 54, 15494 (1996).
Nb Weak-Links and RCSJ model
Notes: Well known that Nb Oxides reside in GB
Do they act as JJ?
Model JJ, ideal JJ and RC

## Slide 13
Temperature (K)
∆ (meV)
Bulk Nb WeakLink 1:
Nb Film on Cu
Bulk Nb WeakLink 2:
Bulk Nb WeakLink 3:
  Phys. Rev. Applied 11, 064030 (2019)
Nb Weak-Links and RCSJ model

## Slide 14
Silver surface correspond to
Hdipole = 8 λ
Bdipole = 0.75 Bc2
Period = 200
Frequency ≈ 5 GHz
ĸ = 1
Ƞ = 1
T = 0
RF Vortex Entry and Motion in the Superconductor
Defect
z
Vortex
Semi-loops
rf
Superconductor
Vacuum
Intrinsic Response: Vortex Semi-loops
B. Oripov and S. M. Anlage, Phys. Rev. E, vol. 101, 033306, (2020).
RF vortex semi-loops generated by our probe:

## Slide 15
Harmonic Response of Vortex-Semiloops
Hrf (a.u.)
V3f (nV)
Nb on
Cu Data
Combined Fit
TDGL
RSCJ Fit
Probe background

## Slide 16
Preliminary Results on Nb3Sn
Size: 1 cm 1 cm
Substrate: Nb, thickness: 3 mm
AFM
Nb3Sn film
Cross-section
Surface SEM
Grain size
100 nm – 2 um
Sn-plated Nb and thermally converted Nb3Sn films from Cornell

## Slide 17
Preliminary Data on Thermally-Converted Nb3Sn / Nb from Cornell
Noise floor

## Slide 18
Third Harmonic Response (mV)
Temperature (K)
Bulk Nb Data: Periodicity in Harmonic Response
Input RF Field Amplitude (a.u.)
Input RF Field Amplitude (a.u.)
H1
H2
H3
+0.1 Offset
T = 9.0 K
T = 8.5 K
H1
H2
H3
f = 4.38 GHz
Probe background nonlinearity subtracted
RF Amplitude scale estimate:
11.4 μT/(arb. units) for weak link #1

## Slide 19
Temperature (K)
T (K)
Third Harmonic Response (dBm)
P3f (dBm)
Harmonic Response from Nb3Sn
-150 -140 -130 -120 -110
P3f (dBm)
Pf (dBm)
Pf = -19 dBm

## Slide 20
Harmonic Response from Nb3Sn
Some Points of Discussion
Multiple superconducting transitions are observed
  Tc = 14.6 K, 15.1 K, 15.6 K and ~5.5 K
  Lowest Tc material is strongly nonlinear
A. Godeke, Super. Sci. and Tech. 19 (8), R68 (2006)
The “nose” in P3f(Pf, T) suggests that Nb *may* be playing a role
  Positive slope of P3f vs. T is novel
Large P3f(Pf, T) at low-T and high-Pf may be a sign of vortex semi-loop generated response
  TDGL simulations in progress

## Slide 21
Nb3Sn
Current Status of Our Experiments

## Slide 22
Summary
  2 types of Nb nonlinear response are detected and modeled
  Magnetic Microwave Microscope as a cryogenic RF characterization tool is demonstrated
  Evidence of Sn-deficient Nb3Sn phases observed
  Evidence of Tc = 5.5 K phase in Nb3Sn sample
  Special thanks to Seagate Corp. and Western Digital Corp. for providing magnetic probes
Acknowledgement:
Thomas Bieler
Gianluigi Ciovati
Sergio Calatroni
Pashupati Dhakal
Tobias Junginger
Oleg B Malyshev
Giovanni Terenziani
Anne-Marie Valente-Feliciano
Reza Valizadeh
Stuart Wilde
Matthias Ulf Liepe
Thomas Oseroff
Zeming Sun
Shielded microwave
probe

## Slide 24
Objective: Identify microscopic defects that cause breakdown of SRF cavities
Method:
1) Examine the sample with intense, localized BRF in the superconducting state
2) Measure locally-produced harmonic generation from defects
3) These are currently single-point measurements – no scanning yet
1 mm
Vf +
V3f -
Microwave Source
Low Pass Filter
High Pass Filter
v3f
Spectrum
Analyzer
Superconductor
T. Tai, et al. IEEE Trans. Appl. Supercond. 21, 2615 (2011); 23, 7100104 (2013)