## Slide 1: Overview of Nb3Sn Cavity Progress (for CW machines)
Presented by Liana Shpani
October 5, 2022
Special Thanks to:
Sam Posen and Grigory Eremeev, FNAL
Uttar Pudasaini, JLab
Kensei Umemori and Hayato Ito, KEK
Gabriel Gaitan, Matthias Liepe, Ryan Porter, Neil Stilin, Nicole Verbonceour, Cornell University
for their significant contributions!
Grant No. PHY-1549132
Grant No. DE-SC0008431

## Slide 2: Outline
1. Why Nb3Sn?
2. How do we grow it?
3. State-of-the-art performance
4. Case Study: LCLS-II
5. Remaining Challenges

## Slide 3: Outline
1. Why Nb3Sn?
2. How do we grow it?
3. State-of-the-art performance
4. Case Study: LCLS-II
5. Remaining Challenges

## Slide 4: SRF for Accelerators
Slowed down by factor of approximately 4x109
Input RF power at 1.3 GHz
Goals:
Decrease accelerator length
  Higher accelerating gradients
Need lower surface resistance:
Need superconductors with higher fundamental flux-free field limit
Need superconductors with higher critical temperature
Animation created by Sam Posen
Decrease cooling power

## Slide 5: Nb3Sn: A Very Promising Material
Higher critical temperature :
  lower losses
  higher operating temperature
  can operate at higher frequency
Higher superheating field = higher accelerating gradients:
(T)
(T)
(T)

## Slide 6: Nb3Sn Potential
 | Nb | Nb3Sn
Superheating Field ( | 240 mT | 420 mT
Max. | 55 MV/m | 100 MV/m
Critical Temperature ( | 9 K | 18 K
at 4.2K |  | 
at 2K |  | >
 | Nb | Nb3Sn
 | 240 mT | 420 mT
 | 55 MV/m | 100 MV/m
 | 9 K | 18 K
Q0 given for 1.3 GHz single-cell ILC-shape cavities
Higher energy gain
  Shorter accelerators
Lower cooling cost and complexity
  4.2K operation with high cryo-efficiency (!!)
  No superfluid helium
~2K
~4K
Small Scale
Large Scale

## Slide 7: Outline
1. Why Nb3Sn?
2. How do we grow it?
3. State-of-the-art performance
4. Case Study: LCLS-II
5. Remaining Challenges

## Slide 8: Thermal Vapor Diffusion
Tin source
Secondary heater
Tin crucible
Primary heater
Cavity
Nucleation agent (SnCl2)
UHV Furnace
Coating chamber
S. Posen and M. Liepe, Phys. Rev. ST Accel. Beams 15, 112001 (2014).
“Wuppertal” configuration, i.e., with secondary heater for the tin source
Temperature Profile

## Slide 9: Nb3Sn Coatings
RF Surface
2 μm
≈3 μm
Nb3Sn forms a polycrystalline layer on the surface of the niobium
1 μm
1 μm
Nb
Nb3Sn
Before Coating
After Coating
(cross section)
(surface)

## Slide 10: Stoichiometry and TC
Nb
Sn
Nb3Sn Structure
Nb3Sn
16 – 25% Sn
Nb3Sn Phase Diagram
Must maintain stoichiometry
Tin-depleted Nb3Sn has a low TC

## Slide 11: Stoichiometry and TC
Nb
Sn
Nb3Sn Structure
Must maintain stoichiometry
Tin-depleted Nb3Sn has a low TC
Tc vs. Tin Content
A. Godeke, Supercond. Sci. Tech, 2006
24 to 25% target

## Slide 12: Material Challenges
  Need high quality Nb3Sn films!
Thin films help
Material is brittle
Low thermal conductivity
Small coherence length ξ ~ 3-4 nm
  Sensitive to small defects
  Small first critical field Bc1
    Need to operate in the flux free metastable Meissner state

## Slide 13: Outline
1. Why Nb3Sn?
2. How do we grow it?
3. State-of-the-art performance
4. Case Study: LCLS-II
5. Remaining Challenges

## Slide 14: Cornell Nb3Sn Breakthrough Performance
First non-Nb accelerator cavities ever that outperform Nb at usable gradients!
20× more efficient than Nb at 4.2 K!
S. Posen et al., Applied Physics Letters 106, Issue 8 (2015).

## Slide 15: Nb3Sn Around the World
And many more!

## Slide 16: State-of-the-Art
S. Posen, https://doi.org/10.1088/1361-6668/abc7f7
U. Pudasaini, SRF’19
~4 K operation with at typical CW operating fields achieved at all 3 labs
Current quench fields: 16-22 MV/m (FNAL holds world record)
Reproducible performance!
(Note: Plots are for single cell cavities)

## Slide 17: Ongoing R&D at Cornell
Sample studies to improve nucleation step of vapor diffusion
Electrochemical deposition
Z. Sun et al., in Proc. 2021 International Conference on RF Superconductivity (SRF’21)
Chemical Vapor Deposition (CVD)
G. Gaitan et al., in Proc. 2022 North American Particle Accelerator Conference (NAPAC 2022)
L. Shpani et al., in Proc. 2022 International Particle Accelerator Conference (IPAC 2022)
Thin Film Cavity
N. Verboncoeur et al., in Proc. 2022 International Particle Accelerator Conference (IPAC 2022)
A high field sample host cavity
Nb3Sn Cryomodule R&D
N. Stilin et al., in Proc. 2022 International Particle Accelerator Conference (IPAC 2022)

## Slide 18: Ongoing R&D outside of Cornell (Examples)
FNAL and JLab are working on optimizing the coating process to reduce surface roughness and achieve thinner coatings.
KEK constructed a Nb3Sn coating system, first results obtained in 2021.

## Slide 19: Outline
1. Why Nb3Sn?
2. How do we grow it?
3. State-of-the-art performance
4. Case Study: LCLS-II
5. Remaining Challenges

## Slide 20: Case Study: LCLS-II
Before Coating
After Coating
LCLS-II will be the first XFEL based on 4GeV continuous wave superconducting RF (CW-SRF) accelerator technology.
280 1.3 GHz cavities with of 16 MV/m
Nitrogen-doped niobium SRF cavities can reach high
Operates at 2K

## Slide 21: What if we used Nb3Sn instead?
Before Coating
Nb3Sn at 4.2K
N-doped Nb at 2K
1 W takes 800 W of wall power to cool
1 W takes 200 W of wall power to cool
Using 2K superfluid helium cryoplant.
Using 4K atmospheric cryoplant.

## Slide 22: Outline
1. Why Nb3Sn?
2. How do we grow it?
3. State-of-the-art performance
4. Case Study: LCLS-II
5. Remaining Challenges

## Slide 23: Transferring to Multicell Cavities
C75 cavity made from large grain Nb
Cornell: Multicell coating facility under development.
5-cell 1.5GHz cavity coated and RF tested.
At 4K : 1E10 @ >10 MV/m
C75-RI-04
9-cell 1.3GHz cavities coated and RF tested.
Q0 > 9x109 at quench

## Slide 24: Helium Based Cryomodules
A further challenge is implementing multi-cell cavities in accelerator cryomodules.
G. Eremeev et al., Proceedings LINAC 2016 (MOPLR024)
S. Pokharel et al., Proceedings IPAC 2022 (MOPOTK051)
Nb3Sn cavities for Upgraded Injector Test Facility (UITF) at JLab
Material is brittle – sensitive to deforming
Slow cooldown – need small temperature gradient across cavity
4K operation challenges
  Microphonics

## Slide 25: Conduction Cooled Cryomodules
FNAL Lead: Sam Posen
Nb3Sn for Nuclear Physics (Collaboration ANL/FNAL/Radiabeam)
Nb3Sn for Industrial Accelerators
(Collab. Euclid/FNAL/BNL)
Lead lab
PI: Mike Kelly
Wastewater Treatment

## Slide 26: Key Takeaways
Nb3Sn is a high-potential material for next-generation SRF cavities
  Higher energy gain
  Lower cooling cost and complexity
Nb3Sn coating facilities are established around the World (Cornell, FNAL, JLab, KEK, etc.)
Ongoing R&D will improve Nb3Sn performance of Nb3Sn films
  Thinner films
  Reduced surface roughness
Applications are at early stages
  Multicell Nb3Sn cavities
  Prototype cryomodule testing
  Turn-key compact cryomodules
Stay tuned !