## Slide 1: FRT Developments at CERN
N. Shipman on behalf of:
I. Ben-Zvi, J. Bastard, G. Burt, M. Coly, A. Edwards, C. Jing, A. Kanareykin, A. Macpherson, N. Stapley, H. Timko
Acknowledgements
M. Barnes, D. Barrientos, A. Castilla, F. Gerigk, W. Hofle, P. Kohler, E. Montesinos, G. Pechaud, P. Schneider, D. Smekens, D. Valuch, W. Venturini
Presented at:
ERL Workshop 3-6th October Cornell University

## Slide 2: Introduction
FRTs are a new type of extremely fast non-mechanical tuner
Microphonics suppression with a prototype FRT has been demonstrated
CERN is developing and testing improved FRT designs
Research focus at CERN is now “transient detuning” for HL-LHC
  Compensation of transient beam loading using an FRT

## Slide 3: Agenda
FRTs
Use Cases
Microphonics Suppression Results
Transient Detuning Project
Summary

## Slide 4: FRTs
Introduction to Ferro-Electric Fast Reactive Tuners

## Slide 5: FRT Concept
HV Line
RF Amplifier
Load
Circulator
FPC
FRT
FRT Antenna
An FRT is a shorted co-axial structure containing a ferro-electric element
RF power flows into the FRT and is reflected back to the cavity
Voltage applied to the ferro-electric changes its permittivity
Permittivity change  Phase change of the reflected power  Cavity frequency change
Usually, the FRT would require its own port, although other arrangements have been proposed
Operates outside cryomodule at room temperature
Tunes cavity without mechanical deformation
Tuning speed measured at less than 600ns, limited by HV circuit

## Slide 6: Equivalent Circuit Theory
The admittance of the FRT is:
The change in angular frequency between high voltage states n and m is:
The increase in the system bandwidth due to the FRT in high voltage state n is:
Here the R-over-Q is defined as:
The angular frequency of the cavity without FRT is:
Notation | Meaning
 | Conductance of FRT
 | Susceptance of FRT
 | Coupler turn ratio
 | Cavity voltage
 | Cavity stored energy
Equivalent circuit of FRT connected to cavity
Symbol definitions

## Slide 7: Figure of Merit and Ferro-Electric (FE) Material
FoM allows:
  Comparison of FE-FRT designs
  Estimation of benefit e.g. power reduction
FoM is ~tuning range divided by increase in bandwidth
  Subscripts 1 and 2 refer to the two extreme high voltage ‘end’ states
Material FoM is FoM of a FE capacitor with only dielectric losses
  Material FoM is a theoretical upper limit of FoM
  Would allow comparison of different ferro-electric materials
FE is BaTiO3-SrTiO3 with Mg based additives
  Loss tangent roughly ~ frequency
Parameter | Value
Relative Permittivity | 160
Tunability | 1.4
Tuning Field | 8 Vµm-1
Breakdown Strength | 20 Vµm-1
Thermal Conductivity | 7.02 Wm-1K-1
33 mm
30 mm
A BST(M) Ferroelectric Sample
Loss tangent vs RF frequency
(Courtesy Euclid TechLabs)
FE material parameters

## Slide 8: Use Cases
Microphonics Suppression, RF Switching, Transient Detuning

## Slide 9: Use cases: microphonics suppression
For low beam loading machines RF power is dominated by microphonics
The effect of microphonics can be reduced passively or actively
  Stiffening of cavity
  Isolation of noise sources
  Active feedback e.g. piezo tuners
Residual microphonics require over-coupled FPC
Typically, RF power required is still many times larger than for critical coupling case
Decreasing QL

## Slide 10: Use cases: microphonics suppression
FRTs are an excellent tool for microphonics suppression
  High Tuning speed
    ~600ns measured limited by external HV circuit
  No excitation of mechanical modes
  Simple transfer function/negligible phase delay at frequencies of interest
Peak and average RF power reduced by and respectively
Increased dielectric and conductor losses at higher RF frequencies reduce effectiveness
FRTs can be combined with other suppression technologies
  E.g. piezo tuners
Estimate FRTs could still beneficial up to ~2-3 GHz
  Not experimentally verified
Case study: RF power for PERLE vs Qe with and without FRT
Estimated FRT FoM vs RF frequency

## Slide 11: Use cases: transient detuning
will change so either:
  or must change
Normally, choice between:
  Increased RF power
  Cavity phase errors
Notation | Meaning
 | RF power
 | Cavity phase derivative
 | Detuning
 | Beam Current
RF power required for cavity with beam
Simplifying assumptions
Recently we proposed a new scheme “Transient detuning”
Transient detuning uses FE-FRT to change
  Reduced average RF power (by up to FoM/2)
  Increased phase stability
  Fixed RF bucket position  ideal for injection
In the future, we hope to apply this to HL-LHC, project underway!
Can change
Fixed

## Slide 12: Use cases: transient detuning
RF Amplifier
Load
Circulator
FPC
FRT
FRT Antenna
HV Line
Beam + fixed detuning

## Slide 13: Use cases: transient detuning
RF Amplifier
Load
Circulator
FPC
FRT
FRT Antenna
HV Line
Beam + transient detuning

## Slide 14: Microphonics Suppression Results
Overview of results with prototype FRT

## Slide 15: Microphonics suppression results
Lower order mode of UK4R crab cavity at 374MHz
  Very stiff  very low levels of microphonics  used vibration generator
Euclid Techlabs designed prototype FRT
No slow tuner  driven in Self Excited Loop mode
Chiller, phase shifter, vibration generator
Deliberately simple purely integral feedback used
  More performant solutions surely possible
FE-FRT temp.
Bath temp.
regulation on
bunker opened
Euclid FE-FRT prototype
Temperature regulation with chiller
UK4R on insert
Phase shifter on top plate
Vibration generator

## Slide 16: Microphonics suppression results
Vibration generator set to 37Hz
Spectral density also shows good suppression at higher frequencies e.g. ~600Hz
Peak deviation with correction 1.2Hz
Prototype issues: long transmission line, lossy brazing
  Low FoM
  Little to no RF power reduction
F
No correction
With correction

## Slide 17: Transient Detuning Project
Overview of transient detuning research at CERN

## Slide 18: Transient Detuning Project: Overview
Likely HL-LHC will not have sufficient RF power to capture full beam current at injection
  Install high efficiency Klystrons
  Add new cryomodule
  Transient detuning with FE-FRT
Perfect compensation of beam loading with FRT would reduce RF power requirements 10-fold
  If Qe of FPC is increased by optimal amount
  Would require FE-FRT to handle high reactive power ~500kVar
  Partial compensation can also give significant reductions
If proven feasible transient detuning is elegant and cost-effective solution
  Electricity saving up to ~ 2GWh per year ~1M€ (very rough estimate from French electricity cost on 28.09.22)
Aim: demonstrate an FE-FRT could compensate transient beam loading for HL-LHC at injection
Estimated power reduction vs achievable tuning range with transient detuning

## Slide 19: Transient Detuning Project: TDD0
RF designs of FRT focused on coupled mode scheme
  FRT resonance jumped across cavity resonance
  Greater phase shift and larger tuning range with smaller antenna
  Discontinuous tuning range – not suitable microphonics suppression
Brazeless (compression fit) thin wafers of ferro-electric in vacuum
  Aim: reduced losses + higher biasing electric fields
  + greater change in permittivity at reduced voltage
First prototype TDD0 (Transient Detuning Demonstrator) built and tested on cold LHC cavity
Result: 1.3kHz tuning shift observed with 500V
  Test cut short due to cavity vacuum leak
  TDD0 designed for 10-16kV, voltage limited due to vacuum leak on TDD0
Lessons learned:
  FerrElectric stack sensitive to air gap/compression force
  Care must be taken to apply compression evenly
  Implementation of rigid line in cryostat susceptible to mechanical stress and losses
    Place FRT inside cryostat for next test.
TDD0 produced reproducible 1.3kHz frequency shift on cold LHC cavity with 500V applied across FerroElectric.
Simulated discontinuous frequency shifts of LHC cavity with TDD 0 in different configurations.
TDD 0 design, ferro-electric wafers shown in white.
Left: TDD 0 during assembly, shape of ferro-electric dictated by geometry of samples in stock.
Right: TDD0 installed on top plate.
Top: uneven compression force cracked ceramic.
Left: Large diam. rigid line caused vacuum leak.
Right: Breakdown through ceramic near cracks?

## Slide 20: Transient Detuning Project
LHC LLRF System
  LHC LLRF system is complex and will not be redesigned for HL-LHC
  Transient detuning must work with existing LLRF system
  LHC LLRF system replicated in cavity cold testing area
  No One Turn Feedback Module in last test now installed, waiting to be tested
BLEEP
  Beam Loading Electronic Emulation Project
  Testing with cryomodule with real beam not feasible in initial project timescale
  BLEEP adds correct RF power and phase to input coupler to replicate beam pattern
High Voltage Pulser for biasing FE ceramic
  High voltage pulser design is challenging: must follow bunch train pattern
  HVP ordered capable of running @146kHz, 7kV, for ~10ms
  Final HVP design would need to run continuously
TDD 1
  Fabrication by end of year/Q1 23
  Demonstrate transient detuning @ low power with LLRF, BLEEP, HVP: Q1 23
  Test high power operation: Q2 23
BLEEP replicated beam pattern causes several degrees of uncorrected phase error if One Turn Feedback Module (OTFB) absent from LLRF.
Orange: LHC beam pattern replicated with BLEEP
Blue: Cavity phase controlled with LLRF without OTFB
Green: Target phase for LLRF
Parameter | Value | Parameter | Value
Total Capacitance | 2 nF | Rise, Fall Time | 100ns
High Voltage | 7 kV | Power Supply Rating | 14.4 kW
Energy per pulse | 49mJ | (Dis)charge current | 140 A
Burst Pulse Rate | ~146 kHz | Burst Duration | 10ms
LHC bare cavity preparation on insert
BLEEP and replicated LHC LLRF system in control room of SM18 cavity cold test area.
High Voltage Pulser specification.
High Voltage Pulser for transient detuning tests.

## Slide 21: Summary

## Slide 22: Summary
Microphonics
Excellent microphonics suppression demonstrated
  With very simple feedback
Prototype FRT too lossy
   no RF power reduction demonstrated
  Low hanging fruit!
Presently no FRT microphonics research at CERN
Transient Detuning
CERN R&D focused on transient detuning
  Use case: HL-LHC injection
  Much of research generally useful for FRTs
Elegant but demanding application
  Offers: Large RF power saving and reduced phase errors
  Requires: Large tuning range; high reactive and dissipated powers
TDD 0 built and tested
  TDD0 first coupled mode and FE stack assembly FRT
  1.3kHz tuning already obtained on LHC cavity
  TDD1 coming soon!

## Slide 23: Thank you for your attention
N. Shipman
nicholas.shipman@cern.ch