## Slide 1: Molecular beam epitaxy of Cs-Sb thin films: structure-oriented growth of high efficiency photocathodes
Alice Galdi
Department of Industrial Engineering Università degli Studi di Salerno (Italy)
CLASSE, Cornell University

## Slide 2: People
Jared Maxson
Chad Pennington
Vivek Anil
Maxson group
Shen group
Tomàs Arias
Arias group
J. Kevin Nangoi
Kyle Shen
Chris Parzyck
Hines group
Mellissa Hines
Will DeBenedetti
Jan Balajka
Alice Galdi
Hanjong Paik
Brendan Faeth
Luca Moreschini
Cheng Hu
Darrel Schlom
Elena Echevarria
https://cbb.cornell.edu/ https://www.paradim.org/

## Slide 3: Outline
Motivation:
  Cs3Sb for brighter electron beams
  Surface disorder and emittance degradation
Methods:
  RHEED monitored molecular beam epitaxy
Results: epitaxy of Cs3Sb phase! (first time!)
  First band structure measurements of Cs3Sb thin films
Results: new phase!
  Atomically smooth CsSb films: a visible light photoemitter with enhanced oxygen robustness
Future work and conclusions

## Slide 4: Cs3Sb for low emittance, high current
Beam current: quantum efficiency, laser fluence, lifetime
Mean transverse energy: Intrinsic momentum spread + roughness + laser heating + …
λ=520 nm
~25 meV at 300 K
~8 meV at 90 K
~0.3 mm mrad
λ=690 nm, QE=0.7e-4
B. Dunham et al. APL 102, 034105 (2013)
L. Cultrera et al., Phys. Rev. STAB 18 (2015) 113401
Cs3Sb/Na2KSb: next generation spin polarized photocathode?
V.S. Rusetsky et al, arXiv:2205.03693 [cond-mat.mtrl-sci]

## Slide 5: Drawbacks: reactive, disordered
λ=504 nm
σ=2.4 nm
σ=1.75 nm
Why does this matter for applications?
Because both heterogeneity enhaced by oxidation and roughness degrade MTE
(besides QE degradation in poor vacuum)
Measured surface and surface potential of a Cs3Sb photocathode
G. S. Gevorkyan, PRAB 21, 093401 (2018)
compare to measured:
A. Galdi, et al. The Journal of Chemical Physics 153,144705 (2020)
A Galdi, et al. Applied Physics Letters 118 (24), 244101

## Slide 6: Single crystalline photocathodes: epitaxy
Cs
flux
Sb
flux
Epitaxy is the growth of a crystal layer with one or more well-defined orientations with respect to an underlying crystal seed layer (usually a single crystal substrate)
Substrate
Epitaxial single-oriented films would allow:
Roughness control
Orientation control  surface potential control
Measurements of intrinsic properties (optical constants, band structure, intrinsic MTE…)
Epitaxial
layer
Choose the method: MBE
Select suitable substrates
Identify suitable growth conditions
reaction-interdiffusion
adsorption
diffusion
nucleation
re-evaporation

## Slide 7: Cs3Sb structure and possible epitaxial relations
4 X SiC (a=0.436 nm)
1 X Cs3Sb (a=0.9165 nm)
≈
Sb3-
Cs+
≈5%
≈-1%
Based on previous studies, we selected 3C-SiC as substrate (but also tested: TiO2 , MgF2)
A Galdi, et al. Applied Physics Letters 118 (24), 244101
<100>
1x Sb +3x Cs
1x Sb +3x Cs
1x Sb +3x Cs
1x Sb +3x Cs
Jack and Wachtel (1957)
Sb3-
Cs+

## Slide 8: Previous results
Our work builds on many experimental results obtained via in-operando characterization of the growth of alkali antimonide thin films with different techniques.

## Slide 9: RHEED assisted MBE @ PARADIM
PARADIM Thin Film User Facility
Molecular Beam Epitaxy System
  In Operando high energy electron diffraction (RHEED)
  Pbase = 2x10-9 torr
Sample Transfer System
  In Situ Quantum Efficiency Station (biased pickup coil)
  Pbase = 1x10-9 torr
ARPES/XPS System
  Scientia DA30 electron analyzer
  Fermi Helium Plasma discharge lamp
  Specs XR50 Al/Mg X-ray source
  Pbase = 7x10-11 torr
Sample
15kV e- gun
Detector
Reflection High Energy Electron Diffraction
(RHEED)
Angle Resolved Photoemission Spectroscopy
(ARPES)
Helium plasma discharge lamp
hv=21.22, 40.81 eV
(+X-ray tube
Mg/Al anode
1.254/1.487 keV)
Hemispherical electron analyzer
Epass = 2-100 eV
MBE loadlock
ARPES loadlock
Transfer chamber
STORAGE
MBE
w. RHEED
ARPES
XPS
LEED
QE measuring station
vacuum suitcase
to UHV STM/XPS

## Slide 10: RHEED assisted MBE @ PARADIM
PARADIM Thin Film User Facility
Molecular Beam Epitaxy System
  In Operando high energy electron diffraction (RHEED)
  Pbase = 2x10-9 torr
Sample Transfer System
  In Situ Quantum Efficiency Station (biased pickup coil)
  Pbase = 1x10-9 torr
ARPES/XPS System
  Scientia DA30 electron analyzer
  Fermi Helium Plasma discharge lamp
  Specs XR50 Al/Mg X-ray source
  Pbase = 7x10-11 torr
Sample
15kV e- gun
Detector
Reflection High Energy Electron Diffraction
(RHEED)
Angle Resolved Photoemission Spectroscopy
(ARPES)
Helium plasma discharge lamp
hv=21.22, 40.81 eV
(+X-ray tube
Mg/Al anode
1.254/1.487 keV)
Hemispherical electron analyzer
Epass = 2-100 eV

## Slide 11: The experiment
Cs
Sb
Substrate
heater
Current
Light source
QMB
Cs/In
Sb
Substrate
heater
QMB
RHEED
Typical photocathode growth: Photocurrent monitored
Quantum efficiency oriented
Our growth method:
RHEED monitored
Structure oriented

## Slide 12: Information provided by RHEED
Single crystal
kin
kout
Fluorescent screen
By rotating the sample around its surface normal, we intersect different sets of reciprocal space rods
Real-time
Sub-ML sensitivity
Qualitative probe of surface roughness and crystallinity
Θ
Φ=0°
Φ=45°
Single crystal
High coherence
Film
Reduced coherence
Roughened surface
Film
Polycrystalline domains/impurities

## Slide 13: Temperature study: codeposition
Cs-Sb co-deposition on SiC substrates
  Cs:Sb ratio = 6:1 (as measured by Quartz Crystal Microbalance)
Higher Growth Temperature
Improved Crystal Order
OOP Film Orientation
Reduced Surface Roughness
Reduced Quantum Efficiency
Lower Growth Temperature
Improved Quantum Efficiency
Polycrystalline Films
Polycrystalline
Rough
Fiber texture
Flat
Low crystallinity
Rough
λ=504 nm
Notes: We started the study by observing how the growth temperature affects the samples properties while we deposit at the same time Cs and Sb. The quantum efficiency decreases as we increase the temperature; however, if we look at the structure, we observe that the high quantum efficiency sample is polycrystalline and has a rough surface, the intermediate samples appear to have low crystallinity, but above a certain temperature the structure changes and becomes flat, so that we observe streaks in the rheed pattern. So how can we achieve at the same time a good, ordered crystalline structure and high quantum efficiency?

## Slide 14: Solid Phase (Molecular Beam) Epitaxy
Time
Low Deposition temperature to take advantage of improved Cs sticking coefficient
High temperature Cs anneal to improve crystallinity
T=40°C
T=85°C

## Slide 15: It is epitaxial!
SiC [10]
Cs3Sb [10]
Cs3Sb [11]
SiC [11]
Φ=0°
Φ=45°
e-
e-

## Slide 16: It really is Cs3Sb: XPS and ARPES
C. W. Bates, et al. Thin Solid Films 69, 175 (1980)
XPS: perfect agreement
ARPES: larger bandwidth (Strain? Structure distortion?)

## Slide 17: High efficiency in the ultrathin limit
Grey line and dots represent the data from a codeposited Cs3Sb sample grown by photocurrent-monitored codeposition.
Enhanced QE:
At the photoemission threshold
At small thickness
C.T. Parzyck, A. Galdi et al. Physical Review Letters 128, 114801

## Slide 18: Temperature study: codeposition
Cs-Sb co-deposition on SiC substrates
  Cs:Sb ratio = 6:1 (as measured by Quartz Crystal Microbalance)
Higher Growth Temperature
Improved Crystal Order
OOP Film Orientation
Reduced Surface Roughness
Reduced Quantum Efficiency
Lower Growth Temperature
Improved Quantum Efficiency
Polycrystalline Films
Polycrystalline
Rough
Fiber texture
Flat
Low crystallinity
Rough
λ=504 nm

## Slide 19: Flat co-deposited samples
kin
kout
In vacuum transfer to STM
0.6 nm
Raw
FFT-filtered
Lattice: 0.76 nm x 1.42 nm
FFT
Cs3Sb

## Slide 20: Flat co-deposited samples
CsSb parameters:
  a = 7.34 Å
  b = 7.57 Å
  c =13.27 Å
  P1 structure
Structure and composition data suggest that the compound we are forming is closely related to CsSb

## Slide 21: Current work in PHOEBE @ Cornell U.
TE-meter
Vacuum suitcase
Sample preparation
Photocathode MBE
Clean hood
PHOEBE: PHOtocathode Epitaxy and Beam Experiments laboratory
Study of epitaxial Cs3Sb and CsSb samples: spectral response, lifetime, oxygen resistance, mean transverse energy
Chad Pennington
Elena Echevarria

## Slide 22: Conclusions
Epitaxy of Cs3Sb is achieved using molecular beam epitaxy via monitoring the sample structure with RHEED
State-of-the-art MBE machines and in-situ RHEED allow to explore various growth regimes and efficient optimization of the samples beyond quantum efficiency
High throughput:
  PARADIM experiments: 59 samples grown in 27 days (24h per day)
  PHOEBE: 75 Cs-Sb samples grown between 09/2021 and 08/2022
Structure-oriented growth identifies an interesting phase: CsSb
  Atomically smooth
  Easily achievable via codeposition
  QE ~1% at 400 nm
  Robust against oxidation

## Slide 23: Information provided by RHEED
Epitaxial island growth
kin
kout
Polycrystalline islands
kin
kout
No texture
Textured film
No rotation dependence if the texture axis is out-of-plane (uniaxial)
Rotation dependence if the texture axis is in-plane (biaxial)
Fiber texture
Transmission pattern:
Streaks turn into spots

## Slide 24: Epitaxial Relationship
Substrate
Fully Ordered
Fiber Textured Film
Only c-axis oriented
Partially Ordered Film
Epitaxial Film