## Slide 1: Capability and Prospects for High Current Polarized Beams from GaAs DC Photoguns
Joe Grames
CEBAF Polarized Photogun

## Slide 2: DC guns have demonstrated mA CW beam current from GaAs
JLab 10 kW Upgrade IR FEL DC gun
Gun operating voltage: 350 kV
Sustained beam current: 8 mA CW at 532 nm
Photocathode lifetime at 5 mA CW: 550 h
Total charge extracted from a single bulk GaAs photocathode: 7000 C
Cornell DC gun
Gun operating voltage: 250 kV
Max beam current: 52 mA CW at 532 nm
Total charge extracted from a single bulk GaAs spot: 200 C
V. SHUTTHANANDAN et al., “Surface science analysis of GaAs photocathodes following sustained electron beam delivery”, Phys. Rev. ST Accel. Beams 15, 063501 (2012)
B. Dunham et al., “Record high-average current from a high-brightness photoinjector”, Appl. Phys. Lett. 102, 034105 (2013)
Total CW beam time delivered by a single GaAs wafer: 900 h
Horizontal SF6 tank
Vertical SF6 tank

## Slide 3: First Observation of Polarization from GaAs reported in 1976
light
QE
vacuum
bias
polarimeter
Diced GaAs wafer
780nm
530 nm

## Slide 4: High Polarization GaAs Photocathodes
Images: Pablo Saez PhD Dissertation, Stanford 1997
GaAs Substrate
GaAs(1-x)Px Graded Layer
GaAs0.64P0.36
Buffer
Active Region
2.5mm
2.5mm
100 nm
From Aaron Moy, SVT Assoc and SLAC, PESP2002
QE 1% and Polarization 85%
Strained Superlattice Photocathode
Bulk GaAs
Max P=50%
Strained GaAs
Split degeneracy
Max P=100%

## Slide 5: CEBAF : spin polarization from GaAs photocathodes
….…
Reliable
expectation
Reliable
expectation
GaAs photocathodes with both high QE and POL is the enabling technology.
Chart: Polarization (%)
| 1.67 | 10.4 | 50.5 | 100.5 | 250.5 | 504 | 755 | 1011 | 1.06
 | 85.6704 | 84.5218 | 84.3896 | 85.3479 | 84.9536 | 86.116 | 84.7714 | 85.9647 | 87.1486
Polarization measured by Mott polarimetry at 5 MeV (sampled from beam)

## Slide 6: Diffracted Bragg Reflector (DBR) superlattice
W. Liu, S. Zhang, M. Stutzman, M. Poelker, Y. Chen, W. Lu, and A. Moy, Appl. Phys. Lett. 109, 252104 (2016)
July 2022 (unpublished) results of collaboration between Old Dominion University, Brookhaven National Lab and Jefferson Lab
MOCVD growth of DBR-SLSP by industrial partner
  QE > 2%
  Polarization > 90%
> 10 mA/W

## Slide 7: Polarized electron source landscape…
CW < 1 pC
(< 200 mA)
Pulsed > 1 nC
(< 100 mA)
CW < 1 nC
(> 1000 mA)
Older sources
Newer sources
Prepared table Spring 2022 for Snowmass workshop on Electron Sources …

## Slide 8: CEBAF 12 GeV : cw high-energy electron accelerator
Parameter | Value
Topology | Recirculating LINACS (1– 5.5 pass)
Multiplicity | 4 halls
Energy | 11 GeV (ABC) / 12 GeV (D)
Duty Factor | 100% (1.497 GHz)
Intensity | 170 mA (1 MW dumps)
Polarization | >85%
Helicity | 2 kHz
Spin polarized electron beams for over 25 years...
1.1 GeV SRF LINAC
D
1.1 GeV SRF LINAC
A
C
B
Photoinjector (123 MeV SRF)

## Slide 9: PEPPo : Polarized Electrons for Polarized Positrons
D. Abbott et al., Phys. Rev. Lett. 116 (2016) 214801
P(e+) = 82.2 %
Efficiency >95%
Record for linac positron polarization.
J. Grames, E. Voutier et al.,JLab Experiment E12-11-105 (2011)
8 MeV, 1mA, 85% polarization
PEPPo possible due to support from SLAC E166, DESY, Princeton, Cornell, International Linear Collider Project and the Jefferson Science Associates
Tungsten (1mm)
The spin transfer from e- to e+ was tested in a feasibility experiment at CEBAF in 2012

## Slide 10: What next ?
…many of us imagined constructing a new vault here.
We have been evaluating where to build & stage a new 123 MeV e+ injector…
123 MeV
123 MeV

## Slide 11: PEPPo II : Polarized e+ Prototype Experiment
11
#6 – SRF accelerate e+ to 123 MeV
#4 - Produce e+ accelerate to 50-70 MeV
#2 - SRF accelerate 60-120 MeV
#1 – Compact P-Gun, Wien filter, 10 MeV e- injector
#3 – Extract e- to target
#7 – Transport e+ at 123 MeV to exit LERF
#5 – Injector e+ to linac
Next, we want to build a scalable polarized positron injector at LERF to demonstrate beam
  300 kV polarized gun + Wien filter, demonstrate > 1kC lifetime at milliamp current
  Build up the SRF e- injector 50 – 100 MeV
  Ramp up efforts for high power target 50 – 100 kW, e+ collection and compression
  Complete start-to-end concept in FY23
A e+ collection efficiency of 10-4 requires polarized e- intensities > 1 mA for a program

## Slide 12: Can the CEBAF photo-gun support an e+ program?
PhD work of J. Yoskowitz in preparation for PR-AB
With a >400 C lifetime we could operate at 1 mA for almost 1 week
Positively biasing the photo-gun anode has had a tremendous impact on JLab gun lifetime.

## Slide 13: Optimizing the gun voltage for charge lifetime
Fewer ions created as gun voltage increases
Ion generation largest here
What about the cathode potential, i.e. is there is “best” potential for increasing charge lifetime?

## Slide 14: Modeling ion generation and bombardment
GPT custom element IONATOR simulates electron-impact ionization of residual beam line gasses and tracks outgoing particles.
Simulations of ion back-bombardment predict ions created within the cathode-anode gap, depositing their energy at the photocathode, closely resembles the measured damage pattern.
Measured
PhD work of Josh Yoskowitz
Simulated
Simulated
QE Loss
e- beam
ions
ejected e-
scattered e-
Simulation of biased anode

## Slide 15: Measuring charge lifetime dependence on cathode potential
100 vs. 180 kV
NA-PAC 2022 (WEPA13)
Biased
Exploratory measurement to map out conditions for an experiment at the UITF.

## Slide 16: PES: reducing ion surface density to increase lifetime
J. Grames, et al., Phys. Rev. ST Accel. Beams 14 043501 (2011)
Bulk 532nm
GaAs/GaAsP 780nm
Increasing laser beam size at photocathode has increased charge lifetime…

## Slide 17: GaAs/GaAsP charge lifetime at milliamp current
J. Grames, P. Adderley, J. Hansknecht, R. Kazimi, M. Poelker, D. Moser, M. Stutzman, S. Zhang, “Milliampere beam studies using high polarization photocathodes at the CEBAF Photoinjector” Polarized Sources, Targets and Polarimeters Workshop, Dajeon South Korea (2017)
Days
Trend we want to realize
Measurements were performed without anode biasing
Results from PSTP’17 suggests increasing laser spot size is viable to exceed >500 C lifetime; however we need to build another gun to test this assertion.

## Slide 18: Build a mA polarized gun for e+
  Next, we want to combine our lessons learned and experience with the Magnetized 4mA/300 kV gun and new Polarized CEBAF 200 kV gun to build a new third gun optimized for positron generation…
300 kV Magnetized Beam Electron Source (CsKSb)
C. Hernandez-Garcia et al., Phys. Rev. Accel. Beams 22, 113401 (2019)
R30 inverted geometry ceramic insulator
Conditioned to 350 kV
Demonstrated 4.5 mA CW 300 keV
Operate at >200 kV without field emission
HV conditioning >350 kV (uses R30 inverted ceramic insulator)
Dynamic pressure (during beam delivery) ~ 1x10-12 Torr
CEBAF 200 KV Polarized Gun (GaAs/GaAsP)

## Slide 19: Summary and Outlook
SLSP GaAs photocathodes have been used to make mA intensity with polarization >85 %.
DBR photocathodes offer >10 mA/W, so cathode cooling may not always be necessary
Biasing anode has increased charge lifetime of GaAs/GaAsP in CEBAF 130 kV gun > 400 C
Increasing laser size affords gains up to ratio of increase – increasing area >5mm2 (while managing all the beam) should achieve a charge lifetime > 1000 C in the CEBAF photo-gun.
Optimizing the gun voltage for lifetime remains an important parameter to consider.
It is not unreasonable to imagine sustainable mA beams soon.