## Slide 1
​Building the ASU Cryogun beamline as a photocathodes testing platform
Gevork S. Gevorkyan
October 2022
Center for
BRIGHT BEAMS
A National Science Foundation Science & Technology Center
Ggevorky@asu.edu

## Slide 2: ​Building the ASU Cryogun beamline as a photocathodes testing platform
P. Musumeci, et al, Nucl. Instrum. Meth. A, 907, 209 (2018)
W. H. Li, et al, Structural Dynamics 9.2 024302 (2022)
Contents:
Purpose of this project
Gun design and assembly
Gun cryogenic cooling
Gun voltage conditioning
Design of the beamline for cathode diagnostics

## Slide 3: Purpose – Brightness and Emittance
Beam emittance is
the area occupied in
phase space by the
particle distribution

## Slide 4: Photocathode and Emittance
D. H. Dowell, J. F. schmerge, Phys. Rev. STAB, 12, 074201 (2009)

## Slide 5: Photocathode and Emittance
D. H. Dowell, J. F. schmerge, Phys. Rev. STAB, 12, 074201 (2009)

## Slide 6: Photocathode and Emittance
Non-linear Photoemission
Thermal Effects
Physical Roughness
Chemical Roughness
…
Photocathode Cartoon
Need atomically ordered surface, cold photocathodes!
G. Gevorkyan, et al. Phys. Rev. STAB, 21, 093401 (2018)
P. Saha, et al., Appl. Phys. Lett. 120, 194102 (2022)
Rough vs Smooth Cs3Sb

## Slide 7: Photocathode and Emittance
RHEED Cs3Sb (SiC)
Ag (111)
Cu (100)
Total
Transverse
MTE 25 meV
QE:
S. Karkare, et al, Phys. Rev. Lett., 118, 164802 (2017)
S. Karkare, et al, Phys. Rev. Lett., 125, 054801 (2020)
A. Galdi, et al, Phys. Rev. Lett. 128, 114801 (2022)
MTE expected 25 meV at 300 K
QE:
MTE 5 meV | QE:

## Slide 8: RF and DC Electron Guns
RF Guns
DC Guns
Emission from backplate (copper)
INFN Cathode
D. Alesini, et al, Phys. Rev. Lett. STAB, 18, 092001, (2015)

## Slide 9: ​Building the ASU Cryogun beamline as a photocathodes testing platform
P. Musumeci, et al, Nucl. Instrum. Meth. A, 907, 209 (2018)
W. H. Li, et al, Structural Dynamics 9.2 024302 (2022)
Contents:
Purpose of this beamline
Gun design and assembly
Gun cryogenic cooling
Gun voltage conditioning
Design of the beamline for cathode diagnostics

## Slide 10: ASU Cryocooled DC Electron Gun
H. Lee, et al, Rev. Sci. Instrum., 89, 083303, (2018)
G. Gevorkyan, et al, Proc. NAPAC’19 OPLM16 (2019).
Based on Cornell’s
Cryogun Design
C – Cryoshielding
D – Thin Wall Tube
E – HV plug
F – Omicron Paddle
G – Pierce Electrode
A – Cryostat
B – Sapphire rod
H – Conical Anode

## Slide 11: ASU Cryocooled DC Electron Gun
Pump
Pump

## Slide 12: ASU Cryogun - Cathode
Omicron Paddle
10 MV/m at 200 kV

## Slide 13: ASU Cryogun - Cathode

## Slide 14: ASU Cryogun - Cathode

## Slide 15: Surface Preparation and Assembly
120+C for 50 hours
Activated NEG Pumps
P ~ Torr
Water flosser HPR
C. Hernandez-Garcia, et al, Review of Scientific Instruments, 88.9, 093303 (2017)
Rotary tumbler polishing
CO2 Snow-jet cleaning
Ultrasonic

## Slide 16: ​Building the ASU Cryogun beamline as a photocathodes testing platform
P. Musumeci, et al, Nucl. Instrum. Meth. A, 907, 209 (2018)
W. H. Li, et al, Structural Dynamics 9.2 024302 (2022)
Contents:
Purpose of this beamline
Gun design and assembly
Gun cryogenic cooling
Gun voltage conditioning
Design of the beamline for cathode diagnostics

## Slide 17: Cryocooling of the Gun
Helium Liquifier Plant

## Slide 18: Cryocooling of the Gun
Calibration – Cathode Temperature vs Time

## Slide 19: Cryocooling Calibration of the Gun
Cooling the Electron Gun

## Slide 20: ​Building the ASU Cryogun beamline as a photocathodes testing platform
P. Musumeci, et al, Nucl. Instrum. Meth. A, 907, 209 (2018)
W. H. Li, et al, Structural Dynamics 9.2 024302 (2022)
Contents:
Purpose of this beamline
Gun design and assembly
Gun cryogenic cooling
Gun voltage conditioning
Design of the beamline for cathode diagnostics

## Slide 21: HV Conditioning Status

## Slide 22: HV Conditioning Status

## Slide 23: Electron Gun - first beam in progress!

## Slide 24: ​Building the ASU Cryogun beamline as a photocathodes testing platform
P. Musumeci, et al, Nucl. Instrum. Meth. A, 907, 209 (2018)
W. H. Li, et al, Structural Dynamics 9.2 024302 (2022)
Contents:
Purpose of this beamline
Gun design and assembly
Gun cryogenic cooling
Gun voltage conditioning
Design of the beamline for cathode diagnostics

## Slide 25: Design of the beamline
Pinhole scan technique for 4D phase space mapping
Solenoid scan emittance measurements
3.0 GHz deflection cavity for time response
Solenoids
Deflection Cavity
Buncher Cavity
Corrector Coils
Screen
Slit

## Slide 26: Recap – Brightness and emittance
Beam emittance is
the area occupied in
phase space by the
particle distribution

## Slide 27: Emittance measurements
Move the pinhole to probe the beam, Alternatively, move the beam across the pinhole using corrector coils.
M. Gordon, et. al., “Four-dimensional emittance measurements of ultrafast electron diffraction optics corrected up to sextupole order,” Phys. Rev. Accel. Beams 25, 084001 (2022)

## Slide 28: Emittance measurements
Beam Parameters
Beamline Elements
Simulate electrons via GPT
Image electrons with detector
MATLAB Code
Phase Space
(X and Y)
Can measure up to 1 nm.rad with 4% error

## Slide 29: Beamline in progress
Questions? Thank you!