## Slide 1: Raman-based wavelength conversion for seeding and optical pumping of CO2 laser amplifiers
William Li, Brookhaven National Laboratory
AAC, November 6-11, 2022

## Slide 2: Acknowledgments
BNL ATF
  Marcus Babzien, Karl Kusche, Rotem Kupfer (now at LLNL), Igor Pogorelsky, Mikhail Polyanskiy, Mark Palmer
BNL Chemistry
  Furong Wang, James Wishart
BNL Instrumentation
  Luca Cultrera, Triveni Rao
Stony Brook University
  Navid Vafaei-Najafabadi
This work was funded by BNL Laboratory Directed Research and Development grants LDRD-001-21 and LDRD-18-026, and U.S. Department of Energy Office of Science contract DE-SC0012704.

## Slide 3: Why CO2?
Ponderomotive force scales with the square of the wavelength
Applications such as LWFA and HHG benefit from going to long wavelengths
Typically, Ti:sapph lasers, with a wavelength of ~800 nm have been employed in these experiments
CO2 lasers can produce an order of magnitude longer wavelength
Brunetti, Scientific Reports 12, 6703 (2022)
Popmintchev, Science 336, 1287 (2012)

## Slide 4: LWIR laser at the Accelerator Test Facility
Polyanskiy, OSA Continuum 3, 459 (2020)

## Slide 5: Improving performance
Increase seed energy
Optical pumping
Improved energy stability and repetition rate
9.2 μm
4.5 μm
Reduced gain narrowing and pulse length
Polyanskiy, OSA Continuum 3, 459 (2020)

## Slide 6: Higher pump energy
Seed: 2 µJ
Two CO2 amplifiers
Amplification ~1011
Seed: 10 mJ
Single CO2 amplifier
Amplification ~103
Polyanskiy, Photonics 8, 101 (2021)
M. Polyanskiy: WG7+8, Thursday, 2:10 PM

## Slide 7: Raman scattering
How do we generate the necessary wavelengths?
Inelastic scattering with vibrational modes, known as Raman scattering
Commonly used for spectroscopy
Vibrational energy states
Virtual energy states
Stokes
(give energy to vibrations)
Anti-Stokes
(take energy from vibrations)

## Slide 8: Raman conversion
‘Cheap’ high energy laser source ωp
Raman Converter
Residual pump ωp
Converted pump ωp- ωtarget
Nonlinear crystal
Residual pump ωp
Converted pump ωp- ωtarget
ωtarget
Typical Raman shifts are on the order of 1000 cm-1
Perfect for generating LWIR!

## Slide 9: Improving performance
Increase seed energy
9.2 μm
Reduced gain narrowing and pulse length

## Slide 10: Seed generation in calcite
Ti:sapph input
BGSe crystal suppresses two-photon absorption
Calcite chosen for availability and correct vibrational modes
BaGa4Se7
simulated
simulated

## Slide 11: Calcite conversion
Spectrum redshifts as the conversion saturates
“tunable”
Large amount of residual 800 nm and converted 876 nm.
Suitable for DFG in the BGSe crystal.
Recently received BGSe crystals. DFG in near future.

## Slide 12: Improving performance
Optical pumping
Improved energy stability and repetition rate
4.5 μm

## Slide 13: Ionic liquids
Artificial salts that are liquid at room temperature
Can be designed to have specific properties
Selection criteria:
  Transparent at pump and Stokes wavelengths
  Peak Raman cross section at desired shift
  High viscosity (suppressing Brillouin scattering)
  Good stability
Desired shift (~4300nm for optical pumping of CO2) using anions containing nitrile groups (C-N triple bonds)

## Slide 14: Ionic liquids experimental setup

## Slide 15: EMIM DCA Raman conversion
Good spectrum
3x higher efficiency than water
Low Brillouin scattering losses
Good temporal profile

## Slide 16: EMIM DCA Raman conversion
IL not damaged by this process
Good spatial profile

## Slide 17: Future work
Examine other ionic liquids
Employ DFG to produce the actual seed and pump wavelengths

## Slide 18: Conclusion
Typical Raman shift energies suit them for generating LWIR wavelengths through DFG
We have demonstrated appropriate Raman shifts from commonly available solid-state laser wavelengths (Ti:sapph and Nd:YAG)
Raman shifting provides a simple, flexible method for wavelength conversion