## Slide 1
Exploring potential of 3D printed structures in PW laser driven ion acceleration
Sergei Tochitsky, Nuno Lemos, R.A. Simpson, D.A. Mariscal, A. Pak, J. Chou, F. Fiuza, D. Haberberger, A. Haid, and C. Joshi
Neptune Laboratory, Department of Electrical Engineering, UCLA
Lawrence Livermore National Laboratory
Stanford Linear Accelerator National Laboratory
Laboratory for Laser Energetics
General Atomics

## Slide 2
Good Old TNSA mechanism with proton energy scaling Ep∞a0
Petawatt class laser
EL ~ 300-500 J
tL = 500-800 fs
rL ≤ 10mm
IL = 3-5x1020W/cm2
H+
UCLA
-K. Zeil et. al., New J. Phys. 12, 045015 (2010)
GSI-F. Wagner et al, PRL, 116, 205002 (2016);
RAL-A. Higginson et al, Nat. Commun. (2018)
PW Laser Driven Ion Accelerators 2022
GSI, 2016
RAL, 2018
Enhanced TNSA/RT regime in
≥100 nm nanofoils
Emax H+ = 94MeV
AAC-2022

## Slide 3
TIM12
Θ = 0, ɸ = 0
Thomson Spec.
TIM10
Θ = 27, ɸ = 0
EPPS1
1-mm beam
Target
Focused OMEGA EP Laser
~700 TW, 700-800 fs
Along same line of sight but slightly below target
( EPPS Diagnostic)
Proton Beam Imager & Energy Spectrometer (“PROBIES”)
+ RCF layers
New ion acceleration platform: pinted targets
AAC-2022
a0~10-20
General Atomics 3D Printed target
OMEGA EP UCLA’s NLUF experiment 2022-2023.
Notes: We expect with CSA to see a more monoenergetic proton spectrum, perhaps a different spatial distribution, and PROBIES can directly give you that information. EPPS measures energies of up to 10MeV, and PROBIES goes up to 60 MeV+ spatial distribution.

## Slide 4
Dt = 325 ps
A 3D designer microstructure target GA
X-ray
AAC-2022

## Slide 5
Two-Photon Absorption Laser Nanoprinting
Voxel size for l=800 nm, transverse l/4=200 nm, axial ~500 nm
AAC-2022

## Slide 6: 3D log-pile structure works as a system of organized wires in which laser light eventually hits the wire. Targets with stochastic or randomly distributed wires have been also tested.
Dt = 325 ps
A 3D designer microstructure target by GA
X-ray
AAC-2022

## Slide 7
Thompson Parabola Data after 5 scans of imaging plates strong C6+ and p+
C6+
p+
AAC-2022
Chart: Proton Spectrum 10 mm Structure
Chart: Proton Spectrum 50 mm Structure
C6+
p+
Proton Energy
Proton Energy
Proton Num, (MeV-1xSr-1)
Proton Num, (MeV-1xSr-1)
Proton Data for Log-Pile Printed Targets
10 um thick Log-pile structure
50 um thick Log-pile structure
High proton yield >109 is achieved for near-80 MeV favoring shorter interaction length.

## Slide 8
Thompson Parabola data after 5 scans of imaging plates p+ using a 2 mm foil (TNSA shot).
AAC-2022
Electron Number
Electron Energy, MeV
Chart: 
Comparison between foil and log-pile structure
Chart: Proton Spectrum 2 mm CH film
Proton Energy
Proton yield in the case of a log-pile microstructure is comparable with a classical TNSA spectrum. Maximum Ep~60 MeV for a foil is lower indicating the enhanced TNSA regime likely due to additional electron heating in a bulk.
Proton Num, (MeV-1xSr-1)

## Slide 9: NTA @ TIM 14 will be a ~70 layer RCF pack -- Thank you Danielle!
Repeated Drilled out pattern with different thickness
5.5
mm
LLNL 80 MeV Proton Beam Imaging Energy Spectrometer (Probies) (D. Mariscal, PPCF, 63, 2021)
Proton Data from a PROBIES diagnostic
AAC-2022

## Slide 10
RCF stack exposure for a 10 mm microstructured target
AAC-2022
RCF data for a 10 mm Log-pile Target
Nice looking round beam with Emax for protons reaching ~80 MeV .
80 MeV
68
61
56
51
46
40
5
14
20
25
29
33

## Slide 11
Dt = 325 ps
MicrostructuredTarget Modeling (OSIRIS)
X-ray
AAC-2022

## Slide 12
Dt = 325 ps
Sheath Dynamics in Microstructured Target
X-ray
AAC-2022

## Slide 13
Dt = 325 ps
X-ray
Accelerating Field 2D Structure
AAC-2022

## Slide 14: We demonstrate that log-pile 3D printed microstructures irradiated by an intense 1 mm, picosecond laser pulse (a0=10-25) can generate high energy ion beams with a large yield.
Np~109 protons are accelerated to an energy of ~80 MeV in a 10 mm thick log-pile 3D laser printed structure.
Hotter and larger quantity electrons measured for microstructured target in comparison with a foil target indicates that the enhanced sheath field is responsible for observed ion spectra. Physics of electron heating is complex.
PIC simulations of a microstructured log-pile targets show that laser-plasma interaction on a picosecond time scale is related to yet to be expanded wires.
Conclusions
AAC-2022
Log-pile
3D printed
2PP target
Stochastic
Laser printed
2PP target
Thank NNSA (DE-NA0003842) for supporting this study.