## Slide 1: Prospects of Ultralow MTE Photocathodes in Electron Guns
Prof. Siddharth Karkare
(Arizona State University)

## Slide 2: Brightness and Emittance
Beam Brightness, B = Charge density in phase space
- Emittance
According to Liouville’s theorem
brightness remains invariant for Hamiltonian systems (Linacs and microscopes)
Source determines the maximum possible brightness

## Slide 3: Maximum Source Brightness
Ez (5-100MV/m)
Photocathode
Laser pulse
Brightness limited by photocathode MTE and field gradient
>

## Slide 4: What does MTE depend on?
Factors affecting MTE
Emit close to threshold and minimize temperature
Need atomically smooth surfaces
Need high quantum efficiency
Need low transverse momentum states
Band Structure
Many-body Scattering
Non-linear Photoemission
Excess Energy
Surface Non-uniformities
Need small cross-section of electron-phonon-photon interactions
Challenge: Develop materials that satisfy all these criteria
P. Musumeci et a l, Nucl. Instrum. Meth. A, 907, 209 (2018)

## Slide 5: Cu(100) – Smallest MTE measured
Cu(100)
5 meV MTE measured from Cu(100)
Most photoinjectors use MTE ~500 meV
10 meV total energy spread
More than 1 order of magnitude smaller than any existing electron source
(not just photoemission)
Photoemission at the threshold
Cooled to LHe (30K)
Atomically ordered flat surface
Good band-structure
Great for stroboscopic UED applications and electron spectroscopy,
Enables of ultrafast vibrational spectroscopy in EELS – measure ultrafast phonon dynamics.
Karkare et al, Phys. Rev. Lett. 125, 054801 (2020)

## Slide 6: Electron Heating and Multi-photon Emission
Low QE leads to a requirement for high laser power, which heats the electronic system
  Electronic temperature reaches 3000K, ie. MTE of ~ 250 meV
Multi-photon photoemission –
Results in very large excess energy
Electron Heating
Multi-photon/Above-threshold Emission

## Slide 7: Low Electron Affinity Semiconductors
Low electron affinity semiconductors:
Alkali-antimonides, III-Vs activated to NEA
Energy
Position
Vacuum
Cathode
Fermi level
Vacuum level
Band-gap
Very high QE 10-2-10-4 at threshold
Lower multiphoton and heating effects
Already used for high average current applications: ERLs, polarized sources
Calculations show sub-20 meV MTE at large charge densities
Alkali-antimonides show promise

## Slide 8: Alkali-antimonide performance
Cultrera et al, Phys. Rev. ST Accel. Beams 18, 113401 (2015)
Saha et al, Appl. Phys. Lett. 120, 194102 (2022)
Parzyck et al, Phys. Rev. Lett. 128, 114801 (2022)
Surface roughness issue for Alkali-antimonides is solved via use of lattice matched substrates and new growth recipes
Growth on polycrystalline substrate
Growth on lattice-matched substrate
Epitaxy on lattice-matched substrate
650-700 nm

## Slide 9: Testing in high field guns
Development of Multialkali antimonides photocathodes for high brightness photoinjectors, S. Mohanty, on behalf of PITZ & LASA team, (EWPAA 2022), Sep 20 – 22, 2022,Milan
~230 meV MTE in 515 nm at 29 MV/m
- 0.6 eV excess energy
- dark current too high for higher fields
Alkali-antimonides with better surfaces need to be tested at lower excess energies
Cathodes grown via sequential deposition:
Very poor surface quality!!!

## Slide 10: Challenges for use in High Field Guns
Ultra-high-vacuum (UHV) ~ 10-9 -10-10 torr range
UHV cathode transfer, load-lock
Tunable wavelength laser
Cryogenic cooling
Capability to use semiconducting cathode substrates
Some RF guns already have this – Pegasus gun at UCLA, FAST facility at Fermilab, PITZ RF gun, AWA …
Facilities development needed to enable these – underway at LANL and UCLA
50 MV/m fields or higher, even exceeding 100 MV/m
Absolutely Essential
Necessary for lowest possible MTE
Need cathode testing facilities with these requirements

## Slide 11: 2-D coatings for Robustness
Demonstrated protection in QE for Cu photocathodes without increase in MTE via graphene coatings
Liu et al, Appl. Phys. Lett. 110, 041607 (2017)
Knill et al, NAPAC 2022.
Obtaining Gr protected alkali-antimonide surface is challenging!!! – research ongoing

## Slide 12: Beyond Alkali-antimonides – Cs2Te, III-Nitrides…
Pierce et al Appl. Phys. Lett. 118, 124101 (2021)
Cs2Te MTE is limited to ~100 meV due to low work function Cs impurities on surface
- Can it be reduced by better growth techniques and control to give phase pure Cs2Te?
Cultrera et al. Journal of Applied Physics 131, 124902 (2022)
50 meV MTE measured at 10-3 QE at 300 nm
Perfectly ordered surfaces
Need more growth optimizations and characterization
Could emit in visible light
Extremely robust
Cs2Te
III-N heterostructures – Cs free NEA

## Slide 13: Single crystal emitters – use small momentum spread
‘Classical’ metal (m* = m0)
Metal with m* < m0
Small effective masses yield smaller for a given excess energy,
Vacuum level
S. Karkare et al. Phys. Rev. B 95, 075439 (2017)
S. Karkare et al. Phys. Rev. Lett. 118, 164802 (2017)
Demonstrated for the surface state of Ag(111)
Use other low effective mass materials like topological insulators, Dirac semimetals for near zero MTE?

## Slide 14: Nano-structured cathodes
Photonics integrated cathodes
Photonics network integrated into the cathode substrate to deliver pulses of light at specific locations at specific times for um-fs scale spatio temporal shaping and patterned beams
Promising for spatio-temporally shaped beams for structure-wakefield applications
Plasmonic nano-structures
Dreher et al, Nanophotonics 2022; 11(16): 3687–3694
Plasmonic surfaces for nano-scale electron emission
Sub-nm scale beams from flat surfaces
Ideal for laser-dielectric acceleration
Ordered arrays for ordered electron beams?
A.H. Kachwala et al, On-Chip Photonics Integrated Photocathodes, NAPAC, Albuquerque, NM (2022) WEPA65

## Slide 15: Photoemission and Bright Beams Lab @ ASU

## Slide 16: Conclusion
Several Low sub-25 meV cathode technologies have been developed
Testing in high field guns is crucial, lacking but underway
  High cathode field and lower MTE efforts need to merge
Can enable 2-3 orders of magnitude brighter electron beams
Nano-structured cathodes for advanced accelerator applications
Immediate Post-doc Opening:
https://academicjobsonline.org/ajo/jobs/22032
Development of ultra-bright nano-structured photoemission electron sources