## Slide 1: Update on the status of the C-band high gradient program at LANL
Evgenya Simakov, Anna Alexander, Petr Anisimov, W. Brian Haynes, Deepak Rai, Tsuyoshi Tajima, Muhammed Zuboraj Los Alamos National Laboratory
11/10/2022
Managed by Triad National Security, LLC., for the U.S. Department of Energy’s NNSA.

## Slide 2: Outline of this talk
Introduction and LANL C-band project overview
Experimental activities
  CERF-NM: High gradient C-band test stand
  High gradient C-band tests and resultsCARIE: new high gradient RF injector test facility
Summary and near-term plans

## Slide 3: Introduction: why Los Alamos
Achieving high-gradient performance (low breakdown rates, low field emission, new materials for HOM absorption, cathodes at high gradient etc.) is a materials science problem.
Los Alamos is, at core, a materials science laboratory with particular expertise and interest in metallurgy.
Los Alamos also considers itself the steward of accelerator science for the NNSA part of the DOE complex.
Thus, Los Alamos has both an institutional interest in, and capability to address, this problem space.
High gradient C-band work directly aligns with future NNSA and LANL missions.

## Slide 4: LANL must develop accelerators for various national security needs
LANSCE accelerator upgrades:
Applications such as pRad desire higher proton beam energy
 add a booster to current LANSCE linac to increase beam energy to 3-5 GeV
New capabilities: improve accessibility
Material science at LANL will benefit from powerful directional high repetition rate X-ray sources
43 keV photons can be produced with 42 MeV electron beam
43 keV photons are DMMSC relevant
Compact Accelerators: enabling feasibility
Achieving high gradient performance (low breakdown rates, low field emission, new materials for HOM absorption, etc.) is a material science problem.
LANL is, at core, a material science laboratory

## Slide 5: LANL High Gradient C-band research
The goals for LANL’s high gradient project are
To build a C-band (5.712 GHz) high gradient rf breakdown study facility (2019-2022).
To build a C-band cryo-cooled photoinjector study facility (2022-2025).
To conduct material studies.
To develop C-band compact accelerator facility for X-ray production (future).
This work was funded by Los Alamos National Laboratory (LANL) Laboratory Directed Research and Development (LDRD) program and Technology Evaluation and Development (TED) funds.

## Slide 6: LANL C-band Engineering Research Facility (CERF-NM)
CERF-NM was built with $3M of LANL’s internal infrastructure investment.
Powered with a C-band Canon klystron
Conditioned to 50 MW
Frequency 5.712 GHz
300 ns – 1 µs pulse length
Rep rate up to 200 Hz (typical 100 Hz)
Nominal bandwidth 5.707-5.717 GHz

## Slide 7: Schematic of the C-band test stand
FC1
Ion pump and ion gauge
FC2
Dir coupler (FWD, REV)
Cavity
Mode launcher
Radiologically certified for dark currents up to 5 MeV and 10 μA.

## Slide 8: The first two high gradient cavities were tested at CERF-NM in FY21
This C-band high gradient test facility is nationally unique. The first cavities tested at CERF-NM were manufactured at SLAC.

## Slide 9: Peak surface electric fields in excess of 300 MV/m demonstrated in high gradient tests
Breakdown probabilities were recorded for three different pulse lengths for copper and copper-silver cavities.

## Slide 10: We fabricated and conditioned mode-launchers for on-axis coupling with decreased surface magnetic fields
The mode launchers are conditioned up to 20 MW of input power.

## Slide 11: Tests of a benchmark cavity will allow us to establish gradient limitations at C-band as compared to other frequencies
Frequency | 5.712 GHz
Cell length | 1.034 in
a/λ | 0.105
Iris radius | 0.217 in
Q(copper, RT) | 12700
Power for 200 MV/m surface field | 5.3 MW
Several cavities will be tested in FY22:
Copper + brazed (fabricated)
Copper + welded (in fabrication)
Copper-silver, 0.085% silver (in fabrication)
Copper-silver, 2% silver (in fabrication)

## Slide 12: Two a/λ=0.105 cavities were fabricated and tested at high gradients
cavity
mode launcher

## Slide 13: The cavities were conditioned up to the maximum available power at the test stand
The cavities were conditioned at 1 μs pulse length.
Cavity #1:
Maximum coupled power: 14 MW.
Peak surface electric field: 255 MV/m.
Peak surface magnetic field: 373 kA/m.
Cavity #2:
Maximum coupled power: 15 MW.
Peak surface electric field: 308 MV/m.
Peak surface magnetic field: 449 kA/m.

## Slide 14: Remote operation of C-band
We are working to develop capability for round-the-clock operation of CERF-NM while being monitored from LANSCE Central Control Room (CCR).

## Slide 15: Summary and test plans for CERF-NM
LANL C-band high gradient test stand is currently operational
Testing of the SLAC copper beta=0.5 cavities is finished.
We plan to test multiple a/λ = 0.105 cavities fabricated with different methods.
In FY23 we will test the optimized proton booster cavity and ceramic-enhanced accelerator structures
The test stand is open to collaborators.
We consider adding capability to cool cavities under test to cryogenic temperatures.

## Slide 16: CARIE: Cathodes And Rf Interactions in Extremes
A new three-year project was funded at LANL to demonstrate operation of high-quantum-efficiency cathodes in a high-gradient RF injector.
Project builds upon LANL’s expertise in high-gradient C-band and high-QE photocathodes.
The proposed heterostructured cathode will include multiple layers to ensure atomic flatness of the surface, high QE, and the ability to withstand high electric fields with no breakdown.
Target beam parameters: 250 pC, 0.1 μm*rad, B5D = 1016 A/m2.
The project started in October of 2022.

## Slide 17: RF photoinjector considerations
We will fabricate 1.6 cell gun design by UCLA/SLAC.
Questions we are trying to address:
The cathode: there is an idea to grow the cathode straight on the copper wall. This is an engineering challenge. Alternative: INFN plug?
RF coupler design: must take into account integration with the cryo-cooling and the solenoid.
Solenoid: must take into account integration with the cryo-cooling.
Cryo-cooling: cryo-cooler and low rep rate or liquid nitrogen?

## Slide 18: CARIE vault
A location was identified on LANSCE mesa that can accommodate a 20 kW electron beam.
Co-located with a cathode fabrication and characterization facility (ACERT).
The vault was cleaned for the new experiment.
A modulator for the 50 MW C-band klystron is in procurement.

## Slide 19: CARIE vault facility lineout

## Slide 20: RF injector electromagnetic design
1.6 cell RF injector.
Side coupling will be used to accommodate positioning the solenoid right after the injector and the cathode insertion mechanism upstream.
Side coupling is also essential because of a very small iris.
1800 phase advance is achieved by adjusting the length of the two waveguides.
The electromagnetic design is being conducted to minimize surface fields.

## Slide 21: RF injector beamline design (and comparison to 100 pC case)
Parameter | Unit |  | 
Charge |  | 100 | 250
Laser RMS spot size, |  | 129 | 233.5
Laser aperture size |  |  | 
Injection phase |  |  | 
Laser length |  | 5.62 | 6.075
Peak cathode field |  | 240 | 240
Solenoid field |  | 0.5665 | 0.5759
Solenoid FWHM |  | 7.4 | 7.4
Solenoid center |  | 12.5 | 12.5
Parameter | Unit |  | 
Charge |  | 100 | 250
 |  | 129 | 233.5
Laser aperture size |  |  | 
Injection phase |  |  | 
Laser length |  | 5.62 | 6.075
Peak cathode field |  | 240 | 240
Solenoid field |  | 0.5665 | 0.5759
Solenoid FWHM |  | 7.4 | 7.4
Solenoid center |  | 12.5 | 12.5

## Slide 22: GPT simulations: beam emittance and spot size
100 pC case
250 pC case
Notes: GPT output in GDF to SDDS to Python for plotting.

## Slide 23: GPT simulations: beam current and slice emittance at beam waist
100 pC
250 pC

## Slide 24: GPT simulations: beam brightness
100 pC
250 pC

## Slide 25: LANL has plans for further developing its C-band accelerator capabilities
Director Initiative money were allocated in FY22 to jump start this facility.
5-year goal: build operational C-band cryo-cooled copper accelerator.
Ultimate goal: provide 43 keV and 100 keV photon bursts for material studies with ICS