## Slide 1: 9.3 microns Toward next-generation CO2 laser for particle accelerators
2022-11-10
AAC, Long Island, NY
Misha Polyanskiy, Igor Pogorelsky, Marcus Babzien, Rotem Kupfer, William Li, Mark Palmer
Notes: Very special instrument
Novel methods of particle accel.
All the important things

## Slide 2: Motivation for LWIR (example: LWFA)
wake
10 – 20 µm
λ ≈ 1 µm
200 µm
Laser
λ ≈ 10 µm

## Slide 3: Why CO2 laser amplifiers?
SWIR
MWIR
LWIR
NIR
Compilation: Sara Bucht (LLE)
50 MW
CO2 laser amplifiers
5 TW
Notes: Large and complex machines
Applications in
Two bunches of e-
Polygon pattern
Nuclear reaction
Combination e-hv
--- 3 ---

## Slide 4: State of the art
Solid-state seed
High-pressure, mixed-isotope CO2 amplifiers
Chirped-pulse amplification
Polyanskiy et al. OSA Continuum 3, 459 (2020)

## Slide 5: Gain spectrum
P(CO2+N2+He) ≈ 10 atm
16O : 18O ≈ 50 : 50
C16O2 : C16O18O : C18O2 ≈ 25 : 50 : 25
9.2 µm
9.3 µm

## Slide 6: Amplification on 9R branch (1011x)

## Slide 7
2 000x
5 000x [net amplification]
10 000x [losses]
0.1 * 0.9^15 * (1-0.04)^(8*16) = 1e-4
Atotal = 1011

## Slide 8: Amplification on 9R & 9P branches (1011x)

## Slide 9
2 000x
Atotal = 2 000
10 mJ seed laser
mJ+
William Li – AAC’22 WG8 Raman-based wavelength conversion for seeding and optical pumping of CO2 laser amplifiers
Raman
DFG

## Slide 10: Amplification on 9R & 9P branches (2000x)

## Slide 11: Amplification on 9R & 9P branches (2000x)

## Slide 12: Amplification on 9R & 9P branches (2000x)

## Slide 13
Power (TW)
500 fs 15 TW
Now (µJ seed)
mJ seed
Gain spectrum
9P
9R
2 ps 5 TW
Polyanskiy et al. Photonics 8, 101 (2021)
9.2 μm
9.3 μm
With 20% contingency

## Slide 14: Post-compression
Self-phase modulation (SPM)
Self-phase modulation
Funding:
US Department of Energy Accelerator Stewardship Program grant, B&R #KA2601020, KW010102
 | n0 @ 9.2 µm | n2 10-20 J/m2 | GVD fs2/m
NaF | 1.253 | 0.6 | -3150
BaF2 | 1.412 | 1.7 | -2340
KCl | 1.459 | 3.4 | -558
NaCl | 1.500 | 3.5 | -1010
KBr | 1.528 | 4.3 | -303
CsI | 1.740 | 12 | -89.2
AgCl | 1.984 | 17 | -650
AgBr | 2.168 | 20 | -192
ZnS | 2.211 | 25 | -2240
Igor Pogorelsky AAC’22 WG 6 Opportunities for advanced accelerator research with femtosecond long-wavelength lasers
Linear dispersion

## Slide 15: Proof of principle @ 2 ps
278 mJ
Polyanskiy et al. Opt. Express 29, 31714 (2021)
Ø 12.8 mm
In (~2 J)
290 fs
Autocorrelation
2 ps
Out (280 mJ)
2 ps
5 mm dia. beam center
Whole beam
in
out
in
out

## Slide 16: 500 fs  100 fs at full energy
Input beam profile
Temporal pulse structure
Beam focus (IP)

## Slide 17
Power (TW)
500 fs 15 TW
100 fs 25 TW
Now (µJ seed)
mJ seed
Post-compression
Gain spectrum
9P
9R
2 ps 5 TW
1 optical cycle = 31 fs
With 20% contingency
9.2 μm
9.3 μm

## Slide 18: Optical pumping of CO2 amplifiers
Sergei Tochitsky – AAC’22 WG8 Status and prospects of optically pumped high-pressure CO2 amplifiers
24/7 operation
High repetition rate
High CO2 concentrations
4.3 µm: Fe2+: ZnSe
2.8 µm: GaSb diode
Required pump energy (~100 mJ/cm3, <few µs)
Pre-amplifier: ~1 J
Final amplifier: ~1 kJ
R&D
Long-term goal

## Slide 19
State of the art: 5 TW @ 9.2 μm, 2 ps
  Solid-state seed (μJ)
  High-pressure, mixed-isotope CO2 amplifiers
  CPA
Next gen: 25 TW, @ 9.3 μm, 100 fs
  Solid-state seed **mJ**
  Post-compression
  Optical pumping (next-next gen)
Notes: Limited by voltage
Alternating current
Always see accelerating field
Short but intense bunches
Most modern accelerators
--- 6 ---