## Slide 1: Beam Acceleration (SRF) Theme

## Slide 2
ANL: J. Elam
TRIUMF: B. Laxdal
FNAL: S. Posen
Clark Atlanta: G. Japaridze
X. Wang
Optimal Outcome: The advanced methods and surfaces for next-generation SRF cavities that will enable game-changing reduction of cooling power needs (10× lower than traditional bulk Nb cavities), will enable higher temperature operation (well above the 2.17K Lambda point of liquid helium), and will provide higher accelerating fields (2× higher than traditional bulk Nb cavities) for lower cryogenic system costs, energy sustainability, and simpler refrigeration.
Mark Transtrum
BYU
Steve Sibener
U Chicago
Matthias Liepe
Cornell
Theme Leaders
Faculty
Jim Sethna Cornell
Tomás Arias
Cornell
Richard Hennig
U Florida
David Muller
Cornell
Affiliates
Beam Acceleration (SRF) Theme
5/31/23

## Slide 3: Problem Statement
Superconducting RF (SRF) cavities are “gold-standard” for acceleration of high-power, high-brightness beams
  Current generation of SRF cavities has been transformational for accelerator driven sciences
All SRF cavities currently in operation use Niobium as the superconducting material
  But: High cost and complexity of current generation of SRF cavities severely limit use in science and prevent small-scale university and industrial applications
SRF Cryomodule
SRF Linac Cryoplant
5/31/23

## Slide 4: SRF 101
Slowed down by factor of approximately 4x109
Input RF power at 1.3 GHz
1m
Cryoplant efficiency vs. operating temperature
Decrease required cooling power: need superconductors with higher critical temperature
Decrease required cooling power: need smaller surface resistance
Decrease accelerator length: need superconductors with higher fundamental flux-free field limit

## Slide 5
Future CBB (optimal outcome)
4
10
20
40
Cryogenic AC cooling power (W/active meter)/(MV/m)2
Bulk (undoped) niobium cavity at 1.3 GHz, operating at 2K
CBB 2023: 1.3 GHz Nb3Sn cavity, operating at 4K
25
50
100
300
Energy gain/length (MeV/m)
Bulk niobium cavity at 2K
Current Nb3Sn cavity at 4.2K
Future CBB (optimal outcome)
CBB will open paths for even higher fields
Current Progress Towards Ultimate Outcomes

## Slide 6: Why this matters: Applications
Overcoming the cost barrier / enabling sustainable science:
Key: Reduced cryo cooling power and higher temp. operation
  Future FELs
  Electron-Ion collider
  Future circular collider (FCC) …
Advancing the energy frontier:
Key: Increased energy gain / length
Enabling new class of compact, turn-key SRF driven accelerators:
Key: Reduced cryogenic cooling power and simplified cryogenics
  Widespread use of SRF
  Small-scale science accelerators
    High-intensity, high-brightness MeV scale beams
  Industrial and medical applications…
Impact on non-accelerator applications:
  S.C. cavities for quantum computing, dark photon detection …
Future Circular Collider
Electron-Ion Collider
FNAL/DOE Compact Accel. Concept
CBB Nb3Sn material advances
5/31/23
Notes: Advancing Energy Frontier: ILC-future upgrade
Non-accelerator applications: Emphasize quantum computing

## Slide 7: Technical Challenges
Inner surface layer (few 100 nm “RF penetration layer”) determines RF performance of a cavity.
Transformative advances in RF performance require:
  Utilizing compound superconducting materials with larger energy gaps and higher superheating fields
  Growing complex superconducting films with near-ideal stoichiometry and achieving tight control of defects down to the nanoscale
  Exploring optimized structured surfaces and their robustness to vortex entry
  Understanding and controlling the effects that underlie the RF surface resistance and its field dependence
  ➾ Rich, interdisciplinary CBB research program
Niobium
3mm
Liquid Helium
Vacuum with RF fields
Bs=B0eiwt
Nb2O5
Bin
l(0) ~ 40 nm
1m
Bs=B0eiwt
5/31/23

## Slide 8: CBB Integration of Complementary Disciplines
Tight knit interdisciplinary community
Multiscale studies: atomic (Å), nano (mm), meso (mm) & macro (mm) dimensions
Examining materials growth, morphology, stoichiometry and critical relations to RF penetration layer across multiple dimensions
NbO order on (100) Nb
Nb3Sn Cavity
TEM cross section
Surface(001) phonon structure of Nb
Vortex nucleation at grain boundary
Sibener, U Chicago
Muller, Cornell
Arias, Cornell; Sibener U Chicago
Transtrum, BYU
Accelerator Science and Technology
Materials Science
Surface Chemistry
Theoretical Condensed Matter Physics
Experimental Condensed Matter Physics
CBB
Accelerator
Experimentalist
Theorist
Liepe, Cornell
5/31/23

## Slide 9: Connections: Research Loop
Cavity RF Test Accelerator scientists
Note: Supported by NSF and DOE accelerator grants.
Predict Electronic structure theorists, condensed matter theorists
Implement
Material scientist, accelerator scientist
Characterize Chemist, condensed matter exp., accelerator scientists
Sethna Cornell
Transtrum
BYU
Hennig
U Florida
Liepe
Cornell
Posen
FNAL
Laxdal
TRIUMF
Sibener
U Chicago
Muller
Cornell
Arias
Cornell
Synergy: Beam Production
material synthesis
Synergy: Beam Storage & Transport
e.g. nonlinear continuum descriptions
Synergy: Beam Production and Beam Storage & Transport
accel. implementation
Synergy: Beam Production
material characterization
Liepe
Cornell
Liepe
Cornell
Posen
FNAL
CBB enables this unique interdisciplinary research
Paradigm shift in SRF research!
Accelerator
Experimentalist
Theorist
Elam
ANL
Sibener
U Chicago
5/31/23

## Slide 10: Example: Nb-Zr
5/31/23
Arias
Cornell
Hennig
U Florida
Muller
Cornell
Transtrum
BYU
Hire
U Florida
Sitaraman
Cornell
Sun
Cornell
Oseroff
Cornell
Baraissov
Cornell
Francis
BYU
Liepe
Cornell

## Slide 11: SRF Graduate Students and Postdocs
Zhasla Baraissov
Student
Cornell
Gabriel Gaitan
Student
Cornell
Aiden Harbick
Student
BYU
Ajinkya Hire
Student
Florida
Liana Shpani
Student
Cornell
Nathan Sitaraman
Postdoc
Cornell
Caleb Thompson
Student
Chicago
Michael VanDuinen
Student
Chicago
Sarah Willson
Student
Chicago
Zeming Sun
Postdoc
Cornell
5/31/23
Van Do
Student
Chicago
Sam Dong
Student
Chicago
Sadie Seddon-Stettler
Student
Cornell
Notes: Current Students and Postdocs in BDC

## Slide 12: Connections: National Labs and Industry
ILC cost
reduction
High efficiency (2xQ0)
cavity for NSLS-II
National Lab Affiliates:
FNAL: S. Posen
ANL: J. Elam
TRIUMF: B. Laxdal
Nb3Sn R&D
Nb3Sn Workshop
New SRF Materials
SBIR
LCLS-II HE
R&D of N-Doping
5/31/23

## Slide 13
SRF Strategic Plan
The advanced methods and surfaces needed for next-generation SRF cavities that enable game-changing reduction of cooling power, higher temperature operation, and higher accelerating fields for lower cryogenic system costs, energy sustainability, and simpler refrigeration.
FY 22
FY 23
FY 24
FY 25
FY 26
Legacy
Objectives
Deliverables
Surfaces from non-Nb with cooling power <4W/(active meter)/(MV/m)2, corresponding to a 10x reduction in cooling power
Non-Nb surfaces supporting accelerating fields exceeding 50 MV/m.
Higher efficiency and higher fields: Demonstrate higher RF performance in proof-of-principle SRF cavities and study RF superconductivity under extreme conditions
Compact SRF with conduction cooling for turn-key operation
Non-Nb, high-efficiency surfaces capable of sustaining accelerating fields of 25 MV/m
Advanced SRF materials growth: Develop improved growth methods; understand impact of realistic (non-ideal) surfaces on performance
Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys
FCC-ee running energy efficient on Nb3Sn cavities
Determination whether other materials have potential for higher efficiency and/or higher fields above Nb3Sn and Nb-Zr limits
Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates
Decision point: Continue?
Determination whether inhomogeneous surface layers offer significantly increased RF performance over homogeneous materials
Multi-layers and inhomogeneous layers: Increasing RF performance via surfaces by design
Multi-TeV e+e– collider enabled by CBB designed surfaces
Decision point: Continue?
﻿

## Slide 14
SRF Strategic Plan
The advanced methods and surfaces needed for next-generation SRF cavities that enable game-changing reduction of cooling power, higher temperature operation, and higher accelerating fields for lower cryogenic system costs, energy sustainability, and simpler refrigeration.
FY 22
FY 23
FY 24
FY 25
FY 26
Legacy
Objectives
Deliverables
Surfaces from non-Nb with cooling power <4W/(active meter)/(MV/m)2, corresponding to a 10x reduction in cooling power
Non-Nb surfaces supporting accelerating fields exceeding 50 MV/m.
Higher efficiency and higher fields: Demonstrate higher RF performance in proof-of-principle SRF cavities and study RF superconductivity under extreme conditions
Compact SRF with conduction cooling for turn-key operation
Non-Nb, high-efficiency surfaces capable of sustaining accelerating fields of 25 MV/m
Advanced SRF materials growth: Develop improved growth methods; understand impact of realistic (non-ideal) surfaces on performance
Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys
FCC-ee running energy efficient on Nb3Sn cavities
Determination whether other materials have potential for higher efficiency and/or higher fields above Nb3Sn and Nb-Zr limits
Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates
Decision point: Continue?
Determination whether inhomogeneous surface layers offer significantly increased RF performance over homogeneous materials
Multi-layers and inhomogeneous layers: Increasing RF performance via surfaces by design
Multi-TeV e+e– collider enabled by CBB designed surfaces
Decision point: Continue?
﻿

## Slide 15
Phase II – Objective 1
Advanced SRF materials growth: Developing improved growth methods and understanding the impact of realistic (non-ideal) surfaces on performance.
Deliverable 1.1: Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates. (Fall 2026) Met Deliverable 1.1 for Y7
5/31/23
 | Niobium | Nb3Sn
Superheating field | 220 mT | 420 mT
Max. Eacc (theoretical limit) | 55 MV/m | 100 MV/m
 | Niobium | Nb3Sn
Critical Temperature Tc | 9 K | 18 K
Q0 at 4.2 K | 6 x 108 | 6 x 1010
Q0 at 2.0 K | 3 x 1010 | >1011
Why? Nb3Sn offers a path to increased accelerating fields and lower losses.
Challenge? Optimizing Nb3Sn film growth for ideal 25% Sn concentration (stoichiometry), low roughness, ideal film thickness…

## Slide 16
Deliverable 1.1: Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates.
Recent important Nb3Sn growth advances:
  Demonstrated that certain chemical pre-treatments of the Nb substrate oxide improve uniformity of Sn nucleation in vapor diffusion growth ⇒ Important for reduced surface roughness and uniformity of final Nb3Sn film
  Achieved Nb3Sn film on 1.3 GHz cavity via CBB’s novel electrochemical Nb3Sn synthesis ⇒ Smooth, homogeneous, high-purity Nb3Sn film
  Completed system for Nb3Sn growth via CVD ⇒ Will allow for improved control of Nb3Sn film growth
5/31/23
Z. Sun et al., Smooth, homogeneous, high-purity Nb3Sn RF superconducting films by seed-free electrochemical synthesis, arXiv:2302.02054

## Slide 17
Recent important advances in understanding Nb3Sn formation:
  Identified the chemical and physical properties driving uniform Sn nucleation and wetting behavior on oxidized Nb surfaces during Nb3Sn growth
  Inelastic helium atom scattering (HAS) as a probe of surface e--phonon coupling:
    1st fully ab initio theory of inelastic HAS matching experimental intensities from Nb
    Ab initio interpretation of inelastic HAS scattering from niobium oxide
  Predictions of core-level shifts to aid interpretation of initial Sn/NbOx chemistries
  ⇒ Guidance for further Nb3Sn growth optimization
5/31/23
J. Phys. Chem C (2023).
Sn Adsorption and Diffusion on a Nb(100) Oxide
Deliverable 1.1: Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates.
A fully ab initio approach to inelastic atom–surface scattering, Phys. Rev. Lett., in review
Journal of Chemical Physics 156, 124702 (March 2022), DOI: 10.1063/5.0085653

## Slide 18
5/31/23
Recent important theory advances:
  Development of ultrafast force field (UF3) machine learning potentials for Nb-Sn system
    Provides sufficient accuracy for modeling diffusion of Nb and Sn in the bulk, at surfaces, and grain boundaries
    Implementation into the LAMMPS code enables exascale molecular dynamics simulation of the kinetics for realistic systems with millions of atoms
    ⇒ Guidance for further Nb3Sn growth optimization
Deliverable 1.1: Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates.

## Slide 19
Recent important theory advances:
  3D time-dependent Ginzburg-Landau simulations of Sn-depleted regions in Nb3Sn
    Modeled losses mimic quality factors in real-world cavities.
    ⇒ Simulations reveal which defects are responsible for observed performance issues
  Two-domain TDGL simulations to model rough SC-vacuum interface, including field enhancement
  ⇒ Simulations reveal that geometric and material defects have a complex tradeoff between their ability to nucleate magnetic vortices (reducing efficiency) and pinning vortices (preventing quench)
5/31/23
Pinned Vortex
Arrows indicate field direction
Deliverable 1.1: Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates.

## Slide 20
Current and future projects for Deliverable 1.1:
Refinement of Nb3Sn growth via vapor diffusion, electroplating, and CVD.
Studies of Sn nucleation on niobium oxides and diffusion along Nb3Sn grain boundaries.
Ab initio study of elastic HAS Debye-Waller factors for e--ph coupling.
Continued core-level shift studies.
Development and refinement of Nb3Sn growth methods.
Characterizing surface structure, interfacial properties of Nb3Sn films.
Detecting and visualizing growth mechanisms of Nb3Sn that inform optimal growth.
Ab initio study of Nb3Sn surfaces and interfaces.
Machine learning modeling of atomic potentials for Nb3Sn substrates calculations.
Addition of oxygen to the machine learning potential to answer the question of the role of oxygen on the growth of Nb3Sn superconducting thin films
Application of UF3 framework to study the thermodynamics and kinetics of bulk, surfaces, and defects.
Identify rough geometries that are particularly dangerous for vortex nucleation.
Calculate frequency dependence of Hsh within generalized TDGL.
5/31/23
Deliverable 1.1: Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates.

## Slide 21
Phase II – Objective 1
Advanced SRF materials growth: Developing improved growth methods and understanding the impact of realistic (non-ideal) surfaces on performance.
Deliverable 1.2: Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys. (Fall 2026) Met Deliverable 1.2 for Y7
5/31/23
Why? CBB recently predicted that Nb-Zr offers Tc and superheating field above Nb. These might be easier to realize than predicted ultimate limits of Nb3Sn (e.g., due to larger coherence length).
Challenge? Achieving high-Tc phase. Developing Nb-Zr processes that lead to desired high-quality surfaces without performance impacting impurities.
 | Niobium | Nb-Zr
Predicted critical Temperature Tc | 9.2 K | 13 - 16 K
Predicted superheating field | 220 mT | >300 mT ?

## Slide 22
Deliverable 1.2: Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys.
Recent important Nb-Zr growth and performance advances:
  ZrNb(Cx) RF superconducting films with high critical temperatures (13 – 16 K) achieved for the first time under ambient pressure.
    Diffraction patterns of the NbZrCO layer has revealed the structure of the alloy is Fm-3m (rock-salt structure), suggesting the possible carbide nature of the high Tc.
  ⇒ Proof-of-concept RF performance of ZrNb(Cx) on an SRF sample shows BCS resistance that trends lower than reference Nb.
5/31/23
Z. Sun et al., ZrNb(Cx) RF superconducting thin film with high critical temperature in the theoretical limit, arXiv:2302.14410
N.S. Sitaraman et al., ZrNb(Cx) Theory of Nb-Zr Alloy Superconductivity and First Experimental Demonstration for Superconducting Radio-Frequency Cavity Applications, arXiv:2208.10678

## Slide 23
Recent important theoretical advances:
Direct, microscopically detailed ab initio prediction of Nb-Zr performance
  Prediction of Jahn-Teller-Peierls upper bound encompassing observed Tc
  Identification of actual potential structure corresponding to observed Tc
⇒ Provided insights into interpretation of observed Nb-Zr surface performance and chemistries
5/31/23
Enhanced surface superconductivity of niobium by zirconium doping, Phys. Rev. Applied, in review
Deliverable 1.2: Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys.

## Slide 24
Current and future projects for Deliverable 1.2:
  Development and refinement of Nb-Zr growth methods.
  Nb-Zr layer characterization.
  Exploration of Tc’s for realizable Nb-Zr structures.
  Exploration of energies and Tc’s for rocksalt (Nb,Zr)-(O,N) phases.
  Detecting and visualizing alloy growth mechanisms of Zr-Nb that inform optimal growth procedures.
  Development of Zr doped and/or alloyed Nb-Zr growth methods.
  Nb-Zr layer characterization.
  Develop a Nb-Zr-X UF3 potential to study the stability of bulk and surface phases
5/31/23
Deliverable 1.2: Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys.

## Slide 25
Phase II – Objective 1
Advanced SRF materials growth: Developing improved growth methods and understanding the impact of realistic (non-ideal) surfaces on performance.
Deliverable 1.3: Determine if other materials have potential for higher efficiency and/or higher fields above Nb3Sn and Nb-Zr limits.
5/31/23
Why? Other materials might offer an easier path towards exceeding RF performance beyond Nb limitations and/or higher ultimate limits than Nb3Sn and Nb-Zr.
Challenge? Large search space. Can performance predictions be realized on real surfaces?
Oxide eliminators | bcc-phase alloys | A15-phase alloys
Nb+Pd and Nb+Au passivating layers | Nb+Hf | Nb+Al
CBB identified additional materials for further investigation. Examples:

## Slide 26
5/31/23
Recent theory-driven advances:
Prediction of surface deposition of Au/Nb and Pd/Nb
Prediction of Nb1-x(Au,Pb)x mixing energies and solubility
Prediction of Nb1-x(Au,Pb)x impact on electronic density of states
Computational prediction of Nb-stabilization of MoB2 superconductor
⇒ Provides guidance for down-selection of alternative materials and growth methods for further exploration
Deliverable 1.3: Determine if other materials have potential for higher efficiency and/or higher fields above Nb3Sn and Nb-Zr limits.

## Slide 27
5/31/23
Current and future projects for Deliverable 1.3:
  Connect atomic-scale surface structure to its effects on superconductive properties of other material surfaces prepared in situ.
  Proof-of-concept growth and RF test of these surface candidates using the Cornell Sample-Host-Cavity.
  Predict impact of dissolved Au,Pd in Nb on Tc
  Predict superconductivity of Nb surface with and without Au, Pd.
  Predict interfacial contact resistance between Au,Pd layer and Nb.
  Extend study of alternatives to Nb and Nb3Sn superconductors to focus on multi-component transition metal compounds and alloys, including borides.
Deliverable 1.3: Determine if other materials have potential for higher efficiency and/or higher fields above Nb3Sn and Nb-Zr limits.

## Slide 28
SRF Strategic Plan
The advanced methods and surfaces needed for next-generation SRF cavities that enable game-changing reduction of cooling power, higher temperature operation, and higher accelerating fields for lower cryogenic system costs, energy sustainability, and simpler refrigeration.
FY 22
FY 23
FY 24
FY 25
FY 26
Legacy
Objectives
Deliverables
Surfaces from non-Nb with cooling power <4W/(active meter)/(MV/m)2, corresponding to a 10x reduction in cooling power
Non-Nb surfaces supporting accelerating fields exceeding 50 MV/m.
Higher efficiency and higher fields: Demonstrate higher RF performance in proof-of-principle SRF cavities and study RF superconductivity under extreme conditions
Compact SRF with conduction cooling for turn-key operation
Non-Nb, high-efficiency surfaces capable of sustaining accelerating fields of 25 MV/m
Advanced SRF materials growth: Develop improved growth methods; understand impact of realistic (non-ideal) surfaces on performance
Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys
FCC-ee running energy efficient on Nb3Sn cavities
Determination whether other materials have potential for higher efficiency and/or higher fields above Nb3Sn and Nb-Zr limits
Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates
Decision point: Continue?
Determination whether inhomogeneous surface layers offer significantly increased RF performance over homogeneous materials
Multi-layers and inhomogeneous layers: Increasing RF performance via surfaces by design
Multi-TeV e+e– collider enabled by CBB designed surfaces
Decision point: Continue?
﻿

## Slide 29
Phase II – Objective 2
Multi-layers and inhomogeneous layers: Increasing RF performance via surfaces by design
Deliverable 2.1: Determine if inhomogeneous surface layers can offer significantly increased RF performance over homogeneous materials. (Decision point 2024: Continue or drop?).
5/31/23
Why? Inhomogeneous surfaces (e.g., multi-layer laminates S’S, S’IS and nm over-layers might offer additional performance gains over bulk superconductors.
Challenge? Can performance predictions be realized on real surfaces? What is the impact of complex (metallic) oxides layers and other surface features on RF performance and its field dependence?

## Slide 30
Recent important theoretical advances:
  Accelerating fields might be raised up to 30% by increasing the effective mass of electrons over a thin surface layer.
  ⇒ Higher fields via surfaces by design
Development of three-fluid theory of anti-Q slope
Theory for impact of hydrides on maximum fields and RF dissipation
  ⇒ CBB theories explain experimentally observed strong field-dependence of RF surface resistance!
5/31/23
Deliverable 2.1: Determine if inhomogeneous surface layers can offer significantly increased RF performance over homogeneous materials.
Physical Review B 106, 104502 (September 2022), DOI: 10.1103/PhysRevB.106.104502
Three fluid theory of anti-Q slope
Impact of hydrides on RF performance

## Slide 31
Deliverable 2.1: Determine if inhomogeneous surface layers can offer significantly increased RF performance over homogeneous materials.
Recent important advances on surface oxide:
  Typical SRF treatments significantly alter the type and thickness of Nb surface oxides.
    Demonstrated that carbide formation induced during baking determines subsequent oxide formation upon air exposure.
    ⇒ Surface oxide strongly impacts RF surface resistance and its field dependence.
  Demonstrated that replacing the native oxide of a sample with a very thin gold passivation layer reduces its surface resistance.
  ⇒ First high-field demonstration of benefits of passivation layer.
  ⇒ Also of high relevance for low-field SRF applications (e.g., qubits for quantum computing)
5/31/23
Zeming Sun et al., Surface oxides, carbides, and impurities on RF superconducting Nb and Nb3Sn: A comprehensive analysis, arXiv:2305.02467 [cond-mat.mtrl-sci]
T. Oseroff et al, Measurements of the amplitude-dependent microwave surface resistance of a proximity-coupled Au/Nb bilayer

## Slide 32
Current and future projects for Deliverable 2.1:
  Continue study on oxide passivation layers, including impact on RF performance.
  Refine three-fluid theory for anti-Q slope.
  Employ three-fluid theory to optimize Q via scattering in surface loss layer
  Connect mesoscopic models to candidate dopants by ab initio models.
5/31/23
Deliverable 2.1: Determine if inhomogeneous surface layers can offer significantly increased RF performance over homogeneous materials.

## Slide 33
SRF Strategic Plan
The advanced methods and surfaces needed for next-generation SRF cavities that enable game-changing reduction of cooling power, higher temperature operation, and higher accelerating fields for lower cryogenic system costs, energy sustainability, and simpler refrigeration.
FY 22
FY 23
FY 24
FY 25
FY 26
Legacy
Objectives
Deliverables
Surfaces from non-Nb with cooling power <4W/(active meter)/(MV/m)2, corresponding to a 10x reduction in cooling power
Non-Nb surfaces supporting accelerating fields exceeding 50 MV/m.
Higher efficiency and higher fields: Demonstrate higher RF performance in proof-of-principle SRF cavities and study RF superconductivity under extreme conditions
Compact SRF with conduction cooling for turn-key operation
Non-Nb, high-efficiency surfaces capable of sustaining accelerating fields of 25 MV/m
Advanced SRF materials growth: Develop improved growth methods; understand impact of realistic (non-ideal) surfaces on performance
Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys
FCC-ee running energy efficient on Nb3Sn cavities
Determination whether other materials have potential for higher efficiency and/or higher fields above Nb3Sn and Nb-Zr limits
Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates
Decision point: Continue?
Determination whether inhomogeneous surface layers offer significantly increased RF performance over homogeneous materials
Multi-layers and inhomogeneous layers: Increasing RF performance via surfaces by design
Multi-TeV e+e– collider enabled by CBB designed surfaces
Decision point: Continue?
﻿
x

## Slide 34
Phase II – Objective 3
Higher efficiency and higher fields: Demonstrate higher RF performance in proof-of-principle SRF cavities and study RF superconductivity under extreme conditions
Deliverable 3.1: Surfaces from non-Nb with cooling power <4W/(active meter)/(MV/m)2, corresponding to a 10x reduction in cooling power. (Fall 2026)
Recent important advances:
  First Nb3Sn SRF cavity coated with new electroplating – annealing process shows reduced BCS resistance approximately 50% lower than vapor-diffused cavities.
  ⇒ Promising path to reduce cooling power well below current 10W/(active meter)/(MV/m)2 achievement (x4 reduction)
Current and future projects for Deliverable 3.1:
  New and refined growth methods (developed under O1 and O2) applied to samples and proof-of-principle cavities to quantify reduction in RF dissipation.
5/31/23
Z. Sun et al., Smooth, homogeneous, high-purity Nb3Sn RF superconducting films by seed-free electrochemical synthesis, arXiv:2302.02054

## Slide 35
Phase II – Objective 3
Higher efficiency and higher fields: Demonstrate higher RF performance in proof-of-principle SRF cavities and study RF superconductivity under extreme conditions
Deliverable 3.2: Non-Nb, high efficiency surfaces capable of sustaining accelerating field of 25 MV/m. (Fall 2023)
Recent important advances:
  Proof-of-principle advanced-shape cavity with reduced surface magnetic field and improved Nb3Sn coating for high fields ready for RF test.
  ⇒ Best Nb3Sn surfaces currently capable of reaching 23 MV/m.
Current and future projects for Deliverable 3.2:
  New and refined growth methods (developed under O1 and O2) applied to samples and proof-of-principle cavities to quantify increase in maximum accelerating field.
5/31/23

## Slide 36
Phase II – Objective 3
Higher efficiency and higher fields: Demonstrate higher RF performance in proof-of-principle SRF cavities and study RF superconductivity under extreme conditions
Deliverable 3.3: Non-Nb surfaces supporting accelerating fields exceeding 50 MV/m. (Fall 2026)
Recent important advances:
  Novel pulsed RF sample host system to measure maximum fields on material samples commissioned.
  ⇒ Will be used for proof of principle field-limit test of CBB Nb-Zr surfaces.
Current and future projects for Deliverable 3.3:
  New and refined growth methods (developed under O1 and O2) applied to samples and proof-of-principle cavities to quantify reduction in RF dissipation.
5/31/23

## Slide 37
SRF Strategic Plan
The advanced methods and surfaces needed for next-generation SRF cavities that enable game-changing reduction of cooling power, higher temperature operation, and higher accelerating fields for lower cryogenic system costs, energy sustainability, and simpler refrigeration.
FY 22
FY 23
FY 24
FY 25
FY 26
Legacy
Objectives
Deliverables
Surfaces from non-Nb with cooling power <4W/(active meter)/(MV/m)2, corresponding to a 10x reduction in cooling power
Non-Nb surfaces supporting accelerating fields exceeding 50 MV/m.
Higher efficiency and higher fields: Demonstrate higher RF performance in proof-of-principle SRF cavities and study RF superconductivity under extreme conditions
Compact SRF with conduction cooling for turn-key operation
Non-Nb, high-efficiency surfaces capable of sustaining accelerating fields of 25 MV/m
Advanced SRF materials growth: Develop improved growth methods; understand impact of realistic (non-ideal) surfaces on performance
Methods of growth and their refinement leading to annually enhanced performance for Nb-Zr alloys
FCC-ee running energy efficient on Nb3Sn cavities
Determination whether other materials have potential for higher efficiency and/or higher fields above Nb3Sn and Nb-Zr limits
Methods of growth and their refinement leading to annually enhanced performance for Nb3Sn on Nb and Cu substrates
Decision point: Continue?
Determination whether inhomogeneous surface layers offer significantly increased RF performance over homogeneous materials
Multi-layers and inhomogeneous layers: Increasing RF performance via surfaces by design
Multi-TeV e+e– collider enabled by CBB designed surfaces
Decision point: Continue?
﻿

## Slide 38: CBB Legacy (by 2026)
Convergence research: Established new directions and connections between accelerator physics, superconductivity, and materials science. Promoted paradigm shift in SRF research.
Knowledge: Transformative understanding of superconductivity and superconductor growth (~50 journal and conference publications).
Workforce: Young scientists are now joining to join the workforce in an area of critical need, e.g., SRF experts for DOE national labs, industry, and academia.
Technology: Next gen. of high-performance, sustainable SRF technology
  Technology for first large-scale science accelerator running on high-performance non-Nb SRF cavities (after ~50 years of Nb based SRF!), e.g., Future Circular Collider (FCC-ee) running on very efficient Nb3Sn cavities
  SRF cavity surfaces enabling a multi-TeV upgrade of the ILC
  Legacy on quantum computing (3D s.c. qubits)
5/31/23

## Slide 39: Examples of CBB Impacts on SRF Technology
Nb3Sn is now a realistic material for next-gen SRF cavities
  New initiatives in Nb3Sn cavity development worldwide
  CBB hosted first Nb3Sn SRF workshop with 140 participants from 45 institutions
Higher Tc Nb3Sn is enabling the development of new class of compact, robust SRF driven accelerators for new applications in science and industry (development funded by DOE at FNAL, Cornell, JLAB)
  Medical device sterilization
  Environmental Remediation
  Wastewater treatment
5/31/23

## Slide 40: Our Output: Highly Trained Scientists
Rachael Farber, Faculty U Kansas
Ryan Porter, Staff Engineer, SLAC
Alison McMillan, Staff Scientist, General Atomics
James Maniscalco, SRF Engineer, SLAC
Jacob Graham, Scientist, NASA
Darren Veit, Teacher
Paul Cueva, Scientist, Corning
Frank Ikponmwen, Scientist, FDA
Alden Pack, Postdoc, Sandia Nat. Lab
Biswas Rijal, Postdoc, SUNY Buffalo
Jeffrey Sayler, Engineer, LASP, Boulder CO
Aron Tesfamichael, MS
Danilo Liarte, Young Investigator São Paulo State U
Andy Linschied, Scientist, TomTom
Mariah Brown, MS, Math Teacher
Brianna Harris, MS, Physics Teacher
Daniel Hall, Sr. Design Engineer, ASML
Nilanjan Banerjee, Postdoc, U Chicago
Srindhi Mula, PhD candidate, TU Delft
Michelle Kelley
Postdoc, RPI
Thomas Oseroff
Research Assoc.
Cornell
Nathan Sitaraman
Postdoc, Cornell
Benjamin Francis
Chief Scientist, Achilles Heel Tech
Academia
Industry
National Lab/Gov

## Slide 41
Summary
Nb-Zr alloy on Nb plate (electroplating + annealing)
5/31/23
“Sub-Monolayer and Monolayer Sn Adsorption and Diffusion Behavior on Oxidized Nb(100)” Sarah A. Willson, Rachael G. Farber, Ajinkya Hire, Richard Hennig, and S. J. Sibener, J. Phys. Chem. C, 127, 6, 3339-3348 (2023)
TDGL simulations of field enhancement from rough surfaces
A fully ab initio approach to inelastic atom–surface scattering
Phys. Rev. Lett., in review
Three-fluid model of anti-Q slope
Enhanced surface superconductivity of niobium by zirconium doping
Phys. Rev. Applied, in review
  Computational prediction of Nb-stabilization of MoB2 superconductor.