## Slide 1
Beam Production
Jared Maxson, Asst. Professor, Cornell University
Richard
Hennig
U. Florida
Tomas
Arias
Cornell.
Melissa
Hines
Cornell
Kyle
Shen
Cornell
Pietro
Musumeci
UCLA
Ivan
Bazarov
Cornell
theme leaders
Optimal outcome: Methods for x100 brighter electron sources through better photocathodes, enabling better X-ray sources, colliders and electron imaging.
Jared
Maxson
Cornell
Siddharth Karkare
ASU
Jamie
Rosenzweig
UCLA

## Slide 2: Why Brighter Sources?
Most impactful areas:
1. Transformed X-Ray Free Electron Lasers
LCLS @ SLAC
100X brighter
2. Mesoscale Ultrafast Electron Diffraction
Today
100XBrighter
By 2026: Develop electron sources to enable these applications
AND
Higher power and photon energy x-rays
3. Time-resolved atomic resolution STEM
fs motion
Brighter photoemission sources
Compact XFELS

## Slide 3: Electron Beam Brightness
Beam Brightness, B = Charge density in phase space
- Emittance
According to Liouville’s theorem
Brightness remains invariant for Hamiltonian systems (Linacs)
Source determines the maximum possible brightness

## Slide 4: Maximum Beam Brightness
Space Charge? Brightness limited by photocathode MTE and field gradient
Ez (5-100MV/m)
Photocathode
Laser pulse
Increase
I. Bazarov et al., Phys. Rev. Lett. 102, 104801 (2009)
(charge density limitation)
>
Typical MTE used in photoinjectors is ~500 meV
MTE Mean Transverse Energy
Laser spot size
No space charge? Brightness limited by MTE and source size.
Notes: Space charge only here; include small size too!

## Slide 5: What is MTE limited by?
CBB discovers factors affecting MTE
Emit close to threshold and minimize temperature
Need atomically smooth surfaces
Need high quantum efficiency
Need low transverse momentum states
Band Structure
Many-body Scattering
Non-linear Photoemission
Excess Energy
Surface Non-uniformities
Need small cross-section of electron-phonon-photon interactions
Challenge: Develop materials that satisfy all these criteria
P. Musumeci et al. Nucl. Instrum. Meth. A, 907, 209 (2018)
Bae et al. Jour. Appl. Phys., 124,. 244903, (2018)
Nangoi et al Phys. Rev. B 104, 115132 (2021)
Notes: Larger energy than necessary—talk to figure.

## Slide 6: Interdiscplinary Team
Computational modeling
of electronic structure and emission
Materials characterization
Accelerator Testing
Materials growth
Cycle happens on a weekly basis
Demonstrate ‘more than sum of parts’

## Slide 7: Cross-theme Cohesion
Strong connection to Beam Dynamics and Control:
  Need optimized beam dynamics to conserve low MTE (or emittance)
  In cases with
  significant space charge, or
  aberrations/ field nonlinearities
  Brightness will depend strongly on the beam dynamics!
Small MTE
High density
Bad
Transport
Large
Low
Several faculty in both themes

## Slide 8: Key Achievements (2016-2022)
1. Demonstration of 5 meV MTE
  – two orders of magnitude higher brightness of low current density applications
2. Effects of non-linear photoemission on MTE
  – limits MTE in for high current density applications
  3. Development of ultrasmooth ordered alkali-antimonide films
    – can give low MTE for high current density applications
4. Development of robust coating techniques for vacuum sensitive cathodes
  – essential for protecting vacuum sensitive cathodes in extreme conditions
5. Sub-nm emittance measurement diagnostics in accelerators
(together with BDC theme)
  – critical for low emittance and high brightness measurements
Karkare et al Phys. Rev. Lett. 125, 054801(2020) – Editor’s suggestion
Bae et al. J. Appl. Phys., 124,. 244903, (2018)
Parzyck et al, Phys. Rev. Lett. 128, 114801 (2022) – Editor’s suggestion
Patent Pending
M. Gordon et al. Phys Rev Accel. Beams, Phys. Rev. Accel. Beams 25, 084001 (2022)
Notes: These have impacted a lot of research in accelerators and elsewhere

## Slide 9: New in 2023—What I’ll tell you today
1. Demonstration of 5 meV MTE
  – two orders of magnitude higher brightness of low current density applications
  NEW: Understanding MTE from polycrystalline materials
2. Effects of non-linear photoemission on MTE
  – limits MTE in for high current density applications
  NEW: Experimental measurements confirm calculations
  3. Development of ultrasmooth ordered alkali-antimonide films
    – can give low MTE for high current density applications
    NEW: New alkali antimonide phases and new materials
4. Development of robust coating techniques for vacuum sensitive cathodes
  – essential for protecting vacuum sensitive cathodes in extreme conditions
  NEW: high current / high field tests and new theoretical understanding
5. Sub-nm emittance measurement diagnostics in accelerators
(together with BDC theme)
  – critical for low emittance and high brightness measurements
Karkare et al Phys. Rev. Lett. 125, 054801(2020) – Editor’s suggestion
Bae et al. J. Appl. Phys., 124,. 244903, (2018)
Parzyck et al, Phys. Rev. Lett. 128, 114801 (2022) – Editor’s suggestion
Patent Pending
M. Gordon et al. Phys Rev Accel. Beams, Phys. Rev. Accel. Beams 25, 084001 (2022)

## Slide 10: PHC Graduate Students and Postdocs
Vivek Anil,
Cornell
Daniel Franklin, NIU
David Garcia, UCLA
Jason Gibson, U Florida
Tariqul Hasan, NIU
Mariam Hasany, Cornell
Ali Kachwala, ASU
Gerard Lawler, UCLA
Sam Levenson, Cornell
Joshua Mann, UCLA
Priyadarshini Bhattacharyya, ASU
Azriel Finsterer, Cornell
Chad Pennington, Cornell
Annabel Selino, Cornell
Tyler Wu, Cornell
Amy Zhu, Cornell
Elena Echeverria, Cornell
Notes: Current Students and Postdocs in PHC

## Slide 11: Partnerships
Theme PHC is strongly connected to Beam Storage and Transport—we hold regular joint meetings, multiple overlap areas.
National Laboratory and industry partners:
Cathode characterization
Photoinjector Physics
Emittance Diagnostics
Nanofabrication
With theme 3: Space charge simulations with low MTE cathodes
Photocathode
simulation
RF gun load-lock development
Cathodes for semiconductor metrology
Photocathode development
xLight:
High power electron sources
Cathodes for electron
microscopes

## Slide 12: CBB Theme 1 Objectives
Objective 5 statement (short format)
current

## Slide 13: Objective 1
Develop photocathodes for high peak intensity generation with <5 meV MTE
Already demonstrated 5 meV MTE for low peak intensity applications
(Key accomplishment 1)
5 meV MTE measured from Cu(100)
Most photoinjectors use MTE ~500 meV
Non-linear effects will limit MTE in metals to few 100 meV for large charge densities (theory)
Photoemission at the threshold
Cooled to LHe (30K)
Atomically ordered flat surface
Good band-structure
Notes: Remove deliveres roadmap

## Slide 14: Objective 1
Develop photocathodes for high peak intensity generation with <5 meV MTE
Already demonstrated 5 meV MTE for low peak intensity applications
(Key accomplishment 1)
5 meV MTE measured from Cu(100)
Most photoinjectors use MTE ~500 meV
New 2023: experimental confirmation of theory
C. Knill et al., in prep.
Use high QE cathodes to minimize laser fluence and non-linear effects
Photoemission at the threshold
Cooled to LHe (30K)
Atomically ordered flat surface
Good band-structure
Notes: Remove deliveres roadmap

## Slide 15: Objective 1
Develop photocathodes for high peak intensity generation with <5 meV MTE
Objective 1, Theory Deliverable (1.3): First principles predictions of MTE and QE spectral response for relevant photocathode materials
Lots of new results here. Each are well-integrated with other objectives.
I will call them out as we go along.
New theoretical results on QE and MTE of disordered surfaces (P. Saha et al, JAP 2023)
First-principles calculations of electron transmission through graphene (and other monolayer protection layers)
Excellent DFT agreement with ARPES data from a new alkali antimonide phase.
Theory
Look out for this symbol:

## Slide 16: Objective 1
Develop photocathodes for high peak intensity generation with <5 meV MTE
Deliverable 1.1: A photocathode with MTE < 35 meV and QE > 10-3 at low or moderate laser fluence and at room temperature
New data: a smaller work function for poly-crystalline Cs3Sb than anticipated. MTE arises from excess energy of impurity states, not surface roughness
A. Kachwala, P. Saha, et al., in prep.
~40 meV MTE
@ QE
Notes: STO Is very smooth—much smoother than Si film.

## Slide 17: Objective 1
Develop photocathodes for high peak intensity generation with <5 meV MTE
Deliverable 1.1: A photocathode with MTE < 35 meV and QE > 10-3 at low or moderate laser fluence and at room temperature
Our emphasis now: single crystal photocathodes, and QE engineering.
High red efficiency
Smooth enough for
optical interference
E. Echeverria
+ C. Pennington
Notes: Keep transfer and science separate.
Simplify explanation--QE engineering opens the door.

## Slide 18: Objective 1
Develop photocathodes for high peak intensity generation with <5 meV MTE
Deliverable 1.1: A photocathode with MTE < 35 meV and QE > 10-3 at low or moderate laser fluence and at room temperature
Not just alkali antimonides! A visible light Dirac semimetal emitter: Na3Bi
Grown at PARADIM facility at Cornell
Work function of 2.5 eV
V. Anil, E. Echeverria, C. Pennington
Notes: Emphasize work in progress, other dirac semimetals.

## Slide 19: Objective 1
Develop photocathodes for high peak intensity generation with <5 meV MTE
Prediction of <20meV MTE even at large laser fluences for ordered alkali-antimonides
(Key accomplishment 2)
Deliverable 1.2 (Priority): A photocathode with MTE < 35 meV and QE > 10-3 at laser fluences in excess of 50 µJ/cm2 by developing cryo-cooled single-crystal, epitaxial alkali antimonides or other materials
Optimizations of a potential injector for LCLS-II HE
Nearly doubles x-ray photon energy at LCLS-2-HE
Greater FEL output
Smaller new FELs
  Theme 3 CBB Result
Partnership:
Ongoing DOE project with SLAC to transfer cathode recipes for use in the LCLS-2-HE SRF gun. Cathode is robust enough for LCLS-2-HE gun
Theory
Notes: Delete the plot on right and replace with text (bold)
Call out knowledge tranfer here (connect other pieces)

## Slide 20: Objective 2
Design materials for long-lived cathodes in extreme electric field and high average current
Protective graphene coatings
UHV graphene coating technique to protect an air sensitive thin film of various oxidation-sensitive metals such as Magnesium. Demonstration of protection of an alkali-antimonide film is underway
Robust activation overlayers
Cs-Sb based coatings to activate GaAs to negative electron affinity for robust high QE emission
Inert high QE cathodes
Cs-free, air stable cathodes based on GaN heterostructures.
Demonstrated QE of 10-3, with MTE of 100 meV.
Patent Pending
Notes: Mention patent.

## Slide 21: Objective 2
Design materials for long-lived cathodes in extreme electric field and high average current
We’ve spent significant effort getting a cathode test “ecosystem” up and running in CBB, both for
High Average Current (10s of mA)
High Electric fields (100 MV/m and greater)

## Slide 22: Objective 2
High Field Test Site 1: UCLA Pegasus
NCRF S-band gun capable of up to 100 MV/m. Equipped with load lock for vacuum cathode transfer.
Demonstrated cathode transfer from Cornell.
Cornell alkali antimonide cathodes helped access much higher charge for THz FEL experiments.
More tests planned this year.

## Slide 23: Objective 2
High Field Test Sites at Collaborating National Labs
We have ongoing collaborations with FNAL and ANL to test photocathodes in their high gradient guns.
FNAL: FAST/IOTA, and L-band gun and SRF injector
Cathode tests to begin this summer (Cornell and NIU photocathodes)

## Slide 24: Objective 2
High Field Test Sites at Collaborating National Labs
We have ongoing collaborations with FNAL and ANL to test photocathodes in their high gradient guns.
Argonne Wakefield Accelerator Facility: Various high gradient guns
AWA cathode test stand
AWA Drive and Witness Linacs
BDC talk will discuss beam dynamics studies upcoming at UCLA, FNAL, ANL

## Slide 25: Objective 2
High Field Test Site 2: UCLA CYBORG (in commissioning)
NCRF cryogenic (65 K) c-band (~6 GHz) very high field (>120 MV/m) test station.
Will be upgraded to include vacuum load lock.
UV (250-350nm)
Alignment Laser
Doublet
Gun
Solenoid
YAG or DRZ screen
Gun Cryostat
Faraday Cup
Dipole
G. Lawler

## Slide 26: Objective 2
High Average Current Test Site: HERACLES @ Cornell
The only university test-setup for very high average current photocathode tests (multiple 10s of mA)

## Slide 27: Objective 2: More robust coatings for GaAs
In-gun testing is a must. Example: Sb-Cs-O activation for GaAs in HERACLES
Test chamber lifetime (vacuum poisoning): 5-10x longer than traditional activation (Cs-O).
Lifetime in gun only ~50% improved—ion back bombardment has similar effects on the Cs and the Cs-Sb-O.
Cs-O
alone
J.K. Bae et al, AIP Advances, 2023
Low Current
High Current (1 mA)

## Slide 28: Objective 2: A more robust alkali antimonide
Alkali antimonides are full of surprises: A “new” phase of Cs-Sb is a more robust high efficiency visible light photocathode. Cs3Sb --> Cs1Sb
STM: Atomically Flat
ARPES matches Theory!
Good QE and >10x lifetime!
C. T. Parzyck, C. A. Pennington, W. J. I. DeBenedetti, J. Balajka, E. Echeverria, J. K. Nangoi, V. Anil, A. Galdi, in prep.
Theory
Notes: Too much time on flatness.

## Slide 29: Objective 2: A more robust alkali antimonide
Alkali antimonides are full of surprises: A “new” phase of Cs-Sb is a more robust high efficiency visible light photocathode. Cs3Sb --> Cs1Sb
STM: Atomically Flat
Theory prediction of Phase diagram
Good QE and >10x lifetime!
J. Gibson and A. Hire
Theory
C. T. Parzyck, C. A. Pennington, W. J. I. DeBenedetti, J. Balajka, E. Echeverria, J. K. Nangoi, V. Anil, A. Galdi, in prep.

## Slide 30: Objective 2: Understanding Graphene Protection
New theoretical result: understanding the transmission of electrons through graphene and other 2DM.
Lippman Schwinger Eqn for QM Scattering
E (eV)
0
0.5
0
1
Graphene
hBN
E (eV)
0
0.5
0
1
T. Wu
Transmission
Reflection
Reflection
Transmission
Theory
Transmission
Reflection
E (eV)
0
0.5
0
1
NbSe2

## Slide 31: Objective 3
Approach fundamental brightness limits with nanostructured photoemitters
Can we obtain the quantum limit of emittance/brightness by manipulating emission area along with low MTE?
I will focus on the first deliverable, as it is presently the main focus of our activities, and enables the other two.

## Slide 32: Objective 3
Approach fundamental brightness limits with nanostructured photoemitters
Deliverable 3.1 (priority): A photoemission electron source with sub-100 nm spot size
Recent developments:
Commissioned the PEEM at ASU in conjunction with a tunable wavelength pulsed laser to get sub-40 nm spatial resolution
Current Status/Plans:
Test performance of immersion lens based focusing
Resolve issues with plasmonic focusing and work function nano-patterning
Performed first tests of plasmonic focusing and work function nano-patterining
Plasmonic focusing spiral structures show emission hotspots due to nanofabrication imperfections
Cu patch on Pt observed in PEEM under 260nm illumination.
Surface impurities cause work functions to be inverted
Impact: 10x improved resolution for UED
End user: JOEL/IDES and HiRES at LBNL
2023: New design to eliminate hotspots
2023: New prep method to reduce contamination

## Slide 33: Objective 3
Approach fundamental brightness limits with nanostructured photoemitters
New in 2023: Understanding emittance growth in plasmonic nano-emitter arrays
Plasmonic grooves enhance light absorption and localize emission. Edge fields can grow emittance.
Leads to emittance asymmetry!
C. Pierce et al., PRA, 2023.
Notes: Nanoscale geometry affects how well the beam focuses

## Slide 34: Our Output: Highly Trained Scientists
Alice Galdi, Faculty, U Salerno
William Li, Postdoc, BNL
J. Kevin Nangoi, Postdoc, UCSB
Jan Balajka, Postdoc, TU Wien
Joshua Paul, Postdoc, Argonne
Eylene Pirez, Head Digital Media, Geodesic Pictures
Erik Skibinski, PhD
Jorge Giner Navarro, Researcher, CIEMAT
Will DeBenedetti, Postdoc, LANL
Dulanga Somaratne, PhD
Jared Maxson, Faculty, Cornell
Siddharth Karkare, Faculty, ASU
Alex Bernstein, NSA
Matt Andorf, Research Assoc., Cornell
Oksana Chubenko, Faculty, NIU
Jai Kwan Bae, Postdoc SLAC
Chris Knill, R&D Scientist Honeywell
Pallavi Saha, Postdoc, BNL
Nathan Majernik, Staff Scientist SLAC
Academia
Industry
National Lab/Gov

## Slide 35: CBB Legacy
Convergence Science
Photoemission sources: a branch of the new discipline, accelerator materials.
Knowledge
Deeper understanding of fundamental photoemission processes relevant to electron sources
Workforce
Training several graduate students in the field of accelerator physics (electron sources) – an area of critical need for current and future accelerator projects
Technology and applications
By 2026: Develop and deploy transformative electron source technology for:
  Free Electron Lasers
  Particle colliders Macro-molecule single-shot UED
  Atomic scale time-resolved electron microscopy
Growing Convergence Research
NSF Big Idea
Understanding the Rules of Life
NSF Big Idea
Quantum Leap
NSF Big Idea
Notes: Power of Accelerator Materials…