## Slide 1: Mechanistic Investigations of the Substrate-Mediated Factors Influencing Nb3Sn Film Growth Sarah Willson, Rachael Farber, Ajinkya Hire, Van Do, Richard Hennig, Steven Sibener
CBB Annual Meeting 2023

## Slide 2: Nb3Sn Cavity SRF Performance is Limited By Near-Surface Defects that Quench Superconductivity
U. Pudasaini, et al. Supercond. Sci. Technol. 32, 045008 (2019).
Sn-depleted
region
interface
Stoichiometric and structural inhomogeneities, surface roughness, grain size, etc.
Sn segregation on SRF cavity surface
Nb3Sn Sample Supplied by R. Porter (Cornell Univ., SLAC)
400 nm
Impacts
Superconducting critical temperature, accelerating gradients, quality factor, etc.

## Slide 3: Conducting Growth Studies for Optimal Nb3Sn Films
Nb3Sn growth and quality dependent on:
1. Deposition conditions
Relationship between Sn vapor flux and Nb substrate deposition temperature
  Insufficient Sn flux  Sn-deficient regions
  Excess Sn flux  persistence of Sn hot spots
2. Nb substrate morphology
Nb surface sites determine initial Nb-Sn interfacial interactions
  Nucleating agent typically used to stabilize adlayers
Many Nb oxidation states and structures with unique energetics
Nb3Sn Growth – Vapor Deposition
T: 500 -1000 ºC
T: 950 -1200 ºC
Coating
Incorporation
Nb substrate
Sn atoms
Nb3Sn film
It is not well understood which specific Nb features influence Sn nucleation and alloy growth

## Slide 4: Experimental Techniques
Ultra-high vacuum chamber with in situ:
Nb substrate modification
  Annealing ( < 1700 °C), Ar+ sputtering, gas dosing
    Control over oxidation, roughness, contaminants, etc.
Nb3Sn growth
  3 independent electron beam evaporation cells
  Vapor flux calibrated with quartz crystal microbalance (QCM) to sub-monolayer (ML) precision
  Variable substrate deposition temperature
Surface characterization
  Auger electron spectroscopy (AES)
  X-ray photoelectron spectroscopy (XPS)
  Scanning tunneling microscopy/spectroscopy (STM/STS)
Ex situ analysis
Scanning electron microscopy (SEM)
Energy dispersive spectroscopy (EDX)
Grazing incidence X-ray diffraction (GIXRD)
Atomic force microscopy (AFM)
STM Chamber
Cleaning & Analysis Chamber
Growth Chamber

## Slide 5: Outline
Examining Nb3Sn film growth across coverage regimes
How can we leverage surface chemistry techniques to better understand reactivity of these SRF interfaces?
Can studying Nb and Nb3Sn surface behavior inform optimal film growth efforts?
Comparing morphology and oxidation pathways for:
  Nb substrate
  Nb3Sn film
Sub-monolayer
5 nm
30 nm
Full Nb3Sn film
Thickness
1 μm
Initial film growth
Sn wetting & nucleation
Atomic interactions

## Slide 6: Niobium Oxidation at Sn Deposition Temperatures
Nb2O5
  Near-amorphous structure with many possible crystalline phases
  Rapid reformation from either from either bulk precipitation or dissociative chemisorption of environmental H2O/O2
NbO
  High temperature annealing ( >1530 ºC) forms various reconstructions
  (3×1)-O/Nb(100) forms a highly ordered “ladder” structure
STM of (3×1)-O Nb(100)
ladder rung
ladder rows
ladder edge
(3×1)-O/Nb(100) unit cell
S.A. Willson, R.G. Farber, A.C. Hire, R.G. Hennig, S.J. Sibener, J. Phys. Chem. C 2023, 127, 6, 3339–3348

## Slide 7: Nb Oxidation Impact on Sn Nucleation and Nb3Sn Growth
Compared Sn nucleation and initial Nb3Sn film growth for Sn deposited on polycrystalline Nb in either a NbO or Nb2O5 state
  Films grown under same coating conditions (Tdep: 850 - 900ºC)
  Similar Nb3Sn film morphologies
  More Sn nucleation sites on Nb2O5
    Growth of new intermetallic domains
More oxidized Nb surface enhances Sn nucleation and aids in the formation of new intermetallic domains
Nb2O5
NbO
vs.
Nb3Sn film
Sn islands on Nb
New intermetallic domains & more Sn islands
30 nm Nb3Sn films

## Slide 8: Niobium Oxidation at Sn Deposition Temperatures
Is oxygen playing a role in Nb3Sn coordination?
Low temperature annealing reduces Nb2O5  NbO
  Same BE and O at. % as NbO with disordered structure
During heated deposition on Nb2O5, Sn is interfacing with a NbO with different available binding sites
Is Sn adsorption unfavorable at specific (3×1)-O/Nb(100) surface sites?
15 nm
Nb2O5+ 300 ºC  NbO
Nb+5

## Slide 9: Sn Nucleation on (3×1)-O/Nb(100)
Sn unable to form uniform layer on (3×1)-O/Nb(100) surface
Increased (3×1)-O/Nb(100) defect density
  Higher proportion of edge sites not containing the characteristic (3×1) coordination
  Sn persists at higher temperatures due to favorable defects on Nb surface
Sn + 850 ºC anneal
Sn + 850 ºC anneal
Farber, R.G., Willson, S.A., Sibener, S.J. JVST A 39, 063212 (2021)
Sn fully desorbed
Sn remaining on surface
Surface defects do impact Sn desorption rates and improve nucleation
High defect density (31.3 %)
Medium defect density (17.8 %)

## Slide 10: (3×1)-O/Nb(100) Binding Energies
Both experimental and theoretical results suggest instability of Sn adlayers and atoms along the on (3×1)-O rung sites
DFT calculations done by Ajinkya Hire (Hennig Group)
  Identified only 2 favorite Sn adsorption sites
  No converged Sn overlayer on (3×1)-O/Nb(100) with experimental atomic spacing
Sn diffusing to ladder edge sites
adsorbed Sn atoms
Evidence for specific
(3×1)-O/Nb(100) surface sites inhibiting Sn nucleation
S.A. Willson, R.G. Farber, A.C. Hire, R.G. Hennig, S.J. Sibener, J. Phys. Chem. C 2023, 127, 6, 3339–3348
Nanoscale structure drives Sn stability on the surface

## Slide 11: Outline
Comparing morphology and oxidation pathways for:
  Nb substrate
  Nb3Sn film
    CBB collaborators demonstrated
      Persistence of Nb3Sn oxides
      Impact of oxides on field dependence & SRF performance
Z. Sun et al., arXiv:2305.02467 [cond-mat.mtrl-sci]

## Slide 12: Varying Surface Morphology of Nb3Sn Grains
AFM
SEM
Different stoichiometry, roughness, and thermal stability of Nb3Sn indicate varying SRF performance
3 Distinct Nb3Sn Grains
Type 1 Smooth, stoichiometric Nb3Sn
  Only found in films > 275 nm thick
  Evidence of coalescing
  Higher thermal stability, resistance to degradation
Type 2 Corrugated, Sn-deficient
  30 – 50 nm surface buckling
  Largest surface area
  Sn deficiency throughout film, not segregated to the surface region
  Observed for all film growth conditions and thicknesses, preferentially found at surface
Type 3: Rough, Sn-rich
  ~ 50 – 100 nm spherical grains
  Higher roughness determined by grain size
  Observed across all films

## Slide 13: Nb3Sn Surface Stability and Oxidation Pathways
Nb+2
Nb+5
Sn+4
XPS: Nb3Sn Exposed to Atmosphere
XPS: Thermal Degradation of Deteriorating Nb3Sn
Energetically unfavorable terminations prone to:
  Reconstructions (i.e. NbO/Nb(100)  (3×1)-O/Nb(100))
  Reactivity (oxidation, contamination, etc.)
Observed 2 Distinct Oxidation Pathways
Atmosphere Exposure
  Nb3Sn does not form an oxide post-deposition (UHV, in situ)
  Post-oxygen exposure: formation of Nb(V)–Sn(IV)–O complex
    Oxide shift in both Nb, Sn XPS doublets
    Fully reducible – gentle annealing fully removes oxygen
Annealing Sn-deficient Nb3Sn
  Post-deposition annealing drives Sn segregation via precipitation & desorption
  Film deterioration: in situ formation of Nb(II)-Sn(II/IV)-O complex
    Oxide distinct from atmospheric-driven complex
    Sn oxide resistant to annealing under UHV
Sn+2,4

## Slide 14: Nb3Sn Surface Stability and Oxidation Pathways
Secondary e-
Backscattered e-
Energetically unfavorable terminations prone to:
  Reconstructions (i.e. NbO/Nb(100)  (3×1)-O/Nb(100))
  Reactivity (oxidation, contamination, etc.)
Observed 2 Distinct Oxidation Pathways
Atmosphere Exposure
  Nb3Sn does not form an oxide post-deposition (UHV, in situ)
  Post-oxygen exposure: formation of Nb(V)–Sn(IV)–O complex
    Oxide shift in both Nb, Sn XPS doublets
    Fully reducible – gentle annealing fully removes oxygen
Annealing Sn-deficient Nb3Sn
  Post-deposition annealing drives Sn segregation via precipitation & desorption
  Film deterioration: in situ formation of Nb(II)-Sn(II/IV)-O complex
    Oxide distinct from atmospheric-driven complex
    Sn oxide resistant to annealing under UHV
  Insulating Sn oxide regions identified with BSE mapping
    Morphologic & chemical marker to Nb3Sn decomposition

## Slide 15: Summary
Compared morphology and oxidation pathways for:
  Nb substrate
    Demonstrated structural factors that limit alloy growth on a less oxidized Nb surface
  Nb3Sn film
    Identified Nb3Sn grain morphologies, stabilities, and oxidation processes
Studies have provided a broad overview of Nb3Sn growth and optimization ranging from:
Contributes to the overall SRF/CBB mission to understand complex reactive interfaces for industrial implementation
Atomic-surface dynamics
Mesoscale materials growth
10 nm
Sn adsorption and incorporation
Nb3Sn Morphologies
Nb3Sn reactivity & stability

## Slide 16: Thank you for listening!
Special thanks to
Sibener Group
  Prof. Steve Sibener
  Prof. Rachael Farber
  Grad student Van Do
  Undergrad student Helena Lew-Kiedrowska
CBB
  SRF Theme
This work was supported by the U.S. National Science Foundation under Award PHY-1549132, the Center for Bright Beams.

## Slide 17: Nb Oxidation Impact on Sn Nucleation and Nb3Sn Growth
Compared Sn nucleation and initial Nb3Sn film growth for NbO or Nb2O5 polycrystalline Nb
  Films grown under same coating conditions
  Similar Nb3Sn film coverage and morphology
  More Sn nucleation on Nb2O5
    Growth of new intermetallic domains
Impact of varying Nb oxidation/structure is much less significant than the crystallographic orientation
Nb2O5
NbO
vs.
Nb3Sn film
Sn islands on Nb
New intermetallic domains
Crystallographic orientation is the dominating factor in early stages of Nb3Sn film growth
Nb(100)
Nb(111)
vs.
High domain coverage
Poor nucleation

## Slide 18: Varying Surface Morphology of Nb3Sn Grains
Preference for thicker films
3 Distinct Nb3Sn Grains
Type 1 Smooth, stoichiometric Nb3Sn
  Only found in films > 275 nm thick
  Evidence of coalescing
  Higher thermal stability, resistance to degradation
Type 2 Corrugated, Sn-deficient
  30 – 50 nm buckling at surface
  Largest surface area
  Sn deficiency throughout film, not segregated to the surface region
  Observed for all film growth conditions and thicknesses
Type 3: Rough, Sn-rich
  ~ 50 – 100 nm spherical grains
  Higher roughness determined by grain size
  Observed across all films
Diffraction of Nb3Sn Films
Small domain, always present
Associating surface morphology with grain orientation
Dominating at surface & in thin films