## Slide 1: Experimental set-up and motivation
~5-11 mm
Near-Field
Far-Field
~1 m
Near-field and far-field HEDM performed at the FAST beamline using the using the Rotational and Axial Motion System (RAMS2) loading frame
Mg-1Y (wt%)
Mg-3Zn-0.1Ca (wt%)
Goal: understand alloying effect of Y and Zn + Ca on twinning and <c+a> slip
(important deformation mechanisms in the hcp crystal structure)

## Slide 2
Beam Run Timeline
Mg-1Y specimen
(before loading)
Mg-1Y specimen
(during tensile loading)
Mg-3Zn-0.1Ca
Specimen
(before loading)
Mg-3Zn-0.1Ca
Specimen
(during compressive loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(before loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(during compressive loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(after un-loading)

## Slide 3
Mg-1Y specimen
(before loading)
Mg-1Y specimen
(during tensile loading)
Mg-3Zn-0.1Ca
Specimen
(during compressive loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(during compressive loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(after un-loading)
Mg-3Zn-0.1Ca
Specimen
(before loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(before loading)

## Slide 4
Mg-1Y specimen
(before loading)
Mg-1Y specimen
(during tensile loading)
Mg-3Zn-0.1Ca
Specimen
(during compressive loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(during compressive loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(after un-loading)
Mg-3Zn-0.1Ca
Specimen
(before loading)
2nd
Mg-3Zn-0.1Ca
Specimen
(before loading)
Mg-1Y specimen
(during tensile loading)
2nd Mg-3Zn-0.1Ca
Specimen
(during compressive loading)

## Slide 5
Mg-1Y (mg1y-1-nf_#)
(~50 µm diameter)
Near Field scans on specimens before loading
Mg-3Zn-0.1Ca (zx30-t1-nf_#)
(~150 µm diameter)

## Slide 6
Near Field scans on specimens before loading: Signs of pre-deformation deformation!
Zoomed in view zx30-t1-nf_29
Structure within spots suggests material experienced some deformation before the start of our loading experiment (during specimen machining/transport/loading?)
As a remote user in a mixed on-site/remote team, I’d feel more comfortable taking a first look at the NF data on the dashboard than using NoMachine