## Slide 1: Cathodes for high gradient SRF injectors
Ziye Yin Graduate Research Assistant yin@frib.msu.edu
Material for Bright Beams Workshop 2025

## Slide 2: Outline
Cathode Requirement for High-Gradient SRF Photoinjectors
  Superconducting RF photoinjectors
  Cathode requirement and candidates
Cathode Material Candidates
  Superconducting photocathodes : Nb, Pb
  Normal conducting metal cathodes : Cu, Mg
  Semiconductor cathodes : Cs2Te, K2CsSb, GaAs
Progress on Cathodes Testing in the LCLS-II HE SRF gun
  SRF Cavity test progress
  Cathode plug and K2CsSb cathode preparation
Summary and outlook

## Slide 3: Superconducting RF photo-injector
cryomodule
SC cavity
cathode
solenoid
E field
Driven laser
FPC
[1] Lewellen,J. etc. (2022). Status of the SLAC/MSU SRF Gun Development Project. Proceedings of the 5th North American Particle Accelerator Conference, NAPAC2022
[2] Bazarov, I. etc. (2009). Maximum Achievable Beam Brightness from Photoinjectors. Physical Review Letters, 102(10), 104801
LCLS-II-HE SRF Gun[1] (QWR)
SRF photoinjector sketch (elliptical)
High Brightness e- beam with High Repetition Rate e.g. 0.1 mmmrad @100pC @1MHz
cathode gradient and cathode MTE (Mean Transverse Energy)[2] e.g. 30MV/m and 184meV
Key determinants

## Slide 4: Cathode requirement and candidates
General requirement:
QE (quantum efficiency), thermal emittance, lifetime, response time
Surface roughness[1]  lower MTE and lower dark current
Special requirement for SRF injectors:
Cryogenic temperature: thermal conductivity, thermal expansion, heat load from laser and RF power
Multipacting: low SEY (secondary electron yield)
Avoid Contamination
Material candidates:
Metal: Superconducting / normal conducting  Robust and clean, but low QE
Semiconductor  High QE but fragile
[1] Gevorkyan, G. et al. (2018). Effects of physical and chemical surface roughness on the brightness of electron beams from photocathodes.
[2] Rao, T., & Dowell, D. H. (2013). An engineering guide to photoinjectors.

## Slide 5: Cathode requirement and candidates
cathode | Driven Laser | QE(%) @ room Temp. | Work function/ EG+EA (eV) | Theoretical thermal emittance(µm/mm)
Nb | UV | ~0.001 | 4.3 | 
Pb | UV | ~0.016 | 4.0 | 
Cu | UV | ~0.014 | 4.6 | 
Mg | UV | ~0.62 | 3.6 | 
Cs2Te | UV (262nm) | 10 | 3.5 | 0.9
K2CsSb | Green (532nm) | 5 | 2.1 | 0.38
GaAs(Cs,O) | Green (532nm) | 10 | 1.4 | 0.44
cathode | Driven Laser | QE(%) @ room Temp. | Work function/ EG+EA (eV) | Theoretical thermal emittance(µm/mm)
Nb | UV | ~0.001 | 4.3 | 
Pb | UV | ~0.016 | 4.0 | 
Cu | UV | ~0.014 | 4.6 | 
Mg | UV | ~0.62 | 3.6 | 
Cs2Te | UV (262nm) | 10 | 3.5 | 0.9
K2CsSb | Green (532nm) | 5 | 2.1 | 0.38
GaAs(Cs,O) | Green (532nm) | 10 | 1.4 | 0.44
[1] Rao, T., & Dowell, D. H. (2013). An engineering guide to photoinjectors.

## Slide 6: Cathode material candidates – SC metal – Nb/Pb
Directly use back wall of Nb cavity or coat Pb
[1] Smedley, J. etc.(2005). Photoemission studies on niobium for superconducting photoinjectors.
[2] Smedley, J. etc.(2008). Lead photocathodes.
Spectra response of Pb[2]
(QE)1/2 vs (field)1/2 of Nb[1]
6.5e-5@266nm
1.0e-4@248nm @1MV/m
2.8e-4@193nm
Max 2.72e-3@213nm, 1MV/m
Higher photon energy
 Higher MTE

## Slide 7: Cathode material candidates – SC metal – Nb/Pb
Nb cathode for UED/UEM application
Charge requirement is low <pC
Pb coated on Nb due to higher QE
Arc deposition gives best results
[1] Liu, A. etc. (2019). Optimization of an SRF Gun Design for UEM Applications.
[2] Nietubyć, R. etc. (2018). Optimization of cathodic arc deposition and pulsed plasma melting techniques for growing smooth superconducting Pb photoemissive films for SRF injectors.
Euclid Techlabs Schematic SRF photogun-based UEM system[1]
DESY 1.6cell SRF gun[2]
cathode QE[2]
Max QE 0.2%@200nm

## Slide 8: Cathode material candidates – NC metal – Cu/Mg
Robust, good rf properties and thermal conductivity, low dark current and SEY
Thermal isolation from Cavity (same for semiconductor) : choke cavity and cathode stalk
Cu: low QE (<10-4) but good for initial diagnostic purpose
Mg: high QE up to 0.5%
MSU/KEK 1.3GHz 1.5cell SRF gun
LCLS-II HE QWR SRF gun
A challenging mission to transfer cathode without contamination
Cathode plug
Cathode plug

## Slide 9: Cathode material candidates – NC metal – Cu/Mg
Performance of cathode in real injector @ HZDR 3.5cell 1.3GHz SRF gun
[1] Teichert, J. et al.(2014) Commissioning of an improved superconducting RF photo injector at ELBE.
[2] Teichert, J. et al. (2021). Successful user operation of a superconducting radio-frequency photoelectron gun with Mg cathodes. Physical Review Accelerators and Beams, 24(3), 033401.
Cu cathode performance[1]
Mg cathode performance[2]
Cu: ~0.5 mm mrad / mm @ 1pC @6MV/m
Mg: ~3 mm mrad / mm @ 250pC @ 14.5MV/m
Over one-year long operation
*same laser

## Slide 10: Cathode material candidates – Semiconductor – Cs2Te
Successful operation @ HZDR 3.5cell 1.3GHz SRF gun
high average current (1 mA) and low emittance (1 mm mrad @ 77 pC)
[1] Xiang, R. et al. (2010). Cs2Te normal conducting photocathodes in the superconducting rf gun. Physical Review Special Topics - Accelerators and Beams, 13(4), 043501.
[2] Xiang, R., & Schaber, J. (2022). Review of Recent Progress on Advanced Photocathodes for Superconducting RF Guns. Micromachines, 13(8), 1241.
thermal isolation
Cs contamination
field emission
multipacting
high QE (1-10%) @ UV
relatively robust
high gradient (100MV/m)
demonstrated in NCRF guns
evaporators
Cs
Te
Mo substrate performance[1]
Cu substrate performance[2]
Lifetime > one year
Without cavity warm up

## Slide 11: Cathode material candidates – Semiconductor – K2CsSb
High QE in green wavelength, low thermal emittance
So ideal but unstable and complicated fabrication
Smoother
Sequential deposition to co-deposition[1]
Coating temperature dependence[3]
Substrate dependence[5][6]
Epitaxy growth[7]
[1] Feng, J. et al. (2017). Near atomically smooth alkali antimonide photocathode thin films. Journal of Applied Physics, 121(4), 044904.
[2] Mamun, M. A. A. et al. (2016). Effect of Sb thickness on the performance of bialkali-antimonide photocathodes.
[3] Mohanty, S. K. et al. (2023). Development and Characterization of Multi-Alkali Antimonide Photocathodes for High-Brightness RF Photoinjectors. Micromachines, 14(6), 1182.
[4] Guo, L. et al. (2025). Improved robustness of sequentially deposited potassium cesium antimonide photocathodes achieved by increasing the potassium content towards theoretical stoichiometry. Scientific Reports, 15(1), 2900.
[5] Guo, L. et al. (2017). Substrate dependence of CsK2Sb photo-cathode performance. Progress of Theoretical and Experimental Physics, 2017(3).
[6] Smedley, J. et al. (2009). K2CsSb Cathode Development. AIP Conference Proceedings, 1062–1066.
[7] Parzyck, C. T. et al. (2022). Single-Crystal Alkali Antimonide Photocathodes: High Efficiency in the Ultrathin Limit. Physical Review Letters, 128(11), 114801.
[8] Wang, G. et al. (2018). Overcoming the quantum efficiency-lifetime tradeoff of photocathodes by coating with atomically thin two-dimensional nanomaterials. Npj 2D Materials and Applications, 2(1), 17.
[9] Yamaguchi, H. et al. (2017). Active bialkali photocathodes on free-standing graphene substrates. Npj 2D Materials and Applications, 1(1), 12.
Stronger
Sb thickness dependence[2]
Stoichiometry dependence[4]
Graphene/2D protection layer[8][9]

## Slide 12: Cathode material candidates – Semiconductor – K2CsSb
[1] Petrushina, I. et al. (2020). High-Brightness Continuous-Wave Electron Beams from Superconducting Radio-Frequency Photoemission Gun. Physical Review Letters, 124(24), 244801.
[2] Wang, E. et al. (2021). Long lifetime of bialkali photocathodes operating in high gradient superconducting radio frequency gun. Scientific Reports, 11(1), 4477.
[3] Huamu, Xie (2023). Successful operation of K2CsSb photocathode in DC-SRF-II gun. Talk at Photocathode Physics for Photoinjectors(P3) Workshop.
QE evolution at BNL SRF gun[1][2]
Current evolution at PKU DC-SRF-II gun[3]
0.28 um @ 20pC; 0.43 um @ 50pC; 0.58 um @ 100pC
16 hours operation time @ PKU
Gradient @ 18MV/m
0.3 um @ 100pC; 0.57 um @ 600pC
one month operation time @ BNL

## Slide 13: Cathode material candidates – Semiconductor – GaAs
High QE at green wavelength
Polarized beam generation (Cs, O layer)
Successful test in BNL 2025
Super fragile, still long way to go
[1] Litvinenko, V. et al. (2025). Breakthrough in Generation of Polarized Electron Beams: Unveiling the World’s First RF Electron Gun with GaAs Photocathode.
QE start from 0.05%; lifetime 24hrs; charge lifetime 1.3mC for CW
GaAs cathode assembly[1]
GaAs QE and charge evolution[1]

## Slide 14: Progress on Cathodes Testing in the LCLS-II HE SRF gun
Successful test of the blank cavity (without cathode port) > 30MV/m
Cold test results
Cold mass
Cathode stalk
Full assembly
Next step is cavity test with cathode stalk in new cryomodule
With Cu plug (dark current could be measured)

## Slide 15: Progress on Cathodes Testing in the LCLS-II HE SRF gun
K2CsSb has been successfully fabricated at FRIB
Sequential deposition
Si and Nb substrate
Ongoing modification for LCLS-II HE gun suitcase
Co-deposition ability
Mo layer on Cu plug substrate
[1] Yin,Ziye, et al. (2024). Development of Bi-Alkali antimonide photocathodes for a 1.3 GHz superconducting rf photo-injector.
Cathode preparation chamber
Fabricated K2CsSb cathode spectra response[1]

## Slide 16: Progress on Cathodes Testing in the LCLS-II HE SRF gun
A diagnostic beam was tested by a 20KeV DC gun
Cathode can be directly transferred to DC gun
Laser system is built by ourselves (ongoing)
515nm, 1ps, 40.625MHz, 0.1mW
electron 100fC/bunch and 1uA average current
Beamline picture
gun
solenoid
BPM
mirror chamber
faraday cup
& screen
faraday cup
& screen
Bending magnet
pulsed laser system
Cathode chamber
DC gun chamber

## Slide 17: Summary and Outlook
LCLS-II HE needs 0.1mm *mrad @ 100pC initial electron beam
High gradient SRF photoinjector is being developed, blank cavity is verified
Cathode is one of the key component of it
Metal are clean and robust but not qualified as a cathode
Semiconductor photocathodes especially K2CsSb have the potential to meet the requirements but still need further effort

## Slide 18: Acknowledgement
Thanks for everyone helping with this talk:
John Smedley, SLAC
John Lewellen, LANL
Ting Xu, FRIB
Taro Konomi, FRIB
Rong Xiang, HZDR
Erdong Wang, BNL

## Slide 19: Q&A
Thank you for your attention!

## Slide 20: Back up slides: cathode test timeline
Task | Description | Year 1 |  |  |  | Year 2 |  |  | 
1 | Beam line and laser system design |  |  |  |  |  |  |  | 
2 | Cathode shape optimization |  |  |  |  |  |  |  | 
3 | Plasma processing development |  |  |  |  |  |  |  | 
4 | Procurements and fabrication |  |  |  |  |  |  |  | 
5 | Cathode growth system development |  |  |  |  |  |  |  | 
6 | Bunker preparation |  |  |  |  |  |  |  | 
7 | Device hazard analysis and review for beam tests in bunker |  |  |  |  |  |  |  | 
8 | Cryomodule cool down and Run 1 |  |  |  |  |  |  |  | 
9 | Cryomodule rework (if needed) |  |  |  |  |  |  |  | 
10 | Cryomodule cool down and Run 2 |  |  |  |  |  |  |  | 
11 | Cryomodule cool down and Run 3 |  |  |  |  |  |  |  | 
This summer Cu plug will be tested, and dark current will be measured
Semiconductor test plan is within next two years