## Slide 1: Modeling Photoemission in Alkali Antimonides from Ab Initio Many-body Theory Richard Schier & Caterina Cocchi Carl von Ossietzky Universität Oldenburg , Germany Friedrich-Schiller-Universität Jena, Germany July 16, 2025

## Slide 2: Motivation
Previous works:
Understand photocathode materials, especially alkali-antimonides, with ab initio many-body methods
© HZB / Dirk Laubner
R. Schier et al., Adv. Theory Simul. 7, 2400680 (2024)
R. Schier & C. Cocchi, Phys. Rev. Mat. 9, 053804 (2025)
R. Schier et al., Phys. Rev. Mat. 6, 125001 (2022)
C. Xu et al., Electron. Struct. 7, 015001 (2025)
Surface properties:
High-throughput
screening:
Electronic band structure
& optical spectrum:

## Slide 3: Three Step Model
ħω
Excitation (I)
Emission (III)
Scattering (II)
Bulk
Surface
e-
W. E. Spicer, Phys. Rev. 112, 1 (1958)
C. N. Berglund & W. E. Spicer, Phys. Rev. 136, A1030 (1964)
Recent implementations based on DFT:
E. R. Antoniuk et al.,
Phys. Rev. B 101, 235447 (2020)
P. Saha et al.,
J. Appl. Phys. 133, 053102 (2023)
We present an implementation of the three step model with results from many-body theory.
DFT is a ground-state theory and does not cover electron-electron / electron-hole correlations!

## Slide 4: Theory Workflow
Ground state: Kohn-Sham equations
Electron-electron correlation: Self-energy correction
Electron-hole correlation: Bethe-Salpeter equation (BSE)
DFT
G0W0
BSE
W. Kohn and L. J. Sham, Phys. Rev. 140, A1133 (1965)
L. Hedin, Phys. Rev. 139, A796 (1965)
E. E. Salpeter and H. A. Bethe, Phys. Rev. 84, 1232 (1951)
Accurate band gap
Optical spectrum
Excitonic weights

## Slide 5: Electronic & Optical Properties of K3Sb
Band Structure
Energy [eV]
5
4
3
2
1
0
-1
-2
-3
A
H
Γ
L
K
M
Im εM
Energy [eV]
R. Schier & C. Cocchi,
Phys. Rev. Materials 9, 053804 (2025)
Optical Spectrum
Hexagonal K3Sb
G0W0 DFT
Excitonic Weights
A
H
Γ
L
K
M
Energy [eV]
=
Ⱶ

## Slide 6: Step I: Excitation
Im εM averaged over all components
Energy [eV]
Im εM
Excitation
Emission
Scattering

## Slide 7: Step II: Transport / Scattering
Scattering can be covered through Monte Carlo simulations.
[P. Gupta et al., J. Appl. Phys. 121, 215702 (2017)]
Scattering is negligible in semiconducting thin films.
No scattering in this model.
Excitation
Emission
Scattering

## Slide 8: Step III: Emission
Energy Photon [eV]
Im εM
Excitation
Emission
Scattering
Energy Electron [eV]
Energy distribution of excited electrons
P(E)
Optical Spectrum

## Slide 9: Emission Probability
Simple approximation for PEmission (E): potential step
Energy electron [eV]
PEmission
ħω
e-
Here: V0 from experiment
[W. E. Spicer, Phys. Rev. 112, 1 (1958)]
R. Schier et al., Phys. Rev. Mat. 6, 125001 (2022)
V0
Alternative: surface slab calculation:

## Slide 10: Emission by Photon Energy
Photon Energy [eV]
PEmission

## Slide 11: Final Result
Photon Energy [eV]
Photon Energy [eV]
PEmission
Im εM
Photon Energy [eV]
Im εM * PEmission
Hexagonal K3Sb

## Slide 12
Experimental data from W. E. Spicer, Phys. Rev. 112, 1 (1958)
Comparison with Exp. Spectral Response
QE
Photon Energy [eV]
Hexagonal K3Sb

## Slide 13: Results for other Alkali Antimonides
Cs3Sb
cubic
Na3Sb
hexagonal
CsK2Sb
cubic

## Slide 14: Example 2: Na3Sb
Experimental data from W. E. Spicer, Phys. Rev. 112, 1 (1958)
Photon Energy [eV]
QE
Hexagonal Na3Sb

## Slide 15: Example 3: Cs3Sb
Experimental data from P. Saha et al., Appl. Phys. Lett. 120, 194102 (2022)
Photon Energy [eV]
QE
Cubic Cs3Sb

## Slide 16: Example 4: CsK2Sb
Experimental data from L. Guo and M. Katoh, Phys. Rev Accelerators and Beams 22, 033401 (2019)
Photon Energy [eV]
QE
Cubic CsK2Sb

## Slide 17: Summary & Conclusions
We adopted Spicer’s Three-Step-Model to create a description of the photoemission process based on the results from ab initio many-body perturbation-theory.
This goes beyond works based solely on DFT, as we now include electron-electron & electron-hole correlations.
Computational costs are higher than with DFT, but we already have a large set of results from previous works.
Project No. 490940284
Special Thanks to Thorsten Kamps & Team