## Slide 1: SRF for future accelerators: What performance do we need?
Materials for Bright Beams Workshop
July 16, 2025
Gianluigi Ciovati

## Slide 2: DO PROJECTS DRIVE R&D ON SRF PERFORMANCE?
The TESLA Technology Collaboration (1992): Develop SRF for the future TeV Linear Collider
Increase the accelerating gradient by a factor of 5
Reduce cost per MV by a factor 20
Make possible pulsed operation
C. Pagani, “European Overview of TESLA Technology Related Activities”, TESLA TTC Meeting, DESY, 30 March - 1 April 2004
Notes: From 5 to 25 MV/m
New cryomodule concept and Industrialization
3 cavity productions from 4 European industries: Accel, Cerca, Dornier, Zanon
The 800 GeV upgrade (from 500 GeV) requires an accelerating field gradient of 35 MV/m

## Slide 3: ILC: HIGH-GRADIENT R&D
2013: The ILC Technical Design Report is released. Cavities operating in a cryomodule at Eacc = 31.5 MV/m with Q0>1×1010 at 2 K
2011: 16 cavities meeting the ILC specification of Eacc = 35 MV/m with Q0>8×109 at 2 K with 90% yield in a vertical test setup
R. Geng et al., “Progress of ILC high gradient SRF cavity R&D at Jefferson Lab”, Proc. IPAC2011, San Sebastian, Spain, p. 334.
D Broemmelsiek et al., “Record high-gradient SRF beam acceleration at Fermilab”, New J. Phys. 20, 113018 (2018).
2018: ILC-type CM achieves <Eacc> = 32.2 MV/m with <Q0>9×109 at 2 K
Notes: 500 GeV CM
Cavities built by AES and RI
Global effort DESY, JLab, FNAL, KEK and Cornell

## Slide 4: HIGH-GRADIENT: STATE OF THE ART
K. Saito, “Gradient Yield Improvement Efforts for Single and Multi-Cells and Progress for Very High Gradient Cavities”, Proc. SRF2007, Beijing, China, p. 82.
W. Singer et al., “Development of large grain cavities”, Phys. Rev. ST Accel. Beams 16, 012003 (2013).
Single-cell: 59 MV/m (223 mT) at 2 K
Reentrant shape
9-cell: 45.5 MV/m (194 mT) at 2 K
Large-grain Nb
Notes: 2007. Collab. Between KEK/Cornell. Not reproduced
2013. Large-grain Q0 close to 2e10

## Slide 5: DO RESULTS FROM R&D ENABLE NEW PROJECTS?
P. Dhakal, G. Ciovati and G. R. Myneni, “A path to higher Q0 with large-grain Nb cavities”, Proc. IPAC2012, New Orleans, LA, May 20-25, 2012, p. 2426.
A. Grassellino et al., “Nitrogen and argon doping of niobium for superconducting radio frequency cavities: a pathway to highly efficient accelerating structures”, Supercond. Sci. Technol. 26, 102001 (2013).
D. Gonnella et al., “Industrial cavity production: lessons learned to push the boundaries of nitrogen doping”, Proc. SRF2019, Dresden, Germany, May 19-24, 2019, p. 1199.
LCLS-II

## Slide 6: THE SRF TREE
SRF R&D
ADS
ICS
Discovery Machines
Industrial Machines
ERL

## Slide 7: DISCOVERY MACHINES: LINEAR COLLIDER
F. Furuta et al., “High Gradient Results of ICHIRO 9-Cell Cavity in Collaboration With KEK and Jlab”, Proc. SRF’11, Chicago, IL, USA, p. 386.
R. Geng et al., “Performance of First Prototype Multi-Cell Low-Surface-Field Shape Cavity”, Proc. SRF'19, Dresden, Germany, Jun.-Jul. 2019, p. 222.
S. Posen, “Review of Thermal Treatments: Effects, Reliability, and Open Questions”, SRF’23, Grand Rapids, MI, USA, June 25-30, 2023.
“The International Linear Collider Machine Staging Report 2017”: considered options for higher Eacc = 35 MV/m
“Ichiro” cavity: 40 MV/m (2010)
“LSF” cavity: 32 MV/m (2019)
<Eacc> = 40 MV/m in standard ILC cavities
Notes: Cold EP + 2-step baking

## Slide 8: DISCOVERY MACHINES: LINEAR COLLIDER
S. Belomestnykh et al., “HELEN: traveling wave SRF linear collider Higgs factory”, Proc. IPAC’23, Venice, Italy, May 2023, p. 788.
F. Furuta et al., "Progress and challenges in traveling-wave (TW) SRF cavity", in Proc. LINAC2024, Chicago, IL, USA, Aug. 2024, p. 621.
Proposal for a 250 GeV linear collider based on TW SRF:
p/2 mode, Bp/Eacc~2.88 mT/(MV/m)
High-power feedback waveguide
Challenges:
Cavity fabrication
Tuning of the feedback waveguide
Notes: Bp/Eacc ~30% less than ILC
Constant acceleration through the cavity

## Slide 9: DISCOVERY MACHINES: FCC-ee
F. Peauger et al., “FCC-ee SRF Cavity Design and RF Powering Scheme”, FCC Week 2024, San Francisco, CA, USA, June 11, 2024.
S. Posen et al., “Advances in Nb3Sn superconducting radiofrequency cavities towards first practical accelerator applications”, Supercond. Sci. Technol. 34 025007 (2021).
A lepton collider with CoM collision energies between 90 and 350 GeV
High beam current → strong HOM damping
800 MHz 6-cell
Q0=3×1010 at Eacc=20 MV/m, 2 K
400 MHz 2-cell
Q0=2.7×109 at Eacc=10.6 MV/m, 4.5 K
Nb/Cu
650 MHz single-cell, Nb3Sn
Notes: CoM of 350 GeV to study ttbar (top quark and its antiparticle) production
800 MHz Nb: 30 W at 2 K, Nb3Sn: 50 W at 4 K

## Slide 10: DISCOVERY MACHINES: MUON COLLIDER
https://www.muoncollider.us/posts/accelerator/#super-conducting-rf
V. Chouhan et al., “"Excellent performance of 650 MHz single-cell niobium cavity after electropolishing", Proc. LINAC2024, Chicago, IL, USA, Aug. 2024, p. 692.
Possible range of RF frequency: 325 MHz, 650 MHz/800 MHz, 1300 MHz
“PIP-II like”
Challenges:
Achieving 20 MV/m at 4 K in 325 MHz cavities (Nb/Cu)
Achieving 38 MV/m at 2 K in 650 MHz Nb cavities
53.3 MV/m in 650 MHz single-cell!
Notes: SRF cavities will be used in the muon acceleration chain from the SRF linac (0.255 – 1.25 GeV) through dog-bone RLAs (1.25 – 63 GeV) to RCSs (up to the final energy). Along this chain of accelerators, the RF frequency would change from 325 MHz to 1300 Hz and accelerating gradients from 20 MV/m to 38 MV/m.
Synergies with FCC-ee

## Slide 11: ACCELERATOR DRIVEN SYSTEMS (ADS)
~1 GeV, ~25 mA, CW proton linac
162.5 MHz
325 MHz
650 MHz
Cost
Reliability
B. Mustapha et al., “A compact Linac design for an accelerator driven system”, Proc. LINAC2014, Geneva, Switzerland, Aug. 31-Sept. 5, 2014, p. 52.
SRF cavities operating at Bp ~ 70 mT
Cryoplant with cooling power of ~2.4 kW at 2.1 K
Nb3Sn cavities: ~2.4 kW at 4 K
Reduce power consumption by a factor ~3.5
Reduce capital cost by a factor ~3
Notes: JAEA-ADS, China ADS
x Optimized superconducting cavity design for high voltage and low cryogenic losses.
x Superconducting solenoid focusing inside cryomodules to minimize warm transitions and consequently the number of required cryomodules.
x Cold BPMs attached to SC cavities inside the cryomodule to reduce the number of diagnostics required between cryomodules
x Horizontal and vertical steering correctors are built into the solenoids requiring no additional space for correctors along the beam-line.

## Slide 12: ENERGY RECOVERY LINACS (ERL)
T. Konomi et al., “Damped superconducting structure for EUV light source based on energy recovery linac”, Phys. Rev. Accel. Beams 26, 121601 (2023).
ERL-based Free Electron Laser for EUV lithography
800 MeV, 9.75 mA SRF Linac:
64× 9-cell, 1.3 GHz cavities
Eacc=12.5 MV/m, Q0=1×1010 → ~1000 W at 2 K
10 kW @ 13.5 nm
Nb3Sn cavities: ~1000 W at 4 K
Reduce power consumption by a factor ~3.5
Reduce capital cost by a factor ~3

## Slide 13: INVERSE COMPTON SCATTERING (ICS) SOURCES
K. E. Deitrick et al.,, “High-brilliance, high-flux compact inverse Compton light source”, Phys. Rev. Accel. Beams 21, 080703 (2018).
High x-rays flux:
Low emittance
High repetition rate
Four 500 MHz double-spoke Nb cavities, Bp~50 mT, ~150 W at 4 K
x-rays
SRF Linac
25 MeV, 100 MHz rep. rate, 1 mA
Nb3Sn, Q0~2×1010 → ~10 W at 4 K
Notes: Directional and quasi-monochromatic laboratory scale X-ray source
X-ray energies in the range of 10 keV to 180 keV are of significant interest, as these energies are suitable for various applications including medical imaging and materials science.
10-35 keV:
This range is particularly useful for applications like K-edge subtraction (KES) and phase contrast imaging in medical imaging

## Slide 14: REDUCE HELIUM CONSUMPTION
A. Nordrum, “The era of cheap helium is over—and that’s already causing problems”, MIT Technology Review, February 25, 2024.
T. Koettig et al, “Semi-Dry Cavity Cooling of SRF Cavities at Temperatures above 4.5 K”, FCC Week 2025, Vienna, Austria, May 19-23, 2025.
T. Proslier et al., “3D additive fabrication of Cu cavity with cooling channeling at CEA”, TFSRF2024, Saclay, France, Sep. 16-20, 2024.
Helium price, per cubic meter
Notes: Prices listed are estimates for Grade-A helium sold by private industry.

## Slide 15: INDUSTRIAL SRF LINACS
C. Boulware et al., ” High-power Two-pass Superconducting Electron Linac for Medical Radioisotope Production”, SRF’23 Grand Rapids, MI, USA, June 25-30, 2023.
Niowave has built and is operating a 20 MeV SRF linac for the production of medical isotopes Ac-225 and Mo-99
2-pass, 10-40% duty cycle, up to 40 MeV
3-gap reentrant cell, 350 MHz cavity
  Bp = 58 mT, Pc = 29 W at 10 MeV
110 W at 4 K LHe refrigerator
Nb3Sn, Q0~2×1010 → ~4.5 W at 4 K
Notes: In use for more than 10 years.
Refrigerator: 100 kW wall-plug power

## Slide 16: INDUSTRIAL SRF LINACS
R.C. Dhuley et al., ”Design of a 10 MeV, 1000 kW average power electron-beam accelerator for wastewater treatment applications”, Phys. Rev. Accel. Beams 25, 041601 (2022).
Z. Yang et al., ” Stable acceleration of a LHe-Free Nb3Sn demo SRF e-linac”, Supercond. Sci. Technol. 38 015009 (2025).
Growing demand for compact & efficient high-power (>100 kW) CW electron linacs, <10 MeV:
Environmental remediation
Phytosanitary treatment
Medical device sterilization
Accelerated a pulsed beam to 1.9 MeV
Nb3Sn
&
Cryocoolers

## Slide 17: CONDUCTION COOLED SRF
G. Ciovati et al., ” Development of a prototype superconducting radio-frequency cavity for conduction-cooled accelerators”, Phys. Rev. Accel. Beams 26, 044701 (2023).
The highest Bp achieved so far in a conduction cooled Nb3Sn SRF cavity is 50 mT (Eacc~13 MV/m)
Cryooolers: 9 W at 4.2 K (fixed temperature) or 5 W at 4 K
Improve the reproducibility in the Nb3Sn coating process
Deal with the brittleness of the material
Deal with thermoelectric currents
Need to

## Slide 18: CONCLUSIONS
Cost will be an important parameter determining the fate of future large-scale discovery machines
High-Q and high gradient in low-frequency (650 – 800 MHz) cavities
High-Q with higher-Tc SC for 4 K operation
  Cryocoolers for industrial linacs
The performance we need will have to be demonstrated, reliably, by cavity vendors
The history of SRF R&D is full of surprises: keep experimenting!
QUESTIONS?
Notes: Structures for high-current operation