## Slide 1
Nb: State of the art performance (both for accelerators and quantum), challenges, and opportunities for material science
Materials for Bright Beams Workshop
Daniel Bafia, on behalf of APS-TD and SQMS Directorates
July 16, 2025
FERMILAB-SLIDES-25-0149-SQMS-TD

## Slide 2: Niobium for Particle Accelerators and Quantum Computers
Goals of presentation:
Showcase state-of-the-art Nb performance for accelerators and quantum
Highlight key material challenges and targeted research efforts
Explore complementary materials issues relevant for both fields
https://lcls.slac.stanford.edu/lcls-ii/ldesign-and-performance
Accelerators
(SQMS) Quantum Computers
M. Bal et al npj Quant Inf. 10, 43 (2025)
T. Kim et al arXiv:2506.03286
2-D
3-D
Bulk Nb
Nb film
https://www.hep.ucl.ac.uk/~jpc/all/ulthesis/node15.html
Increasing performance  materials issues

## Slide 3: Outline
Niobium for Accelerators
  Current state-of-the-art and challenges for improved performance
  Recent R&D to address challenges
Niobium for Quantum Computing
  Current state-of-the-art challenges for improved performance
  Recent R&D to address challenges
Open Questions and Opportunities for Complementary Materials Studies for Quantum and Accelerators
Conclusion

## Slide 4: State-of-the-Art Nb SRF Cavity Performance for Accelerators
Larger Q0/higher gradient  lower $$
RF field
State-of-the-Art FNAL Cavities Post Various Treatments
50 MV/m
6e10

## Slide 5: Exploring the Role of Impurities in Nb: Nitrogen
Why does dilute N enhance Q0?
SRF Cavity Studies
D. Bafia et al. PRAppl 23, 054052 (2025)
T. Kubo PRAppl 17, 014018 (2022)
New Theoretical Models
F. Herman and R. Hlubina PRB 104, 094519 (2021)
Studies highlight the importance of N in optimal inelastic scattering
Less NbH? Anti Q-slope?
N-Doped
EP
PCTS Studies on Cutouts
N-Doped
EP
N. Groll et al. arXiv:1805.06359
Nb SRF Cavity Conductivity Measurement

## Slide 6: Exploring the Role of Impurities in Nb: Oxygen
Why does baking enable performance tuning?
Cavity Performance Post Various in situ Baking
Mid-T Bake
75/120 C
120 C
TE1RI003 Post Sequential 120C Baking
Calculated O Depth Profile
T = 2K
f0 = 1.3 GHz
Diffusion Depth
D. Bafia et al. Proc. of SRF’21
Tracking Quench Field of 1.3 GHz Cavities with O Diffusion Depth
A. Romanenko et al. Proc. of SRF’19
ToF SIMS Studies on Cutouts
Baking drives the inward diffusion of O  reduces H!
D. Bafia et al. Proc. of SRF’21
Able to tune performance by diffusing O via baking
  Due to reduction of NbH
Do O and N perform the same function in Nb? Which is better?
See H. Hu’s talk Tomorrow at 8 AM

## Slide 7: O Impurity Tailoring + Optimized Electropolishing: the Key to Unlocking Record-Breaking Performance
Optimized EP + 120C baking on HB 650 MHz
Cathode-N
+50 MV/m!
+50 MV/m!
V. Chouhan et al., NIMPRA 1051, 168234 (2023)
Cold EP + 75/120C Baking on 1.3 GHz Cavity
Require optimized EP parameters/design to reduce H uptake and surface roughness
Materials problem: Which is more important? What other parameters influence?
75/120 C

## Slide 8: Understanding Flux Pinning and Vortex Driven Dissipation
Flux may be trapped at strong pinning centers
Mat. problem: What are these pinning centers?
Grain boundaries? NbH? Dislocations?
A. Romanenko et al JAP 115, 184903 (2014)
Using poorly expelling low RRR cavities to further study
S. Posen et al. JAP 119. 213903 (2016)
K. Howard et al. APS GPS 2025
Courtesy of S. Posen
Characterizing vortex dissipation (Sensitivity)
See K. Howard’s poster Thurs. evening
M. Martinello et al. 109, 062601 (2016)
M. Checchin et al. APL 112, 072601 (2018)

## Slide 9: Beyond Bulk Niobium: Improving Nb Film Performance
Nb film on copper cavities exhibit “medium-field Q-slope”  why?
B. Abdisatarov et al SUST 38, 075006 (2025)
DC HiPIMS Deposition System @ CERN
Performance of Nb Film on Nb Cavity Post Subsequent Annealing
Materials Studies on Nb Film on Nb Samples Post Baking
ToF-SIMS studies reveal reduction in H upon annealing
 Less NbH
EBSD reveals reduction in LMAD upon annealing
 Heals defects
Subsequent annealing reduces MFQS!

## Slide 10: Outline
Niobium for Accelerators
  Current state-of-the-art and challenges for improved performance
  Recent R&D to address challenges
Niobium for Quantum Computing
  Current state-of-the-art challenges for improved performance
  Recent R&D to address challenges
Open Questions and Opportunities for Complementary Materials Studies for Quantum and Accelerators
Conclusion

## Slide 11: Superconducting Quantum Technology and the Necessity for Materials Science
SQMS Quantum Architectures
M. Bal et al npj Quantum Information 10, 43 (2024)
T. Kim et al arXiv:2506.03286
2-D
3-D
Longer T1  better quantum computer

## Slide 12: State-of-the-Art T1 for Superconducting Quantum Architectures
Question: What T1 do we need to make a quantum computer?
Answer: TBD, but T1 >> 1 ms
Architecture | “OK” T1 [ms] | "Good” T1 [ms] | State-of-the-Art T1 [ms] | 
2-D | > 0.05 | 0.1 – 0.3 | 1.681 | 
3-D | > 0.05 | 0.3 - 1 | 1 mode2 25.6 | 2 modes3 20.6,15.6
[1] M. Bland et al. arXiv:2503.14798, [2] O. Milul et al. PRX Quantum 4, 030336 (2023), [3] T. Kim et al arXiv:2506.03286
T1 Performance Benchmarks by Architecture
How can we push these values further?

## Slide 13: Exploring the Role of Defects in Niobium Films
Do defects in Nb (impurities, grains boundaries, etc.) presently limit our T1?
DC HiPIMS Deposition System @ CERN
B. Abdisatarov et al. APL 125, 124002 (2024)
Parameter | Nb Film | Bulk Nb
RRR | 20 | 300
Grain Size [μm] | ~0.5 | 50
Impurity conc. | high | Moderately high
Oxide Thickness [nm] | 3.2 | 5.0
Comparing Material Properties of Nb Film Cavity vs Bulk Nb Cavity
Comparing RF Performance of Nb Film Cavity vs Bulk Nb at mK
Different Nb material yields nearly identical performance!
No

## Slide 14: Identifying O-Vacancies in Nb2O5 as a Major Source of TLS
How to minimize O vac in Nb2O5?
More crystalline oxides?
Encapsulation
in situ 200℃/1h
in situ 200℃/5h
in situ 200℃/5h
in situ 340℃/5h
Missing O- Counts in Nb2O5 Post Baking in ToF-SIMS
TLS-Driven RF Loss of Nb Cavity Post Baking
Correlating TLS Loss and Missing O- Counts
M. Bal et al npj Quantum Information 10, 43 (2024)
Y. Kalboussi et al. PRApplied 23, 044023 (2025)
O vacancies in Nb2O5 drive TLS
D. Bafia et al. PRApplied 22, 024035 (2024)

## Slide 15: Using Findings to Enhance T1: Encapsulation
Capped Nb qubits with various materials to prevent Nb2O5 formation
Resulted in dramatic improvement in T1
  25 μs  600 μs
Outstanding ?’s
  Optimal capping?
  Minimization of other losses?
T1 of 2-D Transmon Qubits with Various Encapsulation Schemes
Demonstration of Very Long T1
M. Bal et al npj Quantum Information 10, 43 (2024)

## Slide 16: Other Potentially Limiting Mechanisms: Niobium Hydrides
NbH found on niobium thin films in qubits
Some studies show that increased H content increases RF loss
Outstanding ?’s: How lossy are NbH? How do we reduce NbH?
J. Lee et al. arXiv:2108.10385
C. G. Torres-Castanedo et al Adv. Funct. Mater 34, 2401365 (2024)
May explain “aging” in qubits?

## Slide 17: Quantifying the Role of Magnetic Field in Quantum Devices
3-D Cavities
2-D Qubits
Outstanding ?’s: how/where are vortices trapped in qubits? What about other materials like aluminum?
D. Bafia et al. arXiv:2503.14616, under review at APL
B. Abdisatarov et al. arXiv:2506.02187
Does trapped flux significantly impact T1?
Sensitivity vs Temperature
T1 Post Cooling in Various Btrap
S = 2 nΩ/mG @ 10 mK, decreases with temperature  Well modeled by theory
T1 significantly impacted post trapping large Btrap; also decreases stdev
Depends

## Slide 18: Outline
Niobium for Accelerators
  Current state-of-the-art and challenges for improved performance
  Recent R&D to address challenges
Niobium for Quantum Computing
  Current state-of-the-art challenges for improved performance
  Recent R&D to address challenges
Open Questions and Opportunities for Complementary Materials Studies for Quantum and Accelerators
Conclusion

## Slide 19: Comparing Loss Mechanisms for Accelerators and Quantum
Loss Mechanism | Nb for Accelerators | Nb for Quantum Computing
Trapped Magnetic Flux |  | 
Vortex Dissipation |  | 
Surface Oxide (Nb₂O₅) TLS |  | 
Hydrogen Contamination |  | 
Dislocations / Cold Work |  | 
Grain Boundaries |  | 
Non-uniform Impurity Doping |  | ?
Dielectric Loss (substrate) | N/A | 
Two-Level Systems (TLS) |  | 
Chemical Etching |  | 
M. Bal et al npj Quantum Information 10, 43 (2025)
2-D
3-D
Accelerators
Quantum Architectures
T. Kim et al arXiv:2506.03286
Complementary Materials Problems

## Slide 20: Research Needs to Address Complementary Materials Issues and Talks @ This Workshop Which Might Help With These Issues
New growth techniques
  Electro-deposition, zone refining, additive manufacturing—any potential for better control over impurities?
Characterization needs
  Nanoscale mapping of oxides, dislocation networks, impurity segregation.
    Vivek Anil (ARPES and low energy photoemission), Matthew Gordon: (photocathodes for Quantum Micro), Eric Lechner (Correlation between surface defects and RF performance using STM)
  Cross-section TEM, atom probe tomography, synchrotron techniques.
    Zhaslan Baraissov (Surface characterization of SRF surfaces)
  Studying Vortices in Nb films and bulk
    Steven Anlage (Investigation of local microwaves properties and pinned vortex response in SRF materials), Aiden Harbick (Impact of surface structure and vortex entry on RF dissipation)
Interface engineering
  Passivation strategies to reduce TLS (e.g., ALD, HF dip + vacuum venting)
Impurity management
  Controlled interstitial doping (e.g., N, O, C) to tailor mean free path.
    Hannah Hu (Nb Treatments)
Theory
  Cristobal Mendez (How can DFT guide SRF materials development), Alexander Gurevich gap in understanding of RF dissipation

## Slide 21: Conclusion:
State-of-the-art performance achieved in both SRF accelerators and quantum devices using Nb
  Key limitations remain: hydrogen, oxide defects, vortices, dielectrics losses, grain boundaries, etc
Materials-driven strategies (optimized EP, impurity tailoring, encapsulation) have realized performance gains
Unifying theme: Progress hinges on atomic-scale control and advanced characterization techniques
Rich opportunities for opportunities for complementarity and synergistic collaborations between accelerator and quantum communities

## Slide 22
This work was produced by FermiForward Discovery Group, LLC under Contract No. 89243024CSC000002 with the U.S. Department of Energy, Office of Science, Office of High Energy Physics.This material is based upon work supported by the U.S. Department of Energy, Office of Science, National Quantum Information Science Research Centers, Superconducting Quantum Materials and Systems Center (SQMS) under contract number DE-AC02-07CH11359.
THANK YOU