## Slide 1: Nb3Sn: State-of-the-art performance, challenges and opportunities for materials science
Grigory Eremeev
Materials for Bright Beams Workshop 2025
July 16, 2025
FERMILAB-SLIDES-25-0158-TD

## Slide 2: State-of-the-art performance
01

## Slide 3: Nb3Sn Cavities: Higher superheating field
  Hc ~ 540 mT  Hsh ~ 0.84·Hc = 450 mT 
  Eacc ~ Hpk/4  Eacc ~ 100 MV/m
Nb cavities reach high accelerating gradients
Many limiting mechanisms in Nb SRF cavities have been understood and mitigated
State-of-the-art Nb cavities are reaching very close to the superheating field Hsh of niobium
Nb3Sn, an s-wave superconductor with large energy gap and twice as high Hsh as niobium, offers the potential for even high accelerating gradients
Material | Nb | Nb3Sn
Tc [K] | 9.25 | 18.3
ρn [μΩcm] | 0.1 | ~ 5
Hsh(0) [T] | 0.24 | ~ 0.45
Δ [meV] | 1.45 | ~ 3.1
QBCS @ 2K | ~ 5·1010 | ~ 5·1014
QBCS @ 4K | ~ 5·108 | ~ 5·1010
Eacc [MV/m] | ~ 50 | ~ 100

## Slide 4: Nb3Sn Cavities: High Q0 at higher temperature
  Δ ~ 3.1 meV  Rs ≥ 5 nΩ @ 4.3K @ ~ 1 GHz
Nb3Sn has larger energy gap than niobium and (relatively) low normal conducting resistivity
Higher Q0 at higher temperatures
  Q0 > 1010 at 4 K
  Can use cryocoolers instead of liquefier cryoplant
Reduce the capital and operating cost for high duty factor small and medium-size accelerators

## Slide 5: Short overview of past work
“Wuppertal”
configuration
Nb3Sn was discovered in 1953 by B. Matthias et al.
Material development in 70-80s by Siemens AG, Karlsruhe, Cornell University, University of Wuppertal and CERN
Development at Wuppertal led to high Q and Eacc ~ 15 MV/m, limited by strong Q-slope
G. Müller, P. Kneisel, D. Mansen, H.Piel, J. Pouryamout, R. W. Röth, EPAC’96
Q vs E without strong Q-slope at Cornell in 2013
S. Posen et al., SRF’13

## Slide 6: Nb3Sn development world-wide
2009
2012
2018 - 2023
2015

## Slide 7: State-of-the-art R&D cavities
N. Stilin, Ph.D. dissertation, 2024; J.Hao et al., TTC’25; Z.Yang et al, TTC’23
The highest accelerating gradient is above Eacc = 20 MV/m
The cavity was coated and measured at Fermilab
The record performance is attributed to thinner “shiny” coating
Coatings world-wide reached practical accelerating gradients above Eacc = 10 MV/m

## Slide 8: Best accelerator cavities
Posen et al., Supercond. Sci. Technol. 34 (2021) 025007
Eremeev et al., SRF’23 & LINAC’24
Multicell accelerator cavities reach Eacc above 10 MV/m
Several projects are underway to integrate cavities into operational cryomodules
CEBAF cryomodule with two Nb3Sn-coated cavities has been recently measured with total voltage gain > 10 MV

## Slide 9: Best accelerator cavities
QWR cavities were coated within ANL-FNAL collaboration
T. Petersen et al., HIAT’25
Nb3Sn films offer advantages at lower frequencies at 4 K compared to Nb
The best 145 MHz QWR cavity reached unprecedented Bpk = 108 mT
Such Bpk corresponds to Eacc > 25 MV/m in elliptical SRF cavity

## Slide 10: Challenges and Opportunities (or how did we get here and how do we move beyond)
02

## Slide 11: What causes Q-slope?
SIMS to identify Titanium contamination (myself) -> Ti covers.
Message: data prompted everyone to use covers to protect for Ti.
Also talk about Sn in GB and about more impurities in Nb3Sn
May be split into two slides: talk about Ti and covers, then in the next slide about Sn rich and Sn deficient GB
Cornell’s cavity did not have Q-slope, while Wuppertal’s and, later, Jlab’s did…why?
Eremeev, SRF’15
Titanium from NbTi flanges was one of the differences noted in the coating between Cornell and Jlab coated samples
The finding prompted coating facilities to use Nb cover to restrict uptake of Ti during Nb3Sn coating

## Slide 12: Titanium in Nb3Sn
SIMS to identify Titanium contamination (myself) -> Ti covers.
Message: data prompted everyone to use covers to protect for Ti.
Also talk about Sn in GB and about more impurities in Nb3Sn
May be split into two slides: talk about Ti and covers, then in the next slide about Sn rich and Sn deficient GB
All coatings of cavities with NbTi flanges use Nb covers
Several other approaches to protect the coatings (and the furnace) from titanium contamination are explored
Ti uptake is studied and needs to be quantified to link it to Q0 field dependence
See N. Tagdulang’s poster

## Slide 13: Sn flux and Nb3Sn nucleation
Becker et al., Appl. Phys. Lett. 106, 082602 (2015)
L. Shpani et al., SRF’23
Sn flux early in the coating process strongly impacts Nb3Sn coating
Sn deficiency early in the coating is linked to patchy regions, voids, and Sn-deficient regions
Niobium anodization before the coating has been the approach to improve Sn seeding

## Slide 14: Source temperature spike to promote nucleation
PlaceholdL. Shpani et al., SRF’23
S Posen et al 2021 Supercond. Sci. Technol. 34 025007
In addition to anodization, Sn nucleation has been improved by increasing the temperature of Sn source during the nucleation stage
Alternative approaches such as Sn electroplating improves Sn distribution over the surface and may be more suitable for hard-to-reach areas

## Slide 15: GB driven growth of Nb3Sn
U. Pudasaini, J. Vac. Sci. Technol. A 37, 051509 (2019)
Carlson J et al 2021 cavities Phys. Rev. B 103 024516
Nb3Sn film grows in columnar grains driven by Sn diffusion through the grain boundaries
Nb3Sn grain orientation is uncorrelated to underlying Nb, which explains excellent results achieved with both fine-grain and large-grain niobium
Sn diffusion via grain boundaries leads to the potential of Sn enrichment at the grain boundaries
Sn-rich GB will lead to Tc reduction and early vortex nucleation

## Slide 16: Roughness of Nb3Sn
R. Porter et al, SRF’19
Eric M Lechner et al 2025 Supercond. Sci. Technol. 38 01LT01
Surface roughness of Nb3Sn films has been linked to performance degradation due to field enhancement
The highest Eacc has been achieved with thin Nb3Sn coating that had lower surface roughness

## Slide 17: Mechanical polishing to reduce roughness
E. Viklund et al 2024 Supercond. Sci. Technol. 37 025009
Centrifugal barrel polishing is an effective way to reduce surface roughness of Nb3Sn films
Polished Nb3Sn films have surface roughness better than that of electropolished niobium
The light re-coating process is used to heal film damage and close cracks in the film
The light re-coating process has been shown to be effective to improve degraded cavities

## Slide 18: Material science enables applications
Material science studies improved the understanding of Nb3Sn film growth and their RF properties
Several improvement in deposition process were developed based on the insights from material science
Understanding the composition coupled with improved theoretical understanding will lead to further improvement in material properties

## Slide 19: Conclusion
Bpk above 100 mT have been achieved
Further understanding via careful designs of experiment and use of analytical tools is the key to realizing Nb3Sn high field potential
Nb3Sn cavities at several coating facilities world-wide demonstrate performance suitable for accelerator applications