## Slide 1: How can DFT guide SRF materials development? Materials for Bright Beams Workshop 2025 Speaker: Cristóbal Méndez, Cornell University

## Slide 2: Outline
Why DFT in SRF?
Introduction to Density Functional Theory
Applications of DFT in SRF
Van Do
University of Chicago
Sadie Seddon-Stettler
Cornell University
Nathan Sitaraman
Cornell University
Michael Van Duinen
University of Chicago

## Slide 3: Research loop for better SRF materials
- Formation energies of dopants, vacancies, etc
- Surface energies
- Grain boundaries
- Superconducting parameters
Experiments
DFT Calculations
Flexible, Accurate
No experimental input needed!
Screening of materials,
Predictions
Results
- Minimize losses
- Reduce required cooling
- Etc

## Slide 4: Brief introduction to DFT
What it is: Solves Kohn–Sham equations for ground-state electron density ρ(r) → total energy E[ρ]
In a periodic crystal potential, we only need to solve for one small cell (unit cell) to recover the full, infinite crystal’s band structure. (Bloch theorem)
What we obtain:
Band structure & density of states (DOS)
Phonon spectrum
Surface/defect energies, diffusion barriers
Electron densities
Initial guess:
Solve Kohn-Sham equations
Calculate
Self-consistent?
Calculate Energy, Forces, etc

## Slide 5: Case Study #1: Superconductivity
BCS theory and Cooper pairs
Electrons can attract each other if mediated by a phonon
The stronger the electron-phonon interaction, the stronger the effect

## Slide 6: Case Study #1: Superconductivity
Modeling phonons is relatively easy using DFT
Calculate ‘spring constants’ between atoms in the lattice
Use force matrix to calculate phonon dispersion
Zarea, M., Ueki, H., & Sauls, J. A. (2023). Effects of anisotropy and disorder on the superconducting properties of niobium. Frontiers in Physics, 11, 1269872.
Supercell

## Slide 7: Case Study #1: Superconductivity
Sitaraman, N. S., Sun, Z., Francis, B., Hire, A. C., Oseroff, T., Baraissov, Z., ... & Transtrum, M. K. (2022). Theory of nb-zr alloy superconductivity and first experimental demonstration for superconducting radio-frequency cavity applications. arXiv preprint arXiv:2208.10678.
El-ph coupling constant
Log-avg phonon frequency
McMillan formula
Eliashberg spectral function
BCS formula

## Slide 8: Case Study #2: Layered structures
Motivation:
Nb reacts with oxygen and forms native oxides
Lowers the quality factor of Nb cavities
Our approach at CBB: using metallic capping layers to prevent oxide formation
Challenge: To find the best capping material (as inert as possible)
?
Figure by Van Do (University of Chicago)
Before: 😔
After: 😁

## Slide 9: Case Study #2: Layered structures
Estimate oxygen affinity with interstitial energy
Interstitial Formation Energy:
Quantifies how likely is that a contaminant (O, N, H) will form in the bulk of different materials
O N H

## Slide 10: Case Study #2: Layered structures
Question: Are these materials going to form a stable layer?
Surface Energy:
Useful to predict stability of different surface orientations
Interface Energy:
Quantifies interface stability of two materials
First to suggest alloys for protective layers in SRF!
Nb
Metal
New surface
New interface

## Slide 11: Case Study #2: Layered structures
Capping layers in practice: Using Au
(3x1)-O/Nb(100)
1 ML Au
STM images from Van Do, University of Chicago
Au island formation
Chang, R. D., Shumiya, N., McLellan, R. A., Zhang, Y., Bland, M. P., Bahrami, F., ... & De Leon, N. P. (2025). Eliminating surface oxides of superconducting circuits with noble metal encapsulation. Physical review letters, 134(9), 097001.
Au
AuPd

## Slide 12: Case Study #2: Layered structures
Nb
Au
Oxygen
Thick layer of Au
Bad for superconductivity 😔
Nb
Thin layer of Au
Thin layer of adhesive metal
Better superconductivity😁
Nb

## Slide 13: Case Study #2: Layered structures
Nb
Metal
Metal/Au interface
Metal/Nb interface
Au
Poster: Oxide mitigation with protective layers on Nb (today)

## Slide 14: Case Study #3: Helium Atom Scattering
Motivation:
Surface superconductivity is critical for SRF
Electron-phonon coupling constant can be inferred from Helium Atom Scattering (HAS) measurements
Attenuation of specular peak (elastic scattering), known as the Debye-Waller (DW) factor
Figures from Sibener group

## Slide 15: Case Study #3: Helium Atom Scattering
DFT beyond energies and forces: electron density
We calculated the scattering surface and its thermal vibrations
Used that to calculate DW factor fully ab-initio (for the first time)!
Now can understand how different surface phonons contribute to surface superconductivity
(3x1)-O/Nb(100) surface: Highly corrugated
Nb(100) surface: Low corrugation

## Slide 16: Summary
Great potential for DFT in the exploration of new materials in SRF
Direct calculation of superconducting to discover new alloys (Nb-Zr)
Prediction of protective capping layers (Au/Nb, AuPt/Nb, AuPd/Nb) and interface layers (Cu, Fe)
Link HAS and surface superconductivity to individual phonons
Open for collaboration!
  cam559@cornell.edu