## Slide 1: Correlations Between RF Performance and Surface Defects via STM
7/17/25
Eric M. Lechner
Work presented is based on: Lechner, Eric M., et al. "Characterization of dissipative regions of a N-doped superconducting radio-frequency cavity." Frontiers in Electronic Materials 3 (2023): 1235918.
https://doi.org/10.3389/femat.2023.1235918

## Slide 2: Outline
RF Performance and Temperature Mapping of a N-doped Cavity
Scanning Tunneling Microscopy (STM)
STM Results
  Tunneling Spectroscopy
  Vortex Imaging
  Local estimates of surface resistance

## Slide 3: RF Performance of an N-doped Cavity
Implied an exponential form of Rs: Decrease in Rs(Bp) is primarily due to the pre-exponential factor. Consistent with previous results [1].
Cool-down dependent surface resistance points to vortex losses.
No noticeable non-linearity in Ri due to vortex contribution in this range.
Test 1 – 1.5K/min
Test 2 – 5K/min
Test 1
800 ºC/30 min N doping in 25 mTorr of N2 followed by 800 ºC/30 min vacuum heat treatment +10 µm EP
[1] Ciovati, Gianluigi, Pashupati Dhakal, and A. Gurevich. Applied Physics Letters 104.9 (2014).

## Slide 4: Temperature Mapping
Test 2 – 5K/min
Test 1 – 1.5K/min
Unfolded temperature maps show decrease in power dissipated with enhanced temperature gradient.
Eight samples were cut via CNC milling for further investigation (STM, XPS, SEM)
Empty symbols show the increase in power dissipated after quench.
Location A was the quench location

## Slide 5: Scanning Tunneling Microscopy
Electron Tunneling
Ns is a key ingredient determining Rs
[1] Gurevich, Alex. Superconductor Science and Technology 30.3 (2017): 034004.
[1]
e-
eV
Energy
Density of states
Probes directly the density of states
Local probe
The Nb oxide is too thick for vacuum tunneling. To remove this, the surface has been Ar ion milled.

## Slide 6: Scanning Tunneling Spectroscopy – Grid Spectroscopy
Similar but hotspots have a a low-delta tail
Hot spots have a wider distribution of Dynes broadening parameter.
Wider distribution of effective normal layer thickness
Larger distribution of the contact resistance between S and N layer – away from optimal value.
Model used:
A. Gurevich, T. Kubo PRB 96, 184515 (2017)
[1] Gurevich, Alex, and Takayuki Kubo. Physical Review B 96.18 (2017): 184515.

## Slide 7: Scanning Tunneling Spectroscopy – Line Spectroscopy
Observation of in-gap states
May indicate the presence of magnetic impurities possibly originating from Nb suboxides
Exists on all sample, but higher density of such defects in hot-spots
Line spectra across region with in-gap states found in grid spectroscopy
Sample G – hot spot

## Slide 8: Scanning Tunneling Spectroscopy - Vortex Imaging
Provides an estimate for and
Strong fluctuations of vortex core shape is observed. Likely due to the spatial variations of the impurity potential.
Hot spot G shows strong pinning, likely explaining the persistent excess RF dissipation
,

## Slide 9: Calculating Rs of the Proximity-Coupled System
- fitting parameter
Parameters used in calculation of Rs determined via RF measurement or STM
With STM and RF measurements a local surface resistance due to the proximity effect can be calculated.
Wider distribution of surface resistance observed in hot spots.
Compared with vortex losses, the hot spot proximity-coupled losses are small.
Yet a correlation between hot spots and degraded SC properties exist. Are these locations where flux first nucleates? Maybe the tail of low- values indicates the presence of nanohydrides
RBCS
Rs

## Slide 10: Summary
Scanning tunneling microscopy is a powerful tool for studying spatial variations of key quantities that govern surface resistance.
We have quantified the effects of a thin normal metal on top of a superconductor and computed the surface resistance in the low-field thin proximity coupled normal layer limit.
The effect of the degraded superconducting and proximity coupled parameters account for a small contribution to the hot spot intensity, yet a correlation between hot spots and these degraded properties exists. This may point towards these defects assisting in nucleating vortices.

## Slide 11: Acknowledgments
Basu Dev Oli
Junki Makita
Gigi Ciovati
Alex Gurevich
Maria Iavarone

## Slide 12: QUESTIONS?