## Slide 1: Nb3Sn Growth Methods & Material Characterization
July 17, 2025
Uttar Pudasaini

## Slide 2: Outline
Nb3Sn for Accelerator Cavities
Overview of Growth Methods
Importance of Material Characterization
Characterization Insight into Vapor-diffused Nb3Sn
Summary

## Slide 3: Nb3Sn for SRF Accelerator Cavity Applications
Potential for 4 K operation performance like Nb cavities @ 2 K simplify cryogenic systems
Transformational technology enable new application of SRF accelerators & reduces costs
Brittleness & low thermal conductivity use in thin-film form only
 | Nb | Nb3Sn
Tc (K) | 9.25 | 18.3
Hsh (mT) | 220 | 425
QBCS at 2 K | 5×1010 | 5×1014
QBCS at 4 K | 5×108 | 5×1010
Eacc (MV/m) | 50 | 100
*Approximate values

## Slide 4: Growth Challenge
Adequate phase and composition required
Thickness enough to screen RF currents from material below the Nb3Sn layer
Uniform material growth on the entire cavity structure
Godeke A 2006 A review of the properties of Nb3Sn and their variation with A15 composition, morphology and strain state Supercond. Sci. Technol. 19 R68–80
J. P. Charlesworth, I. Macphail and P. E. Madsen, "Experimental work on the Nb-tin constitution diagram and related studies," J. Mater. Sci., vol. 5, (7), pp. 580-603, 1970.

## Slide 5: Nb3Sn Growth Methods in Progress
High-temperature Nb-Sn Diffusion-based Methods for Nb3Sn/Nb
  Sn Vapor diffusion (Cornell U., JLab, Fermilab, KEK, IMP, Peking U., SARI)
Temperature (
R&D 1.3 single-cell cavity performance
Since the 1970s
Create Sn-vapor and transfer to the interior surface of Nb cavity
So far ‘THE’ technique to produce practical Nb3Sn cavities
“Wuppertal” or “Siemens” configuration
U.Pudasaini et al. “Managing Sn-Supply to Tune Surface Characteristics of Vapor-Diffusion Coating of Nb3Sn”, SRF'21, East Lansing, MI, USA, Jun.-Jul. 2021,
S. Posen et al. “Advances in Nb3Sn superconducting radiofrequency cavities towards first practical accelerator applications” Superconductor Science and Technology. 2021 Jan 11;34(2):025007.
D. Hall, “New Insights into the Limitations on the Efficiency and Achievable Gradients in Nb3Sn SRF Cavities”, PhD thesis, Cornell University (2017).
G. Jiang et al.. Understanding and optimization of the coating process of the radio-frequency Nb3Sn thin film superconducting cavities using tin vapor diffusion method. Applied Surface Science. 2024 Jan 15;643:158708.
>1010 @ >20 MV/m at 4 K
w/ Secondary heater for Sn source

## Slide 6: Nb3Sn Growth Methods in Progress
High-temperature Nb-Sn Diffusion-based Methods for Nb3Sn/Nb
  Sn Vapor diffusion (Cornell U., JLab, Fermilab, KEK, IMP, Peking U., SARI)
  Sn-electroplating on Nb followed by thermal diffusion (Cornell U.)
Z. Sun, Zeming, et al. "Smooth, homogeneous, high-purity Nb3Sn superconducting RF resonant cavity by seed-free electrochemical synthesis." Superconductor Science and Technology 36.11 (2023): 115003.
Deposit Sn on Nb
Converts into Nb3Sn on Nb
Significantly smoother surfaces compared to vapor diffusion and lower BCS resistance
Performance comparable to vapor-diffused Nb3Sn
Q>1010 @ 12 MV/m @ 4.2 K

## Slide 7: Nb3Sn Growth Methods in Progress
High-temperature Nb-Sn Diffusion-based Methods for Nb3Sn/Nb
  Sn Vapor diffusion (Cornell U., JLab, Fermilab, KEK, IMP, Peking U., SARI)
  Sn-electroplating on Nb followed by thermal diffusion (Cornell U.)
  Liquid Sn dipping (INFN) for Nb3Sn targets for Nb3Sn/Cu cavity
C. Pira et al., “Progress in European Thin Film Activities”, in Proc. 21th Int. Conf. RF Supercond. (SRF'23), Grand Rapids, MI, USA, Jun. 2023, pp. 607-614. doi:10.18429/JACoW-SRF2023-WECAA01

## Slide 8: Nb3Sn Growth Methods in Progress
Magnetron Sputtering for Nb3Sn/Cu
  DC magnetron sputtering (ODU*, JLab, CERN, INFN, STFC, Cornell U., Peking U.)
  High Power Impulse Magnetron Sputtering - HiPIMS (CERN, JLab, STFC)
Sputter Nb-Sn on Cu – low temperature suitable for Cu
Tc still lower than the theoretical value
Moving towards cavity coatings
*for 2.6 GHz Nb cavity
C. Pira et al., “Progress in European Thin Film Activities”, in Proc. 21th Int. Conf. RF Supercond. (SRF'23), Grand Rapids, MI, USA, Jun. 2023, pp. 607-614. doi:10.18429/JACoW-SRF2023-WECAA01

## Slide 9: Nb3Sn Growth Methods in Progress
Others for Nb3Sn/Cu
  Chemical vapor deposition (Ultramet, Cornell U.)
  Nb-Bronze diffusion-based method (IMP, HZB, e2P, MagLab at FSU, and Peking U.)
9
Reaction between Nb and Cu-Sn solid solution
Avoid high temperatures ~700°C works for Nb3Sn/Cu
Follows ternary Cu-Sn-Nb system Avoid the Nb6 Sn5 and NbSn2
Withanage, W.K., Juliao, A. and Cooley, L.D., 2021. Rapid Nb3Sn film growth by sputtering Nb on hot bronze. Superconductor Science and Technology, 34(6), p.06LT01.
Ming Lu et. al. The 11th Workshop on TFSRF2024, France
Electrodeposition

## Slide 10: Need for Material Characterization
Assess the material quality
Provide feedback on the coating process
Correlate with RF performance
Identify defects
Guide to understand and optimize the growth methods
Structure
Composition
Morphology
Layer thickness
Uniformity

## Slide 11
Vapor Diffusion – The Current Mainstream Technique
Average grain size: 1-2 microns
Composition: 24 -25 at.% Sn.
Micro-roughness
Columnar grains extending to Nb3Sn-Nb interface.
Coating thickness: 1-2 µm
Temperature (
U. Pudasaini, G.V. Eremeev, M.J. Kelley, C.E. Reece, and J. Tuggle, “Investigation of Structural Development of Nb3Sn on Nb in the Two Step Diffusion Coating”, North American Particle Accelerator Conf. (NAPAC'16), Chicago, IL, USA, Sep. 2016, paper MOPLR023.
2 µm
EBSD

## Slide 12: “Patchy” Region
U. Pudasaini, G.V. Eremeev, M.J. Kelley, C.E. Reece, and J. Tuggle, “Surface Studies of Nb3Sn Coated Samples Prepared under Different Coating Conditions”, in Proc. 18th International Conference on RF Superconductivity, Lanzhau, China, July 2017, paper TUPB069.
~ 250 nm
~ 1.75 µm
Could be very thin Potentially affects RF performance
Only a few grain boundaries perimeter for Sn diffusion slow growth
Prone areas Out-of-sight regions not directly exposed to Sn/SnCl2 vapor
Solutions
  Pre-anodization
  Sufficient Sn-flux at the initial stage adjust Sn sources and temperatures
Low Sn flux → Epitaxial growth of Nb3 Sn on Nb
J. Lee, et al. "Atomic-scale analyses of Nb3Sn on Nb prepared by vapor diffusion for superconducting radiofrequency cavity applications: a correlative study." Superconductor Science and Technology 32.2 (2018): 024001.
Atomically-resolved HR-STEM image of the Nb3Sn/Nb interface

## Slide 13: Sn Residues
Cavity covered with Nb plates during the coating
Sn-vapor condensation at the end of the process
Specific challenge for us
Mitigation approaches
3
2
Points 2 and 3: High Sn
SEM image
Elemental Mapping of Sn by Auger spectroscopy
Scanning Auger Microscopy (SAM)
AFM

## Slide 14: Titanium Contamination from NbTi Flange
Cornell (No Q-slope)
JLab (Q-slope)
J. Tuggle et al, 2018. Secondary ion mass spectrometry for superconducting radiofrequency cavity materials. Journal of Vacuum Science & Technology B, Nanotechnology and Microelectronics: Materials, Processing, Measurement, and Phenomena, 36(5), p.052907.
U. Pudasaini et al. "Surface Studies of Nb3Sn Coated Samples Prepared under Different Coating Conditions." SRF 2017: THPB069.
At Wuppertal, the potential source of Ti could be Ti foils, used as getter material in the furnace.
M. Peiniger, PhD dissertation, Wuppertal University (1989)
Ti evaporation from NbTi flanges
Cause field dependence of Q0 degradation in Nb cavities.
Dhakal, P., et al. "Effect of high temperature heat treatments on the quality factor of a large-grain superconducting radio-frequency niobium cavity." Physical Review Special Topics-Accelerators and Beams 16.4 (2013): 042001.
Similar microstructure, composition, and topography.
Ti-free Hygiene adopted after the furnace upgrade in 2017 resulted in the first cavity without “Wuppertal slope”.
Risk of coating cavities with NbTi flanges?
SIMS depth profile from Nb samples with ceramic flange covers
SIMS Depth Profile
AFM

## Slide 15: RF Performance vs. Material Characteristics
Performance | “Good” | Annealed – “bad”
Average grain size (µm) | 0.96 ± 0.06 | 1.11 ± 0.08
Average roughness (nm), 50 µm scan | 73 ± 8 | 98 ± 5
Average thickness (µm) | 1.20 ± 0.12 | 1.75 ± 0.15
GB composition |  | Sn-deficient
No Sn-rich GBs but Sn-deficient regions close to the Nb3Sn-Nb interface
Sample with annealing features – Sn-deficient GBs
Exhausted Sn
Annealed
Q>1010 @ >17MV/m at 4 K
Q~109 @ 5 MV/m at 4 K
TEM Cross-Section with Elemental Mapping
TEM Cross-Section with Elemental Mapping

## Slide 16: Grain-boundary Segregation
Atom-probe Tomography
Line profile across GB

## Slide 17: Surface Topography
Grooved grain boundaries and substantial surface roughness.
Surface roughness poses threats to the stability of the Meissner state
Magnetic field enhancement and superheating field suppression
Improvement on process design and post-processing
5 µm
200 nm
5 µm
500 nm
5 μm
1 µm
Eric Lechner et al 2025 Supercond. Sci. Technol. 38 01LT01
AFM
TEM
SEM CS

## Slide 18: Coating onto 2.6 GHz Nb Cavity Using Cylindrical Sputter Coater
Frank Batten College of
Engineering & Technology
Old Dominion University
Equator region samples
Top beam region samples
Plasma interaction with the beam tube sample surface during deposition produces Nb3Sn grains without voids.
2 µm
600 0C – 3 h, 950 0C – 1 h
600 0C – 3 h , 950 0C – 1 h
Voids ~23% (area)
Slide courtesy: M.S. Shakel, ODU
Co-sputtering from Nb-Sn targets
More details in the poster today!

## Slide 19: Cu Diffusion in Sputtered-Nb3Sn
1 μm
2 μm.
E A Ilyina et al 2019 Supercond. Sci. Technol. 32 035002

## Slide 20: Summary
Multiple growth methods are under pursuit for Nb₃Sn-coated Nb and Cu cavities.
Material characterization is vital for process feedback and performance optimization.
Process improvements targeting identified defects have improved vapor-diffused Nb₃Sn performance.
Could further performance gains hinge on addressing yet-to-be-revealed “defects”—calling for deeper, targeted material characterization?

## Slide 21: Acknowledgements
A-M. Valente-Feliciano, E. Lechner, M. J. Kelley, O. Trofimova
G. Eremeev, S. Posen, M. Liepe
Work supported by the U.S. Department of Energy, Office of Science, Office of Nuclear Physics under contract DE-AC05-06OR23177.

## Slide 22: Thank you for your attention! Questions?