## Slide 1: A Surface Chemist’s Tools Applied to Study SRF Surfaces and Treatments
Michael Van Duinen, University of Chicago
Materials for Bright Beams Workshop July 17th, 2025
Van Do1, Aiden Harbick2, Michelle M. Kelley3, Helena Lew-Kiedrowska1, Cristobal Méndez3, Liana Shpani3, Caleb Thompson1, Sarah Willson1, Matthias Liepe3, Mark Transtrum2, Tomás Arias3, Steven J. Sibener1
1 = University of Chicago, 2 = Brigham Young University, 3 = Cornell University

## Slide 2: Niobium in SRF Cavities: Why? Why Not?
Superconducting Radio Frequency cavities accelerate particles in particle accelerators
  High-energy, AC field
  Superconductive materials prevent field losses
@FermiLab on GIPHY

## Slide 3: Niobium in SRF Cavities: Why? Why Not?
Superconducting Radio Frequency cavities accelerate particles in particle accelerators
  High-energy, AC field
  Superconductive materials prevent field losses
Niobium is state-of-the-art for SRF cavities
@FermiLab on GIPHY

## Slide 4: Niobium in SRF Cavities: Why? Why Not?
Superconducting Radio Frequency cavities accelerate particles in particle accelerators
  High-energy, AC field
  Superconductive materials prevent field losses
Niobium is state-of-the-art for SRF cavities
Nb has room for improvement
  Cryocooling is very costly at 2 K (helium boiling point ~ 4 K)
@FermiLab on GIPHY

## Slide 5: Niobium in SRF Cavities: Why? Why Not?
Superconducting Radio Frequency cavities accelerate particles in particle accelerators
  High-energy, AC field
  Superconductive materials prevent field losses
Niobium is state-of-the-art for SRF cavities
Nb has room for improvement
  Cryocooling is very costly at 2 K (helium boiling point ~ 4 K)
Current SRF cavity research is focused on developing new Nb-based materials at the Nb surface.
@FermiLab on GIPHY

## Slide 6: 2-Pronged Approach to Improving Nb Superconducting Performance
Issue 1: Oxide is deleterious to superconducting performance
  Niobium very readily oxidizes even in vacuum conditions
  Incredibly high temperatures to remove
Solution 1: Suppress the oxide
  Capping layers that don’t oxidize (i.e. Au)
  “Sacrificial” layers with strong oxidation potential (i.e. Zr)
Issue 2: Niobium is nearing its fundamental material limits
  Decades of research have pinned down excellent cleaning techniques
Solution 2: Develop material with stronger superconducting properties at surface
  Nb3Sn
  Nb with trace N (discussed at the end)
Notes: Needs slide before this
”higher performance”

## Slide 7: Fundamental Chemical Questions Underlying the Approaches to Achieving Higher Performance
Oxide
”Oxide” is a catch-all term for many oxygen-containing Nb phases
  Nb2O5 insulating
  NbO2 a semiconductor
  NbO mild superconductor with many surface phases
Nb3Sn
Chemical homogeneity
  Narrow range of acceptable Sn proportions, ~23-26% Sn
Structural homogeneity
  Generally shown that smoother surfaces allow for better superconducting performance
To what extent does the presence of NbO modify superconducting performance at the surface?
What specific chemical and structural surface features limit Nb3Sn performance, and how do they arise?

## Slide 8: Fundamental Chemical Questions Underlying the Approaches to Achieving Higher Performance
Oxide
”Oxide” is a catch-all term for many oxygen-containing Nb phases
  Nb2O5 insulating
  NbO2 a semiconductor
  NbO mild superconductor with many surface phases
Nb3Sn
Chemical homogeneity
  Narrow range of acceptable Sn proportions, ~23-26% Sn
Structural homogeneity
  Generally expected that smoother surfaces allow for better superconducting performance
To what extent does the presence of NbO modify superconducting performance at the surface?
What specific chemical and structural surface features limit Nb3Sn performance, and how do they arise?

## Slide 9: Helium Atom Scattering (HAS) Instrument
Ion gun
Electron Energy Analyzer
Electron gun
AES
LEED
Quadrupole Mass Spectrometer (QMS)
Ionizer
Beam QMS
Chopper wheel
Nozzle
Skimmer
Sample/Heater
He
Bell Jar
Rotating Detector
Beamline
Beam energy: 6.5 meV (30 K) to 96.8 meV (450 K)
Ultra-high vacuum (UHV, Bell Jar ~110-10 Torr)
Detector angle range: ~35°
Sample temperature: 300 K – 2400 K
Notes: Be sure to brag; mention resolution

## Slide 10: HAS is a Surface-Sensitive, Inert, In Situ Probe
Measures surface atomic properties through electronic corrugation
  Good energy match with low-energy single phonons
  Can capture ensemble dynamical properties like mean-squared displacement
Interacts with electron cloud ~3 Å above the surface
HAS uses the periodicity of surface electronic corrugation to capture ensemble surface atomic properties.
Notes: Helium is chemically inert, and the beam is low energy
Reliably heat to 2400 K and measure up to 1750 K Have a good Eliashberg response

## Slide 11: Surface Electron-Phonon Coupling (SEPC) Constant
Electronic motion linked to nuclear motion
Crucial to Eliashberg theory of superconductivity
  Extension of BCS
  jkfadskljfalkdjsflkajsdflkjasdkfljasdlkjflsdakjflkasdjfjffkjadslkfjaklsdjfalksdjflaksjdflkajfdlkasjdflksdjf
Surface EPC
Constant
Number of
Free Electrons
Workfunction
Fermi
Wavevector
The surface EPC constant helps us better understand the relationship between electronic and nuclear motion at the surface.
Incident, Surface-Normal Beam Wavevector
C. J. Thompson, M. Van Duinen, C. Mendez, S. A. Willson, V. Do, T. A. Arias, S. J. Sibener. J. Phys. Chem. C 128 (25), 10714-10722 (2024).
Debye-Waller
Slope
11

## Slide 12: Foundational Studies on the Metallic Nb(100)
Surface modifies chemical and physical properties
Bulk Nb EPC known, but not surface
Finding metallic Nb(100) surface EPC is an important foundation towards understanding the SEPC on other materials.
C. J. Thompson, M. F. Van Duinen, M. M. Kelley, T. A. Arias, S. J. Sibener. J. Phys. Chem. C 128 (14), 6149-6157 (2024).
Notes: Elements on Auger Label diffraction peaks

## Slide 13: SEPC at the Metallic Nb(100) Surface
 | EPC | TC (K) | Critical field (T) | Superheating field (T) | Band Gap (meV)
Nb bulk *literature values | 1.01, 0.92 | 9 | 0.21 | 0.25 | 2.8
Nb(100) | 0.50 | 1.4 – 3.6 | 0.14 | 0.17 - 0.22 | 1.1 – 2.1
 |  | TC (K) | Critical field (T) | Superheating field (T) | Band Gap (meV)
Nb bulk *literature values | 1.01, 0.92 | 9 | 0.21 | 0.25 | 2.8
Nb(100) | 0.50 | 1.4 – 3.6 |  | 0.17 - 0.22 | 1.1 – 2.1
This study represents the very first SEPC results on any niobium surface from HAS or any other method.
C. J. Thompson, M. F. Van Duinen, M. M. Kelley, T. A. Arias, S. J. Sibener. J. Phys. Chem. C 128 (14), 6149-6157 (2024).
13
Notes: Same as earlier

## Slide 14: HAS Demonstrated In Situ That the (3x1)-O Nb Reconstruction Persists up to 1130 K
Other methods studied the surface after, not during, temperature treatments
(3x1)-O stable up to 1130 K without evolution of structural disorder
HAS reveals in situ the stability of the (3x1)-O reconstruction at temperatures relevant to doping and alloy formation processes.
A. A. McMillan, J. D. Graham, S. A. Willson, R. G. Farber, C. J. Thompson, S. J. Sibener. Superconduct. Sci. Technol. 33, 105012 (2020).
Notes: Stable up to 1130 K, gesture at figure
At high temps, this is the system present at the (100) surface

## Slide 15: (3x1)-O Reconstruction EPC a Natural Next Step
The (3x1)-O Nb(100) is a more thermally stable and chemically relevant model system for the Nb SRF surface than the metallic Nb(100).
C. J. Thompson, M. Van Duinen, C. Mendez, S. A. Willson, V. Do, T. A. Arias, S. J. Sibener. J. Phys. Chem. C 128 (25), 10714-10722 (2024).
Oxygen remains on Nb unless heated to ~2400 K
(3x1)-O reconstruction is thermally and kinetically stable
Many previous studies have worked with (3x1)-O
15

## Slide 16: The Oxide Reduces Superconductivity Even Further
 | EPC | TC (K) | Critical field (T) | Superheating field (T) | Band Gap (meV)
Nb bulk *literature values | 1.01, 0.92 | 9 | 0.21 | 0.25 | 2.8
Nb(100) | 0.50 | 1.4 – 3.6 | 0.14 | 0.16 | 1.0
(3x1)-O/ Nb(100) | 0.20 | 6.2 * 10-4 K | - | - | -
 |  | TC (K) | Critical field (T) | Superheating field (T) | Band Gap (meV)
Nb bulk *literature values | 1.01, 0.92 | 9 | 0.21 | 0.25 | 2.8
Nb(100) | 0.50 | 1.4 – 3.6 |  |  | 
(3x1)-O/ Nb(100) | 0.20 |  | - | - | -
HAS provides the first study that demonstrates and quantifies in situ the reduction in superconducting performance in Nb due to any NbO phase.
C. J. Thompson, M. Van Duinen, C. Mendez, S. A. Willson, V. Do, T. A. Arias, S. J. Sibener. J. Phys. Chem. C 128 (25), 10714-10722 (2024).
16
Notes: First measurements of the surface EPC of the oxide/metal, both substantially reduced from bulk

## Slide 17: New Theory Matches Metallic and (3x1)-O Data
The Arias group’s new calculations allow for a precise and physically realistic treatment of the helium-surface interaction.
C. Mendez, C. J. Thompson, M. Van Duinen, S. J. Sibener, T. A. Arias. J. Phys. Chem. C 128 (25), 10714-10722 (2024).
17
Cristobal
Mendez
Talk at 3:30!
Electron Density of Surface Unit Cells
Simulated Debye-Waller Slopes with HAS Data
Notes: Electron density is not immediately apparent/understandable

## Slide 18: Fundamental Chemical Questions Underlying the Solutions to Achieving Higher Performance
Oxide
”Oxide” is a catch-all term for many oxygen-containing Nb phases
  Nb2O5 insulating
  NbO2 a semiconductor
  NbO mild superconductor with many surface phases
Nb3Sn
Chemical homogeneity
  Narrow range of acceptable Sn proportions, ~23-26% Sn
Structural homogeneity
  Generally expected that smoother surfaces allow for better superconducting performance
To what extent does the presence of NbO modify superconducting performance at the surface?
What specific chemical and structural surface features limit Nb3Sn performance, and how do they arise?

## Slide 19: A Multidisciplinary Approach to Nb3Sn Surface Chemistry
Liana Shpani
Liepe Group, Cornell University
Nb3Sn thin film fabrication, large-scale RF testing
Talk at 9:18 AM today!
Aiden Harbick
Transtrum Group, BYU
Simulations of structural and chemical defects
Talk at 4:42 PM today!
Van Do, Sarah Willson, Helena Lew-Kiedrowska
Sibener Group, University of Chicago
Ultra-high vacuum surface chemical thin film growth development and characterizations of Nb3Sn on NbO

## Slide 20: Superheating Field Calculations Show Stoichiometry Limits
Sn composition in Nb3Sn has an especially limited range for superconducting performance to outperform Nb.
Nb is a Type-II superconductor
  First critical field: normal conducting vortices form
  Second critical field: material becomes fully normally conducting
Superheating field (Hsh) is when SRF performance breaks down
  Operationally defined
S. A. Willson, A. V. Harbick, L. Shpani, V. Do, H. Lew-Kiedrowska, M. U. Liepe, M. K. Transtrum, S. J. Sibener. Phys. Rev. Res 6, 043133 (2024).

## Slide 21: 2 Recipes for UHV Replication of Nb3Sn Development Procedures
Nb3Sn thin film development well-known for creating Sn-rich and Sn-deficient regions
Recipe 1
  Lower flux overall
  Promote large, Sn-deficient grains
Recipe 2
  Higher flux, more akin to large-scale Nb3Sn development procedures
  More Sn-rich regions

## Slide 22: Sn Islands Are Both a Compositional and Structural Hindrance to SRF Performance
Sn islands are more detrimental to superconducting performance than their stoichiometry alone would suggest, and the larger and more embedded the island is, the larger its effect on superconducting performance.
S. A. Willson, A. V. Harbick, L. Shpani, V. Do, H. Lew-Kiedrowska, M. U. Liepe, M. K. Transtrum, S. J. Sibener. Phys. Rev. Res 6, 043133 (2024).
Notes: Why an issue?

## Slide 23: Corrugations Arise on Large, Sn-Deficient Grains
Sn-deficient regions also have a compounding geometric effect on superconducting performance, with worse superconducting performance the narrower and farther apart the corrugations are.
S. A. Willson, A. V. Harbick, L. Shpani, V. Do, H. Lew-Kiedrowska, M. U. Liepe, M. K. Transtrum, S. J. Sibener. Phys. Rev. Res 6, 043133 (2024).

## Slide 24: Next Steps: N-Doping and HAS
Nitrogen Doping
  Increases overall Q0
  Shorter exposure time, hotter surface
Nitrogen Infusion
  Offsets high-field Q-slope
  Longer exposure times, cooler surface
NbN has too low Hsh
  Electropolished off
Nitrogen Doping
Nitrogen Infusion
The relationship between N content and SEPC for a variety of different N reconstructions on both oxidized and metallic Nb(100) remains to be thoroughly and quantitatively explored.
A. Grassellino, A. Romanenko1, D. Sergatskov, O. Melnychuk, Y. Trenikhina, et al. Supercond. Sci. Technol. 26, 102001 (2013).
A. Grassellino, A. Romanenko, Y. Trenikhina, M. Checchin, M Martinello, et al. Supercond. Sci. Technol. 30, 094004 (2017).

## Slide 25: Next Steps: Au Capping Layers
Au has very low oxidation potential
Au only beneficial to SRF cavities at 0.1 nm thickness
Au diffusion and low Au-Nb affinity present challenges
While it is known that Au can be helpful for oxide suppression and improving SRF performance, how to develop and maintain a 0.1 nm layer and the chemical details of its challenges remain to be known.
T. Oseroff, M. U. Liepe, Z. Sun. 21st Int. Conf. RF Supercond. TUCBA01 369-373 (2023).

## Slide 26: Summary
Taking SRF materials to the next level will require ongoing collaboration centered in the materials’ surface atomic chemistry.

## Slide 27: Acknowledgments
Sibener Lab (UChicago)
  Van Do
  Caleb Thompson
  Sarah Willson
  Helena Lew-Kiedrowska
Arias Group (Cornell)
  Cristobal Mendez
  Michelle M Kelley
Liepe Group (Cornell)
  Liana Shpani
Transtrum Group (BYU)
  Aiden Harbick