## Slide 1: Surface characterization of Nb3Sn surfaces with STEM
Z. Baraissov, Z. Sun, M.Liepe, D. Muller
10 nm
Electrochemical Synthesis (Electroplating) ‘wet’
Vapor Diffusion
(Wuppertal method) ‘dry’
ADF
EELS segmentation
Electroplated samples have Sn/SnO/SnO2 on the surface which acts as a surface defect with Tc ~ 3.7K
Vapor diffused oxide contains admixture of Nb and Sn oxides, and higher oxygen vacancy
Revealing lattice distortions near metal-oxide interface
10 Å

## Slide 2: Material: Nb3Sn (vapor diffused vs electroplated)
Tin source (1250 °C )
Tin crucible
Heaters
Coating chamber
( 1100 °C )
Cavity/sample
Vacuum
( < 10-5 Torr )
Nucleation agent ( SnCl2 )
Vapour diffusion using furnace
Electrochemical synthesis
Conventional method
Electroplating followed by annealing to obtain stochiometric Nb3Sn
Developed by Z.Sun, M.Liepe ; cavity annealing L. Shpani.
Roughness reduced 4-5 times
Sun, Z., Baraissov, Z., et al (2023). Smooth, homogeneous, high-purity Nb3Sn superconducting RF resonant cavity by seed-free electrochemical synthesis. Superconductor Science and Technology, 36(11), 115003.

## Slide 3: RF performance tests
Measurements from Liana Shpani
Lower BCS resistance, higher residual
Performance to structure correlation is critical : why quench early?
Which defects add to residual resistance?

## Slide 4: STEM and Electron Energy Loss Spectroscopy
Electron beam
lenses
ADF
Detector
Electron Energy Loss Spectrometer
sample
Increasing
energy loss
record all energies at 1 spot in the sample
Energy loss (eV)
Intensity
Ti 3d
Ni 3d
Nd 4f
O 2p
STEM-EELS provide access to:
atomic-scale elemental and chemical information
local electronic structure and unoccupied density of states
Goodge, Berit H., et al. "Resolving the polar interface of infinite-layer nickelate thin films." Nature materials 22.4 (2023): 466-473.

## Slide 5: EELS of Nb oxides: Reference
J. Appl. Phys.. 2011;110(12). doi:10.1063/1.3665193
Probe Nb valence state
Probe oxidation state
Notes: The electron is excited from the O 1s core level (binding energy ~ 530 eV, depending on chemical environment).
It is promoted into unoccupied conduction band states—these are primarily composed of O 2p orbitals hybridized with the metal cation orbitals (for example Nb 4d in Nb oxides or Si 3s/3p in SiO₂).
Because pure O 2p states alone don’t form the conduction band in oxides, the final states are actually mixed:
In transition metal oxides (like Nb₂O₅), the O 2p orbitals are strongly hybridized with Nb 4d orbitals.
The ratio of the two peaks reflects empty orbital populations ratio t₂g/eg , which is 6/4 for Nb₂O₅ and decreasing toward 3/4 for NbO. [3] In contrast, the vapor-diffused sample’s oxide shows a weaker first peak, suggesting a high density of oxygen vacancies or incomplete oxidation.

## Slide 6: Sn-M edge and O-K edge
10 nm
Electroplated
Vapor Diffused
Fine features present in electroplated oxide are washed out in the vapor diffused sample
( higher O vacancies)
Bach, David, et al. "EELS of niobium and stoichiometric niobium-oxide phases—Part I: Plasmon and near-edges fine structure." Microscopy and Microanalysis 15.6 (2009): 505-523.

## Slide 7: Phase separation of tin oxides
10 nm
10 nm
The tin on the surface has lower oxygen content, i.e. metallic tin+ surface oxidation
Non-negligible tin concentration within the oxide (blue region)
The tin rich region on the interface has the highest oxygen amount, suggesting that tin appears as part of the oxide
Does tin appear as metal or a part of an oxide?
Notes: 1) ADF images

## Slide 8: Nb-M edge and Ca-L edge
10 nm
Significant Ca contamination in the vapor diffused sample
Different shift in Nb-M edge for two samples
Electroplated
Vapor Diffused
Ca-L
Nb-M3
Nb-M2

## Slide 9: Anodized oxide can host contaminants
Nb-M edgemap
O-K edgemap
Ca-L edgemap
Nb + O + Ca
Nb
Oxide after anodization
Protective
layer
The top layer is very porous and contains Ca, Nb, O, while the bottom layer is fully oxidized
50 nm

## Slide 10
De Marzi, Gianluca, et al. "Strain sensitivity and superconducting properties of Nb3Sn from first principles calculations." Journal of Physics: Condensed Matter 25.13 (2013): 135702.
Nb-Nb distance impacts DOS and Tc
Material | Shortest Nb-Nb bond (A)
Nb | 2.86
Nb3Sn | 2.65
bcc Nb
bcc Nb3Sn
Parallel to [100]
[111]
How to measure the Nb-Nb distance in 3D?

## Slide 11: Multislice Electron Ptychography
Jiang, Yi, et al. "Electron ptychography of 2D materials to deep sub-ångström resolution." Nature 559.7714 (2018): 343-349.

## Slide 12: Conventional HAADF imaging
Nb3Sn
Nb
Protective layer
HAADF imaging provides adequate lateral resolution, but lacks depth resolution
Amorphous oxide
Nb3Sn

## Slide 13: Results:Unit cell distortions at the interface
Distortions and rotations of unit cell are present near the interface
Possible sources of distortion – point defects and oxygen interstitials
Amorphous oxide
Nb3Sn
z

## Slide 14: Phase difference in Nb and Sn
Atom classification
Distribution of phase for different atomic species
Possibility of measuring anti-site defects in 3D

## Slide 15: Disorder at the oxide/metal interface: out-of-plane
Lattice distortions and rotations are prevalent at the oxide/metal interface
Lattice relaxes to the bulk value within two monolayers
Z=7 nm
10 Å

## Slide 16: Summary
EELS measurements show presence of tin/tin oxide on the surface of the EP sample, which acts as a surface defect with Tc ~ 3.7K
Higher oxygen vacancy concentration in vapor diffused oxide
Lower valence for vapor diffused oxide
Lattice distortions near metal-oxide interface and interstitials
EELS segmentation

## Slide 17: Acknowledgments
Muller group @ Cornell
SRF group @ Cornell
Prof Matthias Liepe
Dr Zeming Sun
(Now at Bruker)
CBB is supported by the NSF STC program, grant # PHY-1549132.
Facilities support from CCMR, an NSF MRSEC, grant DMR-1719875
Liana Shpani

## Slide 18: Spectral segmentation of the EELS dataset
Nb-M3
O-K
Top oxide has similar Nb valence (no energy shift)
EELS spectral map segmented
50 nm
Blue: Fully oxidized Nb2O5
Green: CaxNb2O4
Red: Nb + interstitial O

## Slide 19: Nb valence tracking over the interface
We observe a lower energy shift for VD (1.7 eV for VD vs 2.3 eV for EP) compared to bulk Nb3Sn.
Both measurements agree on the absolute value of Nb M3 peak for bulk Nb3Sn within uncertainty
Separate bonding state for the interfacial layer
10 nm
Bulk Nb3Sn
Surface oxide
Is there a bonding change for Nb at the interface?
Nb 5+
Nb 4+

## Slide 20: Oxygen interstitials
Interatomic vector angle
Object phase
Interatomic vector distance
5 Å

## Slide 21: O-K fine feature comparison
Bach, David, et al. "EELS of niobium and stoichiometric niobium-oxide phases—Part I: Plasmon and near-edges fine structure." Microscopy and Microanalysis 15.6 (2009): 505-523.
Bottom layer is a fully oxidized Nb2O5
Local bonding and coordination for the top layer is closer to NbO2
50 nm
Kumada, N., and N. Kinomiura. "Preparation and crystal structure of a new reduced calcium niobium oxide: CaNb2O4." Journal of Solid State Chemistry 147.2 (1999): 671-675.
17 possible phases of CaxNbyO
Notes: The electron is excited from the O 1s core level (binding energy ~ 530 eV, depending on chemical environment).
It is promoted into unoccupied conduction band states—these are primarily composed of O 2p orbitals hybridized with the metal cation orbitals (for example Nb 4d in Nb oxides or Si 3s/3p in SiO₂).
Because pure O 2p states alone don’t form the conduction band in oxides, the final states are actually mixed:
In transition metal oxides (like Nb₂O₅), the O 2p orbitals are strongly hybridized with Nb 4d orbitals.
The ratio of the two peaks reflects empty orbital populations ratio t₂g/eg , which is 6/4 for Nb₂O₅ and decreasing toward 3/4 for NbO. [3] In contrast, the vapor-diffused sample’s oxide shows a weaker first peak, suggesting a high density of oxygen vacancies or incomplete oxidation.

## Slide 22: XPS comparison of VD and EC
Mixed Sn and Nb oxides in vapor-diffused and separate layer of SnO on the surface of the electroplated sample

## Slide 23: Previous work: NbSn anti-site defects
10 Å
Sn-L edgemap
Nb-L edgemap
Composite map of Nb and Sn
Nb atoms, that are 1Å apart, can be distinguished
Nb signal in the Sn atomic sites is detected
Drawbacks:
Very high dose (over 6000 times more than ptychography)
Defects are formed during imaging
Sum of the projection (no depth resolution)