## Slide 1: Impact of RF pulse structure on breakdown in the short-pulse regime.
Materials for Bright Beams workshop
erhtjhtyhy
Chunguang Jing
Euclid Techlabs LLC,
Argonne National Laboratory
7/17/2025

## Slide 2: outline
Dependence of Gradient on RF pulse length
  Scaling law?
  Observation from CLIC 30GHz era
  Discovery of BIAR (breakdown insensitive accelerator regime) at AWA
Make a short RF pulse case for >500MeV/m gradient
Challenges and R&D work

## Slide 3
Dependence of Gradient on RF pulse length

## Slide 4
Relevant history of studying RF breakdowns dependences on rf pulse length
Theoretical model
Experimental efforts

## Slide 5
Empirical scaling law
BDRE305
A. Grudiev et al., Phys. Rev. ST-AB, 12, 102001 (2009).
Empirical formula summarized from decade of high gradient accelerator research (x+ka bands)
110 MV/m
SLAC Breakdown and pulse heating study 2010 (from F. Wang, AAC10 presentation)
SLAC Breakdown study 2008 (from V.A. Dolgashev, AAC10 presentation)
Freq. | Pulse length (ns) | Max. Grad. (MV/m)
S-band at FERMI 2.0 | 700 | 28
C-band in Japan | 300 | 50
X-band at CERN | 180 | 120
Shorter pulse length
Shorter pulse length

## Slide 6
A 30-cell structure with Mo irises and low ES/EA largely exceeded the CLIC accelerating field requirements without any damage
190 MV/m accelerating gradient in first cell - tested with beam ! (but only 16 ns pulse length)
Observation from CLIC 30GHz era
30-cell clamped tungsten-iris structure

## Slide 7: Discovery of BIAR (breakdown insensitive accelerator regime) at AWA-I
Single-cell structure
- Optimized for maximum transient gradient
Normal cell properties (11.7 GHz) | 
Iris diameter | 6.1 mm
Iris thickness | 2.9 mm
Phase advance | 120 degree
Quality factor | 6070
Shunt impedance r/Q | 1.4x104 Ω/m
Group velocity | 0.0114c
80%
92%
93%
100%
- The input matching cell has higher gradient and surface field than the normal cell

## Slide 8
Main pulse
Secondary pulse
Input
pulse
RF conditioning
Experimental setup
Main pulse
Secondary pulse
Normal transmitted pulse
- 7.7x104 pulses accumulated at 2 Hz repetition
Conditioning
Testing
Discovery of BIAR at AWA-II

## Slide 9
BD type I
BD type II
- Distorted main pulse
- Disappeared after conditioning
- Likely to be caused by multipacting
Main pulse
Secondary pulse
H. Xu et al., PRAB 22, 021002 (2019)
- Blocked secondary pulse and normal main pulse
- Probability decreases after conditioning
- Likely to be caused by RF breakdown
Main pulse
Secondary pulse
Discovery of BIAR at AWA-III

## Slide 10: Long-pulse high-power test at Tsinghua
RF conditioning
Experimental setup
- 2.3x107 pulses accumulated at 40 Hz repetition
- Driven by klystron with pulse compressor
Y. Jiang et al., IEEE Trans. Microw. Theory Tech., 69, 1586-1593, (2021)
Courtesy of Hao Zha

## Slide 11: Results discussion (I)
Comparison of short and long pulse results
Fit to BDRE30
Accelerating gradient of the normal cell and the input matching cell reaches 270 MV/m and 310 MV/m
Surface field of the input matching cell reaches 500 MV/m
Gradient improved at least twofold using short pulse (limited conditioning period, only secondary pulse taken into consideration)
BDR vs. pulse length doesn’t follow the empirical scaling law in short-pulse regime
New physics of RF breakdown in short-pulse regime
Eap1/6 =Const.

## Slide 12
Breakdown Insensitive Acceleration Regime (BIAR)
RF causes BD and plasma generation
RF pulse
0 ns
Plasma expansion to block RF transmission
after ~10 ns
ANL: ϕ10-20 μm
Tsinghua: ϕ30-100 μm
Transmitted RF pulse and accelerated beam not influenced by RF breakdown
Reduced structure damage due to limited energy available for breakdown avalanche
Results discussion (II)

## Slide 13
PETS
beam
RF
Prototype TW-gun
Reflection signal from bi-directional coupler
a
a
b
b
c
c
d
d
Quick ramp-up
Dark current loading
Conditioning & dark current reduction
Achieved 350MV/m on cathode
Observed strong dark current loading regime but quickly conditioned away
It only took 70k pulses for a full condition
Back to 200MV/m to 250MV/m region, no breakdown, no measurable dark current
Euclid, SBIR Grant #DE-SC0018709, 2020
Another example: short pulse RF photogun

## Slide 14
Make a short RF pulse case
for
>500MeV/m gradient

## Slide 15
What’s a creditable route for SWFA to achieve 500MeV/m of geographical gradient?
AWA is currently developing an X-band accelerator operating in the short pulse regime.
Simply scale this structure to 11.7*3=35.1GHz, then R/Q is the same, Vg is the same, then 600MW will build up 540 MV/m. If double the power from PETS to 1.2GW, the gradient will be 764 MV/m. If the fill factor is 0.7, the geographical gradient will be 535MeV/m.
But, the beam aperture will be <1.5mm. (ref. CLIC 30GHz has aperture 2.4mm~3.2mm.)
Parameters | Designed Values
Freq. | 11.7 GHz
Filling time | 6 ns
Structure length | 25 cm
Input Power | 600 MW
Gradient | 180 MV/m

## Slide 16
50nC/bunch~400MW
Simply scale AWA’s X-band PETS to 11.7*3=35.1GHz, then R/Q is the same, Vg is the same, then we still need to maintain 30cm to get 1.2GW by 16.7nC/bunch (assuming F~1), but the beam aperture only 17.6mm/3=5.9mm.
On the power source side

## Slide 17
Challenges and R&D work

## Slide 18
Accelerators Subject to study tailed to short pulse regime
  Main accelerating structure
  Power extractor
  Drive beam production

## Slide 19: single bunch applications
 | Klystron power | Energy gain | MeV/(MW*Trf[us]) per Str.
S-band standard | 50MW, 3us | 50MeV in 3m (16.7MeV/m) | 0.33
NLC Xband | 75MW x 2=150MW, 1.6us, compress to 450MW, 400ns | 270MeV in 6.5m ( 6 structures, total 5.4m structures,83% fill factor, 50MeV/m) | 1.5
CLIC-Kly Xband | 53MW x 2=106MW, 2us, compress to 170MW x 2=340MW, 334ns | 276MeV in 4.6m (80% fill factor, 8 structures, 0.46m ea., 75MeV/m) | 2.43
CLIC-TBA Xband | 132MW from ea. PETS, 176.5ns | 46MeV in 57.5cm (80% fill factor, 2 structures, 23cm ea. , 100MeV/m) | 2
Short Pulse X-band-TBA | 537MW from ea. DPETS, 22ns | 36MeV in 37.5cm (80% fill factor, one structure, 30cm, 120MeV/m) | 3
Short pulse X-band Kly | 20MW, 1us, compress to 250MW, 10ns | 40MeV in 25cm (80% fill factor, one structure, 20cm, 200MeV/m) | 16*
If we use this as a Figure of Merit for an accelerating structure,
Def: RF usage rate
Notes: One drive beam to rule them all (simple), drive beam gives the accelerator designer frequency freedom
Could energy jitter get translated to timing jitter in the kickers?

## Slide 20
Thanks for your attention!