## Slide 1: Ab-initio Cu alloy design for high-gradient accelerators
Gaoxue Wang, Evgenya I. Simakov, Danny Perez
07/17/2025
LA-UR-22-20111

## Slide 2: Outline
Introduction
- Figure of merit (FOM)
Computational details
- Ab-initio material properties modeling and validation
FOM of dilute Cu alloys
- What alloy is good? At what solute concentration?
Summary

## Slide 3: RF breakdown
Breakdown probability is dependent on the material of the cavity
Cu-Ag alloys show improved breakdown resistance
Can we computationally screen the periodic table to identify the optimal solute and concentration?
Simakov, Dolgashev, Tantawi, 2018

## Slide 4: FOM overview
FOM:
  Critical stress to move dislocations / Thermal stress created by RF dissipation
Tradeoffs:
  Good: Adding solute atoms can improve strength: limit plastic deformation under thermal loading
  Bad: Adding solute atoms can increase RF dissipation and thermal stresses: increase driving force for plastic deformation
Chemical space: Dilute binary Cu alloys

## Slide 5: FOM #1: Critical stress to move dislocations
Labusch–Nabarro (LN) model: Critical resolved shear stress required for dislocation motion:
With:
Two key parameters:
Size misfit
Modulus misfit
Johan Zander et al., Computational Materials Science 41 (2007) 86–95
M. Z. Butt, Journal of Materials Science 28 (1993) 2557-2576

## Slide 6: FOM #2: Thermal stress created by RF dissipation
Heating due to RF losses can be estimated from the solution of the heat equation:
Material properties
Accelerator parameters
Perry B. Wilson. In ITP Conference on Future High Energy Colliders.
University of California, Santa Barbara, October 1996.
Assuming that the surface is free to relax in z only, the corresponding in-plane thermal stress is

## Slide 7: Calculating the FOM requires:
Electrical and thermal conductivity:
- SPRKKR
Lattice constant: direct structure relaxation
Mechanical properties: finite distortion
Thermal expansion coefficient: quasi-harmonic approximation
These quantities need to be computed vs solute concentration.
This requires tens of DFT calculations per solute per concentration (!)

## Slide 8: Electrical and thermal conductivity
Experiments from: Han, Seung Zeon, Eun-Ae Choi, Sung Hwan Lim, Sangshik Kim, and Jehyun Lee. "Alloy design strategies to increase strength and its trade-offs together." Progress in Materials Science 117 (2021): 100720.
Experiments
Resistivity (µOhm*cm)
SPRKKR

## Slide 9: Electrical and thermal conductivity
(*Normalized by conductivity of pure Cu)
SPRKKR 3% solute at 300K

## Slide 10: Thermal expansion coefficients
Calculated using the Quasi-harmonic approximation (QHA)

## Slide 11: Bulk and shear modulus
Experimental data from: Ledbetter, H. M., and E. R. Naimon. "Elastic properties of metals and alloys. II. Copper." Journal of physical and chemical reference data 3, no. 4 (1974): 897-935.

## Slide 12: FOM #1: Critical stress to move dislocations
In, Hg, Cd, and Au show stronger strengthening effects.
CRSS is linearly correlated with lattice mismatch with Cu.

## Slide 13: FOM #2: Thermal stress created by RF dissipation
(unloaded gradient, RF pulse length, impedance)
Estimated from DFT
with SQS structures
SPRKKR
Ag, Cd, Zn, Au and Mg induce relatively small thermal stress.

## Slide 14: Combined FOM
Maximum solubility in copper:
Ag (5 at.% 1100K), Cd (2.07 at.% 820K), Hg (~5 at.% 930 K ),
Mg (7 at.% 1008K), In (11 at.% 850K)
CuAg, CuCd, CuHg, CuAu, CuIn, and CuMg stand out.

## Slide 15: Summary
FOM: Tradeoff between solid solution strengthening and thermal stress
Identify binary Cu alloys that are promising for high gradient accelerator design
Future work:
Extend to multicomponent alloys
Validate predictions experimentally
Wang, Gaoxue, Evgenya I. Simakov, and Danny Perez. Applied Physics Letters 120, no. 13 (2022): 134101.
Wang, Gaoxue, Evgenya I. Simakov, and Danny Perez. Journal of Applied Physics 132, no. 17 (2022).

## Slide 16: Acknowledgements
C-band and CARIE team
LANL LDRD: 20200057DR, 20190079DR, 20230011DR
Thanks for your attention.