## Slide 1
MICHIGAN STATE UNIVERSITY MAP LAB COLLEGE OF ENGINEERING
Surface effects in RF breakdown
Sergey V. Baryshev
Department of Electrical and Computer Engineering,
Chemical Engineering and Materials Science
Michigan State University, MI 48824, USA
Materials for Bright Beams Workshop 2025 – 7/17/2025

## Slide 2
CARIE Project (Cathodes and RF Interactions In Extremes)
Surface effects in RF breakdown
Acknowledgments
Accelerator Science and Engineering Traineeship students:
Ryo Shinohara, Mitch Schneider, Ben Sims and Emily Jevarjian
AOT and T-1, LANL: Evgenia Simakov and Dany Perez
Taha Posos (now at FNAL), Oksana Chubenko (now at NIU), Stas Baturin (now at ITMO University)
High Energy Physics:
ASET – Cooperative Agreement DE-SC 0018362
Award No. DE-SC 0020429

## Slide 3
Surface effects in RF breakdown
Outline
Part 1. Vacuum breakdown – it is nice to meet you
Part 2. Metals and semiconductors are different
Part 3. Current saturation: space charge time vs tunneling time vs transit time
Part 4. Semiconductor in high field
Part 5. Conclusions and outlook

## Slide 4
Sharp emitter formation scenarios
Part 1 -- Vacuum breakdown
RF Breakdown Mechanics
Step-wise view of breakdown

## Slide 5
Major heating effects
Part 1 -- Vacuum breakdown
Thermal Runaway
Copper evaporation
J. Phys. D: Appl. Phys. 51 225203 (2018)

## Slide 6
Part 1 -- Vacuum breakdown
Nottingham Heating
CNT: stable 2,000 K (meff~1/2m0)
NCD: runaway 4,500 K (meff~1/18m0)
Baturin et al, J. Phys. D: Appl. Phys. 52, 325301 (2019)

## Slide 7
Part 2 -- Metals vs. semiconductors
More Insight from Nanodiamond and CNT
Emission area measured
nanodiamond CNT fiber
Posos et al, ACS Appl. Electron. Mater. 3, 4990 (2021)
j<<107 A/cm2
j<<107 A/cm2

## Slide 8
Part 2 -- Metals vs. semiconductors
Possible Saturation Effects
Vacuum space charge
Barbour et al, Phys. Rev. 92, 45 (1953)
Foreign molecules
Dean and Chalamala, APL 76, 375 (2000)
Limiting resistor
Luginsland et al, APL 69, 2770 (1996)
??? physical nature of
the limiting resistor ???
work function 𝜙 effect

## Slide 9
Part 3 -- Current saturation: space charge time vs tunneling time vs transit time
Model Formulation
Filippetto et al, Phys. Rev. Accel. Beams 17, 024201 (2014)

## Slide 10
E (V/m)
t(E) (s)
tt
tFN
tsc
Part 3 -- Current saturation: space charge time vs tunneling time vs transit time
Metal Case Study: high 𝜙 (5 eV)
j(E) (A/m2)
log(j(E))
E (V/m)
β=100
n=1029 m-3
R=10 µm

## Slide 11
E (V/m)
t(E) (s)
tt
tFN
tsc
Part 3 -- Current saturation: space charge time vs tunneling time vs transit time
Metal Case Study: low 𝜙 (2.5 eV)
j(E) (A/m2)
log(j(E))
E (V/m)
β=100
n=1029 m-3
R=10 µm

## Slide 12
Part 3 -- Current saturation: space charge time vs tunneling time vs transit time
Semiconductor Case Study: high 𝜙 (5 eV)
tt
tFN
tsc
E (V/m)
t(E) (s)
j(E) (A/m2)
log(j(E))
E (V/m)
β=100
n=1024 m-3
R=10 µm
vsat=105 m/s
ε=10

## Slide 13
Band structure
Stratton
Poisson
Part 4 -- Semiconductor in high field
Stratton–Baskin–Lvov–Fursey (SBLF) Formalism
Chubenko et al,
JAP 125, 205303 (2019)

## Slide 14
Band structure
\
Part 4 -- Semiconductor in high field
How about Cs2Te???
Scientific Reports 15, 2780 (2025)
Computational domain
2

## Slide 15
Part 4 -- Semiconductor in high field
Current and Temperature Single Pulse Transients
Shinohara et al, J. Vac. Sci. Technol. B 43, 034003 (2025)

## Slide 16
Beyond the saturation: dielectric/avalanche breakdown
Part 4 -- Semiconductor in high field
1D Heating Summary for Cs2Te
  enough heating to consider thermal stress induced surface evolution
  see Shinohara et al, PRAB 27, 053101 (2024)
375 Hz reprate
E vs H field effects
+40 K
+60 K
≈10 MV/m
≈105 m/s
0.15 V/ps
300 MV/m@5 GHz hits 50 nm Cs2Te with 0.075 V/ps!!!
Shinohara et al, J. Vac. Sci. Technol. B 43, 034003 (2025)
Notes: Field Emission
  Current Saturation: insufficient current for meaningful heating to take place for relevant range of parameter
Pulsed Heating
  Comparatively Larger heating expected
Single Pulse:
  Δ𝑇≈40 K
  Enough heating to consider thermal stress induced surface evolution
Multiple Pulse:
  Δ𝑇≈60 K
  Again, enough heating to consider surface evolution

## Slide 17
Surfaces in high gradient breakdown to due terminal runaway caused by Joule and/or Nottingham effects
Joule and Nottingham effects can curb due to current saturation
Saturation in metals is caused by space charge effect
Saturation in semiconductors is caused by charge supply (limiting resistor effect)
how many electrons available, term n5/3
how fast/far they travel, term vsat
how much emission surface available, term R2
In Cs2Te (in its standard intrinsic form) dark current saturates: Cs2Te is immune to thermal runaway!
Nevertheless, in the new era of high-f 200+ MV/m it is possible to observe new breakdown regimes
Part 5 -- Conclusions and outlook
Final Thoughts