## Slide 1: Spin polarized photocathode studies at Cornell
Matthew Andorf

## Slide 2: Ivan Bazarov Jared Maxson Adam Bartnik Elena Echevarria Sam Levenson, Ben Dickensheets Mark Reamon Abbigail Flint
Works supported by:
DOE-HEP DE-SC0025356
DOE-NP DE-SC0025663
NSF-PHY-1549132 (CBB)
SC0025663
SC0025663
SC0025663

## Slide 3: Spin Polarized Electron Beams

## Slide 4: GaAs Affinity state and ESP
Cs-O forms a strong dipole layer which lowers the vacuum energy
  Negative Electron Affinity state (NEA) occurs when conduction band minimum is larger than vacuum energy
At NEA, bandgap energy photons (circularly polarized) excite from HH/LH bands resulting in 50% ESP
Higher ESP achieavable by:
  Straining the lattice, lifting degeneracy allowing theoretically 100% ESP
  Operating in slight PEA (at the expense of QE)

## Slide 5: Traditional NEA activation
NEA is typically achieved by depositing a monolayer of Cs-Oxidant onto the GaAs surface can be done by:
  Co-deposition: Cs is deposited until QE peaks, at which point an oxidant is leaked while Cs source remains on
  Yo-yo method: the cathode is over cesiated at which point the cesium source turns off. It is then exposed to an oxidant until the QE peaks, the oxidant is then turned off and cesium source back on. The cycle is repeated numerous times

## Slide 6: High current spin polarization
Charge lifetime: The amount of current extracted before the QE degrades by 1/e
  1000 C is state of the art6 hours at 50 ma!

## Slide 7: Sb based activation recipes
Bae et al, “Improved lifetime of a high spin polarization superlattice photocathode (2020)”
Various activation recipes were tried and compared with Cs-O2 activation:
All methods achieved NEA
  Overall, Cs-O2 produced the highest QE while Cs-Sb had the worse
  Including O2 in the activation improved QE of Sb containing recipes
The QE was monitored over time to determine robustness
  All Sb activations outperformed pure Cs-O2 and pure Cs-Sb had the longest lifetime.
Co-deposition of Cs-Sb-O finds a happy middle ground
  10x Improved lifetime over Cs-O activation.
  10x improved QE over Cs-Sb activation

## Slide 8: Cs-O-Sb activation tradeoffs
Cs-O-Sb co-deposition recipe was further refined through scanning the Sb layer thickness:
  QE and electron spin-polarization decrease with Sb layer thickness
  0.12 nm layer results in only a small QE decrease while preserving max spin-polarization!

## Slide 9: The HERACLES Beamline
A beamline dedicated to the study of high current beam running:
Former CU-ERL gun. Recommissioned to 10 mA @ 200 KeV
Ion clearing electrodes
75 kW beam dump
Unique facility for high current photocathode testing on a university campus!

## Slide 10: Cs-Sb-O operation at high current
Photocathode operated with 532 nm light
Operation at 1 mA, typical run extracted 10-15 C of charge
Lifetime compared using Cs-O activation and Cs-Sb-O activation
  No substantial change in operational lifetime observed
Lifetime in growth chamber

## Slide 11: GaN as a novel spin polarized source
  Wurtzite or Zinc-Blende orientation
  >50% QE achievable with W-pGaN
  Comparable spin relaxation time to GaAs (~5 ns)
  Could be strained for high polarization
  3.2 eV band gap is conveniently at the second harmonic of Ti:Sapphire
  Less Cs to get to NEA stronger bond to Cs?
  NEA with Cs only
  Smaller SO splitting compared to GaAs (compare 340 meV to 17/5 meV for GaN)

## Slide 12: GaN ESP measurement
1032 nm pulsed femtosecond laser 20 W
Optical Parametric Amplifier Tunable 600-800 nm 2% efficiency
SHG
BiBO crystal
Linear polarizer and quarter-wave plate
Diffraction grating
“First ever” demonstration of electron spin photoemission from a GaN photocathode!
Tunable (360—400 nm), narrowband (1.4 nm) UV source developed to resolve ESP curve in photon energy
ESP observed from both Wurzite (hexagonal) and Zinc-Blende (cubic) GaN.
  Unexpected long tail observed with Wurzite phase
  ESP observed in cubic phase comparable to bulk GaAS value!
  On going project to introduce strain to GaN for >50% ESP

## Slide 13: CsI surface treatment of GaAs/GaN
Cesium Iodide has been used as the photoemitter material in Ring Imaging CHerenkov (RICH) detectors
We were investigating the possibility of using it for NEA activation (similar to Sb approach)
  Had been used in conjunction with laser activation to improve metal cathode QE (Chemical Physics Letters 621 (2015) 155–159)
cycle of deposition and heating resulted 20x better lifetime!
GaAs

## Slide 14: CsI surface treatment of GaAs/GaN
GaN
GaAs
Improvement in lifetime NOT the result of longer heating time
ESP is not degraded with improved lifetime
Similar improvements observed with GaN!

## Slide 15: AFM analysis

## Slide 16: XPS analysis
Q. Zhu, M. Hines.
XPS analysis shows clear presence of Iodine before heating but none after!
Post heated surface shows suppression of Cs-oxide while Cs sub-oxide present
Cs-suboxide robust to exposure of water/oxygen up to 625 L

## Slide 17: Spin polarized Alkali-Antimonide PC
Rusetsky et al. reported spin polarized photoemission alkali antimonide
  Cs3Sb NEA layer on Na2KSb
  Photoluminescence (PL) Al0.11Ga0.89As detector
  Circular PL degree correlated to ESP
  Calibrated with an NEA GaAs photocathode
Alkali-antimonides are robust, efficient emitters!
Active project at Cornell to confirm ESP measurements using Mott polarimetry

## Slide 18: Conclusion
Summary
Antimony based NEA activation of GaAS
  Improved robustness to vacuum poisoning
  Trade-off between QE, ESP and lifetime
  No improvement at high current operation
GaN as a spin-polarized photoemitter
  Naturally more robust than GaAs
  ESP measured for both hexagonal and cubic phases
    Cubic GaN ESP comparable to bulk GaAs
  On going project to apply many techniques developed for GaAs on GaN
    Alternative activation layers
    Strained lattice for high ESP
    Bragg reflector for high QE
CsI surface treatment
  20x improvement in dark lifetime
  Works for both GaN and GaAs
  Testing if compatible with antimony based NEA activation