## Slide 1: Air stable III-Nitride photocathodes
Materials for Bright Beams Workshop 2025
Luca Cultrera
Instrumentation Department - Brookhaven National Lab

## Slide 2
Material | QE | Laser | Response time | Electric field | Vacuum | Lifetime | MTE
Copper | 1e-5 | UV | Sub-ps | 120 MV/m | 1e-9 Torr | months | 500 meV
Cs2Te | 1e-1 | UV | Sub-ps | 80 MV/m | 1e-9 Torr | months | 500 meV
GaAs | 1e-2 | IR | 10s of ps | 5 MV/m | 1e-12 Torr | days | 50 meV
Cs2KSb | 1e-1 | VIS | ps | 20 MV/m | 1e-10 Torr | months | 100 meV
The perfect photocathode does not exist yet!
What we want from a photocathode?
High QE, operation with Visible or Infrared laser, short response time, compatible with high electric field and poor vacuum levels, with a long lifetime and a small MTE

## Slide 3: Why the III-nitrides?
Established industrial technology;
  LEDs;
  High power electronics;
Photocathode R&D;
  Solar blind detectors;
Band gap tunability:
  Matching to laser wavelength;
Engineering perspectives:
  Multi Quantum Well;
  Distributed Bragg Reflectors;
  Resonant tunneling Barriers;
Wavelength tunability
(0001)
Polar bonds non-symmetric
1-10 MV/m internal fields
Strong polarization fields
(0001)
Psp
(000-1)
Psp

## Slide 4: Surface engineering to achieve NEA
Nitrogen polar photocathodes
Utilize direction of polarization and depletion charge
Removes need for highly doped cap structure or Cs
Delta-doped cap layer
Growth of thin, highly doped n+GaN cap layer
Increased downward band bending at surface, NEA
Activation by Cs:O surface treatment
Utilizing p-type bulk and Cs/Cs-O surface layer
Cs/Cs-O creates tunneling barrier at surface
Reactive to air and water
J. Fu et al., Optik 125, 1451 (2014).
N. Tripathi, et al., Appl. Phys. Lett. 97, 052107 (2010).
Marini, et al, J. Appl. Phy. 124, 113101 (2018).
4
p-GaN
Cs-O
p-GaN
n+-GaN
N-polar p-GaN
u-GaN
Notes: To get the effective negative electron affinity, a thin cap layer is used to modify the surface and induce downward band-bending. First with a Cs/Cs-O surface treatment on p-GaN which creates a dipole at the surface acting as a tunneling barrier for electrons, thus lowering the effective negative electron affinity. However, the Cs surface treatment is highly reactive to air and moisture, leading to the requirement to fabricate, package and test devices without breaking vacuum increasing the cost and complexity of device use. Our group has pioneered Cs-free III-nitride photocathode detectors. First using a highly doped n+GaN cap on Ga-polar p-GaN. The n+ cap layer increases the magnitude of downward surface band bending, lower the effective electron affinity at the surface. However the high doping concentration results in an increase in electron scattering at the surface. To eliminate the need for such high n-type doping in the cap layer. N-polar photocathodes were proposed. In the N-polar orientation the polarization and depletion charge are aligned and positive at the surface, increasing the magnitude of band bending and lowering the vacuum level with the use of an unintentionally doped cap layer.

## Slide 5: Leveraging the polarization field and get rid of Cs!!
Can we achieve air stable Negative Electron Affinity condition?
Compatible with “poor vacuum” conditions and operation in RF gun
(000-1)
Simulation with polarization
J. Marini et al., J. Appl. Phys. 124, 113101 (2018)
Mild HCl chemical etch required to remove surface oxide after air exposure
Peak QE up to 12% at 6 eV
sapphire
AlN
N-polar
u-GaN
N-polar
p-GaN
u-GaN cap

## Slide 6: QE and lifetime
Two N-polar GaN samples from the same MOCVD growth run
HCl and heat cleaning @500C
Peak at 23%!!
QE stable above 10-3 level !!
25 uW @ 265 nm
Bias -18 V
10-10Torr
L. Cultrera et al., J. Appl. Phys. 131, 124902 (2022)

## Slide 7: MTE as function of photon energy and location
Low QE sample
High QE sample
QE~3x10-6
QE~1.5x10-5
QE~1x10-4
QE~1x10-3
QE~6x10-6
Free space beam expansion as function of voltage
H. Lee, Rev. Sci. Instr. 86, 073309 (2015)
Local MTE
Local QE
e- beam images as the laser spot (50um r.m.s. @265nm) moves vertically on the cathode
L. Cultrera et al., J. Appl. Phys. 131, 124902 (2022)
Compare with a typical Cu photocathode
QE~1e-4 and MTE ~500 meV @266 nm

## Slide 8: Surface morphology
nm
nm
Typical of N-polar growth: Hexagonal base pyramidal shaped hillocks – size comparable with laser spot
Additional studies required to mitigate their presence and study compatibility with high electric fields
Sharp LEED pattern
Confocal microscope imaging
L. Cultrera et al., J. Appl. Phys. 131, 124902 (2022)

## Slide 9: PEEM imaging uniformity of emission
fov=172 um
MCP=1430 V
C/s= 1.1920e+09
Hg lamp
N-polar GaN s0583
HCl rinse followed by IPA rinse with N2 blow dry and annealing in UHV to 300C
PEEM allows to correlate QE and morphology
Large non-uniformity of emission across the surfaces
For photoinjector operation +/-10% is typically required to mitigate non uniformity in the charge distribution in the electron bunches

## Slide 10: What we learned so far?
N-polar III-Nitrides photocathodes shows promising performances in terms of QE, MTE, lifetime and handling between the production facility and their possible use in electron gun.
Morphology of the surface -hillocks- and non uniform photoemission may be detrimental to electron beam performances and requires more investigation.
III-Nitrides do not require UHV transportation or storage, and a simple chemical etch is sufficient to restore emission properties

## Slide 11: What next? Leverage Eg tunability
Operating photocathodes in electron guns with deep UV photon poses some challenges:
  1 mA of photocurrent with QE of about 1x10-3 requires 4.6W @266nm –some applications require 100 mA-
  spatial and temporal laser pulse shaping required for optimizing electron beam dynamics
  Optical transport is challenging
III-Nitrides provide a versatile platform to engineer photocathode structures that can operate in the range 3.1-3.6 eV where optical transport and laser shape manipulation is less problematic even at high average power.

## Slide 12: Alloy space for Eg target 3.1-3.6 eV
InxGa1-xN
AlxGa1-xN
AlxIn1-xN
Al0.1Ga0.9N
Al0.7In0.3N
In0.1Ga0.9N
Al0.6In0.4N
R.R. Pela et al, Appl. Phys. Lett. 98, 151907 (2011)
Target emission range requires p-InxAlyGa1-x-yN with Eg slightly larger than EC-EF=φs=3.1–3.6 eV
Effective negative electron affinity (NEA) must be achieved
  InN has very high EA (~5.6–5.8 eV)
  AlN has much lower EA (~0.6–1.9 eV)
By alloying InN with AlN, target Eg can be attained with EA lower than that of GaN (~4.1 eV)
Sakalauskas, E., et al. J. Appl. Phys. 110.1 (2011).
Lin, S., et al Appl. Phys. Express 5 031003 (2012)
Bermudez, V., et al. J. Appl. Phys. 89, 1991 (2001)
Notes: Based on the targeted operation at 3.1-3.6 eV we have identified boundaries

## Slide 13: MOCVD growth conditions
Growth completed using Veeco D180 MOCVD in the Wide Band Gap Optronix Lab at SUNY Albany
TMGa, TMAl, and TMIn precursors for Ga, Al, and In, respectively
Before quaternary growth, ternary InAlN must be developed
Initial growths targeted In0.18Al0.82N to lattice-match GaN substrates
Growth temperatures kept ≤800 °C to promote In incorporation
N2 used as precursor carrier gas to minimize parasitic reactions with H2
Notes: To grow the material, we used a Veeco D180 MOCVD. Our initial growths targeted InAlN with 18% In to lattice-match with GaN. This allowed us to use Ga- and N-polar GaN substrates to easily grow metal- and N-polar material. To promote In incorporation, growth temperature was kept at or below 800 C, and N2 was used as the carrier gas to minimize parasitic reactions with H2.

## Slide 14: Lattice-Matched InAlN Overgrowth on GaN
Target strain-free In0.18Al0.82N lattice-matched to GaN to allow high-quality overgrowth on GaN
Co-load , u-GaN substrates
Growth of target In0.18Al0.82N results in plastic relaxation (cracking) on smooth Ga-polar surface
Few/no cracks observed when grown on N-polar GaN
Cracking suggests tensiley strained film→In% smaller than target (higher Eg)
RMS: 0.5 nm
RMS: 3.5 nm
Notes: As I mentioned, we targeted 18 In% to allow for high quality overgrowth, and based on the surface morphology of the material (smooth on Ga-polar GaN and full of hexagonal hillock structures on N-polar GaN), the polarity of the overgrown material matched that of the substrate. However, the surface of the metal-polar material was covered in a dense network of cracks due to tensile strain, which implies that the overgrowth was not lattice-matched to GaN.

## Slide 15: XRD analysis
XRD ω-2θ indicates slightly In% higher on N‐polar (~2.6%) GaN than on Ga-polar (~2%)
Growth rate very low→~20 nm/hr
GaN
InAlN overgrowth on GaN appears to match underlying polarity
In% always low, largely insensitive to metal precursor flow ratio
Al outcompetes In for Group-III sites
Decreasing growth temperature and increasing substrate lattice parameter may encourage In incorporation
Notes: And in fact, XRD analysis indicates very low In%, below 5% for both metal- and N-polar materials. This result was also insensitive to variation in metal precursor flow ratio; the Al always outcompeted the In for group-III sites. This indicates then, that to increase In incorporation, the growth temperature must be reduced. Growth directly on sapphire (which has a larger lattice parameter) may also be useful, as the large lattice mismatch may reduce adatom mobility and increase the In sticking coefficient.

## Slide 16: Uniform indium incorporation proven to be challenging

## Slide 17: InAlN and InAlN:Mg on sapphire
Higher In% growth possible on sapphire
2θ-θ XRD scans run between strain-free (002) reflection of InN and AlN to identify ternary Bragg condition
Assuming 0% strain, InAlN samples grown at 750 °C with and without Mg doping have In% of 22.5% and 25%, respectively.
  InAlN:Mg grown at 700 °C has In% of 40%
Tgrowth=700 °C
w/Mg
Tgrowth=750 °C
w/Mg
Tgrowth=750 °C
w/o Mg
2θ-θ XRD
Notes: And indeed, we found that growth at lower temperatures increased the In%, with the highest In% and highest quality material grown directly on sapphire. I have shown here XRD scans showing the InAlN peaks of undoped material grown at 750C, Mg-doped material grown at 750C, and Mg-doped material grown at 700C. Assuming the films are fully relaxed, this gives In% of 25% for undoped InAlN, and slightly lower 22.5% for Mg-doped when grown at 750C. This may be due to the Mg competing with the In for group-III sites. However, at 700C, we successfully achieved 40 In% InAlN doped with Mg.

## Slide 18: Photoemission measurement
Photoemission measurement performed at ASU and BNL
  Retarding potential – total kinetic energy distribution
  Photoluminescence – Electronic band gap
  Photocurrent - Quantum Efficiency
  Vacuum system operates at levels of 1x10-11 Torr or better
  Light sources used includes (UV LEDs, Lamps+mono, laser diodes, OPA)
  Typical surface preparation includes HCl+IPA etch, N2 blow dry and annealing in UHV to 300C

## Slide 19: InxAl1-xN N-polar g4515_s2218f
The PL structure at 2.19 eV could be due to a defect state or defect-related band -YL1 (Yellow Luminescence)-observed at room temperature. Reshchikov et al. [1] have also reported this feature for undoped GaN.
[1] Reshchikov et al. Sci. Rep. 7, 9297 (2017).
Photoluminescence inferred band gap is consistent with a higher In% content than the one inferred by XRD (37% rather than 31%)

## Slide 20: InxAl1-xN N-polar g4515_s2218f
  Retarding potential – total kinetic energy distribution
  The max of kinetic energy is derived as difference between the rise and fall of photocurrent generated from the sample at a defined wavelength (240 nm here) as function of the retarding potential.
𝜑 =5.16 eV -1.3 eV= 3.86eV before annealing
𝜑 =5.16 eV -1.5 eV= 3.66eV after annealing
Eaffinity= (3.86-3.33) eV= 0.53 eV before annealing
Eaffinity= (3.66-3.33) eV= 0.33 eV after annealing
Bandgap inferred from PL is 3.33 eV

## Slide 21: InxAl1-xN N-polar g4515_s2218f
Eg =3.33 eV
GaN
AlInN
Effective Ea =0.33 eV
Eb =??? eV
Ea =??? eV
Initial photoemission measurements carried out with a photon energy of 3.6 eV revealed very low QE value of about 1x10-7
Exposing the photocathode surface to alternating fluxes of Cs vapors and oxygen allow the formation of a strong surface dipole that lowers the effective Ea (typically used to achieve Negative Electron Affinity in III-V and III-nitrides)
No NEA evidence in QE
GaN NEA
10-3 QE @ 3.6eV
Notes: What is the thickness of the AlInN? 50 nm?
What is the doping level if any…

## Slide 22: Outlook
N-polar InxAlyGa(1-x-y)N are promising materials for photocathodes designed to produce high-brightness electron beams
Growth of high-quality In-rich III-N alloys difficult due to In coalescence and lattice strain associated with high In content
  InxAl(1-x)N with up to 40% In successfully grown and doped with Mg
Ongoing studies continue to induce N-polar growth on sapphire by nitridating surface, and adding Ga to achieve quaternary InAlGaN growth
Photoemission studies revealed non uniform emission from photocathode surfaces
Negative Electron Affinity has not yet been achieved

## Slide 23: Thank you!!
Acknowledgement to DOE HEP Office of Science for funding (DE-SC00024192)
F. S. Shahedipour-Sandvik, A. Lanjani, B. McEwen, S. Omranpour (State University of New York-Albany),
E. Rocco (Naval Research Lab),
V. Meyers (Sandia National Lab),
M. Moeini Rizi, L. Lathpandura, S. Karkare (Arizona State University)

## Slide 24: Backup

## Slide 25: Optimization of the growth conditions
Tgrowth=700 °C
w/Mg
Hall characteristics
[h+]sheet: ~1∙1013 cm-2
μ: ~0.1 cm2/V∙s
ρsheet: 2.7∙106 Ω/□
Growth performed at 70 torr, V/III=6,800, N2 carrier gas
InAlN highly lattice mismatched to sapphire→ reliable ω-2θ challenging
2θ-θ XRD scans run between strain-free (002) reflection of InN and AlN to identify ternary Bragg condition
Assuming 0% strain, g4491, has In% of 40%.
Strain effects not yet accounted for in XRD→ In% contains uncertainty
g4491
g4511
Reducing TMIn flow by 50%
RMS 2.45 nm
On sapphire
On sapphire
RMS 1.7 nm

## Slide 26
g4513_s2254 (InGaN Growth on uGaN template)
5 μm x 5 μm AFM scan of this growth with RMS roughness of ~8 nm
~25% InxGa1-xN (Flat)
(002) Omega-2Theta XRD scan on this sample (blue line) and RADS fitted XRD simulation (red line) showing ~25% InxGa1-xN assuming 100% relaxation
Note: Accurate thickness needs to be measured by cross-section SEM, but is estimated to be ~150-200 nm

## Slide 27: g4515_s2218 (InAlN:Mg Growth on N-polar GaN template)
Cross-section SEM shows <50 nm InAlN:Mg. Identifying an InAlN sharp peak (grown on N-polar GaN) was difficult in the Omega-2Theta XRD scan due to low intensity (thickness)
5 μm x 5 μm AFM scan of InAlN:Mg on N-polar GaN template with RMS roughness of ~3 nm
Chart: Omega (deg)
Omega XRD scan of InAlN:Mg on sapphire. A peak at ~17.2° corresponds to ~x = 30% in InxAl1-xN based on Bragg conditions of InN and AlN (assuming 100% relaxation)

## Slide 28: Spin polarized emission from GaN
https://doi.org/10.1063/5.0215746
Net spin polarized electron photoemission from GaN activated to NEA has been recently measured by Mott polarimetry
Polarization is lower than strained GaAs (up to 92%) and likely affected by reduced HH-LH separation and reduced spin relaxation times
https://doi.org/10.1103/PhysRevB.81.155216
Spin relaxation times can be increased in GaN by cryocooling the samples
At LN2 temperature spin relaxation is larger than 200 ps
Timing is compatible with operation in photoguns
Notes: Pol= (up – down)/(up+down)

## Slide 29: Spin polarized electron emission
LH
HH
CH
Achieving electron photoemission with net spin polarization requires removal of energy degeneracy in valence bands
III-Nitrides can leverage spitting from crystal field and spin orbit coupling to increase HH-LH energy separation
https://doi.org/10.3390/app10010232
https://doi.org/10.1063/1.3603015
Upgrading the UHV system for spin polarization
with a sample holder capable of cryo-temperatures
Notes: In a degenerate HH-LH bands
The maximal pol is (3-1)/(3+1)=0.5 (50%)