## Slide 1
Center for
BRIGHT BEAMS
A National Science Foundation Science & Technology Center
Physics of Photocathodes for Photoinjectors workshop, ASU
November 13th, 2025
Near-threshold Photoemission Characterization of K2CsSb Photocathodes
Peter Owusu
Advisor: Dr. Siddharth Karkare

## Slide 2: Introduction
Image credit: SLAC National Accelerator Laboratory
High performance of future accelerators/colliders demands brighter electron beams
Electron Beam Brightness

## Slide 3: How do we Decrease MTE
By reducing Excess Energy but also reduces QE.
Alkali-antimonide photocathodes overcome this limit, offering high charge densities even at low fluence.

## Slide 4: Most Commonly Used Alkali-Antimonides
Cs3Sb
K2CsSb
Na2KSb

## Slide 5: Prior Near-threshold Photoemission Characterization Work on Cs3Sb

## Slide 6: Electron Energy Distribution and Work Function
Work function was determined as 1.5 ± 0.10 eV
MTE does not get to the RT thermal limit, ~25 meV
Why?

## Slide 7
Why the Knee?
Are other High QE materials better emitters near threshold?
Will the other high QE materials actually get to kBT at threshold?

## Slide 8: Near-threshold Photoemission Characterization of K2CsSb Photocathodes

## Slide 9
200nm-2000nm tunable wavelength laser
MBE-style thin film growth chamber
UHV Atomic Force Microscope
Photoemisison Electron Microscope
meV-scale energy-momentum analyzer
200 keV cryocooled DC electron gun
UHV Transfer Line
He liquifier
Photoemission and
Bright Beams Lab,
ASU

## Slide 10: Electron Energy Distribution and Work function Determination
Work function was determined as 1.65 ± 0.10 eV

## Slide 11: Spectral Response of K₂CsSb
Near threshold, exponential dependence of QE on photon energy is observed.
Both growths show similar spectral behavior

## Slide 12: MTE Measurements

## Slide 13: Comparison of K2CsSb with Cs3Sb

## Slide 14: Comparison of QE spectral slopes

## Slide 15: Comparison of MTEs with Eexcess/3

## Slide 16: Overlay of High Energy Tails of EDCs
K2CsSb
Cs3Sb

## Slide 17: Acknowledgement
Anagha Ullattuparambil (Lead Co-author)
Jo Mama
Professor Siddharth Karkare