## Slide 1: Nb surface oxide and anodization effects on tin nucleation for Nb3Sn growth
Liana Shpani
In collaboration with: Van Do, Jasper Brown, and Gabriel Gaitan
Steven Sibener from University of Chicago, and Matthias Liepe from Cornell University
July 9th, 2026
Research funded by Center for Bright Beams, NSF award PHY-1549132

## Slide 2: Nb3Sn performance and nucleation challenge
Why Nb3Sn?
Film quality is limited by non-uniform nucleation in early stages
Higher Tc than Nb (18 K vs 9 K)
20-30x more efficient than Nb at 4.2K
Quality factor
Accelerating gradient (MV/m)
Nb
Nb3Sn
Lower cooling cost and complexity due to higher operating temperatures
Potential to reach higher accelerating gradients compared to Nb
Growth: thermal vapor diffusion
Non-stoichiometric regions degrade RF performance

## Slide 3: How can we improve tin nucleation?
Pre-anodization of the substrate
= Electrochemically growing an oxide on the Nb substrate
Add of SnCl2 nucleating agent
Higher vapor pressure than metallic Sn at lower temperatures
Interacts with the substrate surface at earlier stages of coating
Sn
Cl
Cl
When the oxide is soluble in the electrolyte, you can grow a porous oxide
Does SnCl2 bind preferentially to specific features?
Why does anodizing the surface help? Can we separate the physical vs chemical contributions?
Study Nb oxide surface roughness and dissolution kinetics to understand early-stage SnCl2 nucleation with the goal of optimizing substrate preparation and coating recipes
This talk:

## Slide 4: Niobium oxide study
High purity Nb samples cut from sheets used for SRF cavity fabrication were chemically polished (buffered chemical polish and electropolish)
Samples were annealed following the vapor diffusion temperature profile ramp to nucleation temperatures
Sample | Ramp rate
C1 (control) | 3 C/min
A1 (anodized, porous) | 3 C/min
A2 (anodized, porous) | 7 C/min
Jasper Brown
Van Do
Characterization Methods
Atomic Force Microscopy (AFM)
Surface topography, before/after anneal
X-ray photoelectron spectroscopy (XPS)
Oxidation state, throughout heating
in-situ
Scanning Electron Microscopy (SEM) / Energy Dispersive Spectroscopy (EDS)
Imaging + elemental composition
ex-situ
Focus: pre-nucleation surface evolution
Sample | Ramp rate
C1 (control) | 3 ℃/min
A1 (anodized, porous) | 3 ℃/min
A2 (anodized, porous) | 7 ℃/min

## Slide 5: Surface topography and roughness
Anodized surface has a rough texture consisting of pores and intersecting bumps, which persist after annealing when all the Nb2O5 is gone.
Power Spectral Density (nm4)
Spatial frequency (nm-1)
Anodized
Control
Mean values trend toward higher roughness post-anneal, but uncertainties overlap
Anodization process impacts the metallic substrate and the resulting roughness is irreversible when Nb2O5 is reduced.
Rougher
Root Mean Squared (nm)
Image Size

## Slide 6: Oxide dissolution kinetics
Control (3℃ /min)
Anodized (3℃ /min)
Anodized (7℃ /min)
peaks disappear at higher temperatures for the anodized samples compared to the control
Assuming first-order kinetics, reduction rate follows Arrhenius form:
Use fitted parameters to model thickness of Nb2O5 as a function of the temperature profile in the furnace
Frequency factor
Activation energy
Extracted from XPS data

## Slide 7: Modeling what’s happening in the furnace
We can use temperature profile as an input to predict when we run out of SnCl2 in the crucible and % remaining of Nb2O5 layer:
Ramp to nucleation
SnCl2
In this example, SnCl2 vapor starts interacting with the Nb2O5 surfaces as early as 180℃ and is exhausted very early in the ramp process.
Native
Anodized
In this example, SnCl2 vapor is exhausted early in the degas process.
Degas at 180℃
SnCl2
Native
Anodized

## Slide 8: SnCl2 evaporation study
Using Gabriel’s CVD furnace:
Experiment if any SnCl2 deposition takes place at low temperatures (close to degas)
  SnCl2 interacts with three different types of oxides:
No flow,
high vacuum
Native
oxide
Anodized
with NaOH
Anodized
with H2SO4
Smoother oxide
Porous oxide
Want to compare how SnCl2 binds to native vs anodized oxides, and compare two anodization electrolyte choices
Gabriel Gaitan

## Slide 9: Post 200℃ bake with SnCl2 results
400 nm
Porous
400 nm
Native
400 nm
Smooth
Nb5+
Nb0 and Nb2+
Cl 2p
Oxidized Sn
No visible tin droplets
Most tin signal
Only sample with chlorine signal

## Slide 10: Surface chemistry reveals Na contamination
Na 1s
Jasper Brown
XPS showed that Na peak persisted after annealing in UHV
Electrolyte incorporation in the oxide during anodization
However, Na was not detected in any sample after being baked with SnCl2 present in the chamber!
Samples anodized with NaOH had traces of Na at the surface
Van Do
Control

## Slide 11: Takeaways and next steps
Surface roughness persists after oxide reduction through annealing: helpful to separate chemical vs roughness effects in future nucleation studies
SnCl2 interacts with the Nb surface earlier than previously assumed (as early as degas): important for understanding what actually drives nucleation
Next steps
Vapor diffusion furnace:
  Degas-only run: quantify SnCl2 evaporation and deposition, anodized vs. not anodized
  Vary anodization recipe to test effect of oxide morphology on nucleation and film quality
CVD furnace:
  SnCl2 deposition on anodized vs anodized + annealed samples: same roughness, but only one retains Nb2O5
Thank you for your attention!
Porous/rough oxides show potential for improved nucleation: no droplets but more tin
  promising direction for better final films