## Slide 1: Zone Plates in the Ultrafast Regime
Anagha Ullattuparambil
aullattu@asu.edu
CBB Annual Meeting – 07/10/2026
Advisor – Siddharth Karkare Arizona State University

## Slide 2: Zone plate
Final aim - Brightest electron source ever!
Electron microscopy applications
Ultrafast applications:
Ultrafast electron diffraction/microscopy
Free-electron lasers (FELs)
…
What are the effects of using ultrashort pulses on the focusing properties of a zone plate?
Can an integrated zone-plate photocathode be used for pulsed electron applications?
Pulsed electron beams are produced by shining ultrashort laser pulses onto a photocathode.
A tabletop TEM (Transmission Electron Microscope)

## Slide 3: Zone plate beyond continuous wave optics
Zone plates are designed for monochromatic, continuous-wave (CW) illumination.
All conventional zone-plate theory assumes:
When illumination becomes pulsed:
Is the focus still unchanged?
Does the electron emission spot size remain the same?
Does the electron pulse remain short?
Ultrafast laser illumination:
(1) Spectral bandwidth
(2) Temporal delay
Photoemitting layer (Cs3Sb/K2CsSb)

## Slide 4: 1. Spectral bandwidth
A finite pulse duration implies a finite wavelength spread .
For a zone plate;
The zone plate is chromatic.
Incident light
e-
e-
Incident light
e-
e-
532
533
531
For
Wavelength (nm)
For a 150 fs laser pulse, corresponds to 2.8 nm.
For
Different wavelength components focus at different axial positions.

## Slide 5: 2. Temporal delay
a
b
f
The arrival time difference between wavefronts originating from the center versus the outermost edges of the zone plate.

## Slide 6: 2. Temporal delay
a
b
The arrival time difference between wavefronts originating from the center versus the outermost edges of the zone plate.

## Slide 7: 2. Temporal delay
a
b
Outer edge rays reach the focus only after the central pulse has departed.
The arrival time difference between wavefronts originating from the center versus the outermost edges of the zone plate
Notes: If the two rings arrive together,
T(r)-T(r')=0,
then
R_a(r,r')=1.
They interfere fully.
If they arrive separated by much more than the pulse duration,
|T(r)-T(r')|\gg \sigma_t,
then
R_a(r,r')\approx 0.
They no longer interfere with each other.

## Slide 8: 2. Temporal delay – why is it specific for zone plates?
Light coming from the center and the edges reaches the focus at the same time
Conventional lens
Light from the edges arrives late
Zone plate

## Slide 9: NA and Temporal delay
a
b
f
R
Small NA
Large NA
Larger the NA, larger is the path difference between the central and edge rays.
a
b
f
R
Focal length | NA | 
1 mm | 0.3 | 0.16 ps
1 mm | 0.7 | 1.33 ps
Focal length | NA | 
1 mm | 0.3 | 0.16 ps
1 mm | 0.7 | 1.33 ps
If > : mutual interference is strongly suppressed.

## Slide 10: How can it affect the focus?
The focus is not formed instantaneously, but sequentially.
(1) First, the center zones create a low-resolution focus.
(2) Edge zones follow, building the high-resolution focus.
Notes: So, how exactly does this geometric time delay affect the focus?
When we look at a time-resolved picture of the focus, we find that it doesn't just appear instantaneously. Because the light from different zones arrives at different times, the focus forms sequentially.
As you can see noted in image_26558a.png, the center zones create a low-resolution focus, which is then followed by the high-resolution focus by the edge zones.
Even though diffraction around any single ring is completely coherent, the arrival times of these individual foci are spread out. This causes an effectively incoherent addition of fields at the focal plane over time.
Next, let's see what our experimental data shows us when this time-dependent focus formation takes place

## Slide 11: Zone plate in ultrafast regime
Expect a larger spot size and a temporally elongated electron pulse.
Finite spectral bandwidth
Temporal delay

## Slide 12: Experimental Results
532 nm pulsed laser
Pulse width = 150 fs
Repetition rate = 500kHz

## Slide 13
Diffraction is coherent around a given zone
Why time delay is not affecting the spot size(FWHM)?

## Slide 14: Why time delay is not affecting the spot size(FWHM)?
Diffraction is coherent around a given zone
The addition of the individual foci arrives at different times and therefore does not interfere with one another.

## Slide 15: Why time delay is not affecting the spot size(FWHM)?
Diffraction is coherent around a given zone
The addition of the individual foci arrives at different times and therefore, interference is suppressed.
Autocorrelation term:
It measures how much the pulses from two regions of the zone plate overlap in time.
CW limit,
Ultrafast limit,
f0
Two points (or rings) on the zone plate aperture
Pulse width standard deviation
Time delay compared to the central ray.

## Slide 16: Why time delay is not affecting the spot size(FWHM)?
Autocorrelation term:
Temporally weighted focal intensity at radius :
Two points on the zone plate plane
Design focal length
Radial coordinate in the focal plane
Contribution of radius r
Zone plate transmission
Radius of the zone plate.
f0
Focal plane

## Slide 17: Results
Intensity in the focal plane
Encircled Power
The cumulative fraction of total optical power within a circle of radius in the focal plane.
f0 | NA |  | 
1 mm | 0.3 | 150 fs | 160 fs
f0 | NA |  | 
1 mm | 0.3 | 150 fs | 160 fs

## Slide 18: Results
The effects worsen as the pulse duration decreases.
Intensity in the focal plane
Encircled Power
f0 | NA |  | 
1 mm | 0.3 | 80 fs | 160 fs
f0 | NA |  | 
1 mm | 0.3 | 80 fs | 160 fs

## Slide 19: Results
The effects worsen as the NA increases.
Intensity in the focal plane
Encircled Power
f0 | NA |  | 
1 mm | 0.7 | 80 fs | 1.33 ps
f0 | NA |  | 
1 mm | 0.7 | 80 fs | 1.33 ps

## Slide 20: Results
Intensity in the focal plane
Encircled Power
f0 | NA |  | 
1 mm | 0.7 | 150 fs | 1.33 ps
f0 | NA |  | 
1 mm | 0.7 | 150 fs | 1.33 ps

## Slide 21: Results
Shifting to an ultra-short focal length drastically reduces the pulsed-light effects.
Intensity in the focal plane
Encircled Power
f0 | NA |  | 
0.1 mm | 0.7 | 150 fs | 133 fs
f0 | NA |  | 
0.1 mm | 0.7 | 150 fs | 133 fs
<

## Slide 22: 2. Why is the spot size unaffected by spectral bandwidth?
Different wavelengths are focused at different points along the axial direction.
532
533
531
2.8 nm
Wavelength (nm)

## Slide 23
Different wavelengths are focused at different points along the axial direction.
Design wavelength focuses at
Incident light
e-
e-
z = f0
2. Why is the spot size unaffected by spectral bandwidth?

## Slide 24
Incident light
e-
e-
Different wavelengths are focused at different points along the axial direction.
Design wavelength focuses at
Longer wavelengths focus at
z = f0
2. Why is the spot size unaffected by spectral bandwidth?

## Slide 25
Incident light
e-
e-
Different wavelengths are focused at different points along the axial direction.
Design wavelength focuses at
Longer wavelengths focus at
Shorter wavelengths focus at
z = f0
2. Why is the spot size unaffected by spectral bandwidth?

## Slide 26
Different wavelengths are focused at different points along the axial direction.
They produce a significantly larger spot at the focal plane, .
Their power is distributed over a larger area.
Incident light
e-
e-
z = f0
2. Why is the spot size unaffected by spectral bandwidth?

## Slide 27: 2. Why is the spot size unaffected by spectral bandwidth?
Different wavelengths are focused at different points along the axial direction.
They produce a significantly larger spot at the focal plane, .
Their power is distributed over a larger area.
Adding the intensities from different wavelength components gives:
Intensity contribution from wavelength at a radial distance from the axis at the focal plane
spectral weight of that wavelength components.
Incident light
e-
e-
The intensity contribution from the design wavelength ( dominates the final focus.
z = f0
Notes: After adding the intensities from different wavelength components, weighted by the spectral power distribution, the intensity contribution from the design wavelength dominates the final focus.
After adding the intensities from different wavelength components, weighted by the spectral power distribution, the intensity contribution from the design wavelength 〖(𝜆〗_1) dominates the final focus.

## Slide 28: Summary
We are working on developing a similar model to explain the finite spectral bandwidth effects.
Pulsed sources can still produce a small focal spot, but with reduced efficiency and a longer temporal response.
When illumination becomes pulsed:
Is the focus still unchanged? No, temporally elongated
Does the electron emission spot size remain the same? Yes, the FWHM remains the same.
Does the electron pulse remain short? No, temporally elongated
The effects can be reduced by reducing the focal length of the zone plate ( by making ≈ ).
A high NA, small focal length zone plate integrated photocathode can be used as a high brightness pulsed electron source.

## Slide 29: Acknowledgements
Howard Padmore
Mansoure Moeini Rizi
Peter Prah Owusu
Jo Mama
Siddharth Karkare
Thank you for listening

## Slide 32: Results
Shifting to an ultra-short focal length drastically reduces the pulsed-light effects.
Intensity in the focal plane
Encircled Power
f0 | NA |  | 
0.1 mm | 0.7 | 80 fs | 133 fs
f0 | NA |  | 
0.1 mm | 0.7 | 80 fs | 133 fs

## Slide 33: "What is the bandwidth of a zone plate?"
A zone plate is inherently chromatic
BUT, If the incident ultrafast laser pulse has a component of the design wavelength, it may still produce a small spot, but with a huge tail.