## Slide 1: Ab initio modeling of two-level systems in amorphous niobium oxide
Cristóbal Méndez, Tomás Arias
PhD candidate, Cornell University
CBB annual meeting 2026

## Slide 2: Why TLS in Nb for SRF?
Without Nb2O5
With Nb2O5
If we want better SRF cavities, we need to understand and control material loss in Nb.
High-field region
Low-field region

## Slide 3: What are two-level systems (TLS)?
Atomic-scale defects in disordered oxides/interfaces
Two-level systems (TLS): Two nearly equivalent configurations
Quantum tunneling between the two states
Couple to microwave fields via their dipole moments

## Slide 4: What is the microscopic origin of TLS loss in Nb oxide?
The microscopic origin of TLS loss is still unknown
Many mechanisms can produce similar signatures
In Nb and Ta oxides, experiments consistently show that TLS loss:
  increases with amorphous disorder — Oh et al., ACS Nano (2024)
  is strongest in the pentoxide — Ganesan et al., arXiv (2026)
  correlates with oxygen vacancies — Bafia et al., Phys. Rev. Applied (2024)
  is higher in Nb oxide than in Ta oxide — Goronzy et al., arXiv (2025)
Notes: Say that I’m going to show a defect that does all 4 of these

## Slide 5: Potential tunneling species?
The usual suspects: H, N and O.
In Nb bulk:
GHz region

## Slide 6: Hydrogen as a TLS candidate
Incorporates under ambient conditions
Interacts strongly with oxygen vacancies
Small mass ⇒ quantum tunneling
H is a strong TLS candidate, but:
Really hard to see in STEM
We must ID an ensemble of defects
Depth profile from SIMS
Notes: Add a text saying the method of the plot

## Slide 7: Our computational method
Start with 98 amorphous structures from Pritchard and Rondinelli (2025)
Use machine-learning interatomic potentials (MLIPs) for high-throughput screening of TLS candidates
(Done follow up DFT verification)
…
…
Nb2O5-
Ta2O5-
Notes: Replace first bulletpoint with more pictures and … to 98

## Slide 8: Our computational method
Fine-grid search for stable H locations
Locate neighboring pairs of minima
Statistical analysis on ensemble
Compute tunneling profiles (Minimum energy path, NEB)

## Slide 9: Results: Estimated loss
Oxide interface
Native oxide layer
Ta
: TLS density
: dipole moment
: dielectric constant
Notes: Mention loss tangent

## Slide 10: Conclusion
Hydrogen tunneling is a strong TLS candidate in Nb2O5-
  increases with amorphous disorder — Oh et al., ACS Nano (2024) ✅
  is strongest in the pentoxide — Ganesan et al., arXiv (2026) ✅
  correlates with oxygen vacancies — Bafia et al., Phys. Rev. Applied (2024) ✅
  is higher in Nb oxide than in Ta oxide — Goronzy et al., arXiv (2025) ✅
⇒ H control and vacancy suppression are practical routes to lower loss in Nb devices.

## Slide 11
Thank you!
Questions?
This work was supported by the US National Science Foundation under award PHY-1549132, the Center for Bright Beams.

## Slide 13: Backup slides

## Slide 14: Results: Fits for the pentoxides
Number of potential pairs per site
Probability of TLS in the correct freq. range
TLS density:
Density of interstitial sites
H concentration

## Slide 15: Results: H formation energy

## Slide 16: Quartic WKB vs tunneling