## Slide 1: Zone plate Integrated Photocathode for Next Generation Electron Microscopes (and other applications)
Mansoure Rizi 07/10/2026

## Slide 2: Outline
2
Why is this needed?
Our design and fabrication
Brightness measurements
How this technology can be improved?
Notes: Conventional sources get to a brightness of 1e13
Can we do better with nano-focused photoemission sources

## Slide 3: Brightness from present sources for EM
2
Schottky field emitter thermionic tungsten emitter LaB6 emitter
Emitter Type | Thermionic | Thermionic | Schottky FE | Cold FE
Cathode Material | W | LaB6 | ZrO/W (100) | W (310)
Brightness (A/m2.sr) | 1010 | 1011 | 1012 | 1013
Can we go above conventional brightness using a nano-focused photoemission source?
Notes: Why higher brightness matter?
How many electrons can be delivered from a small probe. Higher brightness means better spatial resolution, higher beam current at small probe sizes, and faster imaging
Conventional sources get to a brightness of 1e13
Can we do better with nano-focused photoemission sources

## Slide 4: External lens + back illumination = low NA
3
[1] Photonics. 11(3), 252 (2024)
[2] J. Appl. Phys. 127, 164902 (2020)
Resolution improvement of low-voltage scanning electron microscope by bright and monochromatic electron gun using negative electron affinity photocathode. (a) Configuration of excitation optics. (b) CMOS camera image of reflected excitation light under in-focus condition. (c) Line profile of optical intensity along X and Y axes of (b) [2].
A modified INFN/DESY cathode plug allows microscale spot size in transmission mode with a short focal lens. (Left panel): cross-section view of plug concept. (Center panel): Machined prototype. (Right panel): knife edge beam size measurement yielding RMS spot size at photocathode surf [1]
Relatively long focal length due to geometry
- low NA means relatively large focus
Lens in cathode plug
Notes: microfocusing with a lens in a cathode plug has been shown to work
Low NA due to geometry means relatively poor resolution
We want to go beyond this with high NA planar lens

## Slide 5: Diffractive Solid Immersion Lens (D-SIL)
air
Refractive index n
Zone plate
f
Photoemitting surface: Cs3Sb
4
Limiting resolution for 532 nm
Quartz: n=1.54 s= 0.58 μm
GeS2 : n=2 s= 0.45 μm
Diamond: n=2.42 s= 0.37 μm
GaP: n=3.6 s= 0.25 μm
s = Diffraction-limited spot size=0.51 l/(n sinq)
q = 0.3
Highest NA, smallest focus, easy coupling to a conventional cathode
Zone plate focuses on downstream side of 1 mm thick plate
Focus size reduced by refractive index of substrate
Notes: A zone plate is an optical device that focuses light.
It works like a lens that focuses light with diffraction and is made of concentric rings (zones) that alternate between transparent and opaque.
The radii of the zones are calculated so that light passing through them interferes constructively at the focus point.
- NA = Numerical Aperture of the optical system (zone plate).
- λ = Wavelength of the incoming light (in this case 532 nm).
- dr = Width of the outermost zone of the zone plate=500 nm
- D = Diameter of the zone plate=680 um
fl = Focal length of the zone plate=1 mm
Substrate examples:
1) conventional high index glass at 532 nm, say n=1.56 (BK7) would have s=205 nm
2) chalcogenide glasses like germanium disulphide, n=2 at 532 nm, so s=160 nm
3) semiconductors: GaP is ideal, near zero absorption and n=3.6 at 532 nm so s=89 nm

## Slide 6: Fabrication Based on Lift off
5
S
i
S
u
b
s
t
r
a
t
e
1
8
5
n
m
P
M
M
A
4
9
5
K
2
0
0
n
m
P
M
M
A
9
5
0
K
W
r
i
t
t
e
n
w
i
t
h
E
B
L
D
e
v
e
l
o
p
e
d
i
n
M
I
B
K
:
I
P
A
=
1
:
3
T
r
e
a
t
e
d
w
i
t
h
O
2
P
l
a
s
m
a
E
-
b
e
a
m
e
v
a
p
o
r
a
t
i
o
n
o
f
C
r
(
5
n
m
)
/
A
u
(
1
2
0
n
m
)
L
i
f
t
o
f
f
w
i
t
h
R
e
m
o
v
e
r
P
G
R
i
n
s
e
d
w
i
t
h
I
P
A
S
i
S
u
b
s
t
r
a
t
e
S
i
S
u
b
s
t
r
a
t
e
S
i
S
u
b
s
t
r
a
t
e
Challenges:
Insulating substrate (charge dissipation layer needed)
Range of the size of structures, 50 to 0.266 microns (segmentation of pattern and dose control)
Large size (requires field stitching)

## Slide 7: Design and Process Optimization
Developed a multi-dose zoneplate fabrication process (18 different sections)
Main challenge was resist saturation and overexposure at higher doses.
Divided the design into concentric layers each exposed with a different electron beam dose to optimize feature width and uniformity.
Zoneplate Design (multi-layer dose pattern)
Dose Test Sample (showing variation across dose sets)
6

## Slide 8: Final Structure
Final zone plate on Quartz
7
1 cm
1 cm
zone plate
Gold coating
680 um
Notes: Zone plate is 680 microns in diameter
Rest of 1 cm x 1 cm surface covered with gold

## Slide 9: Higher NA Zoneplate SiC

## Slide 10
7
Gold coating
Zoneplate Fabricated on the SiC Substrate
Notes: Zone plate is 680 microns in diameter
Rest of 1 cm x 1 cm surface covered with gold

## Slide 11
7
Gold coating
Changed the PEC correction parameters: Reduced segment fraction and increased the accuracy.
n=2.681,dr=0.55 lamda, D=716 um
Zoneplate Fabricated on the SiC Substrate
Notes: Zone plate is 680 microns in diameter
Rest of 1 cm x 1 cm surface covered with gold

## Slide 12
7
Gold coating
Zoneplate Fabricated on the SiC Substrate
- Plasma cleaned for 15 min - PMMA 495 A 2.7, 5000 rpm, 30s - Softbake: 180 C for 10 min - PMMA 950 A2.7, 5000 rpm, 30s - Sofbake: 180 C for 10 min - Discharge layer: 3000 rpm 30 s - EBL: Dose: 1000 uC, 1100 uC and 1200 uC,
Current=500 pA - Develop MIBK:IPA at 14C for 30 s
Notes: Zone plate is 680 microns in diameter
Rest of 1 cm x 1 cm surface covered with gold

## Slide 13
7
Gold coating
Zoneplate Fabricated on the SiC Substrate
Notes: Zone plate is 680 microns in diameter
Rest of 1 cm x 1 cm surface covered with gold

## Slide 14: Cs3Sb Growth (PVD)
Cs3Sb
Zone plate cross section
8
1 mm
PEEM
Deposition chamber
Notes: Around 30 nm of cesium antimonide deposited on surface

## Slide 15: Photoemission Electron Microscope(PEEM)
Screen
Projection lenses
Iris Aperture
Stigmator II
Transfer Lens
Contrast Aperture
Objective
Stigmator I
9
CW laser source at 532 nm
e
e
0˚ From Bottom
PEEM images electron source with < 20 nm intrinsic resolution
PEEM Column
e
e
e
e
e
e
e
e
e
e
Notes: Photoemission electron microscopy used to image microfocused electron source
Unique instrument allowing back illumination
< 20 nm intrinsic resolution for threshold photoemission

## Slide 16: PEEM Measurement Zoneplate Fabricated on Quartz
10
Wavelength:532 nm, Power: 2.34 mW, Current =100 nA, QE= 5.8637e-04
For the quartz zone plate the q = 0.32.
=0.51 l/(n q)= 0.58 µm
This is close to the measures FWHM of 0.64 µm

## Slide 17: Mean Transfer Energy Measurement
MTE= = 216 meV
Mean Transverse Energy quantifies the average kinetic energy of emitted electrons parallel to the surface
11
Notes: Its worth noting that in small areas, the surface will be much more perfect than over a large area of polycrystalline sections.
MTE larger than expected…..probably due to contamination

## Slide 18: Zoneplate Spot Brightness
12
=
We have beam rms size, MTE and current so we can calculate beam brightness
brightness is ~ that of a thermionic source…..how can we improve this?

## Slide 19: Increasing Brightness
Near term: Brightness 2 orders higher than cold FEG
smaller outer zone width
high refractive index
Improving efficiency with a blazed phase zoneplate
13
+
Increase ZP efficiency
Reduce focus size
Final Brightness: 1.5 x1013
Better than cold FEG
Final Brightness: 1.5 x1015
This structure potentially will increase brightness by factor of up to 100 above the values above
Notes: Improve QE
improve the ZP efficiency. ZP efficiency for amplitude ZP is 10%. Phase ZP 40%. Blazed ZP 100%
Reduce focus with higher NA, higher refractive index
Use a plasmonic layer to couple to an alkali antimonide
Higher laser power

## Slide 20: Summary
We have a route to achieving brightness several orders higher than present sources
- Increasing the refractive index of the lens using diamond
- Reducing the outermost zone width
- Coupling to a plasmonic Fabry Perot structure with a 10 nm focus size
NOTE:
1) limit might be thermal heating at the focus: best material needs good thermal conductivity:
eg Diamond at 77K thermal conductivity can approach 2e4 W/mK!
2) the material in the nano-focus almost certainly will be a single crystal (lower emittance)
Notes: Just repeat we have a route to 2 orders higher brightness than cold FEG
No flicker noise…..super stable emission
Easy to make an arbitrary focus shape. Ring, line, cross etc.
Heating in the focus may be the limit…..need to simulate this

## Slide 21: Acknowledgements
Siddharth Karkare (Advisor)
Howard Padmore (Co-advisor)
Peter Owusu (Graduate Student)
Anagha Ullattuparambil (Graduate Student)
14

## Slide 22: Summary
We have a route to achieving brightness several orders higher than present sources
- Increasing the refractive index of the lens using diamond
- Reducing the outermost zone width
- Coupling to a plasmonic Fabry Perot structure with a 10 nm focus size
NOTE:
1) limit might be thermal heating at the focus: best material needs good thermal conductivity:
eg Diamond at 77K thermal conductivity can approach 2e4 W/mK!
2) the material in the nano-focus almost certainly will be a single crystal (lower emittance)
Notes: Just repeat we have a route to 2 orders higher brightness than cold FEG
No flicker noise…..super stable emission
Easy to make an arbitrary focus shape. Ring, line, cross etc.
Heating in the focus may be the limit…..need to simulate this

## Slide 23: New Resist
ZEP-520/SF3 EBL Bilayer Fabrication Process
- Standard Chemical Cleaning
- Pre-Bake 200C/3 min.
- SF-6S PMGI coat : 6000rpm/30 s
- Soft bake: 220C/120 s
-ZEP-520A coat: 6000rpm/30 s
-Soft bake: 180C/120 s
-Elionix Exposure (100keV)
Beam current: 500 pA, Beam Diameter: 2 nm
Field size: 1000 um , Dose: 500 uC
ZEP-520 Develop: 0-Xylene(1 min)/IPA rinse
PMGI Develop: AZ 300MIF(7s)/DI H2O rinse
7

## Slide 25: Spatial Resolution of a Zoneplate
4
- NA = Numerical Aperture of the optical system (zone plate).
- λ = Wavelength of the incoming light (in this case 532 nm).
- dr = Width of the outermost zone of the zone plate=500 nm
- D = Diameter of the zone plate=680 um
- fl = Focal length of the zone plate=1 mm
This equation relates the resolution capability of the system to the finest features of the zone plate. The smaller the outermost zone width (dr), the higher the NA, and hence better the focusing capability.
- s = Diffraction-limited spot size (i.e., smallest focus size or resolution limit).
- n= Refractive index of Quartz=1.54
The smallest spot size (spatial resolution) that the zone plate can achieve. It shows that resolution is limited by diffraction and depends linearly on dr.
S=0.61=0.61= =400nm

## Slide 27
Photoemitting surface
ө
f
air
Refractive index n
Zone plate cross section

## Slide 28: Summary
We have a route to achieving brightness several orders higher than present sources
- Increasing the refractive index of the lens using diamond
- Reducing the outermost zone width
NOTE:
1) limit might be thermal heating at the focus: best material needs good thermal conductivity:
eg Diamond at 77K thermal conductivity can approach 2e4 W/mK!
2) the material in the nano-focus almost certainly will be a single crystal (lower emittance)
Notes: Just leave this up…..instead of a thankyou slide.